Solar Vapour Generation by Photo-Reduced Graphene Oxide Membrane

Tieshan YangA*, Han LinA, Keng-Te LinA, Chunsheng GuoB, Scott FraserA, Baohua JiaA

ACentre for Translational Atomaterials, Faculty of Science, Engineering and Technology, Swinburne University of Technology, Melbourne, Australia; BDynamics and Mechanical & Electrical Equipment Engineering Technology Research Centre, Shandong University, Weihai, China.

*tyang@swin.edu.au

Introduction

Water scarcity has become one of the most pressing global challenges. Efficient solar thermal desalination could provide an alternative solution to produce clean water with high efficiency and low cost. Two key issues are considered to enable efficient solar thermal desalination: broadband high absorption in solar spectral range and localized heat management for efficient vapour generation with minimized parasitic thermal loss.[1] Significant progress has been made on both key issues recently. Absorbers with various rational designs have been demonstrated with high solar absorption.[2] In addition, dispersed particles, thin metallic absorbers, porous carbon materials have been used to confine the absorbed energy in a thinner region of the light-absorbing materials for localized heating and more efficient vapour generation.[2, 3]

Results and discussion

Herein, we used a porous photo-reduced graphene oxide (PRGO) membrane for solar thermal vapour generation. The porous PRGO membrane has high absorption, 97% for a 1000 nm thick membrane, over the entire solar spectrum (300-2500 nm) [Fig. 1(a)]. The high absorption enables efficient and effective solar thermal steam generation under one sun illumination [Fig. 1(b)]. We find the overall solar-to-vapour conversion efficiency can be 92.97%. This solar thermal desalination device is based on low-cost porous PRGO materials and scalable manufacturing processes, which promises large-scale applications.

Fig. 1. (a). The absorption spectra of a PRGO membrane in the wavelength range of 300 to 2500 nm, weighted by standard AM 1.5 G solar spectrum. (b). Water mass changes over time using a porous PRGO membrane.

References

1. Li, X., Xu, W., Tang, M., Zhou L., Zhu B., Zhu, S.,& Zhu, J. (2016). Graphene oxide-based efficient and scalable solar desalination under one sun with a confined 2D water path. Proc. Natl. Acad. Sci., 113, 13953-13958.

2. Gao, M., Zhu, L., Peh, C.K. & Ho, G.W. (2019). Solar absorber material and system designs for photothermal water vaporization towards clean water and energy production. Energy Environ. Sci., 12, 841-864.

3. Lin, H., Sturmberg, B.C.P., Lin, K.-T., Yang, Y., Zheng, X., Chong, T.K., de Sterke, C.M. & Jia, B (2019). A 90-nm-thick graphene metamaterial for strong and extremely broadband absorption of unpolarized light. Nat. Photon., 13, 270-276.

Acknowledgement

This work is supported by Australian Research Council through the Discovery Project scheme (DP190103186) and Industrial Transformation Training Centres scheme (IC180100005).