The 2D Transition Metal Dichalcogenide Interface

Wee, Andrew T.S.

Department of Physics, National University of Singapore, 2 Science Drive 3, Singapore 117542

*e-mail: phyweets@nus.edu.sg

We use high resolution scanning tunneling microscopy/spectroscopy (STM/STS) to study the atomic structure and local electronic properties of 2D MoS2 and WSe2 monolayers on HOPG substrates, and show that the electronic bandgaps can be tuned by strain at grain boundaries and dislocations [1,2]. Using PTCDA as a prototype semiconductor organic molecule, we show that a monolayer transition metal dichalcogenide (TMD) can effectively screen an organic-inorganic heterointerface [3]. We demonstrate the fabrication and unravel the electronic properties of a lateral doped/intrinsic heterojunction in 2D WSe2, partially covered with a molecular acceptor C60F48 [4]. We also demonstrate the self-assembly of DAP molecules into a hexagonal porous network on a monolayer MoSe2 surface, as a result of the different electron affinities of the inversion domain boundaries and the pristine MoSe2 domains [5]. Finally, I will discuss our work on 2D VSe2 that confirms it is not intrinsically ferromagnetic, resolving the recent controversy [6,7].

References

[1] Y. L. Huang, Y. F. Chen, W. J. Zhang, S. Y. Quek, C. H. Chen, L. J. Li, W. T. Hsu, W. H. Chang, Y. J. Zheng, W. Chen, A. T. S. Wee, Nature Comm. 6 (2015) 6298.

[2] Y. L. Huang, Z. Ding, W. Zhang, Y. H. Chang, Y. Shi, L. J. Li, Z. Song, Y. J. Zheng, D. Chi, S. Y. Quek, A. T. S. Wee, Nano Letters 16 (2016) 3682.

[3] Y. J. Zheng, Y. L. Huang, Y. F. Chen, W. J. Zhao, G. Eda, C. D. Spataru, W. J. Zhang, Y.-H. Chang, L. J. Li, D. Z. Chi, S. Y. Quek, A. T. S. Wee, ACS Nano 10 (2016) 2476.

[4] Z. Song, T. Schultz, Z. Ding, B. Lei, C. Han, P. Amsalem, T. Lin, D. Chi, S. L. Wong, Y. J. Zheng, M.–Y. Li, L.-J. Li, W. Chen, N. Koch, Y. L. Huang, A. T. S. Wee, ACS Nano 11 (2017) 9128.

[5] X. He, L. Zhang, R. Chua, P. K. J. Wong, Arramel, Y. P. Feng, S. J. Wang, D. Chi, M. Yang, Y. L. Huang, A. T. S. Wee, Nature Comm. 10 (2019) 2847.

[6] P. K. J. Wong, W. Zhang, F. Bussolotti, X. Yin, T. S. Herng, L. Zhang, Y. L. Huang, G. Vinai, S. Krishnamurthi, D. W. Bukhvalov, Y. J. Zheng, R. Chua, A. T. N'Diaye, S. A. Morton, C.‐Y. Yang, K.‐H. Ou Yang, P. Torelli, W. Chen, K. E. J. Goh, J. Ding, M.‐T. Lin, G. Brocks, M. P. de Jong, A. H. Castro Neto, A. T. S. Wee, Adv. Mat. 31 (2019) 1901185.

[7] W. Zhang, L. Zhang, P. K. J. Wong, J. Yuan, G. Vinai, P. Torelli, G. van der Laan, Y. P. Feng, A. T. S. Wee, ACS Nano (2019) doi.org/10.1021/acsnano.9b02996.

CV:

Professor Andrew Wee is Class of ’62 Professor of Physics, and Vice President (University and Global Relations) at the National University of Singapore (NUS). His research interests are in surface and nanoscale science, scanning tunneling microscopy (STM) and synchrotron radiation studies of the molecule-substrate interface, graphene and related 2D materials. A Fellow of the Institute of Physics, UK, the Singapore National Academy of Science, as well as the Institute of Physics Singapore, he has published more than 600 internationally refereed scientific papers. He holds a BA (Honours) in Physics from the University of Cambridge, and a DPhil from the University of Oxford. Prof Wee is an Associate Editor of the journal ACS Nano since 2011, and serves or has served on several international journal editorial boards.