Sustainable 3D-Printed Buriti Oil–Plasticized Carbon Black/PLA Electrochemical Sensor for L-Tyrosine Detection

Gilvana P. Siqueira1,3, Agata Rodak2, Tomasz Swebocki3, Angelika Łepek3, Eduardo M. Richter1, Mateusz Cieślik3, Krzysztof Formela2, Rodrigo A. A. Muñoz1, Jacek Ryl3

1Chemistry Institute, Federal University of Uberlândia, Uberlândia, Minas Gerais, 38400-902, Brazil

2Department of Polymer Technology, Faculty of Chemistry, Gdańsk University of Technology, Gabriela Narutowicza 11/12, Gdańsk 80–233, Poland

3Institute of Nanotechnology and Materials Engineering, Faculty of Applied Physics and Mathematics, Gdansk University of Technology, Gabriela Narutowicza 11/12, Gdansk 80-233, Poland

Corresponding author email (gilvana.siqueira@ufu.br)

Plasticizers are low-molecular-weight compounds that enhance polymer flexibility and processability by increasing chain mobility [1]. The demand for sustainable alternatives to petrochemical plasticizers has promoted the use of bioplasticizers derived from vegetable oils, which are renewable, low-cost, and environmentally friendly [2]. In this context, the circular economy encourages sustainable and recyclable materials to reduce waste and extend product lifecycles [3]. Due to its rich biodiversity, the Amazon region holds great potential for producing vegetable oils such as buriti oil [4]. In additive manufacturing, plasticizers can improve filament printability and composite homogeneity [5]. In this work, we developed conductive filaments composed of 10 wt% buriti oil (BU), 65 wt% polylactic acid (PLA), and 25 wt% carbon black (CB). The resulting filaments exhibited higher flexibility than non-plasticized ones (Fig. 1a). SEM analysis (Fig. 1b) confirmed a homogeneous electrode structure. Using FcDM0 as a redox probe, an approximately 1.6-fold current increase was observed (Fig. 1c), attributed to improved charge transport and percolation, and the electrochemical response of L-tyrosine (L-Tyr) was evaluated, with CB-PLA-BU exhibiting enhanced peak definition due to its superior electrochemical performance. The amperometric calibration curve for L-Tyr (10.0–750.0 µmol L⁻¹, R² = 0.993) obtained with the CB-PLA-BU electrode showed LOD and LOQ of 0.69 µmol L⁻¹ and 2.30 µmol L⁻¹, respectively (Fig. 1d). When applied to human urine samples using standard addition and recovery tests at 10.0 and 50.0 µmol L⁻¹, recoveries of 98.78% and 116.29% were obtained, indicating acceptable accuracy. Thus, the results demonstrate the potential of the 3D-printed lab-made platform with bioplasticizers for the electroanalytical detection of L-Tyr.

Figure 1. (a) Image of the CB-PLA-BU filament; (b) SEM images of electrodes with and without plasticizer; (c) CV responses in 1.0 mmol L⁻¹ FcDM0 in 0.1 mol L⁻¹ KCl, and L-Tyr in BR buffer (pH 2.0), in different electrodes (scan rate = 50 mV s⁻¹; step = 5 mV); (d) Amperometric responses and calibration curve for CB-PLA-BU in BR buffer (pH 2.0), without and with L-Tyr (a-j: 0.0–1000.0 µmol L⁻¹), at +1.1 V vs. Ag|AgCl|KCl(sat.).

Acknowledgements

Gilvana P. Siqueira acknowledges the doctoral scholarship provided by the Fahrenheit Universities program (Gdańsk, Poland) and the Brazilian agency CNPq (141177/2024-1).

References

1. N.R. Amrutha, P.S.K. Murthy, J.P. Reddy, Ind. Crops Prod. 224 (2025) 120360.

2. P. Senthamaraikannan, et al., J. Inorg. Organomet. Polym. (2025).

3. European Union (2023).

4. J.M. Guayasamin, et al., Acta Amazonica (2024).

5. R.D. Crapnell, et al., ACS Sustainable Chem. Eng. (2023).