Probing Activation Reversibility in Ni-Based LDH Electrocatalysts by In Situ EC-Raman Spectroscopy

Madjid Tarabet1, Alice Fiocco2, Guillaume Ducourthial1, Sébastien Legendre1, Luuk Muris3, Alvaro Seijas-Da Silva4, Vicente Vert4, Gonzalo Abellán3

1 Horiba France SAS, 455 Avenue Eugène Avinée, 59120, Loos, France

2 Horiba France SAS, 14, Boulevard Thomas Gobert, Passage Jobin Yvon, 91120 Palaiseau, France

3 Instituto de Ciencia Molecular (ICMol), Universitat de València, Catedrático José Beltrán 2, 46980 Paterna, Valencia, Spain.

4 Matteco Team, S.L., Carrer de Les Noves Tecnologies, 6, 46980 Paterna, Valencia, Spain.

madjid.tarabet@horiba.com

Nickel-based layered double hydroxides (Ni-LDHs) are promising catalysts for the oxygen evolution reaction (OER) in alkaline water electrolyzers. Despite their electrochemical performance, the structural transformations occurring at the electrode–electrolyte interface under realistic operating conditions, from initial activation to long-term polarization, remain incompletely understood.

In this work, in situ EC-Raman spectroscopy is used to monitor these transformations in real time on a series of room-temperature synthesized Ni-based LDH compositions [1], namely NiFe, NiCr and NiFeCr. The excitation wavelength was selected based on UV-Vis measurements to take advantage of resonance enhancement, which improves the detection of spectral features that would otherwise be difficult to resolve, including the formation of chromate species in alkaline medium. Under anodic polarization, the progressive conversion of the LDH toward the active oxyhydroxide phase is followed continuously, and the influence of composition on the onset and kinetics of this transformation is discussed.

Once the activation process is complete, switching to open circuit potential leads to a progressive recovery of the initial LDH spectral signature at the interface. This behavior, observed over timescales exceeding fifteen hours, points to a reversibility of the activation process and raises questions about the actual state of the catalyst under intermittent operating conditions.

[1] Seijas-Da Silva, A., Hartert, A., Oestreicher, V. et al. Scalable synthesis of NiFe-layered double hydroxide for efficient anion exchange membrane electrolysis. Nat Commun 16, 6138 (2025).