Anomalous behavior of interfacial ions at electrocatalytic interfaces

Alfred Larsson1, Marc Koper1, Rik Mom1

1Leiden Institute of Chemistry, Leiden University, Leiden, Netherlands

Ions, together with the solvent, make up half of the solid-liquid interface and shape the local reaction environment, and need to be considered in a holistic view of the “active site”. In this way, cations affect the activity of several important electrocatalytic reactions, including the hydrogen evolution reaction(1), oxygen evolution reaction(2), oxygen reduction(3), CO2 reduction(4), and alcohol oxidation(3).

In this contribution, I will demonstrate how we can directly detect interfacial ions experimentally using soft X-ray absorption spectroscopy (XAS) and electrochemical quartz crystal microbalance. For this, we use mesoporous platinum, with a large ratio between the interfacial and bulk electrolyte in the pores. This allows an otherwise bulk-sensitive technique to provide quantitative data on the concentration and degree of hydration of cations and anions at the platinum electrolyte interface. We have used this methodology to track the interfacial anion and cation concentrations as a function of electrode potential, bulk ion concentration, pH, and anion and cation identity.

This reveals a charging behavior which differs from conventional capacitive models. Under certain conditions, we observe an increasing cation concentration at increasing potential, non-monotonic surface charging, and changes in desolvation behaviour depending on the adsorbates on the Pt surface. This shows how adsorbates reshape surface charge and the ions attracted, altering the local reaction environment.

References

1.	A. Goyal, S. Louisia, P. Moerland, M. T. M. Koper, Cooperative Effect of Cations and Catalyst Structure in Tuning Alkaline Hydrogen Evolution on Pt Electrodes. J. Am. Chem. Soc. 146, 7305-7312 (2024).

2.	M. Görlin et al., Key activity descriptors of nickel-iron oxygen evolution electrocatalysts in the presence of alkali metal cations. Nat. Commun. 11, 6181 (2020).

3.	D. Strmcnik et al., The role of non-covalent interactions in electrocatalytic fuel-cell reactions on platinum. Nature Chemistry 1, 466-472 (2009).

4.	M. C. O. Monteiro et al., Absence of CO2 electroreduction on copper, gold and silver electrodes without metal cations in solution. Nature Catalysis 4, 654-662 (2021).