Comparing Oxygen Release in O3- and O6-Type Lithium-Rich Layered Oxide Positive Electrodes Using OEMS

Khryslyn Arañoa, Guanlan Zhaob, Lisa Duguetc, Aurélie Guéguenc, Laurent Castroc, Claude Delmasb, Marie Guignardb, Irina Profatilovaa

aUniversity Grenoble Alpes, CEA, LITEN, 17 rue des Martyrs, 38000, Grenoble, France

bUniversité de Bordeaux, CNRS, Bordeaux INP, ICMCB, UMR 5026, F-33600 Pessac, France

cToyota Motor Europe NV/SA, Technical Center, 1930 Zaventem, Belgium

khryslyn.arano@cea.fr

As the demand for longer-lasting and lighter energy storage systems continues to grow, especially for electric vehicles and portable electronics, enhancing the energy density of batteries is essential. Lithium-rich layered oxides (LRLOs) are widely considered promising candidates for next-generation lithium-ion battery positive electrode materials due to their high energy densities and specific capacities, often exceeding 250 mAh g⁻¹. However, oxygen release in LRLOs, typically characterized by an O3-type layered structure, plays a critical role in the degradation of their electrochemical performance, ultimately limiting their practical application as high-capacity, high-energy-density positive electrodes. In this study, we investigate gas evolution in a representative O3-type material, Li1.2Mn0.6Ni0.2O2, and compare it with an O6-type stacking structure, Li5/6[Li1/6Ni1/6Mn4/6]O2.

Using online electrochemical mass spectrometry (OEMS), we demonstrate (Fig 1.) a pronounced suppression of oxygen evolution in the O6-type material, attributable to its intrinsically more stable structure. Upon charging to 4.7 V vs Li/Li+, the O3-type cathode releases 298.6 μmol g-1AM of oxygen, whereas the O6-type material generates only 3.5 μmol g-1AM under comparable conditions. Despite this stark difference, both materials deliver reversible subsequent discharge capacities exceeding 200 mAh g-1. In addition, we identify a significant contribution from surface-associated Li2CO3 to gas evolution, particularly in CO2 formation. To our knowledge, this work presents the first systematic investigation of gas evolution in an O6-type LRLO and highlights its strong potential as a next-generation high-energy positive electrode material.

Figure 1. Evolution profile of O2 (m/z = 32) and CO2 (m/z = 44) with the voltage-time curves of O3 and O6 materials cycled against delithiated LFP.