LSMN double perovskite for Na-CO2 battery application

Sandra Sajeev, a Monika Srivastava,a Yoshitaka Aoki,b Damian Kowalski a

a) Faculty of Chemistry, University of Warsaw, Zwirki i Wigury 101, 02-089 Warsaw, Poland

b) Faculty of Engineering, Hokkaido University, Kita-Ku Kita 13, Jo Nishi 8, Sapporo 060-8628, Hokkaido, Japan

s.kannachanpurakkal-sajeev-kumar@uw.edu.pl

Rechargeable sodium-carbon dioxide (Na-CO2) batteries have been proposed as a promising approach for CO2 utilization that can simultaneously reduce CO2 and generate electricity. However, they suffer from several practical limitations, including sluggish CO2 reduction and evolution kinetics and poor cycling stability. In this work, nickel-substituted perovskite oxides, La0.7Sr0.3Mn1-xNixO3 (x = 0, 0.1, 0.3, and 0.5), were employed as catalysts in a Na-CO2 battery operating with 1 mol.dm-3 sodium perchlorate (NaClO4) in tetraethylene glycol dimethyl ether (TEGDME) electrolyte. The La0.7Sr0.3Mn0.9Ni0.1 electrode showed enhanced electrocatalytic activity, with improved specific capacity and stable cycle performance. In-situ Raman spectroscopy reveals the details on formation of the major discharge products, decomposed at relatively low charging potential due to effective electron transfer at the cathode. Substitution of Mn with Ni in La0.7Sr0.3Mn0.9Ni0.1O3 led to enhanced charge-transfer kinetics due to a high surface population of low valence state B site ions (Mn3+). This study highlights Ni-substituted manganite perovskites as efficient electrocatalysts for high-performance Na-CO2 batteries.

(b)

(a)

Figure a) Scheme of Na-CO2 battery with La0.7Sr0.3Mn1-xNixO3 catalyst (LSMN) in the cathode, b) in-situ Raman spectrum of a Na-CO2 battery composed of the La0.7Sr0.3Mn0.5Ni0.5 catalyst.

References

[1] S. Sajeev, M. Vincent, P. Garbacz, M. Strawski, C. Zhu, Y. Aoki, and D. Kowalski, ‘’ The role of Ni substitution in manganite perovskite Li-O2 battery’’, RSC Applied Interfaces. 2025, 2, 1051.

[2] S. Sajeev, P. Henkiel, M. Srivastava, S. Srinivasan, K. Wang, E. Kowalska, and D. Kowalski, “Lithium-ion storage capability of P25, ST01, FP6 and isolated phases of anatase and rutile”, Electrochimica Acta. 2025, 544, 147650.

[3] M. Vincent, D. Kowalski, In-Situ Raman Spectroscopy of Li+ and Na+ storage in Anodic TiO2 Nanotubes: Implications for Battery Design. ACS Appl. Nano Mater. 2023, 6, 8, 6528-6537.