The electronic structure of 1D Pd@Ni nanospikes and their electrochemical activity in oxidation of ethanol

Dariusz Łukowiec 1, Tomasz Wasiak2, Dawid Janas3, Joanna Depciuch4, Jerzy Kubacki5, Stanisław Wacławek6, Adrian Radoń 7 and Alexey Maximenko8

1 Materials Research Laboratory, Faculty of Mechanical Engineering, Silesian University of Technology, Konarskiego 18A St., 44-100 Gliwice, Poland

2 Institute of Chemistry, University of Silesia in Katowice, Szkolna 9 St., 40-006 100 Katowice, Poland

3 Faculty of Chemistry, Silesian University of Technology, B. Krzywoustego 4 St., 44-100 Gliwice, Poland

4 Institute of Nuclear Physics Polish Academy of Sciences, Radzikowskiego 152 St., 31-342 Krakow, Poland

5 Faculty of Science and Technology, Institute of Physics, University of Silesia in Katowice, 75 Pułku Piechoty 1, 41-500 Chorzów, Poland

6 Institute for Nanomaterials, Advanced Technologies and Innovation, Technical University of Liberec, Studentská 1402/2, 461 17 Liberec 1, Czech Republic

7 Departament of Engineering Materials and Biomaterials, Faculty of Mechanical Engineering, Silesian University of Technology, Konarskiego 18A St., 44-100 Gliwice, Poland

8 SOLARIS National Synchrotron Radiation Centre, 30-392, Kraków, Poland

Email: dariusz.lukowiec@polsl.pl

The world's sustained high demand for electricity requires the development of ever more efficient, cost-conscious catalysts for its production. Among the many catalysts based on Pd, combination of PdNi electrocatalyst has gained the great attention. Due to the nano-structural architecture plays a crucial role in the catalytic activity, we synthesized novel Pd@Ni unsupported with carbon black catalyst in form of one-dimensional nickel nanospikes (Ni NSs) decorated by palladium nanoparticles. In this work, the impact of the changing in electronic structure of Pd@Ni catalysts on their catalytic properties was studied in details (XANES, EXAFS, XPS, TEM, in situ FTiR). For small Pd crystals surrounded by a large dispersion of Ni substrate atoms, can refer to an increased metal-substrate interaction, which is associated with an increase in d-state vacancies in the Pd@Ni catalyst [1]. This may imply a greater susceptibility to chemisorption of unsaturated hydrocarbons (acetylene, ethylene), which may be electron donors. The higher number of d-state vacancies in material may indicate greater susceptibility to chemisorption of ethanol molecules, which further improves its catalytic activity. By using two different concentrations of Pd catalyst (0.5 mM and 0.75 mM), an attempt was made to determine the optimal electronic structure for the Pd@Ni system. By using synchrotron X-ray absorption spectroscopy, it was possible to determine the differences in the density of unoccupied Pd d-state in the produced materials, as well as changes in the local structure of the used support - 1D Ni nanospikes. Analysis of valence spectra from X-ray photoelectron spectroscopy (XPS), in turn, confirmed differences in density of states at the Fermi level between the samples and determined d-band center and its width (d width) for each. The conclusions obtained on the correlation between structure and activity can be used in the design of working metal-to-metal supported catalysts used in catalytic oxidation and reduction reactions.

[1] Huang, D., Chang, K., Pong, W. et al. Effect of Ag‐promotion on Pd catalysts by XANES. Catalysis Letters53, 155–159 (1998)