Direct evidence of confinement enabled electrosynthesis towards Urea

Yannick Weidemann1, Pouya Hosseini2, Andrés Rodríguez-Camargo3, Bettina V. Lotsch3, Kristina Tschulik1

1 Chair of Analytical Chemistry, Ruhr University Bochum, 44801 Bochum, Germany

2Chair Atomic scale Characterization, Ruhr University Bochum, 44801 Bochum, Germany

3Nanochemistry Department, Max Planck Institute for Solid State Research, 70569 Stuttgart, Germany

Yannick.Weidemann@ruhr-uni-bochum.de

Electrochemical urea synthesis is a rapidly growing field in part due to its potential to replace the Bosch-Meiser process. Still, this is a non-trivial task. The electrocatalytic synthesis of urea via co-reductive pathways however depends on a multitude of factors.1 Finding suitable electrocatalyst is therefore just as complex, however optimizing existing catalyst remains largely unexplored. One possibility to alter and optimize catalyst selectivity is introducing confining elements.2 Herein, we present the application of a covalent organic framework (COF), to enable reductive urea electrosynthesis on Au electrodes based on the co-reduction of CO2 and NO3− via confinement. We prove this in-situ by employing electrochemical surface enhanced infrared absorption spectroscopy (EC-SEIRAS). We observed the emergence of a carbonyl stretch (1680 cm-1)  band as well as a surface-bound C-N stretch (1450 cm-1) band both likely related to urea on metallic Au modified with a, a electrochemically inert COF containing a  Azo-function in its linker.3 To further validate urea formation, we performed long-term electrolysis and determined a urea formation rate of 5.74±1.73 µMolh cm2 via the coulometric DAMO (diacetylmonoxime) approach. This work highlights the possibilities of identifying and exploiting confinement to steer reaction pathways and selectivity based on knowledge driven electrocatalyst design.

Figure 1: Schematic showing electrochemical urea synthesis with a Covalent organic framework modified Au electrode.

(1)	Costa, G. F.; Escudero-Escribano, M. Electrode-Electrolyte Engineering and In Situ Spectroscopy for Urea Electrosynthesis from Carbon Dioxide and Nitrate Co-Reduction. JACS Au 2025, 5 (4), 1538–1548. https://doi.org/10.1021/jacsau.5c00065.

(2)	Wordsworth, J.; Benedetti, T. M.; Somerville, S. V.; Schuhmann, W.; Tilley, R. D.; Gooding, J. J. The Influence of Nanoconfinement on Electrocatalysis. Angew. Chem. Int. Ed Engl. 2022, 61 (28), 202200755. https://doi.org/10.1002/anie.202200755.

(3)	Weidemann, Y.; Hosseini, P.; Rodríguez-Camargo, A.; Liu, L.; Moussa, B.; Graf, D.; Ochsenfeld, C.; Petersen, P.; Lotsch, B. V.; Tschulik, K. Controlling Confinement: Covalent Organic Frameworks Induced Confinement of Water Probed via EC-SEIRAS; 2026. https://doi.org/10.26434/chemrxiv.15000669/v1.