Spectroelectrochemical and quantum-mechanical insight into electropolymerization of selected carbazole derivatives

Krzysztof Noworyta,1 Julia Owczarska,1 Jyoti,1 Włodzimierz Kutner,1 Evgenia Dmitrieva,2 Renata Rybakiewicz-Sekita,3 Roman Gańczarczyk,4 Sandra Pluczyk-Małek,5 Agnieszka Powała,6 Teresa Żołek6

1 Institute of Physical Chemistry, Polish Academy of Sciences, Kasprzaka 44/52, 01-224 Warsaw, Poland

2 Center of Spectroelectrochemistry, Leibniz Institute for Solid State and Materials Research (IFW), Helmholtzstrasse 20, Dresden 01069, Germany

3 Institute of Mathematics, Faculty of Science and Mathematics, Cardinal Stefan Wyszyński University, Kazimierza Wóycickiego 1/3, 01-938 Warsaw, Poland

4 Warsaw University of Technology, Faculty of Chemistry, Noakowskiego 3, 00-664 Warsaw, Poland

5 Faculty of Chemistry, Silesian University of Technology, Akademicka 2A, 44-100 Gliwice, Poland

6 Department of Organic and Physical Chemistry, Faculty of Pharmacy, Medical University of Warsaw, Banacha 1, 02-097 Warsaw, Poland

knoworyta@ichf.edu.pl

Scheme 1.  Structural formulas of the selected carbazole derivatives studied.

This contribution presents the results of extensive investigations into the electrochemical polymerization of selected carbazole derivatives.  The study focuses on the analysis of the carbazole derivative structure influence on the electrooxidation process itself and the products formed.

Carbazole and its derivatives constitute a large class of aromatic heterocyclic compounds containing nitrogen.  Their extensive, rigid π-conjugate system leads to favorable electronic and charge transport properties.  This feature ensures that they are extensively studied for applications ranging from dyes, photoelectrical materials, supramolecular recognition systems, and medicinal agents.1  The strong advantage of those compounds is their convenient functionalization, allowing synthesis of a variety of derivatives with a range of functional groups introduced both into the carbazole rings and the nitrogen atom.

We have applied carbazole derivatives in chemosensing.3  To this end, we have synthesized a library of carbazole derivatives modified both at the nitrogen atom and at the C3 and C6 atoms of the carbazole core.  Those monomers have been characterized by UV-vis spectroscopy, fluorescence, and voltammetry.  As the electrochemical behavior of the apparently similar monomers has been surprisingly different, we started to study the effect of electrochemical polymerization processes on the structure of the monomers synthesized.4  For that, we have employed the UV-vis-NIR and EPR spectroelectrochemistry coupled with extensive quantum-chemical calculations.

Herein, we present results of investigations of a series of carbazole derivatives with various modifications on the heterocycle nitrogen atom appended, or not, with thiophene substituents in the C3 and C6 position of the carbazole moiety.  UV-vis-NIR and EPR spectroelectrochemical studies, combined with quantum-chemistry calculations, allowed elucidation of the stability of the cation radicals formed and the effects of various structural motifs on the oligomeric and polymeric products generated.  Furthermore, AFM imaging of the polymer films deposited allowed analysis of the monomer structure's influence on the films' morphology.

References

1.	F. Bekkar et al., Polymers, 2020, 12, 2227.

3.	Jyoti et al., J. Mater.  Chem. B, 2022, 10, 6707.

4.	Jyoti et al., Electrochim. Acta, 2022, 429, 140948.

Acknowledgments.  The National Science Center (NCN) grant OPUS25 2023/49/B/NZ7/02718 provided financial support.