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Summary
Thermal energy storage has been used in domestic hot water systems for many years. Virtually all these systems have been based on sensible heating of potable water that is available on demand to meet the needs of consumers. The use of phase-change materials for thermal storage has been investigated by many researchers in the past. They have the potential to provide a high-energy density storage of thermal energy that can be delivered at a nearly constant temperature. The recent advent of commercial products using phase-change materials has incentivized the development and refinement of test methods and standard procedures for evaluating the performance of these devices under repeatable conditions. In this study, two commercially available, latent heat storages were tested according to a pre-existing test method, designed to evaluate similar products. The test data were then analyzed to create performance models for these phase-change material thermal storages. 
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[bookmark: _Hlk131389899]The physics of phase-change material (PCM) storage has been studied by many researchers (Ahmed et al., 2022, Hassan et al., 2016, Radouane, 2022, Teggar et al., 2021). The process involves the latent “heat of fusion” associated with a phase change between a liquid and a solid that occurs without a change in temperature, as demonstrated in Fig. 1. In a recent study, two commercially available phase-change thermal storages were tested in a laboratory environment according to the general requirements of ASHRAE 94.1-2010 (ASHRAE Standards Committee., 2010), to characterize their operations and quantify their overall capacities. Each unit consists of a leakproof container, filled with a salt hydrate with a nominal phase-change temperature of 58°C. Therefore, the storage system requires hot water between 65-80°C to achieve a full charge. Each storage is charged by circulating hot liquid through its integral tube and sheet heat exchanger and discharged by circulating cool liquid through a separate discharge flow loop. The only difference was the capacity of the two units: one weighed 176 kg (unit 1) and the other weighed 129 kg (unit 2). Fig 1: Charging of an ideal Phase-change substance (Radouane, 2022)


A Generalized Test Method and Performance Model for Phase-change Storages
Tests were conducted according to the general requirements of ASHRAE Standard 94.1-2010 for phase-change storages. In addition, constant temperature charge tests were also performed to further understand the relation between the energy stored and the fluid charge temperature (Harrison et al., 2024). An instrumented calorimeter rig was used to function as a controlled heat source for the thermal storages. The calorimeter rig comprised two temperature-controlled heaters, speed-controlled pumps, an expansion tank, a pressure relief valve, air eliminators, a magnetic flowmeter, and temperature sensors. The thermal storages were charged at constant power by running hot water from the calorimeter through the charge loop of the storage. The storages were discharged by running cold “mains” water from the calorimeter through the discharge loop to the drain. 
Due to the nature of phase-change material, supercooling was observed in all discharge tests. Actual power input or output from the storage was calculated from the product of the water mass flow rate, specific heat, and the temperature difference across the inlets and outlets of the storage. 
In terms of modelling the performance of the PCM storages, the concept is to develop a simple “black box” test method and characterization of the storages, which is illustrated with various steps in Fig. 2 below.
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Fig. 2: Flowchart of Model Development
The proposed scheme is to construct a model from experimental testing during typical heating and cooling tests that indicate the energy storage rates and temperature with respect to time. Initially, a PCM storage would undergo sensible heating during the “solid” portion of the heating curve. This is followed by the phase-change portion of the test that proceeds at a relatively constant temperature. During the testing, the energy delivered to the storage will be recorded along with the temperature history, allowing the latent heat of fusion associated with melting of the phase-change material to be estimated. Heating would continue until the outlet temperature of the storage increases indicating the unit is transitioning to the sensible heating of the liquid phase of the PCM material. The effective specific heats occurring during the initial and final stages of the charge cycle would be determined and reported, along with the transition temperature associated with the phase-change. The charge test would be followed with a similar discharge cycle to the same temperatures; the integrated charge and discharge values will define the effectiveness of the storage.
This sequence will be repeated at a range of inlet fluid temperatures both above and below the transition temperature and the net energy stored recorded. It is advantageous to conduct tests in which the supply temperature would be reduced in increments until no latent heating is observed, thereby obtaining a single-phase specific heat value. With this data, it would be possible to construct a general model that will predict the performance of the storage at a range of operational conditions without knowing the details of the storage construction or materials, as depicted in Fig. 3.
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Fig. 3: General Model predicting the performance of the storage based on data from non-intrusive “black box” test method 
Modelling Thermal Storage Performance based on the Energy Stored – Fluid Outlet Temperature Relation
3.1. Developing Curve Fit Equation for Charge Test
Fig. 4 below shows experimental values of energy stored versus the outlet temperature of the charge/discharge fluid. 

[bookmark: _Ref168062388][bookmark: _Toc168065929][bookmark: _Toc169623428][bookmark: _Toc169884723]Fig. 4. Energy Stored vs Fluid Outlet Temperature for Unit 1 Charge Tests
Since with different water flow rates and charge powers, the Energy Stored – Outlet Temperature curves are still in a relatively close position to one another, it can be assumed that this relation is not significantly affected by the flow rate and power. Therefore, it is possible to fit a curve fit through these curves, which will represent the relationship between the outlet temperature and the energy stored. In addition, with the formation of this relationship, the fluid outlet temperature can be considered as the effective temperature that represents the temperature of the storage. 
As described, it is desirable to have a general “black box” model that can describe the performance of a PCM storage based on experimental data. The model should be general and applicable to a wide range of PCM materials and operational modes. In analyzing the data measured for the PCM storage, it became apparent that a higher-order mathematical equation was required to ensure that it would apply to a wide range of operational conditions and to other PCM storages. The Generic Performance Equation for Solar Collector (Hottel & Whillier, 1958, Bliss, 1959) and the PCM Storage Capacity Equation (Lane, 1983) were the inspiration to form a general equation in the first place. 
Hottel-Whillier-Bliss Equation for Solar Collector:
 or 
and G. A. Lane Equation for PCM Storage Capacity:

After considerable analysis, a flexible performance equation was identified. The coefficients for the general equation could be identified through a non-linear regression technique.  The following equation was found to best fit the complex shape of the PCM heating/cooling experimental data, Fig. 5. 
		(eq. 1)
This equation can be broken down into four terms:
· : the energy stored at 0°C in theory.
· : describe the curve in the solid sensible heating section (before phase change).
· : responsible for the S-shape curvature, or the phase change (latent heating) section
· : added in after the material finishes its phase change to describe the curve in the liquid sensible heating section.  is an indicator function with  and 
With:
: energy stored by the storage
: representative temperature at phase change
: temperature at the end of phase change, or at the start of the liquid phase
: fitting constants

[bookmark: _Ref168063510][bookmark: _Toc168065930][bookmark: _Toc169623429][bookmark: _Toc169884724]Fig. 5. Proposed Curve Fit Equation and how its individual term corresponds to the curve shape
Based on the tests conducted on the PCM storage, a value of Tliq = 60°C was identified, which represents the neck of the curve for the transition from the phase change region to the liquid region curve. The remaining terms of the general equation were then identified by regression analysis on the measured data for the 4 constant power charge tests of Unit 1 and 3 charge tests of Unit 2 using eq. 1. Since the proposed equation contains both the linear functions (for the sensible heating section) and the logistic function (for the phase changing section), a non-linear regression analysis is used. Specifically, the Excel add-in, “Solver”, is used to find the 6 unknown parameters (E0, TPC, a, b, c, ∆c) that will minimize the sum of squares of the energy residuals, i.e. .
The final result for each parameter is the average of the regression results calculated from the four tests. The finalized equations for the curve fit are as follows:
Unit 1 – charge:

Unit 2 – charge: 

Fig. 6 shows the curve fit, as a continuous black line, relative to the real test data points.

[bookmark: _Ref168063474][bookmark: _Toc168065937][bookmark: _Toc169623436][bookmark: _Toc169884731]Fig. 6. Curve Fit versus Data Points for Unit 1 Charge Tests
Fig. 7 compares Unit 2 curve fit with Unit 1, and Fig. 8 normalizes the two curves by their total energy capacity.[bookmark: _Ref168407159][bookmark: _Toc169623438][bookmark: _Toc169884733]Fig. 8. Unit 1 & Unit 2 Normalized Charge Curve Fit

[bookmark: _Toc168065763][bookmark: _Toc169779455][bookmark: _Toc169883338][bookmark: _Ref168407145][bookmark: _Toc169623437][bookmark: _Toc169884732]Fig. 7. Unit 1 & Unit 2 Charge Curve Fit

3.2. Proposed Equation for Discharge Test
Based on the discharge data graphs, the water temperature at the end of phase change (Tliq) was approximated to be 54°C for Unit 1 and 53°C for Unit 2.
The same form of equation is applied to the discharge test to describe the relationship between Energy Stored and fluid Outlet Temperature. Using the same non-linear regression method, the parameters for the discharge curve fit equation can be found. The finalized equations for the curve fits are as follow:
Unit 1 – discharge:

Unit 2 – discharge: 

[bookmark: _Ref168063852][bookmark: _Toc168065939]Due to the fact that the fluid inlet temperature is now on the cold side, as well as the effect of supercooling, it is expected that the Energy Stored – Outlet Temperature curve fit for the Discharge will be off to the left of the Charge curve fit, which is demonstrated below in Fig. 9 and Fig. 10. Fig. 10. Charge & Discharge Curve Fits for Unit 2
Fig. 9. Charge & Discharge Curve Fits for Unit 1
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Description automatically generated]3.3. Predicting Performance Data using Proposed Curve Fit Equation
An algorithm has been developed to use the curve fit equation in predicting test data. This algorithm will take the initial state of charge, or the initial energy stored in the storage, the fluid inlet temperature, and the fluid flow rate, to predict the fluid outlet temperature, charge/discharge power as well as the state of charge (energy stored) after a certain time period. 
Fig. 11 describes the algorithm. By knowing the initial state of charge (current energy stored), the outlet temperature can be figured out by using the correlation of the curve fit equation, Fig. 12. Knowing the outlet temperature and along with the provided inlet temperature, the power delivered by the fluid to the PCM storage can be calculated with the heat transfer equation. With a pre-specified time step, the calculated power is then used to find the energy added to the storage, which ultimately leads to the total energy (state of charge) of the storage for the next time step. It should be noted that the shorter the timestep chosen, the more accurate the prediction will be. [bookmark: _Ref168407626][bookmark: _Toc169623443][bookmark: _Toc169884738]Fig. 12. Finding Tout from state of charge
Fig. 11. Algorithm used to predict Test Data from the Curve Fit

[bookmark: _Toc168065765][bookmark: _Toc169779457][bookmark: _Toc169883340]Alternative Approach to Calculate the Storage Temperature
[bookmark: _Toc169779458][bookmark: _Toc169883341]4.1. Using Fluid Inlet Temperature for Modelling
In the previous sections, the storage temperature is represented by the fluid outlet temperature, which is also used in the Energy Stored – Temperature curve fit. However, the fluid inlet temperature could also be used for the modelling if a Flow Factor is added. 

[bookmark: _Ref168064555][bookmark: _Toc168065945][bookmark: _Toc169623447][bookmark: _Toc169884742]Fig. 13. Energy Stored vs Fluid Inlet Temperature for Unit 1 Charge Tests
Fig. 13 above shows the fluid inlet temperature of the same 4 constant power charge tests of Unit 1. Because of the spread-out of the 4 curves due to different charge powers and fluid flow rates, it is not possible to achieve a single performance graph for different flow rates and powers if data is only plotted against the inlet temperature.
To minimize this effect, a set of modified temperatures, , was introduced to better represent the effective storage temperature. The descriptive equation is shown below in (eq. 2), with the unit of  is kW and the unit of  is (kg s-1). 
 (charge) 
or  (discharge)	(eq. 2)
 is a Correction Temperature and is the difference between the inlet temperature () and the effective storage temperature ().  is a Flow Factor with the unit of (kg K kJ-1) and will be responsible for how the  ratio affects the Correction Temperature. The values of  is different for charge and discharge process, and also different for different storages. By performing extrapolation on the effective phase-change temperature  of the different tests (or visually the middle point of each S-curve), with respect to the  fraction, the phase-change temperature at  can be determined. Physically, this is when the inlet and outlet are at the same temperature, and essentially this is also the storage temperature. Fig. 14 and 15 below show how the Correction Temperature  and Flow Factor  is related to the  fraction. Each point on the trendline represents the extrapolation result of one experimental test data.

Fig. 15. Correction Temperature versus (Power/Flow Rate) Fraction for Unit 1 Discharge Test
Fig. 14. Correction Temperature versus (Power/Flow Rate) Fraction for Unit 1 Charge Test 

After replacing  with , the gaps mentioned above are reduced significantly, which is shown below in Fig. 16 for Unit 1 PCM storage. 

[bookmark: _Ref168065245][bookmark: _Toc168065947][bookmark: _Toc169623450][bookmark: _Toc169884745]Fig. 16. Energy Stored vs Effective Temperature T* for Unit 1 Charge Tests
[bookmark: _Toc169779459][bookmark: _Toc169883342]4.2. Curve Fit Equation for T*
With the effective temperature T* representing the temperature of the storage, it is now possible to fit a single Energy Stored – Effective Storage Temperature curve for different flow rates and powers. The same equation form (eq. 1) was used for the regression. The results are shown below. 
Finalized equations for the curve fit:
Unit 1:
Charge   
With: 

Discharge: 
With: 
Unit 2: 	
Charge: 
With: 

Discharge: 
With: 

[bookmark: _Ref169771790][bookmark: _Ref169772700][bookmark: _Toc169779460][bookmark: _Toc169883343]4.3. Predicting Performance Data
An update in the algorithm used to predict test data is necessary since the Energy Stored – Outlet Temperature relation is now replaced by Energy Stored – Effective Storage Temperature (which derives from fluid inlet temperature, flow rate, and power). The algorithm is shown below in Fig. 17 (the two equations used to calculate  and  are specifically for charge test).
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[bookmark: _Ref168668586][bookmark: _Toc169623453][bookmark: _Toc169884748]Fig. 17. Updated Algorithm used to Predict Test Data if  is used for modelling
[bookmark: _Toc169779461][bookmark: _Toc169883344]4.4. Comparison between the two Approaches
Fig. 18 to Fig. 23 compare the data prediction coefficients between the Outlet Temperature approach and the Inlet Temperature approach. The Constant Temperature Charge Test at 75°C Inlet and 3 LPM of Unit 1 was chosen as the example to illustrate this comparison. 
[bookmark: _Ref169623086][bookmark: _Toc169623456][bookmark: _Toc169884751]Fig. 18. Outlet Temperature Correlation (Outlet Temperature approach)
[bookmark: _Ref169623005][bookmark: _Toc169623457][bookmark: _Toc169884752]Fig. 19. Outlet Temperature Correlation (Inlet Temperature approach)


[bookmark: _Toc169623460][bookmark: _Toc169884755]Fig. 22. Power Correlation (Outlet Temperature approach)
[bookmark: _Ref169623096][bookmark: _Toc169623461][bookmark: _Toc169884756]Fig. 23. Power Correlation (Inlet Temperature approach)
[bookmark: _Toc169623458][bookmark: _Toc169884753]Fig. 20. Energy Correlation (Outlet Temperature approach)
[bookmark: _Toc169623459][bookmark: _Toc169884754]Fig. 21. Energy Correlation (Inlet Temperature approach) 

Conclusion
A generalized “black-box” model of the phase-change material (PCM) thermal storage has been derived such that the performance (energy storage capacity versus charge-loop temperature) can be determined at a range of charge-circuit liquid flow rates and power levels. Two approaches have been proposed for the model i.e.,
1. Using the fluid outlet temperature to form a relation with the energy stored, then use this relation to predict the system’s performance, or
2. Using an effective storage temperature , which is derived from the inlet temperature based on different flow rates and power, to form a relation with the energy stored, then use this relation to predict the system’s performance. 
The second approach may be preferable since the fluid inlet temperature is used to derive the model, but it is also more complicated since it requires an additional step of calculating the effective storage temperature. This latter approach is similar to that used to characterize solar collectors, where a general relationship is derived from tests for a specific flow rate, incidence angle of the incident solar radiation, and sky condition, e.g., overcast, cloudy, etc. Operations during real conditions are determined from a repeatable standard test result and then modified by factors determined by individual tests of the parameter, e.g., heat transfer fluid flow rate. The coefficients from a specific test (e.g., flow rate) are then used with the appropriate modifying factors to determine the performance of the device at a specified operational condition.
The results of this study indicate that a non-intrusive “black-box” model is possible for use in characterizing and describing the characteristics of a wide range of PCM storage systems and the development of numerical models for use in full system simulations. In addition, this study and its results may significantly guide the development of standard testing procedures and protocols for product ratings. To achieve this, further testing and analysis for a variety of PCM storage devices, utilizing different PCM formulations, sizing, and design features is recommended.
Recommendations for Future Work
Although these approaches on the modelling of PCM thermal storage may be universal, they have only been developed and verified on one type of PCM storage. As a result, future work on PCM modelling should investigate its application on a range of commercial products with different phase-change materials and configurations. This includes conducting tests and analysis for a variety of PCM storage devices with different PCM formulations, storage sizes and design features
Finally, many modern appliances contain electronic controls that adjust operations based on internal algorithms. The implication of these internal controls may introduce an additional level of characterization required in performance simulations. This is an area for further analysis and is not currently addressed in this study.
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Energy Stored (kWh)




Test 1 (6 kW, 5 LPM)	20	21.0745	22.6797	24.7	27	29.2	31.4	33.5	35.5	37.299999999999997	39.1	40.799999999999997	42.3	43.6	44.9	46.1	47.1	48	48.8	49.5	50.1	50.7	51.2	51.7	52	52.4	52.7	53	53.2	53.5	53.7	53.9	54.1	54.3	54.5	54.6	54.8	55	55.2	55.4	55.6	55.8	56	56.3	56.5	56.8	57.1	57.4	57.8	58.2	58.7	59.4	60.1	61	62.2	63.5	64.900000000000006	66.400000000000006	0	0.21013966666666589	0.41144233333334795	0.6059423333333479	0.79669233333334788	0.98674788888890341	1.1747201111111256	1.3614145555555701	1.5486367777777923	1.7356645555555701	1.9247201111111258	2.1145534444444589	2.3032478888889036	2.4942478888889035	2.6844145555555703	2.8762201111111261	3.0684701111111261	3.2627756666666814	3.4579145555555706	3.6554701111111263	3.8499423333333485	4.047859000000015	4.2433312222222375	4.4414701111111263	4.6405534444444596	4.8405812222222364	5.0396923333333481	5.2404145555555699	5.4402756666666807	5.6399145555555696	5.8394423333333476	6.0398312222222366	6.2404701111111249	6.4429701111111255	6.6449145555555695	6.846192333333347	7.0478034444444582	7.2474423333333471	7.4466645555555697	7.6446645555555692	7.8422756666666809	8.0384701111111259	8.2362756666666801	8.4323867777777917	8.6301367777777909	8.8278867777777918	9.0228590000000146	9.2184423333333481	9.4136090000000152	9.6079145555555705	9.8020534444444589	9.9956923333333485	10.187442333333349	10.37630344444446	10.564081222222239	10.748275666666682	10.929636777777795	11.10855344444446	Test 2 (6 kW, 10 LPM)	24.9	27.2	29.7	31.8	33.9	36.1	37.9	39.9	41.5	43.2	44.6	46	47.4	48.5	49.4	50.3	51.1	51.8	52.3	52.8	53.3	53.6	53.9	54.2	54.5	54.7	54.9	55	55.2	55.4	55.5	55.6	55.8	55.9	56.1	56.2	56.3	56.5	56.6	56.8	57	57.3	57.6	57.9	58.4	59	59.6	60.5	61.4	62.4	63.6	64.7	65.900000000000006	67.099999999999994	68.2	69.5	0.8	0.98888533333333273	1.1775199999999986	1.3663153333333313	1.5554806666666641	1.74429233333333	1.9316999999999966	2.1196603333333299	2.3069509999999966	2.4958606666666761	2.6848720000000084	2.8746096666666743	3.0636893333333406	3.2548793333333403	3.4477640000000056	3.6401373333333389	3.8345510000000047	4.0297923333333383	4.2259653333333382	4.4216900000000052	4.6189146666666714	4.8164106666666715	5.0159220000000042	5.2145043333333376	5.4133126666666742	5.61306333333334	5.8130626666666725	6.0143790000000061	6.2150986666666723	6.4165413333333383	6.6183703333333375	6.8199016666666701	7.0211473333333361	7.2214363333333349	7.4213923333333343	7.6214976666666665	7.8211959999999987	8.0211786666666658	8.2210389999999975	8.4211836666666802	8.619890000000014	8.8169410000000124	9.0138113333333454	9.2092863333333455	9.403559000000012	9.5957493333333446	9.7850710000000092	9.9723373333333427	10.156495666666677	10.340788000000009	10.522201666666673	10.700448333333339	10.877768666666672	11.055868666666671	11.231266000000003	11.395241333333335	Test 3 (3 kW, 10 LPM)	20	22.2	31.4	32.4	33.4	34.4	35.4	36.299999999999997	37.200000000000003	38.1	39	39.9	40.700000000000003	41.5	42.3	43.1	43.9	44.6	45.3	46	46.6	47.2	47.8	48.4	48.9	49.4	49.9	50.3	50.7	51.1	51.5	51.8	52.2	52.5	52.7	53	53.5	53.8	54.9	55.1	55.3	55.5	55.6	55.7	55.9	56.1	56.3	56.3	56.5	56.7	56.8	57.6	58.1	59.1	60.4	62	62.9	63.8	65.7	66.7	67.599999999999994	68.599999999999994	69.599999999999994	70.599999999999994	72.099999999999994	74	75.900000000000006	0	9.5538666666666328E-2	0.82851433333333768	0.91853366666667069	1.008250333333337	1.0978233333333367	1.1860806666666697	1.2754683333333361	1.3632840000000024	1.450569000000002	1.5389110000000015	1.6259083333333344	1.7126146666666675	1.7994103333333338	1.8862520000000003	1.9728283333333332	2.0594460000000065	2.145445666666673	2.2313853333333391	2.317201333333339	2.4030276666666719	2.4886613333333383	2.5745080000000047	2.6598326666666714	2.7462583333333375	2.8325116666666705	2.9184850000000035	3.0057543333333365	3.0927183333333366	3.1795956666666694	3.2651360000000023	3.3516990000000018	3.4387366666666681	3.5254320000000012	3.6121880000000011	3.6988463333333343	3.8725239999999999	4.0456276666666664	4.7444436666666698	4.919952000000003	5.0953516666666685	5.2696963333333349	5.4451356666666673	5.620245999999999	5.9709403333333313	6.3215896666666707	6.6740003333333355	6.8507713333333351	7.2000479999999998	7.5502859999999972	7.8992943333333301	8.8569709999999997	9.2001106666666654	9.5361369999999983	9.8660186666666725	10.186830333333337	10.344485666666667	10.501561333333335	10.810382333333333	10.961247	11.110391666666668	11.258233000000001	11.404459999999998	11.549178999999997	11.763596333333338	12.04181866666667	12.314067666666668	Test 4 (3 kW, 5 LPM)	20	20.399999999999999	21.2	22.4	23.4	24.7	25.8	26.9	28.1	29.1	30.2	31.3	32.200000000000003	33.299999999999997	34.299999999999997	35.200000000000003	36.1	37	37.9	38.799999999999997	39.6	40.4	41.2	41.9	42.7	43.4	48.1	48.6	49	49.4	50.2	50.8	51.4	51.9	52.1	52.3	52.6	52.8	53.3	53.7	54	54.3	54.6	54.8	55	55.3	55.7	55.9	56.1	56.3	56.5	56.9	57.2	57.5	58	58.7	59.3	59.7	60.5	61.3	62.2	63.1	63.6	64.099999999999994	65.099999999999994	66	66.5	67	67.5	68	68.5	69	69.5	69.900000000000006	70.400000000000006	70.900000000000006	71.400000000000006	71.900000000000006	72.3	72.8	73.3	0	0.10260233333333298	0.20112999999999931	0.29551566666667312	0.38785000000000613	0.47924866666667248	0.57002366666667226	0.65958400000000528	0.75027100000000502	0.84049200000000468	0.93056700000000447	1.0199333333333374	1.1084050000000036	1.1965040000000033	1.2844516666666699	1.3729123333333362	1.4597500000000025	1.5465310000000023	1.6327336666666687	1.719300333333335	1.8056503333333345	1.8918003333333342	1.9770263333333338	2.0618799999999999	2.147237333333333	2.2321699999999995	2.996194000000004	3.0805893333333372	3.1655810000000035	3.249999000000003	3.4191316666666691	3.5893603333333357	3.7606113333333346	3.9309333333333334	4.0158566666666662	4.1012789999999999	4.1867123333333396	4.2706970000000055	4.525708666666671	4.7810996666666696	5.0401683333333365	5.2987003333333362	5.5570913333333349	5.815050666666667	6.0723126666666731	6.4149666666666718	6.9257833333333361	7.3488783333333414	7.6032063333333335	7.8569743333333388	8.1103903333333314	8.530929666666669	8.7813430000000015	9.1136273333333335	9.3592999999999993	9.6005393333333302	9.7599343333333284	9.9160983333333288	10.069315333333329	10.221111999999996	10.37132033333333	10.445938000000002	10.520226999999995	10.593200666666666	10.740276333333334	10.811828999999994	10.884000333333333	10.955962000000005	11.028365000000001	11.099843000000007	11.241756000000008	11.311887	11.382202666666672	11.451787333333332	11.521158333333339	11.590046666666666	11.658379000000004	11.725536666666665	11.79221166666667	11.85920733333333	11.924631000000003	Curve Fit	20	21	22	23	24	25	26	27	28	29	30	31	32	33	34	35	36	37	38	39	40	41	42	43	44	45	46	47	48	49	50	51	52	53	54	55	56	57	58	59	60	61	62	63	64	65	66	67	68	69	70	71	72	73	7.3056992900400214E-2	0.1758831750923722	0.27870935728541801	0.38153553948096397	0.48436172168233355	0.58718790389726339	0.69001408614377047	0.7928402684638125	0.89566645095509345	0.99849263384513587	1.1013188176637703	1.2041450036448038	1.3069711946613902	1.409797397404204	1.5126236274537328	1.6154499210920623	1.7182763628088105	1.8211031493538234	1.9239307388956508	2.0267601983638541	2.1295940122943966	2.2324379663438321	2.3353055332215384	2.4382280851602394	2.5412786701754664	2.6446273503114432	2.7486699087011113	2.8543267101139049	2.9637340148451261	3.0818288478279969	3.2199063072727063	3.4032064149536341	3.6851109802418458	4.1647473331205669	4.9747774858001712	6.159037246281164	7.4889578102853456	8.5902773677041466	9.3081584773362813	9.7273044930883295	9.9777966494939285	10.182282979461473	10.349681065578981	10.500777840166768	10.644803870103122	10.785780412170531	10.925444994121214	11.064545736939598	11.203404269498231	11.342158775282766	11.480868606398639	11.619559252509221	11.758241659974679	11.896920529530089	Outlet Temperature (°C)


Energy Stored (kWh)



Test 1 (6 kW, 5 LPM)	20	21.0745	22.6797	24.7	27	29.2	31.4	33.5	35.5	37.299999999999997	39.1	40.799999999999997	42.3	43.6	44.9	46.1	47.1	48	48.8	49.5	50.1	50.7	51.2	51.7	52	52.4	52.7	53	53.2	53.5	53.7	53.9	54.1	54.3	54.5	54.6	54.8	55	55.2	55.4	55.6	55.8	56	56.3	56.5	56.8	57.1	57.4	57.8	58.2	58.7	59.4	60.1	61	62.2	63.5	64.900000000000006	66.400000000000006	0	0.21013966666666589	0.41144233333334795	0.6059423333333479	0.79669233333334788	0.98674788888890341	1.1747201111111256	1.3614145555555701	1.5486367777777923	1.7356645555555701	1.9247201111111258	2.1145534444444589	2.3032478888889036	2.4942478888889035	2.6844145555555703	2.8762201111111261	3.0684701111111261	3.2627756666666814	3.4579145555555706	3.6554701111111263	3.8499423333333485	4.047859000000015	4.2433312222222375	4.4414701111111263	4.6405534444444596	4.8405812222222364	5.0396923333333481	5.2404145555555699	5.4402756666666807	5.6399145555555696	5.8394423333333476	6.0398312222222366	6.2404701111111249	6.4429701111111255	6.6449145555555695	6.846192333333347	7.0478034444444582	7.2474423333333471	7.4466645555555697	7.6446645555555692	7.8422756666666809	8.0384701111111259	8.2362756666666801	8.4323867777777917	8.6301367777777909	8.8278867777777918	9.0228590000000146	9.2184423333333481	9.4136090000000152	9.6079145555555705	9.8020534444444589	9.9956923333333485	10.187442333333349	10.37630344444446	10.564081222222239	10.748275666666682	10.929636777777795	11.10855344444446	Test 2 (6 kW, 10 LPM)	24.9	27.2	29.7	31.8	33.9	36.1	37.9	39.9	41.5	43.2	44.6	46	47.4	48.5	49.4	50.3	51.1	51.8	52.3	52.8	53.3	53.6	53.9	54.2	54.5	54.7	54.9	55	55.2	55.4	55.5	55.6	55.8	55.9	56.1	56.2	56.3	56.5	56.6	56.8	57	57.3	57.6	57.9	58.4	59	59.6	60.5	61.4	62.4	63.6	64.7	65.900000000000006	67.099999999999994	68.2	69.5	0.8	0.98888533333333273	1.1775199999999986	1.3663153333333313	1.5554806666666641	1.74429233333333	1.9316999999999966	2.1196603333333299	2.3069509999999966	2.4958606666666761	2.6848720000000084	2.8746096666666743	3.0636893333333406	3.2548793333333403	3.4477640000000056	3.6401373333333389	3.8345510000000047	4.0297923333333383	4.2259653333333382	4.4216900000000052	4.6189146666666714	4.8164106666666715	5.0159220000000042	5.2145043333333376	5.4133126666666742	5.61306333333334	5.8130626666666725	6.0143790000000061	6.2150986666666723	6.4165413333333383	6.6183703333333375	6.8199016666666701	7.0211473333333361	7.2214363333333349	7.4213923333333343	7.6214976666666665	7.8211959999999987	8.0211786666666658	8.2210389999999975	8.4211836666666802	8.619890000000014	8.8169410000000124	9.0138113333333454	9.2092863333333455	9.403559000000012	9.5957493333333446	9.7850710000000092	9.9723373333333427	10.156495666666677	10.340788000000009	10.522201666666673	10.700448333333339	10.877768666666672	11.055868666666671	11.231266000000003	11.395241333333335	Test 3 (3 kW, 10 LPM)	20	22.2	31.4	32.4	33.4	34.4	35.4	36.299999999999997	37.200000000000003	38.1	39	39.9	40.700000000000003	41.5	42.3	43.1	43.9	44.6	45.3	46	46.6	47.2	47.8	48.4	48.9	49.4	49.9	50.3	50.7	51.1	51.5	51.8	52.2	52.5	52.7	53	53.5	53.8	54.9	55.1	55.3	55.5	55.6	55.7	55.9	56.1	56.3	56.3	56.5	56.7	56.8	57.6	58.1	59.1	60.4	62	62.9	63.8	65.7	66.7	67.599999999999994	68.599999999999994	69.599999999999994	70.599999999999994	72.099999999999994	74	75.900000000000006	0	9.5538666666666328E-2	0.82851433333333768	0.91853366666667069	1.008250333333337	1.0978233333333367	1.1860806666666697	1.2754683333333361	1.3632840000000024	1.450569000000002	1.5389110000000015	1.6259083333333344	1.7126146666666675	1.7994103333333338	1.8862520000000003	1.9728283333333332	2.0594460000000065	2.145445666666673	2.2313853333333391	2.317201333333339	2.4030276666666719	2.4886613333333383	2.5745080000000047	2.6598326666666714	2.7462583333333375	2.8325116666666705	2.9184850000000035	3.0057543333333365	3.0927183333333366	3.1795956666666694	3.2651360000000023	3.3516990000000018	3.4387366666666681	3.5254320000000012	3.6121880000000011	3.6988463333333343	3.8725239999999999	4.0456276666666664	4.7444436666666698	4.919952000000003	5.0953516666666685	5.2696963333333349	5.4451356666666673	5.620245999999999	5.9709403333333313	6.3215896666666707	6.6740003333333355	6.8507713333333351	7.2000479999999998	7.5502859999999972	7.8992943333333301	8.8569709999999997	9.2001106666666654	9.5361369999999983	9.8660186666666725	10.186830333333337	10.344485666666667	10.501561333333335	10.810382333333333	10.961247	11.110391666666668	11.258233000000001	11.404459999999998	11.549178999999997	11.763596333333338	12.04181866666667	12.314067666666668	Test 4 (3 kW, 5 LPM)	20	20.399999999999999	21.2	22.4	23.4	24.7	25.8	26.9	28.1	29.1	30.2	31.3	32.200000000000003	33.299999999999997	34.299999999999997	35.200000000000003	36.1	37	37.9	38.799999999999997	39.6	40.4	41.2	41.9	42.7	43.4	48.1	48.6	49	49.4	50.2	50.8	51.4	51.9	52.1	52.3	52.6	52.8	53.3	53.7	54	54.3	54.6	54.8	55	55.3	55.7	55.9	56.1	56.3	56.5	56.9	57.2	57.5	58	58.7	59.3	59.7	60.5	61.3	62.2	63.1	63.6	64.099999999999994	65.099999999999994	66	66.5	67	67.5	68	68.5	69	69.5	69.900000000000006	70.400000000000006	70.900000000000006	71.400000000000006	71.900000000000006	72.3	72.8	73.3	0	0.10260233333333298	0.20112999999999931	0.29551566666667312	0.38785000000000613	0.47924866666667248	0.57002366666667226	0.65958400000000528	0.75027100000000502	0.84049200000000468	0.93056700000000447	1.0199333333333374	1.1084050000000036	1.1965040000000033	1.2844516666666699	1.3729123333333362	1.4597500000000025	1.5465310000000023	1.6327336666666687	1.719300333333335	1.8056503333333345	1.8918003333333342	1.9770263333333338	2.0618799999999999	2.147237333333333	2.2321699999999995	2.996194000000004	3.0805893333333372	3.1655810000000035	3.249999000000003	3.4191316666666691	3.5893603333333357	3.7606113333333346	3.9309333333333334	4.0158566666666662	4.1012789999999999	4.1867123333333396	4.2706970000000055	4.525708666666671	4.7810996666666696	5.0401683333333365	5.2987003333333362	5.5570913333333349	5.815050666666667	6.0723126666666731	6.4149666666666718	6.9257833333333361	7.3488783333333414	7.6032063333333335	7.8569743333333388	8.1103903333333314	8.530929666666669	8.7813430000000015	9.1136273333333335	9.3592999999999993	9.6005393333333302	9.7599343333333284	9.9160983333333288	10.069315333333329	10.221111999999996	10.37132033333333	10.445938000000002	10.520226999999995	10.593200666666666	10.740276333333334	10.811828999999994	10.884000333333333	10.955962000000005	11.028365000000001	11.099843000000007	11.241756000000008	11.311887	11.382202666666672	11.451787333333332	11.521158333333339	11.590046666666666	11.658379000000004	11.725536666666665	11.79221166666667	11.85920733333333	11.924631000000003	Curve Fit	20	21	22	23	24	25	26	27	28	29	30	31	32	33	34	35	36	37	38	39	40	41	42	43	44	45	46	47	48	49	50	51	52	53	54	55	56	57	58	59	60	61	62	63	64	65	66	67	68	69	70	71	72	73	7.3056992900400214E-2	0.1758831750923722	0.27870935728541801	0.38153553948096397	0.48436172168233355	0.58718790389726339	0.69001408614377047	0.7928402684638125	0.89566645095509345	0.99849263384513587	1.1013188176637703	1.2041450036448038	1.3069711946613902	1.409797397404204	1.5126236274537328	1.6154499210920623	1.7182763628088105	1.8211031493538234	1.9239307388956508	2.0267601983638541	2.1295940122943966	2.2324379663438321	2.3353055332215384	2.4382280851602394	2.5412786701754664	2.6446273503114432	2.7486699087011113	2.8543267101139049	2.9637340148451261	3.0818288478279969	3.2199063072727063	3.4032064149536341	3.6851109802418458	4.1647473331205669	4.9747774858001712	6.159037246281164	7.4889578102853456	8.5902773677041466	9.3081584773362813	9.7273044930883295	9.9777966494939285	10.182282979461473	10.349681065578981	10.500777840166768	10.644803870103122	10.785780412170531	10.925444994121214	11.064545736939598	11.203404269498231	11.342158775282766	11.480868606398639	11.619559252509221	11.758241659974679	11.896920529530089	Outlet Temperature (°C)


Energy Stored (kWh)
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Energy Stored (kWh)




Unit 2	20	20.100000000000001	20.2	20.3	20.399999999999999	20.5	20.6	20.7	20.8	20.9	21	21.1	21.2	21.3	21.4	21.5	21.6	21.7	21.8	21.9	22	22.1	22.2	22.3	22.4	22.5	22.6	22.7	22.8	22.9	23	23.1	23.2	23.3000000000001	23.4	23.5	23.600000000000101	23.7	23.8000000000001	23.900000000000102	24.000000000000099	24.100000000000101	24.200000000000099	24.3000000000001	24.400000000000102	24.500000000000099	24.600000000000101	24.700000000000099	24.8000000000001	24.900000000000102	25.000000000000099	25.100000000000101	25.200000000000099	25.3000000000001	25.400000000000102	25.500000000000099	25.600000000000101	25.700000000000099	25.8000000000001	25.900000000000102	26.000000000000099	26.100000000000101	26.200000000000099	26.3000000000001	26.400000000000102	26.500000000000099	26.600000000000101	26.700000000000099	26.8000000000001	26.900000000000102	27.000000000000099	27.100000000000101	27.200000000000099	27.3000000000001	27.400000000000102	27.500000000000099	27.600000000000101	27.700000000000099	27.8000000000001	27.900000000000102	28.000000000000099	28.100000000000101	28.200000000000099	28.3000000000001	28.400000000000102	28.500000000000099	28.600000000000101	28.700000000000099	28.8000000000001	28.900000000000102	29.000000000000099	29.100000000000101	29.200000000000099	29.3000000000001	29.400000000000102	29.500000000000099	29.600000000000101	29.700000000000099	29.8000000000001	29.900000000000102	30.000000000000099	30.100000000000101	30.200000000000099	30.3000000000001	30.400000000000102	30.500000000000099	30.6000000000002	30.700000000000198	30.8000000000002	30.900000000000201	31.000000000000199	31.1000000000002	31.200000000000198	31.3000000000002	31.400000000000201	31.500000000000199	31.6000000000002	31.700000000000198	31.8000000000002	31.900000000000201	32.000000000000199	32.1000000000002	32.200000000000202	32.300000000000203	32.400000000000198	32.500000000000199	32.6000000000002	32.700000000000202	32.800000000000203	32.900000000000198	33.000000000000199	33.1000000000002	33.200000000000202	33.300000000000203	33.400000000000198	33.500000000000199	33.6000000000002	33.700000000000202	33.800000000000203	33.900000000000198	34.000000000000199	34.1000000000002	34.200000000000202	34.300000000000203	34.400000000000198	34.500000000000199	34.6000000000002	34.700000000000202	34.800000000000203	34.900000000000198	35.000000000000199	35.1000000000002	35.200000000000202	35.300000000000203	35.400000000000198	35.500000000000199	35.6000000000002	35.700000000000202	35.800000000000203	35.900000000000198	36.000000000000199	36.1000000000002	36.200000000000202	36.300000000000203	36.400000000000198	36.500000000000199	36.6000000000002	36.700000000000202	36.800000000000203	36.900000000000198	37.000000000000199	37.1000000000002	37.200000000000202	37.300000000000203	37.400000000000198	37.500000000000199	37.6000000000003	37.700000000000301	37.800000000000303	37.900000000000297	38.000000000000298	38.1000000000003	38.200000000000301	38.300000000000303	38.400000000000297	38.500000000000298	38.6000000000003	38.700000000000301	38.800000000000303	38.900000000000297	39.000000000000298	39.1000000000003	39.200000000000301	39.300000000000303	39.400000000000297	39.500000000000298	39.6000000000003	39.700000000000301	39.800000000000303	39.900000000000297	40.000000000000298	40.1000000000003	40.200000000000301	40.300000000000303	40.400000000000297	40.500000000000298	40.6000000000003	40.700000000000301	40.800000000000303	40.900000000000297	41.000000000000298	41.1000000000003	41.200000000000301	41.300000000000303	41.400000000000297	41.500000000000298	41.6000000000003	41.700000000000301	41.800000000000303	41.900000000000297	42.000000000000298	42.1000000000003	42.200000000000301	42.300000000000303	42.400000000000297	42.500000000000298	42.6000000000003	42.700000000000301	42.800000000000303	42.900000000000297	43.000000000000298	43.1000000000003	43.200000000000301	43.300000000000303	43.400000000000297	43.500000000000298	43.6000000000003	43.700000000000301	43.800000000000303	43.900000000000297	44.000000000000298	44.1000000000003	44.200000000000301	44.300000000000303	44.400000000000297	44.500000000000298	44.6000000000003	44.700000000000401	44.800000000000402	44.900000000000396	45.000000000000398	45.100000000000399	45.200000000000401	45.300000000000402	45.400000000000396	45.500000000000398	45.600000000000399	45.700000000000401	45.800000000000402	45.900000000000396	46.000000000000398	46.100000000000399	46.200000000000401	46.300000000000402	46.400000000000396	46.500000000000398	46.600000000000399	46.700000000000401	46.800000000000402	46.900000000000396	47.000000000000398	47.100000000000399	47.200000000000401	47.300000000000402	47.400000000000396	47.500000000000398	47.600000000000399	47.700000000000401	47.800000000000402	47.900000000000396	48.000000000000398	48.100000000000399	48.200000000000401	48.300000000000402	48.400000000000396	48.500000000000398	48.600000000000399	48.700000000000401	48.800000000000402	48.900000000000396	49.000000000000398	49.100000000000399	49.200000000000401	49.300000000000402	49.400000000000396	49.500000000000398	49.600000000000399	49.700000000000401	49.800000000000402	49.900000000000396	50.000000000000398	50.100000000000399	50.200000000000401	50.300000000000402	50.400000000000396	50.500000000000398	50.600000000000399	50.700000000000401	50.800000000000402	50.900000000000396	51.000000000000398	51.100000000000399	51.200000000000401	51.300000000000402	51.400000000000396	51.500000000000398	51.600000000000399	51.7000000000005	51.800000000000502	51.900000000000503	52.000000000000497	52.100000000000499	52.2000000000005	52.300000000000502	52.400000000000503	52.500000000000497	52.600000000000499	52.7000000000005	52.800000000000502	52.900000000000503	53.000000000000497	53.100000000000499	53.2000000000005	53.300000000000502	53.400000000000503	53.500000000000497	53.600000000000499	53.7000000000005	53.800000000000502	53.900000000000503	54.000000000000497	54.100000000000499	54.2000000000005	54.300000000000502	54.400000000000503	54.500000000000497	54.600000000000499	54.7000000000005	54.800000000000502	54.900000000000503	55.000000000000497	55.100000000000499	55.2000000000005	55.300000000000502	55.400000000000503	55.500000000000497	55.600000000000499	55.7000000000005	55.800000000000502	55.900000000000503	56.000000000000497	56.100000000000499	56.2000000000005	56.300000000000502	56.400000000000503	56.500000000000497	56.600000000000499	56.7000000000005	56.800000000000502	56.900000000000503	57.000000000000497	57.100000000000499	57.2000000000005	57.300000000000502	57.400000000000503	57.500000000000497	57.600000000000499	57.7000000000005	57.800000000000502	57.900000000000503	58.000000000000497	58.100000000000499	58.2000000000005	58.300000000000502	58.400000000000503	58.500000000000497	58.600000000000499	58.7000000000005	58.800000000000601	58.900000000000603	59.000000000000597	59.100000000000598	59.2000000000006	59.300000000000601	59.400000000000603	59.500000000000597	59.600000000000598	59.7000000000006	59.800000000000601	59.900000000000603	60.000000000000597	60.100000000000598	60.2000000000006	60.300000000000601	60.400000000000603	60.500000000000597	60.600000000000598	60.7000000000006	60.800000000000601	60.900000000000603	61.000000000000597	61.100000000000598	61.2000000000006	61.300000000000601	61.400000000000603	61.500000000000597	61.600000000000598	61.7000000000006	61.800000000000601	61.900000000000603	62.000000000000597	62.100000000000598	62.2000000000006	62.300000000000601	62.400000000000603	62.500000000000597	62.600000000000598	62.7000000000006	62.800000000000601	62.900000000000603	63.000000000000597	63.100000000000598	63.2000000000006	63.300000000000601	63.400000000000603	63.500000000000597	63.600000000000598	63.7000000000006	63.800000000000601	63.900000000000603	64.000000000000597	64.100000000000605	64.2000000000006	64.300000000000594	64.400000000000603	64.500000000000597	64.600000000000605	64.7000000000006	64.800000000000594	64.900000000000603	65.000000000000597	65.100000000000605	65.2000000000006	65.300000000000594	65.400000000000603	65.500000000000597	65.600000000000605	65.7000000000006	65.800000000000693	65.900000000000702	66.000000000000696	66.100000000000705	66.200000000000699	66.300000000000693	66.400000000000702	66.500000000000696	66.600000000000705	66.700000000000699	66.800000000000693	66.900000000000702	67.000000000000696	67.100000000000705	67.200000000000699	67.300000000000693	67.400000000000702	67.500000000000696	67.600000000000705	67.700000000000699	67.800000000000693	67.900000000000702	68.000000000000696	68.100000000000705	68.200000000000699	68.300000000000693	68.400000000000702	68.500000000000696	68.600000000000705	68.700000000000699	68.800000000000693	68.900000000000702	69.000000000000696	69.100000000000705	69.200000000000699	69.300000000000693	69.400000000000702	69.500000000000696	69.600000000000705	69.700000000000699	69.800000000000693	69.900000000000702	70.000000000000696	70.100000000000705	70.200000000000699	70.300000000000693	70.400000000000702	70.500000000000696	70.600000000000705	70.700000000000699	70.800000000000693	70.900000000000702	71.000000000000696	71.100000000000705	71.200000000000699	71.300000000000693	71.400000000000702	71.500000000000696	71.600000000000705	71.700000000000699	71.800000000000693	71.900000000000702	72.000000000000696	72.100000000000705	72.200000000000699	72.300000000000693	72.400000000000702	72.500000000000696	72.600000000000705	72.700000000000699	72.800000000000793	72.900000000000801	73.000000000000796	-3.3832743010732079E-3	-2.500956724870042E-3	-1.6186391482339985E-3	-7.3632157113829189E-4	1.4599600644539594E-4	1.0283135845472523E-3	1.910631163199237E-3	2.7929487424352838E-3	3.6752663222915129E-3	4.5575839028061524E-3	5.4399014840199105E-3	6.3222190659759491E-3	7.2045366487200049E-3	8.0868542323008184E-3	8.9691718167699917E-3	9.8514894021824277E-3	1.0733806988596334E-2	1.1616124576073507E-2	1.2498442164679652E-2	1.3380759754484408E-2	1.4263077345561837E-2	1.5145394937990478E-2	1.6027712531853724E-2	1.6910030127240207E-2	1.7792347724243904E-2	1.8674665322964721E-2	1.9556982923508669E-2	2.0439300525988208E-2	2.132161813052294E-2	2.2203935737239677E-2	2.3086253346273199E-2	2.3968570957766507E-2	2.4850888571871434E-2	2.5733206188750146E-2	2.6615523808571157E-2	2.7497841431518913E-2	2.8380159057786361E-2	2.9262476687575749E-2	3.0144794321108188E-2	3.1027111958611988E-2	3.1909429600333244E-2	3.2791747246532416E-2	3.3674064897485839E-2	3.4556382553487135E-2	3.5438700214847907E-2	3.6321017881899002E-2	3.7203335554991807E-2	3.808565323449925E-2	3.8967970920817434E-2	3.9850288614366791E-2	4.0732606315593729E-2	4.161492402497232E-2	4.2497241743005773E-2	4.3379559470228458E-2	4.4261877207207694E-2	4.5144194954545809E-2	4.6026512712882349E-2	4.6908830482896305E-2	4.7791148265308676E-2	4.8673466060884886E-2	4.955578387043761E-2	5.043810169482979E-2	5.1320419534977527E-2	5.2202737391853583E-2	5.3085055266490717E-2	5.396737315998542E-2	5.4849691073501988E-2	5.5732009008276455E-2	5.6614326965621319E-2	5.749664494693002E-2	5.8378962953681932E-2	5.9261280987447977E-2	6.0143599049895878E-2	6.1025917142796468E-2	6.1908235268029785E-2	6.2790553427591961E-2	6.3672871623602453E-2	6.4555189858311449E-2	6.543750813410816E-2	6.631982645352924E-2	6.7202144819267923E-2	6.8084463234183837E-2	6.8966781701313012E-2	6.9849100223879051E-2	7.0731418805304494E-2	7.1613737449223128E-2	7.2496056159493241E-2	7.3378374940211155E-2	7.4260693795726251E-2	7.5143012730656336E-2	7.6025331749904251E-2	7.6907650858675708E-2	7.7789970062497618E-2	7.8672289367238274E-2	7.9554608779128122E-2	8.0436928304782343E-2	8.1319247951224555E-2	8.2201567725911903E-2	8.3083887636762013E-2	8.3966207692181299E-2	8.4848527901095053E-2	8.5730848272979832E-2	8.6613168817897088E-2	8.7495489546529456E-2	8.8377810470219129E-2	8.9260131601008486E-2	9.0142452951684479E-2	9.1024774535820391E-2	9.1907096367830662E-2	9.2789418463018469E-2	9.3671740837631814E-2	9.4554063508921884E-2	9.5436386495204778E-2	9.6318709815927619E-2	9.7201033491737934E-2	9.8083357544558089E-2	9.8965681997663854E-2	9.9848006875767975E-2	0.10073033220510903	0.10161265801354537	0.10249498433065529	0.10337731118784323	0.1042596386184524	0.10514196665788463	0.10602429534372722	0.10690662471588828	0.10778895481673959	0.10867128569126881	0.10955361738724118	0.11043594995537066	0.11131828344950247	0.11220061792680584	0.1130829534479796	0.11396529007746993	0.11484762788370174	0.11572996693932451	0.11661230732147276	0.11749464911204303	0.11837699239798809	0.11925933727162882	0.12014168383098599	0.12102403218013166	0.12190638242956313	0.12278873469659948	0.12367108910580273	0.12455344578942512	0.12543580488788367	0.12631816655026434	0.12720053093485723	0.12808289820972477	0.12896526855330523	0.1298476421550529	0.13073001921611846	0.13161239995007096	0.13249478458366448	0.13337717335765226	0.13425956652765067	0.13514196436505704	0.13602436715802368	0.13690677521249231	0.13778918885329261	0.13867160842530765	0.1395540342947123	0.14043646685028757	0.14131890650481604	0.14220135369656386	0.14308380889085348	0.14396627258173422	0.14484874529375569	0.14573122758385035	0.14661372004333295	0.14749622330002266	0.14837873802049659	0.14926126491248248	0.15014380472739877	0.15102635826305177	0.15190892636649989	0.15279150993709029	0.15367410992969208	0.1545567273581199	0.15543936329877336	0.15632201889449995	0.1572046953586968	0.15808739397966515	0.15897011612523368	0.15985286324766756	0.16073563688887937	0.16161843868596268	0.1625012703770663	0.16338413380763153	0.16426703093701384	0.16514996384551314	0.16603293474183789	0.16691594597102971	0.16779900002287634	0.16868209954084484	0.16956524733156375	0.17044844637489207	0.17133169983460811	0.17221501106975767	0.17309838364670255	0.17398182135191104	0.1748653282055378	0.17574890847584076	0.17663256669448654	0.17751630767279963	0.17840013651901263	0.1792840586565799	0.18016807984361971	0.18105220619355408	0.18193644419702046	0.18282080074513266	0.18370528315417461	0.18458989919181501	0.18547465710493552	0.1863595656491725	0.18724463412027645	0.18812987238740164	0.18901529092844363	0.18990090086755046	0.19078671401494082	0.19167274290916989	0.1925590008619934	0.19344550200598828	0.19433226134509923	0.19521929480828878	0.19610661930648124	0.19699425279300156	0.1978822143277216	0.19877052414514018	0.19965920372663665	0.20054827587715057	0.20143776480655828	0.20232769621603	0.20321809738967023	0.20410899729176146	0.20500042666994975	0.20589241816473167	0.20678500642562286	0.20767822823441051	0.20857212263591615	0.20946673107671948	0.21036209755232152	0.21125826876325096	0.21215529428064858	0.21305322672189481	0.21395212193687665	0.21485203920552731	0.21575304144729934	0.21665519544328901	0.21755857207173879	0.21846324655771479	0.21936929873778419	0.22027681334056529	0.2211858802840726	0.22209659499082637	0.22300905872174895	0.22392337892992342	0.22483966963534627	0.2257580518218629	0.22667865385753616	0.2276016119397587	0.22852707056648522	0.22945518303502627	0.23038611196991204	0.23132002988140554	0.23225711975631264	0.23319757568281069	0.23414160351108734	0.2350894215516551	0.23604126131327899	0.23699736828252577	0.23795800274701481	0.2389234406645174	0.23989397458011599	0.24086991459369728	0.24185158938010604	0.24283934726433803	0.24383355735418819	0.24483461073280222	0.24584292171359792	0.24685892916002486	0.2478830978726192	0.24891592004577767	0.249957916796615	0.25100963976818963	0.25207167280926329	0.25314463373261381	0.25422917615372415	0.25532599141143608	0.25643581057186271	0.25755940651650355	0.25869759611508591	0.25985124248316255	0.26102125732391085	0.26220860335290774	0.26341429680386735	0.26463941001243191	0.26588507407407463	0.26715248157099991	0.26844288936159527	0.26975762142448456	0.27109807174754458	0.27246570725034835	0.27386207072638774	0.27528878378907862	0.2767475498029488	0.27824015677854758	0.27976848020646411	0.28133448580240766	0.28294023213156072	0.28458787307637068	0.28627966010758826	0.28801794431370042	0.28980517813894829	0.2916439167748881	0.29353681914497282	0.29548664841594735	0.29749627196399892	0.29956866071771854	0.30170688779395088	0.30391412633687287	0.30619364646504543	0.30854881122604466	0.31098307145370824	0.31349995941926112	0.31610308116485719	0.31879610740664255	0.32158276289464505	0.32446681411890882	0.32745205525571364	0.33054229225478993	0.33374132497855186	0.33705292731791303	0.34048082522657508	0.34402867263714948	0.3477000252483835	0.35149831220332467	0.35542680571365448	0.35948858872562478	0.36368652076795677	0.36802320217139617	0.3725009369028533	0.37712169431349607	0.38188707015879131	0.38679824730811418	0.39185595662064171	0.39706043852107009	0.40241140586127383	0.40790800870015353	0.41354880167131403	0.41933171463448637	0.42525402731941175	0.43131234866808055	0.4375026015607888	0.44382001357194356	0.45025911434189536	0.45681374007091147	0.46347704554115537	0.47024152395334945	0.4770990347287985	0.48404083927753638	0.49105764457328716	0.49813965421019274	0.50527662644982663	0.51245793860533018	0.51967265695806608	0.52690961126638369	0.5341574728109646	0.54140483483108193	0.54864029414449156	0.55585253271296275	0.56303039791685727	0.57016298033566903	0.57723968789564617	0.58425031533809213	0.59118510807907332	0.59803481966862082	0.60479076221008587	0.61144484926262321	0.6179896309163474	0.62441832089516647	0.63072481570162642	0.636903705966954	0.64295028030410928	0.64886052207925649	0.65463109961560628	0.66025935042192996	0.66574326009594675	0.67108143659054043	0.67627308054970148	0.68131795242228166	0.68621633704775831	0.69096900638075864	0.69557718098287435	0.7000424908635059	0.70436693619844903	0.70855284839782595	0.71260285193576856	0.71651982729465846	0.72030687531825011	0.72481837658513615	0.72920667912108983	0.73347534831992567	0.73762804543118921	0.74166850153332875	0.74560049363597636	0.74942782289815735	0.75315429492373853	0.75678370207432777	0.76031980772285912	0.76376633235787006	0.76712694143864502	0.77040523489458179	0.7736047381579253	0.77672889461708372	0.77978105937770026	0.78276449422020344	0.78568236364539767	0.78853773190349685	0.79133356090663742	0.79407270893009929	0.79675793001304485	0.79939187397540779	0.80197708697347747	0.80451601252264815	0.80701099292162781	0.80946427101807117	0.81187799226106649	0.81425420699111017	0.81659487292313448	0.81890185778279379	0.82117694206053915	0.82342182185203172	0.82563811175716073	0.82782734781334211	0.8299909904418965	0.83213042738914145	0.83424697664642589	0.83634188933564235	0.83841635254886182	0.84047149213260997	0.84250837540896317	0.84452801382715681	0.84653136554068709	0.84851933790606715	0.85049278990041122	0.85245253445590452	0.85439934070999901	0.85633393617083331	0.85825700879795086	0.8601692089988886	0.86207115154259895	0.86396341739104265	0.86584655545055089	0.86772108424480621	0.8695874935114738	0.87144624572465812	0.8732977775454851	0.8751425012031635	0.87698080580898419	0.87881305860567915	0.88063960615463444	0.88246077546341606	0.88427687505604968	0.88608819598847322	0.88789501281153449	0.8896975844838545	0.89149615523683001	0.89329095539397352	0.89508220214674061	0.89687010028891279	0.8986548429115373	0.90043661206036241	0.90221557935761687	0.90399190658992712	0.90576574626408501	0.90753724213230491	0.9093065296885473	0.91107373663740998	0.91283898333701974	0.91460238321730103	0.9163640431749206	0.91812406394615731	0.91988254045887763	0.92163956216474774	0.92339521335274777	0.92514957344500848	0.92690271727593876	0.92865471535555488	0.93040563411788446	0.93215553615527258	0.93390448043936247	0.93565252252950304	0.93739971476927419	0.9391461064717973	0.94089174409446252	0.94263667140366036	0.94438092963008502	0.94612455761514047	0.94786759194894721	0.94961006710043239	0.95135201553994353	0.95309346785481897	0.95483445285830759	0.95657499769221987	0.95831512792367002	0.96005486763623871	0.9617942395158855	0.96353326493190183	0.96527196401319326	0.96701035572015781	0.96874845791241249	0.97048628741260612	0.97222386006654593	0.973961190799842	0.97569829367128147	0.97743518192311085	0.97917186802840894	0.98090836373571766	0.98264468011108741	0.98438082757768874	0.98611681595312639	0.98785265448459536	0.98958835188199468	0.99132391634912442	0.99305935561307423	0.99479467695190427	0.99652988722072733	0.99826499287626558	1	Unit 1	20	20.100000000000001	20.2	20.3	20.399999999999999	20.5	20.6	20.7	20.8	20.9	21	21.1	21.2	21.3	21.4	21.5	21.6	21.7	21.8	21.9	22	22.1	22.2	22.3	22.4	22.5	22.6	22.7	22.8	22.9	23	23.1	23.2	23.3000000000001	23.4	23.5	23.600000000000101	23.7	23.8000000000001	23.900000000000102	24.000000000000099	24.100000000000101	24.200000000000099	24.3000000000001	24.400000000000102	24.500000000000099	24.600000000000101	24.700000000000099	24.8000000000001	24.900000000000102	25.000000000000099	25.100000000000101	25.200000000000099	25.3000000000001	25.400000000000102	25.500000000000099	25.600000000000101	25.700000000000099	25.8000000000001	25.900000000000102	26.000000000000099	26.100000000000101	26.200000000000099	26.3000000000001	26.400000000000102	26.500000000000099	26.600000000000101	26.700000000000099	26.8000000000001	26.900000000000102	27.000000000000099	27.100000000000101	27.200000000000099	27.3000000000001	27.400000000000102	27.500000000000099	27.600000000000101	27.700000000000099	27.8000000000001	27.900000000000102	28.000000000000099	28.100000000000101	28.200000000000099	28.3000000000001	28.400000000000102	28.500000000000099	28.600000000000101	28.700000000000099	28.8000000000001	28.900000000000102	29.000000000000099	29.100000000000101	29.200000000000099	29.3000000000001	29.400000000000102	29.500000000000099	29.600000000000101	29.700000000000099	29.8000000000001	29.900000000000102	30.000000000000099	30.100000000000101	30.200000000000099	30.3000000000001	30.400000000000102	30.500000000000099	30.6000000000002	30.700000000000198	30.8000000000002	30.900000000000201	31.000000000000199	31.1000000000002	31.200000000000198	31.3000000000002	31.400000000000201	31.500000000000199	31.6000000000002	31.700000000000198	31.8000000000002	31.900000000000201	32.000000000000199	32.1000000000002	32.200000000000202	32.300000000000203	32.400000000000198	32.500000000000199	32.6000000000002	32.700000000000202	32.800000000000203	32.900000000000198	33.000000000000199	33.1000000000002	33.200000000000202	33.300000000000203	33.400000000000198	33.500000000000199	33.6000000000002	33.700000000000202	33.800000000000203	33.900000000000198	34.000000000000199	34.1000000000002	34.200000000000202	34.300000000000203	34.400000000000198	34.500000000000199	34.6000000000002	34.700000000000202	34.800000000000203	34.900000000000198	35.000000000000199	35.1000000000002	35.200000000000202	35.300000000000203	35.400000000000198	35.500000000000199	35.6000000000002	35.700000000000202	35.800000000000203	35.900000000000198	36.000000000000199	36.1000000000002	36.200000000000202	36.300000000000203	36.400000000000198	36.500000000000199	36.6000000000002	36.700000000000202	36.800000000000203	36.900000000000198	37.000000000000199	37.1000000000002	37.200000000000202	37.300000000000203	37.400000000000198	37.500000000000199	37.6000000000003	37.700000000000301	37.800000000000303	37.900000000000297	38.000000000000298	38.1000000000003	38.200000000000301	38.300000000000303	38.400000000000297	38.500000000000298	38.6000000000003	38.700000000000301	38.800000000000303	38.900000000000297	39.000000000000298	39.1000000000003	39.200000000000301	39.300000000000303	39.400000000000297	39.500000000000298	39.6000000000003	39.700000000000301	39.800000000000303	39.900000000000297	40.000000000000298	40.1000000000003	40.200000000000301	40.300000000000303	40.400000000000297	40.500000000000298	40.6000000000003	40.700000000000301	40.800000000000303	40.900000000000297	41.000000000000298	41.1000000000003	41.200000000000301	41.300000000000303	41.400000000000297	41.500000000000298	41.6000000000003	41.700000000000301	41.800000000000303	41.900000000000297	42.000000000000298	42.1000000000003	42.200000000000301	42.300000000000303	42.400000000000297	42.500000000000298	42.6000000000003	42.700000000000301	42.800000000000303	42.900000000000297	43.000000000000298	43.1000000000003	43.200000000000301	43.300000000000303	43.400000000000297	43.500000000000298	43.6000000000003	43.700000000000301	43.800000000000303	43.900000000000297	44.000000000000298	44.1000000000003	44.200000000000301	44.300000000000303	44.400000000000297	44.500000000000298	44.6000000000003	44.700000000000401	44.800000000000402	44.900000000000396	45.000000000000398	45.100000000000399	45.200000000000401	45.300000000000402	45.400000000000396	45.500000000000398	45.600000000000399	45.700000000000401	45.800000000000402	45.900000000000396	46.000000000000398	46.100000000000399	46.200000000000401	46.300000000000402	46.400000000000396	46.500000000000398	46.600000000000399	46.700000000000401	46.800000000000402	46.900000000000396	47.000000000000398	47.100000000000399	47.200000000000401	47.300000000000402	47.400000000000396	47.500000000000398	47.600000000000399	47.700000000000401	47.800000000000402	47.900000000000396	48.000000000000398	48.100000000000399	48.200000000000401	48.300000000000402	48.400000000000396	48.500000000000398	48.600000000000399	48.700000000000401	48.800000000000402	48.900000000000396	49.000000000000398	49.100000000000399	49.200000000000401	49.300000000000402	49.400000000000396	49.500000000000398	49.600000000000399	49.700000000000401	49.800000000000402	49.900000000000396	50.000000000000398	50.100000000000399	50.200000000000401	50.300000000000402	50.400000000000396	50.500000000000398	50.600000000000399	50.700000000000401	50.800000000000402	50.900000000000396	51.000000000000398	51.100000000000399	51.200000000000401	51.300000000000402	51.400000000000396	51.500000000000398	51.600000000000399	51.7000000000005	51.800000000000502	51.900000000000503	52.000000000000497	52.100000000000499	52.2000000000005	52.300000000000502	52.400000000000503	52.500000000000497	52.600000000000499	52.7000000000005	52.800000000000502	52.900000000000503	53.000000000000497	53.100000000000499	53.2000000000005	53.300000000000502	53.400000000000503	53.500000000000497	53.600000000000499	53.7000000000005	53.800000000000502	53.900000000000503	54.000000000000497	54.100000000000499	54.2000000000005	54.300000000000502	54.400000000000503	54.500000000000497	54.600000000000499	54.7000000000005	54.800000000000502	54.900000000000503	55.000000000000497	55.100000000000499	55.2000000000005	55.300000000000502	55.400000000000503	55.500000000000497	55.600000000000499	55.7000000000005	55.800000000000502	55.900000000000503	56.000000000000497	56.100000000000499	56.2000000000005	56.300000000000502	56.400000000000503	56.500000000000497	56.600000000000499	56.7000000000005	56.800000000000502	56.900000000000503	57.000000000000497	57.100000000000499	57.2000000000005	57.300000000000502	57.400000000000503	57.500000000000497	57.600000000000499	57.7000000000005	57.800000000000502	57.900000000000503	58.000000000000497	58.100000000000499	58.2000000000005	58.300000000000502	58.400000000000503	58.500000000000497	58.600000000000499	58.7000000000005	58.800000000000601	58.900000000000603	59.000000000000597	59.100000000000598	59.2000000000006	59.300000000000601	59.400000000000603	59.500000000000597	59.600000000000598	59.7000000000006	59.800000000000601	59.900000000000603	60.000000000000597	60.100000000000598	60.2000000000006	60.300000000000601	60.400000000000603	60.500000000000597	60.600000000000598	60.7000000000006	60.800000000000601	60.900000000000603	61.000000000000597	61.100000000000598	61.2000000000006	61.300000000000601	61.400000000000603	61.500000000000597	61.600000000000598	61.7000000000006	61.800000000000601	61.900000000000603	62.000000000000597	62.100000000000598	62.2000000000006	62.300000000000601	62.400000000000603	62.500000000000597	62.600000000000598	62.7000000000006	62.800000000000601	62.900000000000603	63.000000000000597	63.100000000000598	63.2000000000006	63.300000000000601	63.400000000000603	63.500000000000597	63.600000000000598	63.7000000000006	63.800000000000601	63.900000000000603	64.000000000000597	64.100000000000605	64.2000000000006	64.300000000000594	64.400000000000603	64.500000000000597	64.600000000000605	64.7000000000006	64.800000000000594	64.900000000000603	65.000000000000597	65.100000000000605	65.2000000000006	65.300000000000594	65.400000000000603	65.500000000000597	65.600000000000605	65.7000000000006	65.800000000000693	65.900000000000702	66.000000000000696	66.100000000000705	66.200000000000699	66.300000000000693	66.400000000000702	66.500000000000696	66.600000000000705	66.700000000000699	66.800000000000693	66.900000000000702	67.000000000000696	67.100000000000705	67.200000000000699	67.300000000000693	67.400000000000702	67.500000000000696	67.600000000000705	67.700000000000699	67.800000000000693	67.900000000000702	68.000000000000696	68.100000000000705	68.200000000000699	68.300000000000693	68.400000000000702	68.500000000000696	68.600000000000705	68.700000000000699	68.800000000000693	68.900000000000702	69.000000000000696	69.100000000000705	69.200000000000699	69.300000000000693	69.400000000000702	69.500000000000696	69.600000000000705	69.700000000000699	69.800000000000693	69.900000000000702	70.000000000000696	70.100000000000705	70.200000000000699	70.300000000000693	70.400000000000702	70.500000000000696	70.600000000000705	70.700000000000699	70.800000000000693	70.900000000000702	71.000000000000696	71.100000000000705	71.200000000000699	71.300000000000693	71.400000000000702	71.500000000000696	71.600000000000705	71.700000000000699	71.800000000000693	71.900000000000702	72.000000000000696	72.100000000000705	72.200000000000699	72.300000000000693	72.400000000000702	72.500000000000696	72.600000000000705	72.700000000000699	72.800000000000793	72.900000000000801	73.000000000000796	6.1408322194857244E-3	7.0051414492269285E-3	7.8694506789684562E-3	8.733759908710453E-3	9.5980691384528836E-3	1.0462378368195866E-2	1.1326687597939405E-2	1.2190996827683551E-2	1.3055306057428356E-2	1.3919615287173843E-2	1.4783924516920153E-2	1.5648233746667312E-2	1.651254297641536E-2	1.737685220616449E-2	1.8241161435914643E-2	1.9105470665666025E-2	1.9969779895418711E-2	2.0834089125172768E-2	2.1698398354928407E-2	2.2562707584685714E-2	2.3427016814444843E-2	2.4291326044205953E-2	2.515563527396919E-2	2.6019944503734804E-2	2.6884253733502936E-2	2.7748562963273927E-2	2.8612872193047902E-2	2.9477181422825134E-2	3.0341490652605985E-2	3.1205799882390698E-2	3.2070109112179682E-2	3.293441834197329E-2	3.3798727571771922E-2	3.4663036801576876E-2	3.552734603138602E-2	3.6391655261202541E-2	3.7255964491026965E-2	3.8120273720857328E-2	3.8984582950697753E-2	3.9848892180546401E-2	4.0713201410404888E-2	4.1577510640274165E-2	4.2441819870155099E-2	4.3306129100048794E-2	4.4170438329956388E-2	4.503474755987897E-2	4.5899056789818003E-2	4.6763366019774849E-2	4.7627675249751152E-2	4.8491984479748604E-2	4.9356293709769045E-2	5.0220602939814528E-2	5.1084912169887212E-2	5.1949221399989573E-2	5.2813530630124193E-2	5.3677839860293876E-2	5.454214909050184E-2	5.5406458320751285E-2	5.6270767551046021E-2	5.7135076781389967E-2	5.7999386011787446E-2	5.8863695242243254E-2	5.9728004472762497E-2	6.0592313703350775E-2	6.1456622934014153E-2	6.232093216475925E-2	6.3185241395593339E-2	6.4049550626524177E-2	6.4913859857560444E-2	6.5778169088711286E-2	6.6642478319986848E-2	6.750678755139819E-2	6.8371096782957205E-2	6.9235406014676995E-2	7.0099715246571728E-2	7.0964024478656809E-2	7.182833371094903E-2	7.2692642943466626E-2	7.3556952176229567E-2	7.4421261409259434E-2	7.5285570642579805E-2	7.6149879876216256E-2	7.7014189110196668E-2	7.7878498344551447E-2	7.8742807579313567E-2	7.960711681451893E-2	8.0471426050206699E-2	8.1335735286419394E-2	8.2200044523203328E-2	8.3064353760608861E-2	8.3928662998690798E-2	8.4792972237508868E-2	8.5657281477127992E-2	8.6521590717618807E-2	8.7385899959058183E-2	8.8250209201529789E-2	8.9114518445124732E-2	8.9978827689942031E-2	9.0843136936089572E-2	9.1707446183684677E-2	9.2571755432854924E-2	9.343606468373937E-2	9.4300373936489143E-2	9.5164683191268876E-2	9.6028992448257536E-2	9.6893301707649995E-2	9.7757610969659126E-2	9.862192023451391E-2	9.948622950246637E-2	0.1003505387737897	0.10121484804878117	0.10207915732776446	0.10294346661109155	0.10380777589914564	0.10467208519234371	0.10553639449113941	0.10640070379602656	0.10726501310754245	0.10812932242627177	0.10899363175285075	0.10985794108797178	0.1107222504323884	0.11158655978692046	0.11245086915246023	0.11331517852997861	0.11417948792053227	0.11504379732527095	0.11590810674544587	0.11677241618241857	0.11763672563767072	0.11850103511281472	0.1193653446096051	0.12022965412995125	0.12109396367593088	0.12195827324980499	0.12282258285403418	0.12368689249129583	0.12455120216450363	0.12541551187682826	0.12627982163171994	0.12714413143293357	0.12800844128455485	0.12887275119103012	0.12973706115719782	0.13060137118832305	0.13146568129013564	0.13232999146887056	0.13319430173131283	0.1340586120848459	0.13492292253750454	0.13578723309803228	0.13665154377594377	0.13751585458159293	0.13838016552624707	0.13924447662216716	0.14010878788269587	0.14097309932235261	0.14183741095693755	0.14270172280364452	0.14356603488118386	0.1444303472099166	0.14529465981199929	0.14615897271154313	0.14702328593478589	0.14788759951027974	0.14875191346909547	0.14961622784504428	0.15048054267491981	0.15134485799876099	0.15220917386013857	0.15307349030646655	0.15393780738934099	0.15480212516490907	0.15566644369427043	0.15653076304391411	0.15739508328619389	0.15825940449984643	0.1591237267705507	0.15998805019154586	0.16085237486429421	0.16171670089920792	0.16258102841643782	0.16344535754673289	0.1643096884323749	0.16517402122819561	0.16603835610268389	0.16690269323919024	0.16776703283723768	0.16863137511394827	0.16949572030559523	0.17036006866929282	0.17122442048483377	0.17208877605668993	0.17295313571618953	0.17381749982388531	0.17468186877213276	0.1755462429878952	0.1764106229357959	0.17727500912144048	0.17813940209503099	0.17900380245530007	0.1798682108537914	0.18073262799951723	0.18159705466402801	0.18246149168692768	0.1833259399818771	0.18419040054312469	0.18505487445261526	0.18591936288772487	0.18678386712967729	0.18764838857270408	0.18851292873401107	0.18937748926462514	0.19024207196119636	0.19110667877884216	0.19197131184512306	0.19283597347525153	0.19370066618864226	0.19456539272692069	0.19543015607352121	0.19629495947501208	0.19715980646430115	0.19802470088588825	0.19888964692334304	0.19975464912920629	0.20061971245752724	0.20148484229926872	0.20235004452083463	0.20321532550599236	0.20408069220149153	0.20494615216670306	0.20581171362763312	0.20667738553569734	0.2075431776316744	0.20840910051529488	0.20927516572096092	0.21014138580013694	0.2110077744109975	0.21187434641597175	0.21274111798787737	0.21360810672540065	0.21447533177874306	0.21534281398632749	0.21621057602353674	0.21707864256453871	0.21794704045834867	0.21881579892037603	0.21968494974081443	0.22055452751134666	0.2214245698717803	0.22229511777834152	0.22316621579553408	0.22403791241361881	0.22491026039394915	0.22578331714459648	0.22665714512890187	0.22753181230982281	0.22840739263318791	0.22928396655323699	0.23016162160411652	0.23104045302130768	0.23192056441730577	0.23280206851623161	0.23368508795245191	0.23456975613870881	0.23545621820971821	0.23634463204769207	0.23723516939676914	0.2381280170739149	0.23902337828446141	0.23992147405112263	0.24082254476602191	0.24172685187602905	0.24263467971250785	0.24354633747743498	0.24446216139876686	0.24538251706889735	0.24630780198107391	0.24723844827972083	0.24817492574174577	0.24911774500709438	0.25006746107804134	0.25102467710797893	0.25199004850176637	0.25296428735101983	0.25394816722905839	0.25494252837152964	0.25594828327002545	0.2569664227072081	0.2579980222630851	0.25904424932304276	0.26010637061901709	0.26118576033570279	0.26228390881386654	0.2634024318825855	0.26454308085144002	0.26570775319223328	0.26689850393755166	0.26811755782021873	0.26936732217325932	0.27065040060412332	0.27196960744936777	0.27332798300645167	0.27472880952741685	0.2761756279446273	0.27767225528099199	0.27922280267572613	0.28083169393121654	0.28250368445638635	0.28424388044655091	0.28605775809852474	0.28795118261210734	0.28993042667450819	0.29200218806227929	0.29417360592557334	0.29645227524183682	0.29884625884046306	0.30136409630688332	0.30401480897489497	0.3068079001112482	0.30975334928857828	0.31286159983501288	0.31614353814495988	0.31961046354116163	0.32327404729960357	0.32714627939438617	0.33123940149880654	0.33556582480270564	0.34013803128703585	0.34496845724796033	0.3500693580984473	0.35545265380875984	0.36112975479047549	0.36711136859096072	0.37340728845123655	0.38002616558826324	0.38697526798273052	0.39426022946494765	0.4018847939619038	0.40985056085226784	0.41815673841414841	0.42679991327180777	0.43577384447187484	0.44506929126194084	0.45467388372126977	0.46457204503101163	0.4747449733145232	0.48517068959960952	0.49582415656200796	0.50667747035290589	0.51770012508649055	0.52885934660162737	0.54012048908432786	0.55144748523643716	0.56280333809860417	0.57415064056760612	0.58545210724405095	0.59667110261408784	0.60777214975726013	0.6187214047672327	0.62948708379593676	0.64003983195374947	0.65035302604776513	0.66040300612369685	0.67016923379720528	0.67963437823419548	0.68878433321170152	0.6976081708445353	0.70609803922437198	0.714249012356998	0.72205890140915518	0.72952803642998754	0.73665902745839718	0.74345651334587448	0.74992690579963461	0.75607813516674816	0.76191940341292785	0.7674609486654409	0.77271382464123251	0.77768969730830262	0.78240066025759425	0.78685906950961337	0.79107739785071285	0.79506810828695318	0.7988435458117169	0.80241584639607744	0.80579686191548872	0.80899809960888247	0.81203067461305811	0.81490527411327163	0.81763213168850524	0.820221010496337	0.82268119402911377	0.82502148327252423	0.82725019920387033	0.82937518967564439	0.8314038398367859	0.83334308534669255	0.83519942773384159	0.83697895134059108	0.83868734137775103	0.84063124137801581	0.8425142562548642	0.84434098760375798	0.84611571410488728	0.84784241030304353	0.8495247649300226	0.85116619865935128	0.8527698812110821	0.8543387477479587	0.85587551452389754	0.85738269376199183	0.85886260775254886	0.86031740217244557	0.86174905863567375	0.86315940649169776	0.86455013389342961	0.86592279816049833	0.86727883546626805	0.86861956987893818	0.8699462217881837	0.87125991574933914	0.87256168777715093	0.87385249212080773	0.87513320755129953	0.87640464319129452	0.87766754391667634	0.87892259535771733	0.88017042852662131	0.88141162409686091	0.88264671635841585	0.88387619687169183	0.88510051784158095	0.88632009523184219	0.88753531163872634	0.88874651894155754	0.88995404074683027	0.89115817464126923	0.89235919426824162	0.89355735124092195	0.89475287690465577	0.89594598396008751	0.89713686795777736	0.89832570867425376	0.89951267137870872	0.90069790799886396	0.9018815581938967	0.90306375034171182	0.90424460244730576	0.90542422297843805	0.90660271163436423	0.90778016005292805	0.90895665246090529	0.91013226627211385	0.91130707263744648	0.91248113695066246	0.91365451931347075	0.91482727496315752	0.91599945466576016	0.91717110507754185	0.91834226907731964	0.91951298607197518	0.92068329227730505	0.92185322097619993	0.92302280275596771	0.92419206572648427	0.92536103572071648	0.92652973647903314	0.92769818981861918	0.92886641578918572	0.93003443281608822	0.93120225783186583	0.93236990639713868	0.9335373928117231	0.93470473021675049	0.93587193068852459	0.93703900532477824	0.93820596432394765	0.93937281705802844	0.94053957213953143	0.94170623748301541	0.94287282036164	0.94403932745913366	0.94520576491755526	0.94637213838118572	0.9475384530368649	0.94870471365106013	0.94987092460393063	0.95103708992063496	0.95220321330009894	0.95336929814145421	0.95453534756833436	0.95570136445120168	0.95686735142786605	0.95803331092234012	0.95919924516216626	0.96036515619434015	0.96153104589994431	0.96269691600759377	0.96386276810579596	0.96502860365430265	0.96619442399454925	0.96736023035924168	0.96852602388117159	0.96969180560131252	0.97085757647626203	0.97202333738508262	0.97318908913558322	0.97435483247009724	0.97552056807078769	0.97668629656452499	0.97785201852736869	0.97901773448868545	0.98018344493493414	0.98134915031314363	0.98251485103410829	0.98368054747532585	0.98484623998369492	0.98601192887799671	0.98717761445117358	0.98834329697242262	0.9895089766891213	0.99067465382859532	0.99184032859974458	0.99300600119453664	0.99417167178937826	0.99533734054637801	0.99650300761450428	0.99766867313065222	0.99883433722061665	1	Outlet Temperature (°C)


Energy Capacity (non-dimensional)




Charge Curve Fit	20	20.100000000000001	20.2	20.3	20.399999999999999	20.5	20.6	20.7	20.8	20.9	21	21.1	21.2	21.3	21.4	21.5	21.6	21.7	21.8	21.9	22	22.1	22.2	22.3	22.4	22.5	22.6	22.7	22.8	22.9	23	23.1	23.2	23.3000000000001	23.4	23.5	23.600000000000101	23.7	23.8000000000001	23.900000000000102	24.000000000000099	24.100000000000101	24.200000000000099	24.3000000000001	24.400000000000102	24.500000000000099	24.600000000000101	24.700000000000099	24.8000000000001	24.900000000000102	25.000000000000099	25.100000000000101	25.200000000000099	25.3000000000001	25.400000000000102	25.500000000000099	25.600000000000101	25.700000000000099	25.8000000000001	25.900000000000102	26.000000000000099	26.100000000000101	26.200000000000099	26.3000000000001	26.400000000000102	26.500000000000099	26.600000000000101	26.700000000000099	26.8000000000001	26.900000000000102	27.000000000000099	27.100000000000101	27.200000000000099	27.3000000000001	27.400000000000102	27.500000000000099	27.600000000000101	27.700000000000099	27.8000000000001	27.900000000000102	28.000000000000099	28.100000000000101	28.200000000000099	28.3000000000001	28.400000000000102	28.500000000000099	28.600000000000101	28.700000000000099	28.8000000000001	28.900000000000102	29.000000000000099	29.100000000000101	29.200000000000099	29.3000000000001	29.400000000000102	29.500000000000099	29.600000000000101	29.700000000000099	29.8000000000001	29.900000000000102	30.000000000000099	30.100000000000101	30.200000000000099	30.3000000000001	30.400000000000102	30.500000000000099	30.6000000000002	30.700000000000198	30.8000000000002	30.900000000000201	31.000000000000199	31.1000000000002	31.200000000000198	31.3000000000002	31.400000000000201	31.500000000000199	31.6000000000002	31.700000000000198	31.8000000000002	31.900000000000201	32.000000000000199	32.1000000000002	32.200000000000202	32.300000000000203	32.400000000000198	32.500000000000199	32.6000000000002	32.700000000000202	32.800000000000203	32.900000000000198	33.000000000000199	33.1000000000002	33.200000000000202	33.300000000000203	33.400000000000198	33.500000000000199	33.6000000000002	33.700000000000202	33.800000000000203	33.900000000000198	34.000000000000199	34.1000000000002	34.200000000000202	34.300000000000203	34.400000000000198	34.500000000000199	34.6000000000002	34.700000000000202	34.800000000000203	34.900000000000198	35.000000000000199	35.1000000000002	35.200000000000202	35.300000000000203	35.400000000000198	35.500000000000199	35.6000000000002	35.700000000000202	35.800000000000203	35.900000000000198	36.000000000000199	36.1000000000002	36.200000000000202	36.300000000000203	36.400000000000198	36.500000000000199	36.6000000000002	36.700000000000202	36.800000000000203	36.900000000000198	37.000000000000199	37.1000000000002	37.200000000000202	37.300000000000203	37.400000000000198	37.500000000000199	37.6000000000003	37.700000000000301	37.800000000000303	37.900000000000297	38.000000000000298	38.1000000000003	38.200000000000301	38.300000000000303	38.400000000000297	38.500000000000298	38.6000000000003	38.700000000000301	38.800000000000303	38.900000000000297	39.000000000000298	39.1000000000003	39.200000000000301	39.300000000000303	39.400000000000297	39.500000000000298	39.6000000000003	39.700000000000301	39.800000000000303	39.900000000000297	40.000000000000298	40.1000000000003	40.200000000000301	40.300000000000303	40.400000000000297	40.500000000000298	40.6000000000003	40.700000000000301	40.800000000000303	40.900000000000297	41.000000000000298	41.1000000000003	41.200000000000301	41.300000000000303	41.400000000000297	41.500000000000298	41.6000000000003	41.700000000000301	41.800000000000303	41.900000000000297	42.000000000000298	42.1000000000003	42.200000000000301	42.300000000000303	42.400000000000297	42.500000000000298	42.6000000000003	42.700000000000301	42.800000000000303	42.900000000000297	43.000000000000298	43.1000000000003	43.200000000000301	43.300000000000303	43.400000000000297	43.500000000000298	43.6000000000003	43.700000000000301	43.800000000000303	43.900000000000297	44.000000000000298	44.1000000000003	44.200000000000301	44.300000000000303	44.400000000000297	44.500000000000298	44.6000000000003	44.700000000000401	44.800000000000402	44.900000000000396	45.000000000000398	45.100000000000399	45.200000000000401	45.300000000000402	45.400000000000396	45.500000000000398	45.600000000000399	45.700000000000401	45.800000000000402	45.900000000000396	46.000000000000398	46.100000000000399	46.200000000000401	46.300000000000402	46.400000000000396	46.500000000000398	46.600000000000399	46.700000000000401	46.800000000000402	46.900000000000396	47.000000000000398	47.100000000000399	47.200000000000401	47.300000000000402	47.400000000000396	47.500000000000398	47.600000000000399	47.700000000000401	47.800000000000402	47.900000000000396	48.000000000000398	48.100000000000399	48.200000000000401	48.300000000000402	48.400000000000396	48.500000000000398	48.600000000000399	48.700000000000401	48.800000000000402	48.900000000000396	49.000000000000398	49.100000000000399	49.200000000000401	49.300000000000402	49.400000000000396	49.500000000000398	49.600000000000399	49.700000000000401	49.800000000000402	49.900000000000396	50.000000000000398	50.100000000000399	50.200000000000401	50.300000000000402	50.400000000000396	50.500000000000398	50.600000000000399	50.700000000000401	50.800000000000402	50.900000000000396	51.000000000000398	51.100000000000399	51.200000000000401	51.300000000000402	51.400000000000396	51.500000000000398	51.600000000000399	51.7000000000005	51.800000000000502	51.900000000000503	52.000000000000497	52.100000000000499	52.2000000000005	52.300000000000502	52.400000000000503	52.500000000000497	52.600000000000499	52.7000000000005	52.800000000000502	52.900000000000503	53.000000000000497	53.100000000000499	53.2000000000005	53.300000000000502	53.400000000000503	53.500000000000497	53.600000000000499	53.7000000000005	53.800000000000502	53.900000000000503	54.000000000000497	54.100000000000499	54.2000000000005	54.300000000000502	54.400000000000503	54.500000000000497	54.600000000000499	54.7000000000005	54.800000000000502	54.900000000000503	55.000000000000497	55.100000000000499	55.2000000000005	55.300000000000502	55.400000000000503	55.500000000000497	55.600000000000499	55.7000000000005	55.800000000000502	55.900000000000503	56.000000000000497	56.100000000000499	56.2000000000005	56.300000000000502	56.400000000000503	56.500000000000497	56.600000000000499	56.7000000000005	56.800000000000502	56.900000000000503	57.000000000000497	57.100000000000499	57.2000000000005	57.300000000000502	57.400000000000503	57.500000000000497	57.600000000000499	57.7000000000005	57.800000000000502	57.900000000000503	58.000000000000497	58.100000000000499	58.2000000000005	58.300000000000502	58.400000000000503	58.500000000000497	58.600000000000499	58.7000000000005	58.800000000000601	58.900000000000603	59.000000000000597	59.100000000000598	59.2000000000006	59.300000000000601	59.400000000000603	59.500000000000597	59.600000000000598	59.7000000000006	59.800000000000601	59.900000000000603	60.000000000000597	60.100000000000598	60.2000000000006	60.300000000000601	60.400000000000603	60.500000000000597	60.600000000000598	60.7000000000006	60.800000000000601	60.900000000000603	61.000000000000597	61.100000000000598	61.2000000000006	61.300000000000601	61.400000000000603	61.500000000000597	61.600000000000598	61.7000000000006	61.800000000000601	61.900000000000603	62.000000000000597	62.100000000000598	62.2000000000006	62.300000000000601	62.400000000000603	62.500000000000597	62.600000000000598	62.7000000000006	62.800000000000601	62.900000000000603	63.000000000000597	63.100000000000598	63.2000000000006	63.300000000000601	63.400000000000603	63.500000000000597	63.600000000000598	63.7000000000006	63.800000000000601	63.900000000000603	64.000000000000597	64.100000000000605	64.2000000000006	64.300000000000594	64.400000000000603	64.500000000000597	64.600000000000605	64.7000000000006	64.800000000000594	64.900000000000603	65.000000000000597	65.100000000000605	65.2000000000006	65.300000000000594	65.400000000000603	65.500000000000597	65.600000000000605	65.7000000000006	65.800000000000693	65.900000000000702	66.000000000000696	66.100000000000705	66.200000000000699	66.300000000000693	66.400000000000702	66.500000000000696	66.600000000000705	66.700000000000699	66.800000000000693	66.900000000000702	67.000000000000696	67.100000000000705	67.200000000000699	67.300000000000693	67.400000000000702	67.500000000000696	67.600000000000705	67.700000000000699	67.800000000000693	67.900000000000702	68.000000000000696	68.100000000000705	68.200000000000699	68.300000000000693	68.400000000000702	68.500000000000696	68.600000000000705	68.700000000000699	68.800000000000693	68.900000000000702	69.000000000000696	69.100000000000705	69.200000000000699	69.300000000000693	69.400000000000702	69.500000000000696	69.600000000000705	69.700000000000699	69.800000000000693	69.900000000000702	70.000000000000696	70.100000000000705	70.200000000000699	70.300000000000693	70.400000000000702	70.500000000000696	70.600000000000705	70.700000000000699	70.800000000000693	70.900000000000702	71.000000000000696	71.100000000000705	71.200000000000699	71.300000000000693	71.400000000000702	71.500000000000696	71.600000000000705	71.700000000000699	71.800000000000693	71.900000000000702	72.000000000000696	72.100000000000705	72.200000000000699	72.300000000000693	72.400000000000702	72.500000000000696	72.600000000000705	72.700000000000699	72.800000000000793	72.900000000000801	73.000000000000796	-2.5658703828060632E-2	-1.8967219970867026E-2	-1.2275736110390482E-2	-5.5842522464278604E-3	1.1072316212356048E-3	7.7987154928288527E-3	1.4490199368594265E-2	2.1181683248789197E-2	2.7873167133687583E-2	3.4564651023579342E-2	4.125613491877321E-2	4.794761881959652E-2	5.463910272639614E-2	6.1330586639541725E-2	6.8022070559424608E-2	7.4713554486461192E-2	8.1405038421092896E-2	8.8096522363788413E-2	9.4788006315046039E-2	0.10147949027539391	0.10817097424539371	0.11486245822564109	0.12155394221676849	0.12824542621944809	0.13493691023439264	0.14162839426235979	0.14831987830415352	0.15501136236062679	0.16170284643268656	0.16839433052129466	0.17508581462747322	0.18177729875230675	0.18846878289694677	0.19516026706262316	0.20185175125061386	0.20854323546231776	0.21523471969919819	0.22192620396278892	0.22861768825476692	0.23530917257686365	0.2420006569309455	0.24869214131898781	0.25538362574308632	0.26207511020546781	0.26876659470849545	0.27545807925467847	0.28214956384668172	0.2888410484873335	0.29553253317963779	0.30222401792678322	0.30891550273215534	0.31560698759934946	0.32229847253218191	0.32898995753470539	0.3356814426112224	0.34237292776630102	0.34906441300479152	0.3557558983318434	0.36244738375292468	0.36913886927384032	0.37583035490075362	0.38252184064020917	0.38921332649915458	0.39590481248496739	0.40259629860547991	0.40928778486900802	0.41597927128438161	0.42267075786097486	0.42936224460874162	0.43605373153824978	0.44274521866071892	0.44943670598806285	0.45612819353292955	0.46281968130874901	0.46951116932977943	0.47620265761115943	0.48289414616896292	0.48958563502025532	0.49627712418315634	0.50296861367690393	0.50966010352192359	0.51635159373990269	0.52304308435386637	0.52973457538826241	0.53642606686904737	0.54311755882377977	0.54980905128172086	0.55650054427393714	0.56319203783341409	0.56988353199517316	0.57657502679639749	0.58326652227656706	0.58995801847759788	0.59664951544399503	0.60334101322301015	0.61003251186481267	0.61672401142266953	0.6234155119531356	0.6301070135162582	0.63679851617579142	0.64349001999942435	0.65018152505902727	0.65687303143090603	0.6635645391960775	0.67025604844056086	0.67694755925568517	0.68363907173842664	0.69033058599172481	0.69702210212489846	0.70371362025400686	0.71040514050227455	0.71709666300053421	0.72378818788769494	0.73047971531124345	0.73717124542777035	0.74386277840353443	0.75055431441505882	0.7572458536497646	0.76393739630664492	0.7706289425969769	0.77732049274508219	0.78401204698913129	0.79070360558199893	0.79739516879217176	0.80408673690471166	0.81077831022228097	0.81746988906622653	0.82416147377773452	0.8308530647190554	0.83754466227480351	0.84423626685333986	0.85092787888823529	0.85761949883982869	0.86431112719687919	0.87100276447832026	0.87769441123512437	0.88438606805227882	0.89107773555088565	0.89776941439039337	0.90446110527096246	0.91115280893598072	0.91784452617472945	0.92453625782521842	0.93122800477719392	0.93791976797533239	0.94461154842263317	0.95130334718401666	0.95799516539014884	0.96468700424149956	0.9713788650126518	0.97807074905687874	0.98476265781099925	0.99145459280053694	0.99814655564519661	1.004838548064678	1.0115305718848502	1.0182226290443039	1.0249147216013128	1.0316068517412196	1.0382990217842822	1.0449912341940042	1.0516834915859739	1.058375796737256	1.0650681525963603	1.071760562293824	1.0784530291534513	1.085145556704241	1.091838148693056	1.098530809098073	1.1052235421430598	1.1119163523125393	1.1186092443678826	1.1253022233644012	1.1319952946694922	1.1386884639819022	1.1453817373521828	1.1520751212044129	1.1587686223592284	1.1654622480583432	1.1721560059905127	1.1788499043191363	1.1855439517115527	1.1922381573701486	1.1989325310653822	1.2056270831708467	1.2123218247005001	1.2190167673481853	1.2257119235295966	1.2324073064268297	1.2391029300356848	1.245798809215886	1.2524949597443977	1.2591913983720335	1.2658881428835553	1.2725852121614776	1.2792826262538168	1.2859804064460036	1.2926785753372458	1.2993771569215928	1.3060761766740001	1.3127756616417041	1.3194756405412262	1.326176143861362	1.3328772039725183	1.3395788552427896	1.3462811341611922	1.3529840794684886	1.3596877322960796	1.366392136313451	1.3730973378847084	1.3798033862347527	1.3865103336256925	1.3932182355441205	1.3999271508999247	1.4066371422373374	1.4133482759589793	1.4200606225636891	1.4267742568989914	1.4334892584290959	1.440205711519382	1.4469237057383793	1.4536433361783103	1.4603647037953398	1.4670879157707291	1.4738130858941791	1.4805403349707142	1.4872697912525419	1.4940015908974211	1.5007358784551472	1.5074728073838692	1.5142125405980604	1.5209552510500559	1.5277011223472106	1.5344503494068316	1.5412031391511762	1.5479597112449484	1.5547202988778546	1.5614851495949538	1.5682545261776761	1.5750287075785683	1.5818079899129978	1.5885926875112311	1.5953831340345175	1.6021796836589979	1.6089827123314935	1.6157926191014635	1.6226098275336511	1.6294347872062205	1.636267975299398	1.6431098982800614	1.6499610936877858	1.6568221320283949	1.6636936187812708	1.6705761965270403	1.6774705472026372	1.6843773944910885	1.6912975063537781	1.6982316977133489	1.7051808332958205	1.7121458306409432	1.7191276632902668	1.7261273641628654	1.7331460291291576	1.7401848207937505	1.7472449724987509	1.754327792559522	1.7614346687453779	1.768567073018275	1.7757265665430875	1.7829148049836143	1.7901335440990127	1.7973846456558877	1.8046700836718161	1.8119919510065814	1.8193524663178977	1.8267539813988629	1.8341989889147912	1.84169013055746	1.8492302056350978	1.8568221801166789	1.8644691961492281	1.8721745820668592	1.8799418629101796	1.8877747714744426	1.8956772599043803	1.9036535118530447	1.9117079552210803	1.9198452754917423	1.92807042967549	1.9363886608761942	1.9448055134887836	1.9533268490354767	1.9619588626445834	1.9707081001720892	1.9795814759618302	1.9885862912349495	1.9977302530933752	2.0070214941152549	2.0164685925124526	2.0260805928113212	2.035867027007864	2.0458379361369969	2.0560038921828059	2.0663760202423167	2.0769660208392682	2.0877861922665741	2.0988494528164097	2.1101693627351641	2.1217601457165967	2.1336367097204834	2.1458146668756761	2.1583103521957976	2.171140840802765	2.1843239633179801	2.1978783190434323	2.2118232865152767	2.226179030970886	2.2409665082272672	2.2562074644243437	2.2719244310419864	2.2881407145543169	2.3048803800413129	2.3221682280352898	2.3400297638408838	2.3584911585324799	2.3775792008044432	2.397321238828805	2.4177451112642285	2.4388790665615612	2.4607516697273364	2.4833916957401017	2.5068280088680859	2.5310894272133981	2.5562045719106603	2.5822017005393638	2.6091085244720862	2.6369520100771844	2.6657581639264025	2.6955518024262535	2.7263563065969425	2.7581933630633229	2.7910826926965169	2.8250417687485632	2.8600855267505052	2.8962260688889416	2.9334723660282664	2.971829960994008	3.011300677163617	3.0518823368098245	3.0935684939915089	3.1363481870706371	3.1802057161330675	3.2251204506881295	3.2710666730004618	3.3180134622526407	3.3659246244373424	3.4147586724253585	3.4644688600478228	3.5150032732707324	3.5663049806359144	3.6183122441111717	3.6709587903553969	3.7241741411904519	3.7778840008146597	3.8320106960305242	3.8864736645330975	3.9411899851568801	3.9960749429492255	4.0510426210651262	4.1060065107946517	4.1608801305670333	4.2155776445424786	4.2700144714134334	4.3241078742910748	4.3777775230398186	4.4309460211239182	4.4835393899185734	4.5354875044796898	4.5867244759235541	4.6371889767986474	4.6868245070951309	4.7355795997923487	4.7834079660530531	4.8302685813019668	4.8761257144472765	4.9209489033955176	4.9647128807576522	5.0073974542383457	5.0489873466395618	5.0894720006959133	5.1288453541028769	5.167105590107977	5.204254868929727	5.2402990450609614	5.2752473752233051	5.309112221384698	5.3419087528497187	5.3736546509993328	5.4043698198077577	5.4340761048121058	5.4627970227669866	5.4970121837399617	5.5302930073025811	5.5626665333504546	5.5941605287476808	5.6248032899397584	5.6546234617136237	5.6836498720048674	5.7119113824586929	5.7394367542912033	5.7662545288688118	5.7923929223232857	5.8178797334453227	5.8427422640479012	5.8670072509586593	5.8907008087859509	5.9138483826029073	5.9364747097055677	5.9586037896226953	5.9802588615840113	6.0014623886887248	6.0222360480556079	6.0426007262782129	6.0625765195529526	6.0821827378926487	6.1014379128830427	6.1203598084839781	6.1389654344199363	6.1572710617460649	6.175292240215315	6.1930438171096833	6.2105399572337765	6.227794163801665	6.2448192999785439	6.2616276108668414	6.278230745752313	6.2946397804493319	6.3108652396060894	6.3269171188500914	6.342804906671847	6.3585376059606169	6.37412375512032	6.3895714487062927	6.4048883575350466	6.4200817482289683	6.4351585021668551	6.4501251338188341	6.4649878084509522	6.4797523591906252	6.4944243034491533	6.5090088587018586	6.5235109576301822	6.5379352626330522	6.5522861797176564	6.5665678717817437	6.5807842713014972	6.5949390924403506	6.6090358425952873	6.6230778333980318	6.6370681911889955	6.6510098669826343	6.6649056459425662	6.6787581563853777	6.6925698783317653	6.7063431516235186	6.7200801836247015	6.7337830565250103	6.7474537342629164	6.7610940690858339	6.7747058077639819	6.7882905974742478	6.8018499913697363	6.8153854538501841	6.8288983655479365	6.8423900280435195	6.8558616683243887	6.8693144429998689	6.8827494422846947	6.8961676937631209	6.9095701659449871	6.9229577716246036	6.9363313710528924	6.9496917749326412	6.9630397472463468	6.9763760079255892	6.9897012353705215	7.003016068827562	7.0163211106330126	7.0296169283299585	7.0429040566653534	7.0561829994739096	7.0694542314550759	7.0827181998489497	7.0959753260168386	7.1092260069317001	7.1224706165835423	7.1357095073045453	7.148943011018388	7.1621714404180654	7.1753950900762273	7.1886142374918247	7.2018291440767062	7.215040056085523	7.2282472054922104	7.2414508108160351	7.2546510779000997	7.2678482006450302	7.2810423617003588	7.2942337331160783	7.3074224769565879	7.3206087458792188	7.3337926836793583	7.3469744258040866	7.3601540998361301	7.3733318259498644	7.3865077173409022	7.3996818806308848	7.4128544162488188	7.4260254187903554	7.4391949773562693	7.4523631758713265	7.4655300933847037	7.4786958043529754	7.4918603789067353	7.5050238831017335	7.5181863791554706	7.5313479256700857	7.5445085778422811	7.5576683876611357	7.5708274040943362	7.583985673263749	Discharge Curve Fit	20	21	22	23	24	25	26	27	28	29	30	31	32	33	34	35	36	37	38	39	40	41	42	43	44	45	46	47	48	49	50	51	52	53	54	55	56	57	58	59	60	61	62	63	64	65	66	67	68	69	70	71	72	73	-8.9327027544409895E-2	-2.5257297301217809E-2	3.8812432966965571E-2	0.1028821632944993	0.16695189376297936	0.23102162456618383	0.29509135616430276	0.35916108965020938	0.42323082761929492	0.4873005762351777	0.55137035013541413	0.61544018408174006	0.67951016062741831	0.74358047582247322	0.80765159525215613	0.87172462459971711	0.93580218965728401	0.99989052612804241	1.0640044421275878	1.1281791008785436	1.1924979890276737	1.2571592600187829	1.3226328565066001	1.3900312205453313	1.4619760611293005	1.5445812724500245	1.6517521812731388	1.8132839516580503	2.0844638069158998	2.5358898180135836	3.1773442968195718	3.8651935834215196	4.4071321077166914	4.7497514034863784	4.9965156509876865	5.1680613531389756	5.3045199752877918	5.425541594751345	5.5399408476534102	5.6515295248895905	5.7619307875111279	5.8718313517213385	5.981520956542643	6.0911217080610207	6.2006850411120507	6.3102326172122902	6.4197735582149331	6.5293117052729164	6.6388486758460825	6.7483851510215054	6.8579214175935261	6.9674575963263052	7.0769937380715193	7.18652986424192	Outlet Temperature (°C)


Energy Stored (kWh)




Test 1 (6 kW, 5 LPM)	73.163499999999999	71.640199999999993	70.0351	68.286900000000003	66.559100000000001	64.790400000000005	63.042200000000001	61.416699999999999	59.944499999999998	58.625599999999999	57.470399999999998	56.816099999999999	55.660800000000002	54.965600000000002	54.730400000000003	53.963700000000003	53.605899999999998	53.3401	53.115099999999998	52.972000000000001	52.839100000000002	52.706200000000003	52.603999999999999	52.5017	52.389299999999999	52.276800000000001	52.133699999999997	51.9497	51.755400000000002	51.489600000000003	51.152200000000001	50.732999999999997	50.232100000000003	49.659599999999998	48.964399999999998	48.177199999999999	47.2468	46.122199999999999	44.885199999999998	43.576599999999999	42.237299999999998	40.8367	39.384900000000002	37.882100000000001	36.348500000000001	34.784300000000002	33.189500000000002	31.5945	30.091699999999999	28.721699999999998	27.423400000000001	26.288499999999999	25.235499999999998	24.295000000000002	23.466899999999999	22.730799999999999	22.066199999999998	21.514199999999999	11.228563283333344	10.897137727777789	10.5799713388889	10.270070783333344	9.9651502277777873	9.6706905055555659	9.3845946722222315	9.1075130055555658	8.8381968944444544	8.5776213388888998	8.3260621722222332	8.0799849500000107	7.8387943944444558	7.6035368944444555	7.3719699500000111	7.143365783333345	6.9194177277777893	6.6965063388889003	6.4749082833333436	6.2547138388889003	6.0347313388888999	5.8157743944444542	5.5979577277777874	5.3804021722222304	5.1631535611111188	4.9473871722222311	4.7326755055555649	4.5176732833333419	4.3049424500000084	4.0934705055555645	3.8838366166666756	3.6759746722222308	3.4712777277777862	3.2705246722222316	3.0724682833333432	2.8789291166666775	2.6906482833333438	2.508440227777788	2.3327118944444543	2.1653485055555652	2.0066255888888982	1.8554745333333431	1.7134052000000077	1.5801046722222269	1.4564955888888973	1.3423440333333387	1.2374577277777841	1.1423160611111156	1.0571986166666696	0.98051664444444619	0.9120030333333331	0.85138908888888865	0.79714406111111225	0.74866458888889142	0.70567653333333724	0.66743650555555711	0.63317231111111405	0.60304983888889319	Test 2 (6 kW, 10 LPM)	69.5	68	66.5	64.8	63.4	61.9	60.5	59.2	57.9	56.8	55.9	55	54.3	53.5	53	52.7	52.3	52.1	51.9	51.7	51.6	51.4	51.3	51.1	50.9	50.6	50.3	50	49.5	48.9	48.3	47.6	46.8	46	45	43.9	42.7	41.5	40.299999999999997	39	37.799999999999997	36.6	35.4	34.4	33.6	32.5	31.3	30.3	29.3	28.3	27.4	26.6	25.8	25.1	24.4	23.8	10.479139333333338	10.136247388888894	9.8147326666666714	9.5084543333333382	9.2123543333333373	8.9265157222222271	8.6516526666666707	8.3886546111111162	8.1358843333333368	7.8918096111111158	7.654156833333337	7.4230429444444486	7.1972804444444485	6.9757254444444481	6.7574251666666703	6.5423537777777812	6.3300221111111146	6.1196573888888919	5.9103190555555587	5.7019651666666711	5.4946254444444493	5.2878126666666709	5.0818154444444481	4.8766321111111148	4.6718479444444494	4.4684232222222278	4.2663635000000051	4.0656121111111165	3.8667326666666719	3.670785166666672	3.4773479444444497	3.2872632222222276	3.1009907222222282	2.9191518333333395	2.7423043333333386	2.5712829444444498	2.4072440555555623	2.249681000000006	2.0986296111111162	1.9546904444444504	1.8188879444444499	1.6921215555555609	1.5716690555555619	1.4580121111111168	1.3505182222222292	1.2494301666666701	1.1553185000000052	1.0671193333333377	0.9849972222222263	0.90892888888889267	0.83926775000000475	0.77433969444444806	0.71484408333333604	0.66000577777777991	0.60947366666667158	0.56265177777778241	Test 3 (3 kW, 10 LPM)	55.9	55.7	55.3	55	54.7	54.3	54	53.7	53.5	53.3	53.1	52.9	52.8	52.7	52.6	52.5	52.5	52.4	52.3	52.2	52	51.8	51.6	51.4	51	50.7	50.2	49.7	49	48.3	47.4	46.2	45.2	43.7	42.4	40.6	39	37.700000000000003	36	34.6	33.5	32.299999999999997	31.2	30.1	29	28	27	26.1	25.2	24.4	23.6	22.9	22.3	21.8	21.3	20.9	20.6	20.3	20	19.8	19.600000000000001	19.5	19.3	19.2	19	18.899999999999999	18.8	9.2501958555555532	9.0184008555555533	8.7848947444444416	8.5531030777777755	8.3238341888888865	8.0964111333333317	7.8702677999999979	7.64624502222222	7.4237666888888869	7.2026155777777756	6.9827139111111087	6.7637369666666647	6.5455450222222193	6.3282955777777747	6.1115780777777751	5.8955427999999976	5.680299744444441	5.4650311333333299	5.2502589111111071	5.0361091888888856	4.8227947444444403	4.6099180777777731	4.398148633333328	4.1872036333333291	3.9780072444444396	3.7711064111111066	3.5663772444444399	3.3642391888888845	3.1656386333333293	2.9700669666666615	2.779613077777773	2.5949139111111066	2.4173300222222185	2.2469816888888845	2.0852844666666623	1.9302794666666623	1.7881541888888846	1.6539339111111087	1.5273530777777751	1.4106308555555538	1.303586133333333	1.2025694666666666	1.1085450222222217	1.0229487444444452	0.94246432777777756	0.86842760555555643	0.80109438333333394	0.73894135555555707	0.68264368888889138	0.63192410555555689	0.58557130000000157	0.54447646666666749	0.50722807777777845	0.47331749444444604	0.44271971666666943	0.4142227722222227	0.38814155000000206	0.36388246666666824	0.3414297722222237	0.32043782777777885	0.30112841111111166	0.28253474444444571	0.26492730000000186	0.24825574444444598	0.23266032777777923	0.217804161111113	0.20343343888889187	Test 4 (3 kW, 5 LPM)	64.3	64.2	63.9	63.5	62.9	62.2	61.3	60.4	59.4	58.5	57.6	56.8	56.1	55.4	54.8	54.3	53.9	53.5	53.2	53	52.9	52.8	52.7	52.7	52.7	52.6	52.5	52.4	52.2	52.1	51.9	51.7	51.5	51.3	51.1	50.8	50.4	49.8	49.2	48.4	47.5	46.5	45.2	43.9	42.4	41	39.4	37.9	36.299999999999997	34.9	33.4	32	30.6	29.4	28.2	27.1	26.2	25.3	24.4	23.7	23.1	22.6	22.1	21.8	21.4	21.1	20.9	20.6	20.399999999999999	20.2	20.100000000000001	19.899999999999999	19.8	19.7	19.600000000000001	19.5	19.399999999999999	19.3	19.2	19.100000000000001	19.100000000000001	11.30651088611112	11.013077275000009	10.735301441666675	10.45767338611112	10.182526719444454	9.9114164416666757	9.6463161638888977	9.3866781083333422	9.1321672750000094	8.8834692194444536	8.6411158861111197	8.4033083861111191	8.1701031083333397	7.9418278305555621	7.7174569972222287	7.4976297750000063	7.280073386111118	7.0653028305555621	6.8530164416666741	6.6422533861111184	6.432619775000008	6.2233508861111195	6.0148569972222292	5.8066592194444508	5.5993886638888961	5.3921564416666738	5.1853506083333398	4.979626997222228	4.7738111638888947	4.5695442194444507	4.3663694972222284	4.1647706083333391	3.9646511638888944	3.7658758861111172	3.5681650527777826	3.3722433861111165	3.1782417194444506	2.9872031083333397	2.7991922750000047	2.6161358861111168	2.4372172750000054	2.2640194972222272	2.0971979972222261	1.9373540527777831	1.7871594416666703	1.6453934416666716	1.5120686916666735	1.3874374138888932	1.2714370805555593	1.1655020805555623	1.0671766916666758	0.97792444166667281	0.89765466388889337	0.82413221944444714	0.7576339972222268	0.69768096944444835	0.64391399722222431	0.59566344166666951	0.55262863611111435	0.51355413611111445	0.47888538611111287	0.44729374722222381	0.41841294166666643	0.39214271944444512	0.3680424972222216	0.3458223583333293	0.32509594166666034	0.30578491388888374	0.28760413611110636	0.27065266666666155	0.25472269999999675	0.23956598888888792	0.22515175833333245	0.21148809444444439	0.19846641666666542	0.1862886361111098	0.17475991111111	0.16396378888888741	0.15324928055555276	0.14284812500000044	0.13314780555555217	Charge Curve Fit	20	21	22	23	24	25	26	27	28	29	30	31	32	33	34	35	36	37	38	39	40	41	42	43	44	45	46	47	48	49	50	51	52	53	54	55	56	57	58	59	60	61	62	63	64	65	66	67	68	69	70	71	72	73	7.3056992900400214E-2	0.1758831750923722	0.27870935728541801	0.38153553948096397	0.48436172168233355	0.58718790389726339	0.69001408614377047	0.7928402684638125	0.89566645095509345	0.99849263384513587	1.1013188176637703	1.2041450036448038	1.3069711946613902	1.409797397404204	1.5126236274537328	1.6154499210920623	1.7182763628088105	1.8211031493538234	1.9239307388956508	2.0267601983638541	2.1295940122943966	2.2324379663438321	2.3353055332215384	2.4382280851602394	2.5412786701754664	2.6446273503114432	2.7486699087011113	2.8543267101139049	2.9637340148451261	3.0818288478279969	3.2199063072727063	3.4032064149536341	3.6851109802418458	4.1647473331205669	4.9747774858001712	6.159037246281164	7.4889578102853456	8.5902773677041466	9.3081584773362813	9.7273044930883295	9.9777966494939285	10.182282979461473	10.349681065578981	10.500777840166768	10.644803870103122	10.785780412170531	10.925444994121214	11.064545736939598	11.203404269498231	11.342158775282766	11.480868606398639	11.619559252509221	11.758241659974679	11.896920529530089	Discharge Curve Fit	20	21	22	23	24	25	26	27	28	29	30	31	32	33	34	35	36	37	38	39	40	41	42	43	44	45	46	47	48	49	50	51	52	53	54	55	56	57	58	59	60	61	62	63	64	65	66	67	68	69	70	71	72	73	0.29431493348321686	0.37554123488322866	0.45676753628325401	0.53799383768331965	0.61922013908350404	0.7004464404840417	0.78167274188562741	0.86289904329032474	0.94412534470425891	1.0253516461456125	1.1065779476683597	1.187804249432721	1.2690305519143081	1.3502568565249622	1.4314831674556965	1.5127094971474266	1.593935882530688	1.6751624332328159	1.7563894746796189	1.8376179728881983	1.9188507954462126	2.0000964546320286	2.0813802182031629	2.162777086485093	2.2445096399505915	2.3272381092229684	2.4129180276037352	2.5073162432162874	2.6272203801338212	2.8196630980890203	3.2023208652008619	3.9847272578024375	5.244341709713277	6.5290116544144521	7.3509238320851171	7.8630548749446243	8.1714609238133171	8.4013525161215661	8.6035335558079176	8.7962305639471641	8.9857154983305616	9.1741164144333069	9.3621519312857355	9.5500643296094978	9.7379352497120024	9.9257921965804119	10.113644436201216	10.301495090071384	10.48934520974389	10.677195149459369	10.865045028552101	11.052894887222648	11.240744739013506	11.428594588486773	Outlet Temperature (°C)


Energy Stored (kWh)




5 LPM, 6kW	20.100000000000001	20.2	20.2	20.2	20.2	20.2	20.3	20.3	20.3	20.399999999999999	20.399999999999999	20.399999999999999	20.399999999999999	20.399999999999999	20.5	20.5	20.5	20.5	20.6	20.6	20.6	20.6	20.7	20.7	20.7	20.7	20.7	20.8	20.8	20.8	20.8	20.9	20.9	20.9	20.9	21	21	21	21	21	21.1	21.1	21.1	21.1	21.2	21.2	21.2	21.2	21.3	21.3	21.3	21.4	21.4	21.4	21.4	21.4	21.4	21.5	21.5	21.5	21.5	21.5	21.6	21.6	21.6	21.6	21.7	21.7	21.7	21.7	21.8	21.8	21.8	21.8	21.9	21.9	21.9	21.9	21.9	22	22	22	22	22.1	22.1	22.1	22.1	22.2	22.2	22.2	22.2	22.2	22.3	22.3	22.3	22.3	22.4	22.4	22.4	22.4	22.5	22.5	22.5	22.5	22.5	22.6	22.6	22.6	22.6	22.7	22.7	22.7	22.7	22.8	22.8	22.8	22.8	22.9	22.9	22.9	22.9	22.9	23	23	23	23.1	23.1	23.1	23.1	23.1	23.2	23.2	23.2	23.2	23.3	23.3	23.3	23.3	23.4	23.4	23.4	23.4	23.4	23.5	23.5	23.5	23.6	23.6	23.6	23.6	23.6	23.7	23.7	23.7	23.7	23.8	23.8	23.8	23.8	23.9	23.9	23.9	23.9	24	24	24	24	24.1	24.1	24.1	24.1	24.1	24.2	24.2	24.2	24.2	24.3	24.3	24.3	24.3	24.4	24.4	24.4	24.4	24.5	24.5	24.5	24.5	24.6	24.6	24.6	24.6	24.7	24.7	24.7	24.7	24.8	24.8	24.8	24.8	24.9	24.9	24.9	24.9	25	25	25	25	25	25.1	25.1	25.1	25.1	25.2	25.2	25.2	25.2	25.3	25.3	25.3	25.3	25.4	25.4	25.4	25.4	25.5	25.5	25.5	25.5	25.6	25.6	25.6	25.6	25.7	25.7	25.7	25.7	25.8	25.8	25.8	25.8	25.9	25.9	25.9	25.9	26	26	26	26	26	26.1	26.1	26.1	26.2	26.2	26.2	26.2	26.3	26.3	26.3	26.3	26.3	26.4	26.4	26.4	26.4	26.5	26.5	26.5	26.5	26.5	26.6	26.6	26.6	26.7	26.7	26.7	26.7	26.7	26.8	26.8	26.8	26.8	26.9	26.9	26.9	26.9	27	27	27	27	27.1	27.1	27.1	27.1	27.2	27.2	27.2	27.2	27.3	27.3	27.3	27.3	27.4	27.4	27.4	27.4	27.5	27.5	27.5	27.5	27.6	27.6	27.6	27.6	27.7	27.7	27.7	27.7	27.8	27.8	27.8	27.8	27.9	27.9	27.9	27.9	28	28	28	28	28.1	28.1	28.1	28.1	28.2	28.2	28.2	28.2	28.3	28.3	28.3	28.3	28.4	28.4	28.4	28.4	28.5	28.5	28.5	28.5	28.6	28.6	28.6	28.6	28.7	28.7	28.7	28.8	28.8	28.8	28.8	28.8	28.9	28.9	28.9	29	29	29	29	29	29.1	29.1	29.1	29.1	29.2	29.2	29.2	29.2	29.3	29.3	29.3	29.3	29.4	29.4	29.4	29.4	29.5	29.5	29.5	29.5	29.6	29.6	29.6	29.6	29.7	29.7	29.7	29.7	29.8	29.8	29.8	29.9	29.9	29.9	29.9	30	30	30	30	30.1	30.1	30.1	30.1	30.2	30.2	30.2	30.2	30.3	30.3	30.3	30.3	30.4	30.4	30.4	30.4	30.5	30.5	30.5	30.5	30.6	30.6	30.6	30.7	30.7	30.7	30.7	30.7	30.8	30.8	30.8	30.9	30.9	30.9	30.9	31	31	31	31	31	31.1	31.1	31.1	31.1	31.2	31.2	31.2	31.3	31.3	31.3	31.3	31.3	31.4	31.4	31.5	31.5	31.5	31.5	31.5	31.5	31.6	31.6	31.6	31.6	31.7	31.7	31.7	31.7	31.8	31.8	31.8	31.9	31.9	31.9	31.9	31.9	32	32	32	32.1	32.1	32.1	32.1	32.200000000000003	32.200000000000003	32.200000000000003	32.200000000000003	32.299999999999997	32.299999999999997	32.299999999999997	32.299999999999997	32.299999999999997	32.4	32.4	32.4	32.4	32.5	32.5	32.5	32.6	32.6	32.6	32.6	32.700000000000003	32.700000000000003	32.700000000000003	32.700000000000003	32.799999999999997	32.799999999999997	32.799999999999997	32.799999999999997	32.799999999999997	32.9	32.9	32.9	33	33	33	33	33	33.1	33.1	33.1	33.1	33.200000000000003	33.200000000000003	33.200000000000003	33.200000000000003	33.299999999999997	33.299999999999997	33.299999999999997	33.299999999999997	33.4	33.4	33.4	33.4	33.5	33.5	33.5	33.5	33.6	33.6	33.6	33.6	33.700000000000003	33.700000000000003	33.700000000000003	33.700000000000003	33.799999999999997	33.799999999999997	33.799999999999997	33.799999999999997	33.9	33.9	33.9	33.9	34	34	34.1	34.1	34.1	34.1	34.1	34.200000000000003	34.200000000000003	34.200000000000003	34.200000000000003	34.200000000000003	34.299999999999997	34.299999999999997	34.299999999999997	34.299999999999997	34.4	34.4	34.4	34.4	34.5	34.5	34.5	34.5	34.6	34.6	34.6	34.6	34.700000000000003	34.700000000000003	34.700000000000003	34.700000000000003	34.799999999999997	34.799999999999997	34.799999999999997	34.799999999999997	34.9	34.9	34.9	34.9	35	35	35	35	35.1	35.1	35.1	35.200000000000003	35.200000000000003	35.200000000000003	35.200000000000003	35.200000000000003	35.299999999999997	35.299999999999997	35.299999999999997	35.299999999999997	35.4	35.4	35.4	35.4	35.5	35.5	35.5	35.5	35.5	35.6	35.6	35.6	35.6	35.700000000000003	35.700000000000003	35.700000000000003	35.799999999999997	35.799999999999997	35.799999999999997	35.799999999999997	35.799999999999997	35.9	35.9	35.9	35.9	36	36	36	36	36.1	36.1	36.1	36.1	36.200000000000003	36.200000000000003	36.200000000000003	36.200000000000003	36.299999999999997	36.299999999999997	36.299999999999997	36.299999999999997	36.299999999999997	36.4	36.4	36.4	36.4	36.5	36.5	36.5	36.5	36.6	36.6	36.6	36.6	36.6	36.700000000000003	36.700000000000003	36.700000000000003	36.799999999999997	36.799999999999997	36.799999999999997	36.799999999999997	36.799999999999997	36.9	36.9	36.9	36.9	37	37	37	37	37.1	37.1	37.1	37.200000000000003	37.200000000000003	37.200000000000003	37.200000000000003	37.200000000000003	37.200000000000003	37.299999999999997	37.299999999999997	37.299999999999997	37.299999999999997	37.4	37.4	37.4	37.4	37.5	37.5	37.5	37.5	37.6	37.6	37.6	37.6	37.6	37.700000000000003	37.700000000000003	37.700000000000003	37.700000000000003	37.799999999999997	37.799999999999997	37.799999999999997	37.799999999999997	37.799999999999997	37.9	37.9	37.9	37.9	38	38	38	38	38.1	38.1	38.1	38.1	38.1	38.200000000000003	38.200000000000003	38.200000000000003	38.200000000000003	38.299999999999997	38.299999999999997	38.299999999999997	38.299999999999997	38.4	38.4	38.4	38.4	38.5	38.5	38.5	38.5	38.5	38.6	38.6	38.6	38.6	38.6	38.6	38.700000000000003	38.700000000000003	38.700000000000003	38.700000000000003	38.799999999999997	38.799999999999997	38.799999999999997	38.799999999999997	38.9	38.9	38.9	38.9	38.9	39	39	39	39	39.1	39.1	39.1	39.1	39.1	39.200000000000003	39.200000000000003	39.200000000000003	39.200000000000003	39.299999999999997	39.299999999999997	39.299999999999997	39.299999999999997	39.299999999999997	39.4	39.4	39.4	39.4	39.5	39.5	39.5	39.5	39.5	39.6	39.6	39.6	39.6	39.6	39.700000000000003	39.700000000000003	39.700000000000003	39.700000000000003	39.799999999999997	39.799999999999997	39.799999999999997	39.799999999999997	39.9	39.9	39.9	39.9	39.9	39.9	40	40	40	40	40.1	40.1	40.1	40.1	40.200000000000003	40.200000000000003	40.200000000000003	40.200000000000003	40.200000000000003	40.299999999999997	40.299999999999997	40.299999999999997	40.299999999999997	40.299999999999997	40.4	40.4	40.4	40.4	40.5	40.5	40.5	40.5	40.5	40.6	40.6	40.6	40.700000000000003	40.700000000000003	40.700000000000003	40.700000000000003	40.700000000000003	40.700000000000003	40.799999999999997	40.799999999999997	40.799999999999997	40.799999999999997	40.799999999999997	40.9	40.9	40.9	41	41	41	41	41	41	41	41.1	41.1	41.1	41.1	41.2	41.2	41.2	41.2	41.3	41.3	41.3	41.3	41.3	41.3	41.4	41.4	41.4	41.4	41.4	41.5	41.5	41.5	41.5	41.6	41.6	41.6	41.6	41.6	41.6	41.7	41.7	41.7	41.7	41.7	41.8	41.8	41.8	41.8	41.8	41.9	41.9	41.9	41.9	41.9	42	42	42	42	42.1	42.1	42.1	42.1	42.1	42.2	42.2	42.2	42.2	42.2	42.3	42.3	42.3	42.3	42.3	42.4	42.4	42.4	42.4	42.4	42.5	42.5	42.5	42.5	42.5	42.5	42.6	42.6	42.6	42.6	42.7	42.7	42.7	42.7	42.7	42.8	42.8	42.8	42.8	42.8	42.8	42.9	42.9	42.9	42.9	42.9	43	43	43	43	43	43.1	43.1	43.1	43.1	43.1	43.2	43.2	43.2	43.2	43.2	43.2	43.3	43.3	43.3	43.3	43.3	43.4	43.4	43.4	43.4	43.4	43.5	43.5	43.5	43.5	43.5	43.6	43.6	43.6	43.6	43.6	43.6	43.7	43.7	43.7	43.7	43.7	43.8	43.8	43.8	43.8	43.8	43.9	43.9	43.9	43.9	43.9	43.9	43.9	44	44	44	44	44	44.1	44.1	44.1	44.1	44.1	44.1	44.2	44.2	44.2	44.2	44.2	44.3	44.3	44.3	44.3	44.3	44.3	44.4	44.4	44.4	44.4	44.4	44.4	44.5	44.5	44.5	44.5	44.5	44.6	44.6	44.6	44.6	44.6	44.6	44.7	44.7	44.7	44.7	44.7	44.8	44.8	44.8	44.8	44.8	44.8	44.9	44.9	44.9	44.9	44.9	44.9	45	45	45	45	45	45.1	45.1	45.1	45.1	45.1	45.1	45.2	45.2	45.2	45.2	45.2	45.2	45.3	45.3	45.3	45.3	45.3	45.3	45.4	45.4	45.4	45.4	45.4	45.4	45.5	45.5	45.5	45.5	45.5	45.5	45.6	45.6	45.6	45.6	45.6	45.6	45.7	45.7	45.7	45.7	45.7	45.7	45.7	45.8	45.8	45.8	45.8	45.8	45.9	45.9	45.9	45.9	45.9	45.9	46	46	46	46	46	46	46.1	46.1	46.1	46.1	46.1	46.1	46.1	46.2	46.2	46.2	46.2	46.2	46.2	46.3	46.3	46.3	46.3	46.3	46.3	46.4	46.4	46.4	46.4	46.4	46.4	46.4	46.5	46.5	46.5	46.5	46.5	46.5	46.6	46.6	46.6	46.6	46.6	46.6	46.6	46.7	46.7	46.7	46.7	46.7	46.7	46.8	46.8	46.8	46.8	46.8	46.8	46.9	46.9	46.9	46.9	46.9	46.9	46.9	47	47	47	47	47	47	47	47.1	47.1	47.1	47.1	47.1	47.1	47.2	47.2	47.2	47.2	47.2	47.2	47.2	47.3	47.3	47.3	47.3	47.3	47.3	47.3	47.4	47.4	47.4	47.4	47.4	47.4	47.4	47.5	47.5	47.5	47.5	47.5	47.5	47.5	47.6	47.6	47.6	47.6	47.6	47.6	47.6	47.7	47.7	47.7	47.7	47.7	47.7	47.7	47.7	47.8	47.8	47.8	47.8	47.8	47.8	47.8	47.9	47.9	47.9	47.9	47.9	47.9	47.9	48	48	48	48	48	48	48	48.1	48.1	48.1	48.1	48.1	48.1	48.1	48.2	48.2	48.2	48.2	48.2	48.2	48.2	48.2	48.3	48.3	48.3	48.3	48.3	48.3	48.3	48.4	48.4	48.4	48.4	48.4	48.4	48.4	48.4	48.5	48.5	48.5	48.5	48.5	48.5	48.5	48.5	48.6	48.6	48.6	48.6	48.6	48.6	48.6	48.7	48.7	48.7	48.7	48.7	48.7	48.7	48.7	48.7	48.8	48.8	48.8	48.8	48.8	48.8	48.8	48.9	48.9	48.9	48.9	48.9	48.9	48.9	48.9	49	49	49	49	49	49	49	49	49.1	49.1	49.1	49.1	49.1	49.1	49.1	49.1	49.2	49.2	49.2	49.2	49.2	49.2	49.2	49.2	49.2	49.3	49.3	49.3	49.3	49.3	49.3	49.3	49.3	49.4	49.4	49.4	49.4	49.4	49.4	49.4	49.4	49.4	49.5	49.5	49.5	49.5	49.5	49.5	49.5	49.5	49.6	49.6	49.6	49.6	49.6	49.6	49.6	49.6	49.6	49.7	49.7	49.7	49.7	49.7	49.7	49.7	49.7	49.7	49.8	49.8	49.8	49.8	49.8	49.8	49.8	49.8	49.8	49.9	49.9	49.9	49.9	49.9	49.9	49.9	49.9	49.9	50	50	50	50	50	50	50	50	50	50.1	50.1	50.1	50.1	50.1	50.1	50.1	50.1	50.1	50.2	50.2	50.2	50.2	50.2	50.2	50.2	50.2	50.2	50.2	50.3	50.3	50.3	50.3	50.3	50.3	50.3	50.3	50.3	50.3	50.4	50.4	50.4	50.4	50.4	50.4	50.4	50.4	50.4	50.5	50.5	50.5	50.5	50.5	50.5	50.5	50.5	50.5	50.5	50.6	50.6	50.6	50.6	50.6	50.6	50.6	50.6	50.6	50.6	50.7	50.7	50.7	50.7	50.7	50.7	50.7	50.7	50.7	50.7	50.8	50.8	50.8	50.8	50.8	50.8	50.8	50.8	50.8	50.8	50.9	50.9	50.9	50.9	50.9	50.9	50.9	50.9	50.9	50.9	50.9	50.9	51	51	51	51	51	51	51	51	51	51	51.1	51.1	51.1	51.1	51.1	51.1	51.1	51.1	51.1	51.1	51.1	51.2	51.2	51.2	51.2	51.2	51.2	51.2	51.2	51.2	51.2	51.2	51.3	51.3	51.3	51.3	51.3	51.3	51.3	51.3	51.3	51.3	51.3	51.3	51.4	51.4	51.4	51.4	51.4	51.4	51.4	51.4	51.4	51.4	51.4	51.5	51.5	51.5	51.5	51.5	51.5	51.5	51.5	51.5	51.5	51.6	51.6	51.6	51.6	51.6	51.6	51.6	51.6	51.6	51.6	51.6	51.6	51.7	51.7	51.7	51.7	51.7	51.7	51.7	51.7	51.7	51.7	51.7	51.7	51.8	51.8	51.8	51.8	51.8	51.8	51.8	51.8	51.8	51.8	51.8	51.8	51.9	51.9	51.9	51.9	51.9	51.9	51.9	51.9	51.9	51.9	51.9	51.9	52	52	52	52	52	52	52	52	52	52	52	52	52	52.1	52.1	52.1	52.1	52.1	52.1	52.1	52.1	52.1	52.1	52.1	52.1	52.2	52.2	52.2	52.2	52.2	52.2	52.2	52.2	52.2	52.2	52.2	52.2	52.2	52.3	52.3	52.3	52.3	52.3	52.3	52.3	52.3	52.3	52.3	52.3	52.3	52.3	52.4	52.4	52.4	52.4	52.4	52.4	52.4	52.4	52.4	52.4	52.4	52.4	52.4	52.5	52.5	52.5	52.5	52.5	52.5	52.5	52.5	52.5	52.5	52.5	52.5	52.5	52.6	52.6	52.6	52.6	52.6	52.6	52.6	52.6	52.6	52.6	52.6	52.6	52.6	52.6	52.7	52.7	52.7	52.7	52.7	52.7	52.7	52.7	52.7	52.7	52.7	52.7	52.7	52.8	52.8	52.8	52.8	52.8	52.8	52.8	52.8	52.8	52.8	52.8	52.8	52.8	52.8	52.8	52.9	52.9	52.9	52.9	52.9	52.9	52.9	52.9	52.9	52.9	52.9	52.9	52.9	52.9	52.9	53	53	53	53	53	53	53	53	53	53	53	53	53	53	53	53.1	53.1	53.1	53.1	53.1	53.1	53.1	53.1	53.1	53.1	53.1	53.1	53.1	53.1	53.1	53.1	53.2	53.2	53.2	53.2	53.2	53.2	53.2	53.2	53.2	53.2	53.2	53.2	53.2	53.2	53.2	53.3	53.3	53.3	53.3	53.3	53.3	53.3	53.3	53.3	53.3	53.3	53.3	53.3	53.3	53.3	53.3	53.4	53.4	53.4	53.4	53.4	53.4	53.4	53.4	53.4	53.4	53.4	53.4	53.4	53.4	53.4	53.4	53.5	53.5	53.5	53.5	53.5	53.5	53.5	53.5	53.5	53.5	53.5	53.5	53.5	53.5	53.5	53.5	53.5	53.6	53.6	53.6	53.6	53.6	53.6	53.6	53.6	53.6	53.6	53.6	53.6	53.6	53.6	53.6	53.6	53.7	53.7	53.7	53.7	53.7	53.7	53.7	53.7	53.7	53.7	53.7	53.7	53.7	53.7	53.7	53.7	53.7	53.7	53.7	53.8	53.8	53.8	53.8	53.8	53.8	53.8	53.8	53.8	53.8	53.8	53.8	53.8	53.8	53.8	53.8	53.8	53.8	53.9	53.9	53.9	53.9	53.9	53.9	53.9	53.9	53.9	53.9	53.9	53.9	53.9	53.9	53.9	53.9	53.9	54	54	54	54	54	54	54	54	54	54	54	54	54	54	54	54	54	54	54	54	54.1	54.1	54.1	54.1	54.1	54.1	54.1	54.1	54.1	54.1	54.1	54.1	54.1	54.1	54.1	54.1	54.1	54.1	54.1	54.2	54.2	54.2	54.2	54.2	54.2	54.2	54.2	54.2	54.2	54.2	54.2	54.2	54.2	54.2	54.2	54.2	54.2	54.2	54.2	54.3	54.3	54.3	54.3	54.3	54.3	54.3	54.3	54.3	54.3	54.3	54.3	54.3	54.3	54.3	54.3	54.3	54.3	54.3	54.4	54.4	54.4	54.4	54.4	54.4	54.4	54.4	54.4	54.4	54.4	54.4	54.4	54.4	54.4	54.4	54.4	54.4	54.4	54.4	54.5	54.5	54.5	54.5	54.5	54.5	54.5	54.5	54.5	54.5	54.5	54.5	54.5	54.5	54.5	54.5	54.5	54.5	54.5	54.5	54.5	54.6	54.6	54.6	54.6	54.6	54.6	54.6	54.6	54.6	54.6	54.6	54.6	54.6	54.6	54.6	54.6	54.6	54.6	54.6	54.6	54.6	54.6	54.7	54.7	54.7	54.7	54.7	54.7	54.7	54.7	54.7	54.7	54.7	54.7	54.7	54.7	54.7	54.7	54.7	54.7	54.7	54.7	54.7	54.7	54.8	54.8	54.8	54.8	54.8	54.8	54.8	54.8	54.8	54.8	54.8	54.8	54.8	54.8	54.8	54.8	54.8	54.8	54.8	54.8	54.8	54.8	54.9	54.9	54.9	54.9	54.9	54.9	54.9	54.9	54.9	54.9	54.9	54.9	54.9	54.9	54.9	54.9	54.9	54.9	54.9	54.9	54.9	54.9	54.9	55	55	55	55	55	55	55	55	55	55	55	55	55	55	55	55	55	55	55	55	55	55	55.1	55.1	55.1	55.1	55.1	55.1	55.1	55.1	55.1	55.1	55.1	55.1	55.1	55.1	55.1	55.1	55.1	55.1	55.1	55.1	55.1	55.1	55.1	55.1	55.1	55.1	55.1	55.2	55.2	55.2	55.2	55.2	55.2	55.2	55.2	55.2	55.2	55.2	55.2	55.2	55.2	55.2	55.2	55.2	55.2	55.2	55.2	55.2	55.2	55.2	55.2	55.3	55.3	55.3	55.3	55.3	55.3	55.3	55.3	55.3	55.3	55.3	55.3	55.3	55.3	55.3	55.3	55.3	55.3	55.3	55.3	55.3	55.3	55.3	55.3	55.3	55.4	55.4	55.4	55.4	55.4	55.4	55.4	55.4	55.4	55.4	55.4	55.4	55.4	55.4	55.4	55.4	55.4	55.4	55.4	55.4	55.4	55.4	55.4	55.4	55.4	55.4	55.4	55.5	55.5	55.5	55.5	55.5	55.5	55.5	55.5	55.5	55.5	55.5	55.5	55.5	55.5	55.5	55.5	55.5	55.5	55.5	55.5	55.5	55.5	55.5	55.5	55.5	55.5	55.6	55.6	55.6	55.6	55.6	55.6	55.6	55.6	55.6	55.6	55.6	55.6	55.6	55.6	55.6	55.6	55.6	55.6	55.6	55.6	55.6	55.6	55.6	55.6	55.6	55.6	55.6	55.7	55.7	55.7	55.7	55.7	55.7	55.7	55.7	55.7	55.7	55.7	55.7	55.7	55.7	55.7	55.7	55.7	55.7	55.7	55.7	55.7	55.7	55.7	55.7	55.7	55.7	55.7	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.9	55.9	55.9	55.9	55.9	55.9	55.9	55.9	55.9	55.9	55.9	55.9	55.9	55.9	55.9	55.9	55.9	55.9	55.9	55.9	55.9	55.9	55.9	55.9	55.9	55.9	55.9	55.9	55.9	55.9	56	56	56	56	56	56	56	56	56	56	56	56	56	56	56	56	56	56	56	56	56	56	56	56	56	56	56	56	56	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.2	57.1	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	58	58	58	58	58	58	58	58	58	58	58	58	58	58	58	58	58	58	58	58	58	58	58	58	58	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.3	58.3	58.3	58.3	58.3	58.3	58.3	58.3	58.3	58.3	58.3	58.3	58.3	58.3	58.3	58.3	58.3	58.3	58.3	58.3	58.3	58.3	58.3	58.3	58.3	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.5	58.5	58.5	58.5	58.5	58.5	58.5	58.5	58.5	58.5	58.5	58.5	58.5	58.5	58.5	58.5	58.5	58.5	58.5	58.5	58.5	58.5	58.5	58.5	58.5	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.7	58.7	58.7	58.7	58.7	58.7	58.7	58.7	58.7	58.7	58.7	58.7	58.7	58.7	58.7	58.7	58.7	58.7	58.7	58.7	58.7	58.7	58.7	58.7	58.8	58.8	58.8	58.8	58.8	58.8	58.8	58.8	58.8	58.8	58.8	58.8	58.8	58.8	58.8	58.8	58.8	58.8	58.8	58.8	58.8	58.9	58.9	58.9	58.9	58.9	58.9	58.9	58.9	58.9	58.9	58.9	58.9	58.9	58.9	58.9	58.9	58.9	58.9	58.9	58.9	58.9	58.9	59	59	59	59	59	59	59	59	59	59	59	59	59	59	59	59	59	59	59	59	59	59	59.1	59.1	59.1	59.1	59.1	59.1	59.1	59.1	59.1	59.1	59.1	59.1	59.1	59.1	59.1	59.1	59.1	59.1	59.1	59.1	59.1	59.2	59.2	59.2	59.2	59.2	59.2	59.2	59.2	59.2	59.2	59.2	59.2	59.2	59.2	59.2	59.2	59.2	59.2	59.2	59.2	59.2	59.2	59.3	59.3	59.3	59.3	59.3	59.3	59.3	59.3	59.3	59.3	59.3	59.3	59.3	59.3	59.3	59.3	59.3	59.3	59.3	59.3	59.3	59.4	59.4	59.4	59.4	59.4	59.4	59.4	59.4	59.4	59.4	59.4	59.4	59.4	59.4	59.4	59.4	59.4	59.4	59.4	59.4	59.4	59.5	59.5	59.5	59.5	59.5	59.5	59.5	59.5	59.5	59.5	59.5	59.5	59.5	59.5	59.5	59.5	59.5	59.5	59.5	59.5	59.6	59.6	59.6	59.6	59.6	59.6	59.6	59.6	59.6	59.6	59.6	59.6	59.6	59.6	59.6	59.6	59.6	59.6	59.6	59.6	59.7	59.7	59.7	59.7	59.7	59.7	59.7	59.7	59.7	59.7	59.7	59.7	59.7	59.7	59.7	59.7	59.7	59.7	59.7	59.8	59.8	59.8	59.8	59.8	59.8	59.8	59.8	59.8	59.8	59.8	59.8	59.8	59.8	59.8	59.8	59.8	59.8	59.8	59.8	59.9	59.9	59.9	59.9	59.9	59.9	59.9	59.9	59.9	59.9	59.9	59.9	59.9	59.9	59.9	59.9	59.9	59.9	60	60	60	60	60	60	60	60	60	60	60	60	60	60	60	60	60	60	60	60.1	60.1	60.1	60.1	60.1	60.1	60.1	60.1	60.1	60.1	60.1	60.1	60.1	60.1	60.1	60.1	60.1	60.1	60.2	60.2	60.2	60.2	60.2	60.2	60.2	60.2	60.2	60.2	60.2	60.2	60.2	60.2	60.2	60.2	60.2	60.2	60.3	60.3	60.3	60.3	60.3	60.3	60.3	60.3	60.3	60.3	60.3	60.3	60.3	60.3	60.3	60.3	60.3	60.4	60.4	60.4	60.4	60.4	60.4	60.4	60.4	60.4	60.4	60.4	60.4	60.4	60.4	60.4	60.4	60.4	60.5	60.5	60.5	60.5	60.5	60.5	60.5	60.5	60.5	60.5	60.5	60.5	60.5	60.5	60.5	60.5	60.6	60.6	60.6	60.6	60.6	60.6	60.6	60.6	60.6	60.6	60.6	60.6	60.6	60.6	60.6	60.6	60.7	60.7	60.7	60.7	60.7	60.7	60.7	60.7	60.7	60.7	60.7	60.7	60.7	60.7	60.8	60.8	60.8	60.8	60.8	60.8	60.8	60.8	60.8	60.8	60.8	60.8	60.8	60.8	60.8	60.8	60.9	60.9	60.9	60.9	60.9	60.9	60.9	60.9	60.9	60.9	60.9	60.9	60.9	60.9	61	61	61	61	61	61	61	61	61	61	61	61	61	61	61	61.1	61.1	61.1	61.1	61.1	61.1	61.1	61.1	61.1	61.1	61.1	61.1	61.1	61.1	61.2	61.2	61.2	61.2	61.2	61.2	61.2	61.2	61.2	61.2	61.2	61.2	61.2	61.2	61.3	61.3	61.3	61.3	61.3	61.3	61.3	61.3	61.3	61.3	61.3	61.3	61.3	61.3	61.4	61.4	61.4	61.4	61.4	61.4	61.4	61.4	61.4	61.4	61.4	61.4	61.4	61.4	61.5	61.5	61.5	61.5	61.5	61.5	61.5	61.5	61.5	61.5	61.5	61.5	61.5	61.6	61.6	61.6	61.6	61.6	61.6	61.6	61.6	61.6	61.6	61.6	61.6	61.6	61.7	61.7	61.7	61.7	61.7	61.7	61.7	61.7	61.7	61.7	61.7	61.7	61.7	61.8	61.8	61.8	61.8	61.8	61.8	61.8	61.8	61.8	61.8	61.8	61.8	61.9	61.9	61.9	61.9	61.9	61.9	61.9	61.9	61.9	61.9	61.9	61.9	61.9	62	62	62	62	62	62	62	62	62	62	62	62.1	62.1	62.1	62.1	62.1	62.1	62.1	62.1	62.1	62.1	62.1	62.1	62.2	62.2	62.2	62.2	62.2	62.2	62.2	62.2	62.2	62.2	62.2	62.2	62.2	62.3	62.3	62.3	62.3	62.3	62.3	62.3	62.3	62.3	62.3	62.4	62.4	62.4	62.4	62.4	62.4	62.4	62.4	62.4	62.4	62.4	62.4	62.5	62.5	62.5	62.5	62.5	62.5	62.5	62.5	62.5	62.5	62.5	62.6	62.6	62.6	62.6	62.6	62.6	62.6	62.6	62.6	62.6	62.6	62.7	62.7	62.7	62.7	62.7	62.7	62.7	62.7	62.7	62.7	62.7	62.8	62.8	62.8	62.8	62.8	62.8	62.8	62.8	62.8	62.8	62.9	62.9	62.9	62.9	62.9	62.9	62.9	62.9	62.9	62.9	62.9	63	63	63	63	63	63	63	63	63	63	63.1	63.1	63.1	63.1	63.1	63.1	63.1	63.1	63.1	63.1	63.1	63.2	63.2	63.2	63.2	63.2	63.2	63.2	63.2	63.2	63.2	63.3	63.3	63.3	63.3	63.3	63.3	63.3	63.3	63.3	63.3	63.4	63.4	63.4	63.4	63.4	63.4	63.4	63.4	63.4	63.4	63.5	63.5	63.5	63.5	63.5	63.5	63.5	63.5	63.5	63.5	63.6	63.6	63.6	63.6	63.6	63.6	63.6	63.6	63.6	63.6	63.6	63.7	63.7	63.7	63.7	63.7	63.7	63.7	63.7	63.7	63.8	63.8	63.8	63.8	63.8	63.8	63.8	63.8	63.8	63.8	63.9	63.9	63.9	63.9	63.9	63.9	63.9	63.9	63.9	63.9	64	64	64	64	64	64	64	64	64	64.099999999999994	64.099999999999994	64.099999999999994	64.099999999999994	64.099999999999994	64.099999999999994	64.099999999999994	64.099999999999994	64.099999999999994	64.099999999999994	64.2	64.2	64.2	64.2	64.2	64.2	64.2	64.2	64.2	64.2	64.3	64.3	64.3	64.3	64.3	64.3	64.3	64.3	64.3	64.3	64.400000000000006	64.400000000000006	64.400000000000006	64.400000000000006	64.400000000000006	64.400000000000006	64.400000000000006	64.400000000000006	64.400000000000006	64.400000000000006	64.5	64.5	64.5	64.5	64.5	64.5	64.5	64.5	64.5	64.5	64.5	64.599999999999994	64.599999999999994	64.599999999999994	64.599999999999994	64.599999999999994	64.599999999999994	64.599999999999994	64.599999999999994	64.599999999999994	64.599999999999994	64.599999999999994	64.7	64.7	64.7	64.7	64.7	64.7	64.7	64.7	64.7	64.7	64.8	64.8	64.8	64.8	64.8	64.8	64.8	64.8	64.8	64.8	64.900000000000006	64.900000000000006	64.900000000000006	64.900000000000006	64.900000000000006	64.900000000000006	64.900000000000006	64.900000000000006	64.900000000000006	64.900000000000006	64.900000000000006	64.900000000000006	65	65	65	65	65	65	65	65	65	65	65.099999999999994	65.099999999999994	65.099999999999994	65.099999999999994	65.099999999999994	65.099999999999994	65.099999999999994	65.099999999999994	65.099999999999994	65.099999999999994	65.2	65.2	65.2	65.2	65.2	65.2	65.2	65.2	65.2	65.2	65.2	65.3	65.3	65.3	65.3	65.3	65.3	65.3	65.3	65.3	65.3	65.400000000000006	65.400000000000006	65.400000000000006	65.400000000000006	65.400000000000006	65.400000000000006	65.400000000000006	65.400000000000006	65.400000000000006	65.400000000000006	65.5	65.5	65.5	65.5	65.5	65.5	65.5	65.5	65.5	65.5	65.5	65.599999999999994	65.599999999999994	65.599999999999994	65.599999999999994	65.599999999999994	65.599999999999994	65.599999999999994	65.599999999999994	65.599999999999994	65.7	65.7	65.7	65.7	65.7	65.7	65.7	65.7	65.7	65.7	65.8	65.8	65.8	65.8	65.8	65.8	65.8	65.8	65.8	65.8	65.900000000000006	65.900000000000006	65.900000000000006	65.900000000000006	65.900000000000006	65.900000000000006	65.900000000000006	65.900000000000006	65.900000000000006	65.900000000000006	66	66	66	66	66	66	66	66	66	66	66.099999999999994	66.099999999999994	66.099999999999994	66.099999999999994	66.099999999999994	66.099999999999994	66.099999999999994	66.099999999999994	66.099999999999994	66.099999999999994	66.2	66.2	66.2	66.2	66.2	66.2	66.2	66.2	66.2	66.2	66.3	66.3	66.3	66.3	66.3	66.3	66.3	66.3	66.3	66.400000000000006	66.400000000000006	66.400000000000006	66.400000000000006	66.400000000000006	66.400000000000006	66.400000000000006	66.400000000000006	66.400000000000006	66.5	66.5	66.5	66.5	66.5	66.5	66.5	66.5	66.5	66.599999999999994	66.599999999999994	66.599999999999994	66.599999999999994	66.599999999999994	66.599999999999994	66.599999999999994	66.599999999999994	66.599999999999994	66.599999999999994	66.7	66.7	66.7	66.7	66.7	66.7	66.7	66.7	66.7	66.8	66.8	66.8	66.8	66.8	66.8	66.8	66.8	66.8	66.900000000000006	66.900000000000006	66.900000000000006	66.900000000000006	66.900000000000006	66.900000000000006	66.900000000000006	66.900000000000006	66.900000000000006	66.900000000000006	67	67	67	67	67	67	67	67	67	67.099999999999994	67.099999999999994	67.099999999999994	67.099999999999994	67.099999999999994	67.099999999999994	67.099999999999994	67.099999999999994	67.099999999999994	67.2	67.2	67.2	67.2	67.2	67.2	67.2	67.2	67.2	67.3	67.3	67.3	67.3	67.3	67.3	67.3	67.3	67.3	67.400000000000006	67.400000000000006	67.400000000000006	67.400000000000006	67.400000000000006	67.400000000000006	67.400000000000006	67.400000000000006	67.400000000000006	67.5	67.5	67.5	67.5	67.5	67.5	67.5	67.5	67.599999999999994	67.599999999999994	67.599999999999994	67.599999999999994	67.599999999999994	67.599999999999994	67.599999999999994	67.599999999999994	67.599999999999994	67.7	67.7	67.7	67.7	67.7	67.7	67.7	67.7	67.7	67.8	67.8	67.8	67.8	67.8	67.8	67.8	67.8	67.8	67.900000000000006	67.900000000000006	67.900000000000006	67.900000000000006	67.900000000000006	67.900000000000006	67.900000000000006	67.900000000000006	68	68	68	68	68	68	68	68.099999999999994	68.099999999999994	68.099999999999994	68.099999999999994	68.099999999999994	68.099999999999994	68.099999999999994	68.099999999999994	68.099999999999994	68.2	68.2	68.2	68.2	68.2	68.2	68.2	68.2	68.2	68.3	68.3	68.3	68.3	68.3	68.3	68.3	68.3	68.3	68.400000000000006	68.400000000000006	68.400000000000006	68.400000000000006	68.400000000000006	68.400000000000006	68.400000000000006	68.400000000000006	68.400000000000006	68.5	68.5	68.5	68.5	68.5	68.5	68.5	68.5	68.599999999999994	68.599999999999994	68.599999999999994	68.599999999999994	68.599999999999994	68.599999999999994	68.599999999999994	68.7	68.7	68.7	68.7	68.7	68.7	68.7	68.7	68.7	68.8	68.8	68.8	68.8	68.8	68.8	68.8	68.8	68.900000000000006	68.900000000000006	68.900000000000006	68.900000000000006	68.900000000000006	68.900000000000006	68.900000000000006	68.900000000000006	68.900000000000006	69	69	69	69	69	69	69	69	69.099999999999994	69.099999999999994	69.099999999999994	69.099999999999994	69.099999999999994	69.099999999999994	69.099999999999994	69.2	69.2	69.2	69.2	69.2	69.2	69.2	69.2	69.2	69.2	69.3	69.3	69.3	69.3	69.3	69.3	69.3	69.3	69.400000000000006	69.400000000000006	69.400000000000006	69.400000000000006	69.400000000000006	69.400000000000006	69.400000000000006	69.400000000000006	69.5	69.5	69.5	69.5	69.5	69.5	69.5	69.5	69.599999999999994	69.599999999999994	69.599999999999994	69.599999999999994	69.599999999999994	69.599999999999994	69.599999999999994	69.599999999999994	69.7	69.7	69.7	69.7	69.7	69.7	69.7	69.8	69.8	69.8	69.8	69.8	69.8	69.8	69.8	69.900000000000006	69.900000000000006	69.900000000000006	69.900000000000006	69.900000000000006	69.900000000000006	69.900000000000006	69.900000000000006	69.900000000000006	70	70	70	70	70	70	70	70.099999999999994	70.099999999999994	70.099999999999994	70.099999999999994	70.099999999999994	70.099999999999994	70.099999999999994	70.099999999999994	70.2	70.2	70.2	70.2	70.2	70.2	70.2	70.3	70.3	70.3	70.3	70.3	70.3	70.3	70.3	70.400000000000006	0	1.6192083333333332E-3	3.2468527777777777E-3	4.8893694444444441E-3	6.5451972222222224E-3	8.2058916666666662E-3	9.8633416666666657E-3	1.1520791666666665E-2	1.318548611111111E-2	1.4845694444444444E-2	1.6498561111111108E-2	1.8155099999999997E-2	1.9830705555555554E-2	2.1511644444444439E-2	2.3191761111111105E-2	2.4868597222222216E-2	2.6538047222222215E-2	2.8202163888888881E-2	2.987202499999999E-2	3.1541886111111098E-2	3.322511388888888E-2	3.4914530555555545E-2	3.6590544444444435E-2	3.8276247222222212E-2	3.9958236111111101E-2	4.1633211111111103E-2	4.3308186111111105E-2	4.4988936111111107E-2	4.6676702777777773E-2	4.836446944444444E-2	5.005099722222222E-2	5.1722908333333324E-2	5.3393180555555551E-2	5.5066505555555548E-2	5.6743130555555549E-2	5.8414633333333334E-2	6.0090236111111112E-2	6.1764608333333332E-2	6.3439802777777776E-2	6.512550555555556E-2	6.679290555555556E-2	6.8460305555555559E-2	7.0128113888888899E-2	7.1804950000000006E-2	7.3478619444444462E-2	7.5152694444444473E-2	7.6830761111111132E-2	7.850267222222225E-2	8.016369722222226E-2	8.1822275000000042E-2	8.3483708333333365E-2	8.5143997222222254E-2	8.6804286111111142E-2	8.8460925000000037E-2	9.0117969444444473E-2	9.1770958333333361E-2	9.3429941666666697E-2	9.5073605555555579E-2	9.6724161111111137E-2	9.8379988888888922E-2	0.1000402777777778	0.10170016111111113	0.10334550000000002	0.10498801666666668	0.10662851666666669	0.10827103333333335	0.10990829722222224	0.11154916666666669	0.11318883333333335	0.11482609722222224	0.11645975277777781	0.11808940000000004	0.11971143333333337	0.12133506944444448	0.12295626944444449	0.12458663333333338	0.12621859166666671	0.12784975277777783	0.12947055555555559	0.13108936666666671	0.1327069805555556	0.1343285805555556	0.13595336666666669	0.13757402500000002	0.13919151666666668	0.14080623611111115	0.14240262500000003	0.14399901388888892	0.14560383333333335	0.14721380000000001	0.14883168611111111	0.15045234444444447	0.1520613305555556	0.15366323055555559	0.1552651305555556	0.15687430555555559	0.15847305833333336	0.16007377777777781	0.16167804166666672	0.16328112222222227	0.16487454722222225	0.16647644722222224	0.16807598611111113	0.16967355555555558	0.17126876388888893	0.1728614055555556	0.1744696055555556	0.17607780555555561	0.17768639722222226	0.17928138611111116	0.18087128888888893	0.18245845277777784	0.18404718333333339	0.18564100000000006	0.18723716388888895	0.18883332777777781	0.19042910000000002	0.19202291666666671	0.19360929722222225	0.1951956777777778	0.19678440833333335	0.19838096388888893	0.19997947500000002	0.20157798611111113	0.20317375833333337	0.20475441388888893	0.20633506944444449	0.20792145000000006	0.20951056944444449	0.21110321111111116	0.21268970000000006	0.21427580000000007	0.21587157222222228	0.21746108333333342	0.2190370722222223	0.22061111666666672	0.22219216111111117	0.22378832500000007	0.22537675833333337	0.22696130277777782	0.22854195833333338	0.23013225277777782	0.23172020000000004	0.23329774444444448	0.23487528888888895	0.23645827777777784	0.23804360000000005	0.23962736666666673	0.24120763333333337	0.24278323333333335	0.24436335555555558	0.24593740000000003	0.24751650000000003	0.24909910000000002	0.25069174166666669	0.25227123055555556	0.25384760833333336	0.25542359722222224	0.25699491944444447	0.25856663055555557	0.26014339722222224	0.2617244416666667	0.26330743055555561	0.2648900305555556	0.26646601944444448	0.26803928611111111	0.2696098305555556	0.27118123611111111	0.27276305833333336	0.27434488055555561	0.27592436944444448	0.27750346944444448	0.27907564722222222	0.28065319166666669	0.28222918055555557	0.28380828055555557	0.28538084444444445	0.28696500000000003	0.28854954444444447	0.29012670000000002	0.2916919194444445	0.29326596388888887	0.29484000833333329	0.29642105277777775	0.29799593611111108	0.2995688861111111	0.3011479861111111	0.30272708611111115	0.30429346666666668	0.30585636666666666	0.30742963333333334	0.30900834444444442	0.31058322777777775	0.31215849722222216	0.31373144722222218	0.31530899166666659	0.31687459722222217	0.31843827222222215	0.32000542499999995	0.32157412499999993	0.3231447555555555	0.32471616111111107	0.32628679166666663	0.32785549166666661	0.3294207111111111	0.33098090555555554	0.33254844444444442	0.3341210083333333	0.33569241388888882	0.33725995277777771	0.33882517222222214	0.34038768611111109	0.34194981388888884	0.34350923611111106	0.34507445555555555	0.34664238055555552	0.3482087611111111	0.34977475277777781	0.35134229166666664	0.35290480555555559	0.35446384166666672	0.35602481111111117	0.35759544166666674	0.35916800555555556	0.36073941111111113	0.36230695000000002	0.36387023611111108	0.36543468333333334	0.36699565277777779	0.3685489666666667	0.37011766666666668	0.37169100277777778	0.37326047500000004	0.37482070277777779	0.37638940277777783	0.37795500833333334	0.37951675000000001	0.38107390277777781	0.38263374722222226	0.38420747222222229	0.38577965000000008	0.38733718888888896	0.38889126944444452	0.39045571666666673	0.39201784444444449	0.39357346111111119	0.39512907777777784	0.39670125555555563	0.39826879444444452	0.39983633333333335	0.40139425555555558	0.40294910555555558	0.40449972777777776	0.40605573055555555	0.40761173333333328	0.40917349722222224	0.41073679722222223	0.41229241388888888	0.41384649444444443	0.41539865555555555	0.4169462055555555	0.4184949083333333	0.42004706944444442	0.42160383888888886	0.42315868888888886	0.42471353888888885	0.42626454722222218	0.42781248055555554	0.42936079999999999	0.43091411388888889	0.43248049444444442	0.43404110555555553	0.43559787499999997	0.4371538777777777	0.43870449999999994	0.44025512222222213	0.44180228888888878	0.44335252777777767	0.44491890833333325	0.44647721388888878	0.4480366722222221	0.44959497777777763	0.45115328333333315	0.45270928611111094	0.45426605555555538	0.45582282499999982	0.45738305277777758	0.45893517499999981	0.46049194444444425	0.46204756111111089	0.46360241111111089	0.46514498888888872	0.46669522777777761	0.46825046111111096	0.46980876666666649	0.47135669166666649	0.47291346111111093	0.47446523611111091	0.47601432222222206	0.47756148888888872	0.47910865555555537	0.48065735833333312	0.48219841111111089	0.48373946388888872	0.4852820416666665	0.48682309444444433	0.48836949166666649	0.48990710833333317	0.4914447249999998	0.49298615833333315	0.49454216111111093	0.49608435833333309	0.49762044722222198	0.49915539166666639	0.50069756388888864	0.5022283083333331	0.50376401388888858	0.50531655833333311	0.50686910277777752	0.50841168333333309	0.50995426388888865	0.51150219722222201	0.51305013055555537	0.51458659999999978	0.5161310888888887	0.51767824999999978	0.51923194722222199	0.52077567222222199	0.52231786944444414	0.5238658027777775	0.52541373611111086	0.52695631388888864	0.52850271111111091	0.53004910833333307	0.53160549444444416	0.53315379999999979	0.53469905277777763	0.53624544999999979	0.53779184722222195	0.53932946388888869	0.54087586111111086	0.54242302222222194	0.54397018333333313	0.54551161666666648	0.54705304999999982	0.54858990277777753	0.55012637222222194	0.55166398888888868	0.5532046583333331	0.5547445638888886	0.55628638055555524	0.55781444444444417	0.55934938888888852	0.56088318611111077	0.56241736666666642	0.56396376388888858	0.56551016111111074	0.56705579444444409	0.56859531944444419	0.5701249027777775	0.57166442777777748	0.57320204444444423	0.57473698888888858	0.57627880555555533	0.57782062222222208	0.57936319999999986	0.58089543888888873	0.5824276777777776	0.5839637666666665	0.58549718333333312	0.58703098055555536	0.58856246111111099	0.59009508055555548	0.59163956944444429	0.59318138611111104	0.59470945277777776	0.59623675833333334	0.59777017500000007	0.59930817222222232	0.60083813333333347	0.60236733611111126	0.60390380555555567	0.60544218611111111	0.60696987222222232	0.60850519722222229	0.61004014166666665	0.61157508611111111	0.61310694444444447	0.61463880277777772	0.61618023611111106	0.61772128888888889	0.61924783611111112	0.62077021111111119	0.62230095555555565	0.62384010000000001	0.62537044166666667	0.62689964444444446	0.62843534999999995	0.62997105555555555	0.63149532777777773	0.6330195999999999	0.63455072499999987	0.63607879166666659	0.63761292777777778	0.63914782222222222	0.64069421944444449	0.64222418055555563	0.64375072777777786	0.64527461944444453	0.64681032500000002	0.6483361138888889	0.64986569722222221	0.65139641944444449	0.65293670833333328	0.65446553333333324	0.65598828611111104	0.65750762499999993	0.65904104166666655	0.66056683055555543	0.66209299999999982	0.66361803055555546	0.66514116388888878	0.66666391666666658	0.66818818888888876	0.66970601111111094	0.67123369999999982	0.67276176666666654	0.67428679722222218	0.67581068888888884	0.67734410555555558	0.67886496111111116	0.68038278333333335	0.6819032611111111	0.68342980833333333	0.68495635555555556	0.6864798694444445	0.68800186388888884	0.68952955277777772	0.6910488916666665	0.69257012777777771	0.69409060555555546	0.69561677499999985	0.69714294444444425	0.6986683555555554	0.70020024444444429	0.70171882499999982	0.70323740555555547	0.70475864166666657	0.70627987777777779	0.70781329444444441	0.70933490833333335	0.7108519694444444	0.71236903055555556	0.71389824722222228	0.71541265277777788	0.71693161111111114	0.71846846388888896	0.71999880555555562	0.72152914722222239	0.7230587305555557	0.72458527777777793	0.72611525833333357	0.72763383888888911	0.72915355833333351	0.73067858888888915	0.73220361944444479	0.73372751111111145	0.73524646944444472	0.73676315277777804	0.73828740555555583	0.73980408888888916	0.74132380833333344	0.74285301111111124	0.74439062777777798	0.74591717500000021	0.74744106666666688	0.74896458055555581	0.75049532500000016	0.75201731944444461	0.753543488888889	0.75506965833333339	0.75657723888888895	0.7580927833333333	0.75960795000000003	0.76112311666666665	0.76264584166666671	0.76416100555555555	0.7656814833333333	0.76720347777777775	0.76872471388888886	0.77024632777777768	0.77176832222222214	0.77328804166666654	0.77480662222222207	0.77632558055555545	0.77784491944444423	0.77936767222222203	0.78088625277777768	0.78240483333333322	0.78392341388888886	0.78543744166666662	0.78695298611111097	0.78847346388888873	0.78999469999999983	0.79151745277777763	0.79304020555555543	0.79456144166666653	0.79608305555555536	0.79759784166666658	0.79911490277777764	0.80063765555555544	0.80216040833333324	0.80368695555555547	0.80520819166666657	0.80672942777777767	0.80824383333333327	0.80975823888888887	0.81127492222222219	0.81279160555555552	0.81431359999999986	0.81583331944444426	0.81735645277777758	0.81887958611111089	0.82039930555555529	0.82191067777777749	0.8234319138888887	0.8249531499999998	0.82647779999999971	0.828002072222222	0.82952103055555526	0.8310263499999998	0.83253999722222194	0.8340540249999997	0.83556839166666641	0.83708275833333312	0.83860551111111081	0.8401214361111109	0.84163736111111098	0.84314644999999977	0.8446581999999998	0.84616994999999984	0.84768890833333321	0.84921090277777755	0.85073289722222201	0.85225185555555527	0.85376512499999979	0.85526818055555531	0.85677765555555541	0.85829130277777754	0.85981291666666648	0.86132690833333314	0.86284852222222197	0.86436786111111086	0.8658830249999997	0.86739173611111076	0.86890728055555522	0.87042434166666627	0.87194064444444408	0.87346225833333291	0.87498387222222174	0.8765009333333329	0.87801609722222174	0.87952594999999945	0.88104490833333282	0.88256386666666609	0.88408548055555491	0.88560937222222158	0.88712909166666598	0.88863252499999934	0.89013595833333259	0.89163826111111033	0.89315532222222149	0.89467238333333254	0.89618034166666583	0.89769056111111034	0.89921103888888809	0.9007273416666659	0.90224023055555469	0.90375387777777694	0.90526752499999918	0.90678458611111035	0.9083016472222214	0.90980621111111037	0.91130624999999932	0.91281344722222157	0.91431988611111037	0.9158146472222215	0.91733550277777709	0.91885635833333268	0.92038100833333258	0.9218976388888882	0.92341200555555492	0.92493020555555494	0.92644840555555497	0.9279567388888883	0.92946620555555493	0.93098819999999938	0.93250715833333264	0.93401662499999927	0.93553103055555487	0.93704353888888814	0.93855225555555488	0.94005380277777706	0.94157428055555481	0.94309475833333256	0.94461599444444366	0.94613039999999926	0.94764480555555486	0.94915693611111052	0.95066375555555493	0.95216794444444397	0.95368159166666611	0.9551959972222217	0.95670169166666619	0.95820738611111067	0.959717619444444	0.96122785277777734	0.96273922499999953	0.96425097499999957	0.96576386388888835	0.96727485555555504	0.96878660555555507	0.9702968388888884	0.97180707222222162	0.97331351111111053	0.97482070833333268	0.97632411111111039	0.97783016944444368	0.97933888611111042	0.98084911944444364	0.98235935277777697	0.98386541111111026	0.98537146944444354	0.98687449444444353	0.98838662499999919	0.98989837499999922	0.99140595277777699	0.99291694444444367	0.99442869444444371	0.99594044444444374	0.99745219444444377	0.99896508333333256	1.0004794888888882	1.0019954138888882	1.0035132361111105	1.0050249861111105	1.0065329416666662	1.0080348277777771	1.0095416472222216	1.0110503638888884	1.0125621138888883	1.014071208333333	1.015580683333333	1.0170897777777774	1.0186011499999996	1.0201011888888887	1.0216163527777775	1.0231356916666663	1.0246550305555551	1.0261622277777773	1.0276705638888883	1.0291788999999996	1.0306838222222217	1.0321898805555549	1.0336932833333328	1.0351951694444439	1.0367110249999996	1.038226880555555	1.0397318027777773	1.0412352055555549	1.0427386083333328	1.0442461861111105	1.0457579361111105	1.0472708249999994	1.0487837138888882	1.0502981194444438	1.0518196999999994	1.0533238638888884	1.0548238527777773	1.056327255555555	1.0578295583333328	1.059339791666666	1.0608488861111105	1.0623591194444439	1.0638610055555551	1.0653575805555551	1.0668541555555551	1.0683552833333327	1.0698639999999995	1.0713677833333326	1.0728719472222217	1.0743753499999993	1.0758779944444439	1.077382916666666	1.0788942888888882	1.0804060388888883	1.0819174111111105	1.0834287833333327	1.084935980555555	1.0864435583333327	1.0879484805555548	1.089457080555555	1.0909657972222215	1.0924745138888883	1.0939798138888883	1.0954968138888883	1.0970043916666661	1.0985077944444439	1.1000111972222215	1.1015163611111105	1.1030144527777772	1.1045178555555548	1.1060239138888881	1.1075435861111105	1.1090541999999992	1.1105583638888881	1.1120625277777771	1.1135663111111105	1.1150764388888881	1.1165855333333325	1.1180946277777772	1.1196100999999994	1.121121755555555	1.1226236416666662	1.1241209749999994	1.1256246111111106	1.1271297749999996	1.1286391388888883	1.1301391277777773	1.1316501194444439	1.1331678833333327	1.1346806833333329	1.1361818111111106	1.1376961388888884	1.1392150472222218	1.1407328111111108	1.1422411472222218	1.1437468277777774	1.1452619194444438	1.1467812111111104	1.1482974472222216	1.1498035055555549	1.1513118416666659	1.1528318944444438	1.1543576749999993	1.1558705638888882	1.1573902361111104	1.1588995999999991	1.1604101083333325	1.1619127527777771	1.1634237444444435	1.1649464694444436	1.1664695777777769	1.1679771555555547	1.1694813194444436	1.1709838111111104	1.1724889749999994	1.1739983388888884	1.1754987083333326	1.176999077777777	1.1785111138888882	1.1800235333333324	1.1815286972222214	1.1830296611111104	1.1845336805555549	1.1860376999999991	1.1875443916666659	1.1890442111111104	1.1905398305555546	1.1920339222222214	1.1935409944444437	1.1950480666666661	1.1965547583333329	1.1980637388888884	1.1995757749999993	1.2010862833333327	1.2026042527777772	1.2041174333333327	1.2056294694444436	1.2071415055555548	1.2086594749999993	1.2101646388888883	1.2116724749999992	1.2131860388888882	1.2146996027777772	1.2162237194444439	1.2177372833333329	1.2192458833333328	1.2207510472222218	1.2222588833333328	1.2237747388888884	1.2252905944444441	1.2267972861111109	1.2283144888888886	1.2298316916666665	1.2313315111111109	1.2328374388888887	1.2343494749999999	1.2358622749999997	1.2373731666666663	1.2388817666666663	1.2403842583333329	1.241897619444444	1.2434086749999995	1.2449172749999995	1.2464308388888885	1.2479466944444439	1.2494692749999996	1.2509857083333329	1.2524927805555552	1.2540021444444442	1.2555092166666666	1.2570287249999998	1.2585453444444443	1.2600558527777777	1.2615667444444441	1.2630858666666664	1.2645925583333333	1.2661007777777775	1.2676112861111108	1.2691350194444444	1.2706602888888887	1.2721863277777776	1.2737006555555552	1.2752209305555553	1.2767423583333333	1.278263786111111	1.2797754416666665	1.2812941805555553	1.2828060055555555	1.2843255138888887	1.2858367861111111	1.2873480583333334	1.28886795	1.2903916833333333	1.2919169527777778	1.2934339527777776	1.2949580694444445	1.2964818027777778	1.2980040000000002	1.2995219694444444	1.3010263694444444	1.3025462611111109	1.3040661527777775	1.3055732249999998	1.3070802972222222	1.3085982666666665	1.3101143166666664	1.31163075	1.3131471833333332	1.3146636166666668	1.3161823555555556	1.3177068555555556	1.3192238555555553	1.3207408555555553	1.3222684305555554	1.3237921638888888	1.3253128222222221	1.3268400111111109	1.3283631194444443	1.3298929999999998	1.3314213416666665	1.3329516055555555	1.3344738027777776	1.3359902361111111	1.3375066694444444	1.3390192611111109	1.3405217527777777	1.3420242444444446	1.343537988888889	1.3450521194444445	1.3465631750000002	1.3480769194444446	1.3495841333333336	1.3511001833333336	1.3526162333333334	1.3541280583333335	1.3556379611111113	1.3571532416666667	1.3586685222222223	1.3601795777777779	1.3616940916666669	1.3632101416666667	1.3647261916666666	1.3662364805555556	1.3677483055555555	1.3692643555555555	1.3707865527777776	1.3723045222222221	1.3738201888888888	1.3753431527777777	1.3768735861111112	1.3784032472222223	1.379924675	1.3814430305555556	1.3829602333333335	1.384475977777778	1.385982038888889	1.3874880999999999	1.3889983888888888	1.3905163583333331	1.3920409944444443	1.3935636972222223	1.3950747527777778	1.3965831194444445	1.3981077555555557	1.3996389611111113	1.4011748055555557	1.4026920083333336	1.4042092111111115	1.4057237250000005	1.4072414027777782	1.4087579194444451	1.4102674388888894	1.4117838722222227	1.4133158500000005	1.4148458972222229	1.416375944444445	1.4179031333333338	1.4194335666666673	1.4209582027777785	1.4224878638888896	1.424010444444445	1.4255288000000006	1.427042544444445	1.4285714305555564	1.4300933611111117	1.4316028805555561	1.4331085583333338	1.4346243027777783	1.4361427527777784	1.4376639083333338	1.4391776527777784	1.4406883250000007	1.4422032972222232	1.4437167222222231	1.4452413583333343	1.4467635555555565	1.4482932166666675	1.4498186250000009	1.4513432611111119	1.4528678972222231	1.4543900944444454	1.4559120250000008	1.4574358861111119	1.4589640000000008	1.4604928861111119	1.462022986111112	1.4635449166666674	1.4650668472222228	1.4665852972222229	1.4681006555555562	1.4696225861111116	1.4711468333333337	1.4726691500000004	1.4741906916666672	1.4757204027777782	1.4772407861111116	1.4787588500000006	1.480276141666667	1.4817903416666669	1.4833095666666671	1.4848315000000005	1.4863534305555559	1.4878761333333339	1.4893992222222228	1.4909262111111117	1.4924539777777783	1.4939793861111115	1.4955071138888894	1.4970309750000004	1.4985614638888893	1.500088452777778	1.5016018805555558	1.5031168527777783	1.5046322111111115	1.5061627000000004	1.5076904666666671	1.5092019611111116	1.5107227277777782	1.5122454388888893	1.5137720388888891	1.5152966944444448	1.5168217388888894	1.5183401888888892	1.5198667888888893	1.5213887222222227	1.5229168777777782	1.5244415333333339	1.5259658000000005	1.5274869555555561	1.5290116111111118	1.5305440444444451	1.5320764777777787	1.5336085222222231	1.5351409555555566	1.5366648333333344	1.5381891000000012	1.5397094777777789	1.5412356888888898	1.542761900000001	1.5442896666666677	1.5458178222222232	1.5473521638888899	1.5488900277777788	1.550419350000001	1.5519482833333345	1.55347993888889	1.5550264111111121	1.5565685805555565	1.55809751388889	1.5596229472222234	1.5611476027777791	1.5626722583333346	1.5642112972222235	1.5657394527777793	1.5672672194444459	1.5687883750000013	1.570309530555557	1.5718450472222238	1.5733731305555572	1.5749051277777795	1.5764336722222241	1.5779711444444462	1.5795086166666683	1.5810413944444459	1.5825718250000016	1.5840867583333349	1.5856113194444459	1.5871323583333348	1.5886557472222236	1.5901834388888902	1.5917130861111124	1.593235019444446	1.5947623194444458	1.596290794444446	1.5978165305555572	1.599338744444446	1.6008672194444462	1.6024031277777795	1.6039398194444461	1.605473380555557	1.6070146611111125	1.6085539722222235	1.6100851861111125	1.6116128777777792	1.613142916666668	1.6146733472222234	1.6162162027777791	1.6177645694444458	1.6192981305555569	1.6208289527777791	1.6223636861111126	1.6239019416666682	1.6254573916666681	1.6269979944444457	1.6285350777777789	1.6300670750000013	1.6316099305555569	1.6331519972222237	1.6346968194444458	1.6362354666666681	1.637779591666668	1.6393362250000014	1.6408924638888902	1.6424447666666679	1.6439795000000015	1.6455193222222235	1.6470540555555571	1.6486000583333347	1.6501503916666678	1.6516971833333345	1.6532327000000011	1.6547678250000013	1.6563067444444457	1.6578393638888902	1.6593743444444455	1.6609140500000013	1.6624608416666677	1.6640096000000011	1.6655552111111123	1.6670988527777788	1.6686409194444456	1.6701837750000013	1.6717305666666677	1.6732809000000011	1.6748434361111122	1.6764032166666678	1.6779716027777789	1.6795258722222235	1.6810750250000011	1.6826131555555566	1.6841445944444455	1.6856959527777788	1.6872580027777788	1.6888107000000012	1.690347650000001	1.6918905055555566	1.6934313916666679	1.6949776000000012	1.6965285611111123	1.6980718083333346	1.6996103333333346	1.7011453138888901	1.7026802944444457	1.7042272944444457	1.7057739000000012	1.7073096694444456	1.7088450444444458	1.7103863250000013	1.7119384750000013	1.7134846833333346	1.7150269333333346	1.7165552250000011	1.7180858777777788	1.7196277305555565	1.7211798805555565	1.7227359888888898	1.7242893250000011	1.7258470194444453	1.7273952083333342	1.7289275583333341	1.7304686194444452	1.7320191861111121	1.7335838166666675	1.7351480500000007	1.7367073277777785	1.7382594777777785	1.739815586111112	1.7413728833333342	1.7429418944444452	1.7444987944444452	1.7460545083333341	1.7476098250000007	1.7491706861111118	1.750730358333334	1.752292597222223	1.7538487055555563	1.7553965000000009	1.7569534027777787	1.758523611111112	1.7600926222222231	1.7616536666666673	1.7632125472222229	1.7647658833333342	1.7663257333333342	1.7678883722222229	1.7694569861111118	1.7710160388888896	1.7725659305555561	1.7741030305555561	1.7756493361111119	1.7772032111111118	1.7787642555555563	1.7803221138888896	1.7818819638888896	1.7834309444444452	1.7849644805555562	1.786522736111112	1.7880861722222232	1.7896412416666676	1.7911931250000008	1.7927349777777786	1.7942823750000008	1.7958414277777783	1.7974000833333341	1.7989607305555564	1.8005225722222231	1.8020868055555563	1.8036566138888896	1.8052280166666674	1.8067930444444451	1.8083556833333341	1.8099115500000009	1.8114650250000011	1.8130196972222232	1.8145867194444454	1.8161609111111119	1.817727933333334	1.819293361111112	1.8208548055555562	1.822413061111112	1.8239673333333342	1.8255204111111119	1.8270778694444454	1.8286325416666676	1.8301896027777784	1.8317499222222229	1.833303397222223	1.8348552805555562	1.8363964055555564	1.8379502805555565	1.8395226222222232	1.8410965666666674	1.8426528305555563	1.8442075027777785	1.845753808333334	1.8472981222222231	1.8488500250000008	1.8503967166666675	1.8519514250000007	1.8535092833333342	1.8550727194444454	1.8566333666666677	1.8582029027777789	1.8597692333333344	1.8613427777777787	1.8629095083333342	1.8644693583333343	1.8660343861111122	1.8676011166666677	1.8691622361111122	1.8707205500000008	1.8722816694444453	1.8738383333333342	1.8753965888888897	1.8769661250000009	1.8785484833333344	1.8801272361111121	1.8816991750000012	1.8832610972222232	1.8848165638888901	1.8863869000000013	1.8879580388888901	1.8895303805555568	1.891100316666668	1.8926634388888901	1.8942205500000013	1.8957668555555569	1.8973359916666681	1.8989059277777793	1.9004714555555573	1.9020458000000016	1.9036145333333347	1.9051776555555571	1.9067423833333348	1.9083055055555569	1.9098650222222238	1.9114233361111126	1.9129860583333347	1.9145455750000013	1.9161050916666682	1.9176581972222237	1.9192137055555571	1.920772422222224	1.922328333333335	1.9238826416666683	1.9254401555555571	1.9270254277777794	1.9285937611111126	1.9301556833333349	1.9317079861111124	1.9332602888888901	1.9348170000000011	1.9363685027777788	1.937938052777779	1.939523325000001	1.9410984722222235	1.9426611944444456	1.9442243166666677	1.9457970916666676	1.9473747055555566	1.9489442555555565	1.9505198527777787	1.9520869833333343	1.9536501055555566	1.9552140305555563	1.9567847916666674	1.9583640166666674	1.9599367916666672	1.961514405555556	1.9630767277777783	1.9646510722222226	1.9662306277777781	1.9678146916666668	1.9693882750000002	1.9709622611111113	1.9725354388888892	1.9741033722222225	1.9756769166666668	1.9772561416666667	1.9788349638888889	1.9804041111111113	1.9819772888888891	1.9835335361111113	1.9850774222222225	1.9866293250000002	1.9882025027777781	1.989772052777778	1.9913407972222223	1.9929115583333334	1.9944726444444447	1.9960409861111115	1.9976186000000002	1.9992034694444447	2.0007847111111112	2.002362325	2.0039423583333336	2.0055272277777778	2.0071177416666668	2.0087026111111115	2.0102794194444447	2.0118646916666667	2.0134410944444445	2.0150247555555558	2.0165999500000003	2.0181815722222223	2.0197619777777778	2.0213339472222223	2.0229079333333333	2.0244915944444446	2.0260675944444446	2.0276359361111114	2.029206202777778	2.0307728222222226	2.032345927777778	2.0339074166666666	2.035476563888889	2.0370481305555557	2.0386285361111112	2.0402004250000001	2.041768666666667	2.0433336638888893	2.0448951527777779	2.0464598666666669	2.0480330444444448	2.0496138555555556	2.0511841250000002	2.0527584472222227	2.0543364194444447	2.0559164194444448	2.0574964194444445	2.0590639555555561	2.0606427388888893	2.0622280111111113	2.0638140944444445	2.0654018000000001	2.0669870722222226	2.0685674777777776	2.0701418	2.0717193666666667	2.073300177777778	2.0748753111111111	2.0764504444444443	2.0780280111111114	2.079601927777778	2.0811859833333335	2.0827607750000001	2.0843468583333333	2.0859296972222223	2.0875084805555555	2.0890864527777779	2.0906648305555557	2.0922541555555556	2.0938487527777778	2.0954510555555554	2.0970505194444446	2.098645927777778	2.1002247111111112	2.1018132249999999	2.1034029555555556	2.1049934194444444	2.1065851083333333	2.108166325	2.1097487583333336	2.111335652777778	2.1129180861111112	2.1144911944444447	2.1160706444444446	2.1176570305555558	2.1192536111111111	2.1208461138888888	2.1224326027777778	2.1240280111111112	2.1256181500000002	2.1272057583333335	2.1287901027777778	2.130373225	2.1319563472222223	2.1335423250000005	2.135121513888889	2.1367075972222227	2.1382924638888894	2.1398747694444449	2.1414640083333336	2.143051208333334	2.1446392250000006	2.146228055555556	2.1478266750000006	2.1494091083333338	2.1510024277777786	2.1525949305555563	2.1541911027777783	2.1557848277777785	2.1573826333333339	2.1589714638888893	2.1605676361111117	2.1621492583333337	2.1637348277777781	2.1653289611111117	2.1669235027777782	2.1685204916666674	2.1701174805555561	2.1717136555555561	2.1733248527777782	2.1749331777777781	2.1765183388888896	2.1781026833333339	2.1796882527777783	2.1812750444444449	2.1828618361111114	2.1844478138888892	2.1860442416666674	2.1876373888888896	2.1892325861111122	2.1908206027777788	2.1924106583333343	2.1940096861111122	2.1956123861111121	2.1972207111111119	2.1988290361111122	2.2004353111111121	2.202043225000001	2.2036458083333343	2.2052432055555564	2.2068357083333341	2.2084345972222232	2.2100334861111119	2.2116196583333343	2.2132021388888896	2.2147780555555565	2.21635971388889	2.2179413722222234	2.2195200083333346	2.2211023138888901	2.2226789111111125	2.224261216666668	2.2258502611111122	2.2274372527777788	2.2290262972222235	2.2306190333333342	2.2322207944444452	2.23380513888889	2.2353921305555566	2.2369778944444452	2.2385661194444451	2.2401588555555563	2.2417458472222229	2.2433348916666671	2.2449255777777783	2.2465273388888893	2.2481214722222225	2.2497240555555558	2.251320483333334	2.2529095277777782	2.2544928277777783	2.2560822833333338	2.2576832250000005	2.2592895000000004	2.2608846972222225	2.262491591666667	2.2640884305555562	2.2656832166666669	2.2672763638888895	2.2688686888888894	2.2704544500000003	2.2720357000000004	2.2736140777777782	2.2752032305555563	2.2767965083333341	2.278389786111112	2.279969394444445	2.2815514638888894	2.2831597888888893	2.2847664722222225	2.2863657722222226	2.2879671222222222	2.289575255555556	2.2911784361111116	2.2927865694444454	2.2943875111111121	2.295989683333334	2.2975984194444452	2.2992116666666673	2.3008146583333335	2.3024285666666668	2.304037936111111	2.3056526694444441	2.3072636888888889	2.3088841999999996	2.3104978583333331	2.3121065944444443	2.313713688888889	2.3153329611111113	2.316947694444444	2.3185657277777771	2.3201833499999998	2.3218017972222218	2.3234086916666663	2.3250098083333333	2.3265959805555556	2.3281892583333335	2.3297916138888892	2.3313947944444449	2.3329963250000003	2.3345999166666664	2.336200622222222	2.3377988527777775	2.3393979055555554	2.3409887083333332	2.3425695472222223	2.34416695	2.3457742555555554	2.3473823861111107	2.3489913416666663	2.3505879194444446	2.3521877999999998	2.3537979944444447	2.355406538888889	2.3570359472222222	2.3586576944444446	2.3602563361111111	2.3618545666666666	2.3634552722222217	2.3650687694444441	2.3666872166666666	2.3683139166666667	2.3699406166666668	2.3715795694444441	2.373218522222222	2.3748587194444442	2.3764910333333327	2.3781053555555549	2.3797229777777775	2.3813405999999997	2.3829553333333329	2.3845634666666662	2.3861741999999997	2.3877803694444442	2.3893865388888886	2.3909902194444439	2.3925968027777773	2.3941917305555549	2.3957990361111103	2.397404691666666	2.399020663888888	2.400631397222222	2.4022450361111107	2.4038549416666664	2.4054698249999995	2.4070801444444441	2.4086912944444441	2.4103024444444436	2.4119080999999993	2.4135211833333328	2.4151410472222219	2.416762155555555	2.4183695694444443	2.4199803027777778	2.4215839833333335	2.4231884916666666	2.4247938305555556	2.4263954333333331	2.4280153722222222	2.429628597222222	2.4312393333333335	2.432855877777778	2.4344574833333334	2.4360624083333335	2.4376806138888889	2.4393025527777779	2.440911627777778	2.4425223638888895	2.4441431361111112	2.4457735083333332	2.4473963694444447	2.4489971444444447	2.450604558333334	2.4522036722222231	2.4538206305555565	2.4554413250000011	2.4570620194444457	2.4586861305555567	2.4603044000000009	2.4619189138888902	2.4635376000000013	2.4651592083333345	2.4667678666666677	2.4683678111111123	2.4699694166666677	2.4715784916666679	2.4731846611111123	2.4747983388888901	2.4764078444444455	2.4780069166666676	2.4796018138888898	2.4811967111111124	2.4827788111111122	2.4843787555555568	2.4859799444444453	2.4875815500000007	2.4891756138888899	2.4907784416666674	2.4923946250000006	2.4940145638888898	2.4956382583333343	2.4972636222222233	2.4988864833333344	2.5005093444444455	2.5021242277777791	2.503737036111112	2.5053515500000012	2.5069568805555567	2.5085672194444455	2.5101838194444457	2.5117916555555571	2.513398655555557	2.5150119166666682	2.516622672222224	2.5182392722222242	2.5198679944444464	2.5214992027777798	2.5231387583333356	2.5247749750000024	2.5263982527777804	2.5280144361111136	2.5296327055555579	2.5312551472222244	2.5328750861111136	2.5345084250000025	2.5361430250000025	2.5377704888888917	2.5394017305555585	2.5410270944444471	2.5426349305555584	2.5442431833333359	2.5458518527777803	2.547462608333336	2.5490746166666693	2.5506857916666696	2.552317033333336	2.5539457555555587	2.5555858111111145	2.5572258666666703	2.5588617250000034	2.5604783250000036	2.5620890805555594	2.5636994194444482	2.5653164361111154	2.5669422222222265	2.5685785000000041	2.5702030250000041	2.5718342666666709	2.573460052777782	2.5750791222222262	2.5766923138888926	2.5783105444444483	2.579921638888893	2.581529475000004	2.58314983055556	2.5847651777777818	2.5863867666666707	2.588007936111115	2.5896349805555596	2.5912632833333373	2.5928756388888932	2.5944787583333375	2.5960978277777818	2.5977215138888927	2.5993468805555597	2.6009568027777816	2.6025838472222262	2.6042142500000041	2.605838775000004	2.6074645611111151	2.6090974805555596	2.6107291416666709	2.6123675194444487	2.61400715555556	2.6156446583333381	2.6172766750000047	2.6189048916666717	2.6205263555555605	2.6221458444444492	2.6237842222222274	2.6254318333333382	2.6270760861111158	2.6287174000000046	2.6303553583333379	2.6319824027777825	2.6336115444444492	2.635249469444449	2.6368861277777826	2.6385240527777825	2.6401543805555603	2.6417927277777826	2.6434201916666713	2.645049333333338	2.6466814138888939	2.6483218888888942	2.6499682388888939	2.6516032083333383	2.6532386000000048	2.6548845444444491	2.6565250000000051	2.6581536388888942	2.6597970500000048	2.6614434166666716	2.6630935805555604	2.6647382527777825	2.6663846027777827	2.6680309527777823	2.6696718472222267	2.6713056055555602	2.6729339083333379	2.6745815416666709	2.6762131361111159	2.6778354444444488	2.6794674611111158	2.6810965222222269	2.6827264277777827	2.6843601305555604	2.6859771027777821	2.68759953055556	2.6892173416666707	2.6908257194444487	2.6924450722222262	2.6940580944444488	2.6956795583333375	2.6973077750000045	2.6989258611111153	2.7005612527777818	2.7021974888888933	2.7038219083333379	2.7054573000000044	2.7070808750000044	2.7087016222222267	2.7103420805555603	2.7119871805555604	2.7136457888888934	2.7152908888888936	2.7169279694444493	2.7185680055555608	2.7202029750000052	2.7218333027777826	2.7234610972222275	2.7250956444444494	2.726736102777783	2.7283778277777833	2.7299977361111161	2.7316162444444494	2.7332313750000048	2.7348595916666718	2.7364945611111162	2.7381257333333382	2.7397653472222268	2.7414003166666712	2.7430323333333377	2.7446639277777827	2.7463069166666716	2.7479401972222273	2.7495861416666716	2.7512266000000052	2.7528657916666717	2.7545210222222272	2.7561737194444493	2.7578205083333382	2.7594622305555605	2.7611018444444491	2.7627309055555602	2.7643633416666717	2.7659911361111162	2.7676180861111161	2.7692425027777832	2.7708686083333385	2.7725038500000054	2.7741327250000056	2.7757700888888945	2.777412972222228	2.7790428777777834	2.7806761611111166	2.7823081777777836	2.7839397722222281	2.7855722111111172	2.787218155555562	2.7888603027777839	2.7904923194444509	2.7921023861111176	2.7937265916666729	2.7953541916666729	2.7969898583333395	2.798622977777784	2.8002620388888952	2.8019040722222286	2.8035419972222284	2.8051841444444507	2.8068317777777838	2.808476877777784	2.8101304194444507	2.8117738305555617	2.8134100666666728	2.8150444583333396	2.8166792750000065	2.8183081500000067	2.8199378750000066	2.8215731166666735	2.8232113305555622	2.824850816666673	2.8264979444444509	2.8281395527777842	2.8297677694444507	2.8313980972222286	2.8330242027777843	2.8346579055555621	2.8362954083333398	2.8379433833333394	2.8395883861111173	2.8412423027777844	2.8428826388888955	2.8445229750000069	2.8461654333333404	2.8478061916666739	2.8494490722222294	2.8510902555555631	2.8527369583333408	2.8543833250000077	2.856029269444452	2.8576688833333406	2.8593100666666738	2.8609550694444517	2.8625992250000074	2.8642518694444519	2.8659062111111187	2.8675465472222301	2.869183911111119	2.8708229722222303	2.872469675000008	2.8741176500000081	2.8757579861111191	2.8774012916666747	2.8790412027777856	2.880683236111119	2.88232357222223	2.8839664555555635	2.8856101861111192	2.8872560388888968	2.8889103805555636	2.8905664222222303	2.8922292555555633	2.8938734111111191	2.8955141722222302	2.8971519611111192	2.8987910222222304	2.9004215944444525	2.9020572611111191	2.9037161500000077	2.9053711972222298	2.9070145027777854	2.9086616305555633	2.9103108805555631	2.9119618277777852	2.9136115000000076	2.9152666916666741	2.9169231555555628	2.9185864111111179	2.9202390555555624	2.9218810888888957	2.9235222722222289	2.925177888888896	2.9268415694444516	2.9285094222222292	2.9301785555555626	2.9318481166666737	2.9335146888888959	2.9351694555555623	2.9368237972222291	2.938471347222229	2.9401248416666732	2.9417834277777843	2.9434356472222292	2.9450768305555624	2.9467163166666737	2.9483575000000068	2.9500108416666739	2.951656500000007	2.9533051444444518	2.9549589111111185	2.9566122527777852	2.9582643138888964	2.9599069833333407	2.9615328861111183	2.9631643083333405	2.9647961527777853	2.966432666666674	2.9680776694444515	2.9697252194444514	2.9713693750000072	2.9730156527777853	2.9746788111111191	2.9763372722222301	2.9779940277777857	2.979653769444452	2.9813088166666746	2.9829608777777858	2.9846048277777855	2.9862483500000079	2.9878918722222303	2.9895477750000081	2.9912032500000079	2.9928457083333413	2.9944945333333415	2.9961560916666747	2.9978061888888972	2.9994465250000086	3.0010977305555642	3.0027472305555643	3.004400997222231	3.0060551916666753	3.0077008500000089	3.0093482138888974	3.0109930166666756	3.0126331250000087	3.0142719527777864	3.0159133416666752	3.0175470472222305	3.0191918500000083	3.0208375083333419	3.0224757222222309	3.0241024750000083	3.0257330472222304	3.027371875000008	3.0290124111111192	3.0306589222222304	3.0323092750000078	3.0339681638888969	3.035624919444452	3.0372816750000076	3.0389371500000073	3.0405904916666739	3.0422481000000072	3.0438988805555627	3.0455483805555632	3.0471940388888967	3.0488401222222299	3.050470694444452	3.0521101805555628	3.0537445722222296	3.055380413888896	3.0570316194444516	3.0586828250000075	3.0603459833333408	3.0620151166666743	3.0636714444444517	3.0653260666666742	3.0669717250000077	3.0686165277777855	3.0702613305555633	3.071916805555563	3.0735692916666744	3.0752311694444523	3.0769022805555633	3.0785600861111186	3.0802213250000077	3.081886425000008	3.083555986111119	3.0852242666666752	3.0868899861111196	3.088549730555564	3.0901996555555642	3.0918397638888973	3.0934768833333419	3.0951229666666751	3.0967771611111194	3.0984347694444527	3.1000881111111194	3.1017376111111199	3.1033922333333419	3.1050541111111198	3.1067260805555645	3.1083911805555644	3.1100601444444536	3.1117256750000091	3.1133770416666757	3.1150244055555647	3.1166760388888979	3.1183199888888975	3.1199618055555645	3.1215938027777868	3.1232266555555643	3.1248701777777868	3.126512847222231	3.1281482611111198	3.1297926388888975	3.1314400027777864	3.1330965194444533	3.1347564694444534	3.1364280083333425	3.1380974027777868	3.1397783861111201	3.1414494972222311	3.1431094472222312	3.1447651055555648	3.1464186194444532	3.1480642777777867	3.1497086555555649	3.1513543138888984	3.1529999722222319	3.1546597166666763	3.1563258638888985	3.1579868888888987	3.1596581583333427	3.1613213166666765	3.1629904500000094	3.1646581277777877	3.1663090666666767	3.1679630083333437	3.1696165222222321	3.171270036111121	3.1729274111111208	3.1745955166666762	3.1762636222222316	3.1779385944444538	3.1795953500000094	3.1812491166666756	3.1829058722222312	3.1845570777777867	3.1862181027777869	3.187873150000009	3.1895166722222315	3.1911661722222315	3.1928084138888981	3.194461925000009	3.1961051361111199	3.1977483472222312	3.1993902722222312	3.2010321972222311	3.2026814166666755	3.2043276333333424	3.2059665527777872	3.2075998916666761	3.209243102777787	3.2108948972222313	3.2125554944444539	3.2142062750000093	3.2158724194444539	3.2175351500000096	3.219200869444454	3.2208606138888984	3.2225096861111204	3.2241621722222318	3.2258212638888981	3.2274825027777871	3.2291476027777875	3.2308084111111208	3.2324838138888987	3.2341527777777874	3.235808436111121	3.2374692444444544	3.2391201805555658	3.2407779861111212	3.2424435166666767	3.2441090472222323	3.2457582666666767	3.2474022166666767	3.2490418972222326	3.2506811527777884	3.252316138888899	3.2539477111111212	3.2555873916666771	3.2572394527777884	3.2588936472222323	3.260547413888899	3.262201355555566	3.2638548666666769	3.2655122416666766	3.2671773416666765	3.2688330000000101	3.2704805027777879	3.2721224277777883	3.2737733638888993	3.2754290222222329	3.2770803888888995	3.2787300388888996	3.2803801166666773	3.2820233277777886	3.2836681305555664	3.2853133611111218	3.2869560305555661	3.2886134055555658	3.2902652027777881	3.291918716666677	3.2935859638888991	3.2952536416666773	3.296912305555566	3.2985756888888993	3.3002403611111215	3.3018951611111218	3.3035452388888995	3.3052008972222331	3.3068612777777888	3.3085083527777885	3.3101494194444552	3.3117874805555667	3.3134324083333442	3.3150743333333441	3.3167166861111217	3.3183646194444552	3.3200171055555661	3.3216774861111218	3.3233408694444551	3.3250051111111221	3.3266809416666776	3.3283572027777888	3.3300261666666775	3.331691697222233	3.3333533638888997	3.3350068777777886	3.3366599611111218	3.3383147611111221	3.3399657000000111	3.3416316611111223	3.3432980500000111	3.3449610055555663	3.3466222444444553	3.3482757583333442	3.3499266972222332	3.3515754888889	3.3532281444444552	3.3548838027777887	3.3565454694444554	3.3582067083333444	3.3598619388888999	3.3615154500000108	3.3631625250000106	3.3648211888888997	3.3664819972222326	3.3681423777777884	3.3698057611111221	3.3714717194444552	3.3731325277777886	3.3747989166666774	3.3764623000000111	3.3781222500000108	3.3797912138888999	3.3814455833333441	3.3830836444444552	3.3847259972222328	3.3863760750000109	3.388014136111122	3.3896620694444555	3.3913134361111221	3.3929622277777884	3.3945895305555664	3.3962262250000106	3.3978539555555658	3.3994863805555657	3.4011343138888988	3.4027698000000099	3.404417733333343	3.4060686694444544	3.4077208944444544	3.4093718305555658	3.4110180472222327	3.412668555555566	3.4143177750000104	3.4159760083333439	3.4176411083333438	3.4192941916666775	3.420948133333344	3.4226072250000108	3.4242676055555665	3.4259224055555664	3.427573772222233	3.4292174138889	3.4308502666666776	3.4324750083333444	3.4341018861111223	3.4357360194444553	3.437374847222233	3.4390136750000107	3.4406559166666772	3.4423071222222328	3.4439583277777883	3.4456041138888995	3.447250758333344	3.4489016944444555	3.4505388972222333	3.4521868305555663	3.4538476388888997	3.4555187500000106	3.457180847222233	3.4588498111111221	3.4605110500000111	3.4621757222222334	3.4638369611111224	3.4655121250000112	3.4671872888889004	3.4688771277777892	3.4705669666666785	3.4722464472222341	3.4739229055555678	3.4755927277777903	3.4772612638889009	3.47891992777779	3.4805850305555679	3.4822406888889015	3.4838984944444569	3.4855502916666792	3.4871909277777906	3.4888405777777907	3.490489369444457	3.4921437416666792	3.4938062666666792	3.4954623555555679	3.49712500277779	3.4987707888889013	3.5004343000000122	3.5020960861111234	3.5037557138889013	3.5054252666666788	3.50708705277779	3.5087462472222342	3.5104019888889009	3.5120603222222342	3.5137264222222342	3.5153820805555678	3.5170398861111232	3.5187002666666789	3.5203404750000122	3.5219836861111231	3.5236311888889009	3.5252821277777904	3.5269425083333457	3.5286198305555683	3.5302846361111238	3.5319498722222349	3.5336177000000126	3.5352803472222347	3.5369300472222349	3.5385810416666792	3.5402316055555678	3.5418817388889012	3.5435258277777897	3.5451781166666785	3.5468329972222343	3.5484826972222345	3.5501362833333454	3.5517933194444571	3.5534551055555679	3.5551207750000127	3.5567669916666795	3.5584007611111237	3.560032383333346	3.5616640055555684	3.5633167277777904	3.5649759222222346	3.5666433166666791	3.5683171861111234	3.5699824222222341	3.5716511111111231	3.5733081472222343	3.574965183333346	3.5766217888889016	3.5782835722222348	3.579942766666679	3.5816028250000125	3.583262883333346	3.584931572222235	3.586607166666679	3.5882732666666795	3.5899350500000127	3.5916046027777906	3.5932694083333461	3.5949350777777904	3.5965960000000128	3.5982508777777906	3.5999170194444576	3.6015693083333464	3.6032203027777907	3.6048838138889017	3.6065378305555682	3.6081987527777906	3.609851475000013	3.6114985861111242	3.6131556222222354	3.614816975000013	3.6164778972222353	3.6181401138889022	3.6197967194444578	3.62145116666668	3.6231094972222353	3.624771280555569	3.6264322027777913	3.6280819027777911	3.6297398027777916	3.6314020194444585	3.6330820472222363	3.6347520944444582	3.6364034833333472	3.6380618138889025	3.6397231833333468	3.6413914944444579	3.6430736916666797	3.6447518777777912	3.6464179777777912	3.6480780361111247	3.6497294638889026	3.6513886583333468	3.6530400861111243	3.6546915138889022	3.65633646666668	3.6579956611111242	3.6596488138889014	3.6613110305555687	3.6629680694444575	3.6646216555555688	3.6662908361111244	3.6679569777777914	3.6696348361111246	3.671305752777791	3.6729679888889022	3.6746328305555687	3.6762942000000134	3.6779616444444576	3.6796416722222354	3.6813230027777908	3.6830095416666802	3.6846965138889023	3.686377411111124	3.6880483277777905	3.6897006166666793	3.6913429805555684	3.6929853444444571	3.6946372027777907	3.6962925138889018	3.6979499777777907	3.6996113472222349	3.7012688111111238	3.7029332166666795	3.7045963222222351	3.7062681055555684	3.7079407555555686	3.7096108027777905	3.7112917000000127	3.7129626166666791	3.7146300611111238	3.7163040138889012	3.7179736277777899	3.7196393361111233	3.7213145916666788	3.7229989583333452	3.7246672694444563	3.7263329777777896	3.7280047611111229	3.7296769777777894	3.7313517972222341	3.7330313916666782	3.7347000805555672	3.7363683388889006	3.7380262388889007	3.7396980222222345	3.7413728416666792	3.7430372472222344	3.7447125027777899	3.74638385277779	3.7480599750000123	3.7497400027777901	3.751413088888901	3.7530844388889011	3.7547605611111234	3.7564314777777899	3.7580993555555677	3.7597828555555681	3.7614663555555681	3.7631520250000126	3.7648394305555684	3.766521194444457	3.7682038277777905	3.7698847250000123	3.7715673583333453	3.7732408777777899	3.7749213388889014	3.776594858333346	3.7782657750000124	3.7799236722222349	3.781565605555568	3.7832230750000124	3.7848874500000123	3.7865692138889013	3.7882579222222343	3.7899418555555675	3.7916253555555679	3.7933114583333456	3.7949979944444565	3.7966736833333457	3.7983454666666789	3.8000202861111236	3.8016942388889015	3.803363419444457	3.8050430138889011	3.8067200055555679	3.808398730555568	3.8100774555555681	3.8117661638889011	3.8134514000000124	3.8151327305555678	3.8168114555555679	3.8184719555555677	3.8201333222222345	3.8217933888889011	3.8234630027777898	3.82514610277779	3.8268370583333455	3.8285280138889006	3.8302146055555673	3.8318981055555676	3.8335768333333453	3.8352607666666785	3.836940361111123	3.8386186527777895	3.8403034555555671	3.8419912944444565	3.8436708888889006	3.8453491805555671	3.8470213972222336	3.8486931805555669	3.8503536805555671	3.852027633333345	3.8537107000000117	3.855389861111123	3.8570690222222339	3.858758163888901	3.8604582805555676	3.8621566527777897	3.8638349527777898	3.8655298333333454	3.8672251500000119	3.8689078138889008	3.8705795694444562	3.872249144444456	3.8739235194444559	3.8756026944444555	3.877282741666678	3.8789675861111226	3.8806463138889002	3.8823167972222334	3.8839790333333446	3.885655155555567	3.8873312777777893	3.8889961194444558	3.8906739777777894	3.8923492333333449	3.8940275250000114	3.8956962722222337	3.8973654527777892	3.8990402750000115	3.9007211944444564	3.9024042944444566	3.9040817222222342	3.9057569694444565	3.9074326527777901	3.9090991722222346	3.9107539111111236	3.9124125777777903	3.9140808444444568	3.915764816666679	3.917442244444457	3.919120544444457	3.9208058277777904	3.9224836916666797	3.9241550111111243	3.9258224027777908	3.9274871777777904	3.929142905555568	3.9308021055555682	3.9324626055555685	3.9341430666666799	3.9358165861111245	3.9374935777777909	3.9391823500000132	3.9408637055555684	3.9425498611111238	3.9442377611111241	3.9459260972222348	3.9476170500000127	3.9493132388889016	3.9510007027777903	3.9526838027777909	3.9543699583333458	3.9560460777777906	3.9577300500000128	3.9594157694444574	3.9610958166666794	3.9627719361111242	3.9644441277777909	3.9661267916666798	3.9678068388889018	3.9694929944444572	3.9711874388889021	3.9728749027777908	3.9745597472222354	3.9762493916666801	3.9779434000000133	3.979638280555569	3.9813331611111247	3.9830267333333471	3.9847163777777914	3.986402097222236	3.988093050000014	3.9897800777777914	3.991463177777792	3.993149333333347	3.9948315611111251	3.9965168416666805	3.9981929611111253	3.999887841666681	4.00158883055557	4.003284147222236	4.0049838277777923	4.006667800000014	4.0083539555555694	4.010027894444459	4.0117070666666805	4.0133927861111252	4.0150806861111255	4.0167742583333474	4.0184621583333477	4.0201509305555705	4.0218340305555706	4.0235079694444593	4.0251905666666818	4.0268757944444591	4.0285610222222372	4.0302366000000154	4.0319130555555702	4.0335787027777927	4.035256566666682	4.0369326861111263	4.0386210222222374	4.0403071777777928	4.041995513888903	4.0436834138889033	4.0453800416666814	4.0470797222222368	4.0487746027777929	4.050469483333349	4.0521639277777934	4.0538465916666819	4.055521402777793	4.0571944666666822	4.0588771305555715	4.0605519416666818	4.062216280555571	4.0638814916666819	4.0655497583333489	4.0672123527777932	4.068892755555571	4.070589827777793	4.0722838305555715	4.0739769555555716	4.0756740277777936	4.0773645194444601	4.0790664194444597	4.0807731444444606	4.0824776750000158	4.0841725555555719	4.0858691833333491	4.0875549027777938	4.0892401861111276	4.0909376861111273	4.092633438888905	4.0943230833333502	4.0960053111111279	4.0976814305555722	4.0993579861111273	4.1010345416666834	4.102708480555572	4.1043907083333497	4.1060781722222393	4.1077765444444614	4.1094740444444611	4.1111737250000173	4.112871225000017	4.1145530166666839	4.1162308805555723	4.1179126722222392	4.1196136944444612	4.1213076972222398	4.1230021388889062	4.1246939472222399	4.126385316666684	4.1280679138889065	4.1297439305555725	4.131424772222239	4.1331060527777952	4.1347965444444617	4.1364687361111283	4.1381387472222393	4.1398087583333503	4.1414800777777945	4.1431535777777952	4.1448414777777955	4.14652239722224	4.1481937166666842	4.1498563111111286	4.1515223944444619	4.153195458333351	4.1548758611111287	4.156553194444462	4.1582335972222397	4.1599254055555734	4.1616158972222399	4.1633077055555736	4.1650039027777952	4.1667079944444616	4.1683980500000173	4.1700885416666837	4.1717829833333511	4.1734682111111283	4.1751565111111288	4.176841738888907	4.1785344250000174	4.1802257944444623	4.1819246222222404	4.1836212555555727	4.1853043555555729	4.1869830916666846	4.1886622638889062	4.1903362027777957	4.1920083944444624	4.1936830944444621	4.1953613027777958	4.1970320555555727	4.1987093861111289	4.2003932972222398	4.2020798416666842	4.2037606833333507	4.2054463500000177	4.2071263138889066	4.2088049611111291	4.2105007194444619	4.2121920888889059	4.2138821416666836	4.2155695638889066	4.2172534750000175	4.21893212222224	4.2206160333333509	4.222289855555573	4.2239553416666844	4.2256181972222393	4.2272876333333507	4.2289689138889059	4.2306519500000173	4.2323349861111277	4.2340425555555727	4.2357461555555727	4.2374418166666841	4.239120027777795	4.2408021861111287	4.2424821500000176	4.2441665027777953	4.245850855555573	4.2475360833333502	4.2492121000000171	4.250896013888906	4.2525781722222389	4.2542699805555726	4.255970125000017	4.2576724638889054	4.2593831361111283	4.2610942472222391	4.2628018500000167	4.2644984861111279	4.2661964361111275	4.26789263333335	4.2695853194444613	4.271269672222239	4.2729623583333494	4.2746585555555718	4.2763622083333495	4.2780513861111267	4.2797331055555716	4.2814157027777933	4.2830954861111268	4.2847836500000165	4.2864744611111272	4.2881727694444605	4.2898671083333495	4.29155540833335	4.2932485333333501	4.2949390250000166	4.296640925000017	4.2983340500000171	4.30001620833335	4.3017088944444613	4.3033980722222394	4.3050951444444614	4.3068001138889054	4.3084989416666835	4.3101942611111284	4.3118873861111284	4.3135831444444612	4.3152714444444618	4.3169636916666834	4.3186590111111283	4.3203609111111287	4.3220667583333512	4.3237677805555732	4.3254578361111289	4.3271470138889061	4.3288397000000174	4.3305214194444623	4.3321969972222396	4.3338756444444622	4.3355630666666842	4.3372531222222399	4.3389414222222404	4.34062059722224	4.3423089333333511	4.3440033777777955	4.3457039611111288	4.3473962083333513	4.3490809972222397	4.3507578916666843	4.3524444361111287	4.3541397555555736	4.3558328805555737	4.3575194250000182	4.3592147444444631	4.3608933916666848	4.3625808138889077	4.3642629722222406	4.3659473222222411	4.3676404472222412	4.3693199722222413	4.3709955500000186	4.3726680555555744	4.3743335416666858	4.3760012222222411	4.3776684638889085	4.379337900000019	4.3810068972222416	4.3826934416666861	4.3843716500000198	4.3860428388889083	4.3877118361111309	4.3893966250000194	4.3910722027777975	4.3927521666666864	4.394414322222242	4.3960734250000195	4.3977238027777981	4.3993932388889085	4.4010648666666867	4.4027413222222416	4.4044208472222417	4.4060924750000199	4.4077768250000195	4.4094664416666856	4.4111521083333525	4.412834705555575	4.4145102833333523	4.4161832277777968	4.417850908333353	4.4195295555555747	4.4212152222222416	4.4229022055555749	4.4245826083333535	4.4262647666666863	4.4279451694444649	4.4296295194444646	4.4313033416666867	4.4329679527777976	4.4346448472222422	4.4363313916666867	4.4380179361111312	4.4397123777777985	4.4414112055555757	4.4431060861111318	4.4447795861111317	4.4464670083333546	4.4481488000000207	4.4498257916666875	4.4515019111111318	4.4531867555555769	4.4548707277777986	4.4565555722222427	4.4582308194444655	4.4599099916666871	4.461588291666688	4.4632644111111324	4.4649318027777989	4.4666092305555765	4.4682897138889102	4.4699653972222437	4.4716410805555773	4.4733115277777991	4.4749767388889099	4.4766354055555766	4.4783019250000216	4.4799771722222435	4.4816624527777993	4.4833464250000219	4.4850299611111319	4.4866991000000214	4.4883660555555771	4.4900334472222436	4.4917012750000209	4.4933708500000211	4.4950404250000204	4.496707816666687	4.4983734638889095	4.5000529888889096	4.5017356527777981	4.5034218083333535	4.5051127611111319	4.5067845166666869	4.5084462361111317	4.5101175555555759	4.5117936750000212	4.5134689222222431	4.5151332611111323	4.5168067611111322	4.5184724083333547	4.5201424194444657	4.5218207194444657	4.523508619444466	4.525186919444466	4.5268674027777998	4.5285561750000216	4.530248875000022	4.5319341555555779	4.5336142027777999	4.5353003583333553	4.5369865138889107	4.538676158333355	4.5403570777777995	4.5420423583333553	4.543722841666689	4.5454041972222443	4.5470698444444659	4.5487507638889113	4.550434736111133	4.5521060555555781	4.5537630833333553	4.5554244500000225	4.5570827805555787	4.5587402444444676	4.56041029166669	4.5620825083333569	4.5637590638889129	4.5654382250000234	4.5671200166666903	4.5688079166666897	4.5704831638889116	4.5721466305555785	4.573814022222245	4.5754796694444675	4.577153608333357	4.5788292916666897	4.5804984305555791	4.5821610250000226	4.5838214361111342	4.5854870833333576	4.5871566583333578	4.588833213888913	4.5905071527778016	4.5921902527778018	4.5938781527778021	4.5955621250000247	4.597250025000025	4.5989348694444692	4.6006149166666912	4.6022993250000246	4.6039872250000249	4.6056746888889144	4.6073534166666921	4.6090282388889143	4.6107104361111366	4.6123926333333589	4.6140779166666919	4.6157618888889145	4.6174384444444696	4.6191001638889135	4.6207605750000251	4.622430586111137	4.6241128138889147	4.6257928611111359	4.6274742166666911	4.6291542638889132	4.6308303833333575	4.6324951583333576	4.6341673500000242	4.6358456500000242	4.6375169694444685	4.6391852361111354	4.6408513194444678	4.6425174027778011	4.6441878500000238	4.6458630972222457	4.6475448888889117	4.6492249361111337	4.650906291666689	4.6525758666666892	4.6542463138889119	4.6559163250000237	4.6575955000000242	4.6592672833333575	4.6609360305555798	4.6626043416666905	4.6642895777778017	4.665964400000024	4.667630541666691	4.6692975527778025	4.6709597888889132	4.6726215083333571	4.6742919555555797	4.675958038888913	4.6776311027778013	4.6793054777778016	4.6809885777778018	4.6826629527778021	4.6843373277778024	4.6860151916666917	4.6876965472222469	4.6893853194444697	4.6910740916666924	4.6927550111111369	4.6944267666666919	4.6961076861111364	4.6977929694444693	4.6994826138889128	4.7011678972222457	4.7028475083333579	4.7045253722222462	4.7062119638889133	4.7078963722222467	4.7095603444444691	4.7112156388889144	4.7128817805555805	4.7145613750000255	4.716252252777803	4.7179776750000251	4.7197078972222473	4.7214350666666913	4.7231670361111355	4.7248981305555802	4.7266327166666917	4.7283699222222468	4.7301106166666917	4.7318556750000251	4.7336011694444702	4.7353471000000251	4.7370917861111357	4.738835172222247	4.7405859333333584	4.7423353944444697	4.7440831194444693	4.7458347500000251	4.7475779666666922	4.7493198972222466	4.7510541000000241	4.752802466666691	4.7545504055555803	4.7563030666666917	4.7580574444444697	4.75980554444447	4.761548522222248	4.7632842416666925	4.7650131333333592	4.7667505611111372	4.7684815861111369	4.7702151722222483	4.7719479055555825	4.7736752555555819	4.775398786111138	4.777114252777805	4.7788186833333608	4.7805135916666943	4.7822156750000273	4.7839198694444711	4.7856212055555831	4.787317502777805	4.7890079250000275	4.7907088388889161	4.7924114333333607	4.7941001777778052	4.7957868222222491	4.797476825000027	4.7991748027778049	4.8008727805555829	4.8025774722222501	4.8042704472222502	4.8059671777778066	4.8076568138889169	4.8093381027778062	4.8110218944444734	4.8127102777778061	4.8143978277778068	4.816089133333362	4.817780438888918	4.8194659027778064	4.8211455250000288	4.8228230722222509	4.8244877527778067	4.8261594888889174	4.8278382805555839	4.8295199777778066	4.8311987694444731	4.832877144444474	4.8345621611111405	4.8362509111111409	4.8379409055555849	4.8396275805555851	4.8413213111111411	4.8430187777778073	4.8447079444444734	4.8463971111111395	4.8480871055555843	4.8497642361111399	4.8514409527778062	4.8531176694444733	4.8547952166666954	4.8564702722222508	4.8581519694444735	4.8598336666666961	4.8615153638889188	4.8631944638889184	4.8648731527778084	4.8665468888889194	4.868216500000031	4.8698918861111418	4.8715693361111425	4.8732352333333653	4.8749056694444759	4.8765629027778088	4.8782345777778087	4.8799041888889203	4.8815754500000317	4.8832529000000324	4.8849258111111427	4.8865892333333658	4.8882563694444769	4.8899181416666995	4.8915770250000321	4.893233433333366	4.894897680555589	4.8965652277778107	4.8982356638889222	4.8999011472222547	4.9015608555555881	4.9032292277778105	4.9048872861111441	4.906533352777811	4.9081790083333665	4.9098416055555889	4.9115017250000328	4.9131568944444775	4.9148141277778103	4.9164775500000326	4.9181228166666999	4.9197829361111438	4.9214595611111438	4.9231341222222547	4.9248049694444775	4.9264754055555882	4.928135525000032	4.9297911055555881	4.9314508138889215	4.9331216611111444	4.9348032361111445	4.9364947138889219	4.9381861916666994	4.9398636416667001	4.9415344888889221	4.9432065750000334	4.9448724722222552	4.946538369444478	4.948193950000034	4.949846169444478	4.9515086472222558	4.9531690722222557	4.9548192416667005	4.9564755638889224	4.9581310666667004	4.9597853388889224	4.9614355083333672	4.9630811638889227	4.9647305138889228	4.9663847861111448	4.9680464416667007	4.9697064555555901	4.9713640083333672	4.9730137666667007	4.9746495777778117	4.976303508333368	4.9779698166667012	4.9796291111111461	4.9812879944444788	4.9829456388889231	4.9846148361111453	4.9862968250000339	4.9879751000000336	4.9896455361111443	4.9913092416667002	4.9929725388889228	4.9946272194444781	4.9963011833333661	4.9979653000000326	4.9996265444444763	5.0012927138889216	5.0029502666666987	5.0046180750000326	5.0062768583333659	5.0079307194444773	5.0095882722222553	5.0112450055555886	5.0129059527778113	5.0145747388889221	5.0162443500000338	5.0178995194444784	5.0195588138889233	5.0212222361111456	5.0228786444444795	5.0245395916667013	5.0262005388889239	5.0278689111111463	5.0295335694444798	5.0311874305555913	5.0328499083333682	5.0345066416667024	5.0361609138889243	5.0378086222222578	5.0394546888889238	5.0410962444444793	5.0427390305555901	5.044387150000035	5.0460483972222576	5.0477059500000347	5.0493622722222566	5.0510198250000347	5.0526765583333679	5.0543439583333676	5.0560088972222568	5.0576801583333681	5.0593505944444788	5.0610152527778123	5.0626922916667008	5.0643581888889235	5.0660298638889234	5.0676970000000345	5.0693666111111462	5.0710349833333686	5.0726971666667025	5.0743440555555912	5.0759913527778142	5.07764439444448	5.0792929222222583	5.0809414500000365	5.0825953111111479	5.0842483527778137	5.0858960611111472	5.0875499222222587	5.0892037833333701	5.090856005555592	5.0925057638889255	5.0941563444444808	5.0958114361111475	5.0974616055555924	5.0991240833333702	5.1007918944444821	5.1024592944444818	5.1041193111111482	5.1057806694444814	5.1074370777778153	5.1090943111111482	5.1107503055555927	5.1123906305555931	5.114038750000037	5.1156926111111485	5.1173390888889259	5.1189839250000366	5.1206308138889263	5.1222801638889255	5.123921719444481	5.1255665555555918	5.1272113916667026	5.1288615611111474	5.1305211666667025	5.1321861055555917	5.133844888888925	5.1355036722222582	5.1371522000000365	5.1388007277778147	5.1404484361111482	5.1421014777778149	5.1437508277778141	5.145398947222259	5.1470569111111466	5.1487156944444807	5.1503836555555909	5.1520375166667023	5.153688505555591	5.1553477000000356	5.1570126388889248	5.1586693722222581	5.1603277472222588	5.1619746361111476	5.1636276777778143	5.1652770277778135	5.1669136583333692	5.168548238888925	5.1701877416667026	5.1718280666667029	5.1734782361111478	5.1751357888889258	5.1767863694444811	5.1784500777778151	5.1801224000000365	5.1817975944444807	5.1834742194444807	5.1851368166667031	5.1867861666667023	5.1884355166667024	5.1900762500000361	5.1917350333333694	5.193396277777814	5.1950591638889243	5.1967208194444803	5.1983832944444801	5.2000310027778127	5.2016815833333689	5.2033358555555909	5.2049888972222575	5.2066439888889242	5.2083089277778134	5.2099640194444801	5.2116137777778135	5.2132721527778134	5.2149264250000353	5.2165831583333695	5.2182427638889246	5.2198974444444799	5.2215545861111465	5.2232037833333687	5.2248493083333676	5.2264879000000342	5.228133425000034	5.229785883333367	5.2314399722222564	5.2330895750000339	5.2347395861111456	5.2363916361111462	5.2380530666667013	5.2397096055555901	5.2413579861111463	5.2430059583333684	5.2446494444444802	5.2462900750000356	5.2479266277778134	5.2495758250000355	5.2512156388889242	5.2528603472222573	5.254501386111146	5.2561432416667015	5.2577802027778127	5.2594126777778119	5.2610512694444784	5.2626857833333673	5.264325600000034	5.2659670472222571	5.2676191000000347	5.269254022222257	5.2708930222222561	5.2725377333333672	5.2741808111111448	5.2758275611111447	5.2774722722222558	5.2791296250000332	5.280779636111145	5.2824284250000337	5.2840800694444772	5.2857322916667	5.287372513888922	5.2890210416667003	5.2906667000000338	5.2923205611111452	5.2939628250000341	5.2955981527778127	5.2972412305555894	5.2988839000000345	5.3005282027778122	5.3021619000000344	5.3038025305555898	5.3054345972222565	5.3070760444444787	5.3087146361111452	5.3103536361111452	5.3120020166667006	5.3136483583333671	5.3152845027778124	5.3169226861111456	5.3185576055555899	5.3201908944444787	5.3218327500000342	5.323482919444479	5.3251400638889237	5.3268004888889235	5.3284699388889241	5.3301264777778137	5.3317691472222579	5.333408147222257	5.3350430666667013	5.3366812500000345	5.3383304472222566	5.3399804583333683	5.3416394444444792	5.3432870083333679	5.3449215222222568	5.3465625611111447	5.348209719444478	5.3498581000000334	5.3515222166666998	5.3531818222222549	5.3548426583333661	5.3564998027778108	5.3581610472222545	5.3598037166666987	5.3614427166666987	5.3630862027778097	5.3647140500000328	5.3663487916666996	5.367981505555588	5.3696105694444771	5.3712376055555877	5.3728686972222546	5.3744977611111437	5.3761316916666999	5.3777617166666998	5.3793897027778108	5.3810344111111439	5.3826815666666992	5.3843307638889213	5.3859771055555878	5.3876177361111433	5.3892571444444766	5.390899000000033	5.3925477888889217	5.3941900500000326	5.3958298638889222	5.3974660083333665	5.3990853416666997	5.4007075138889222	5.4023272527778117	5.4039469916667002	5.4055736250000335	5.407208952777812	5.4088544777778109	5.4104930694444775	5.4121320694444774	5.4137710694444774	5.4154100694444764	5.4170405027778097	5.418667675000032	5.4203038194444764	5.4219411861111437	5.4235814083333658	5.4252301972222554	5.4268769444444773	5.4285326666666993	5.4301965444444766	5.4318450722222549	5.4334858972222548	5.4351096916666988	5.4367338916666981	5.4383706611111435	5.4400143250000319	5.4416592027778101	5.4433150305555875	5.4449688305555872	5.4466165472222539	5.4482679138889205	5.4499171111111426	5.4515642694444759	5.453221216666698	5.4548740833333644	5.4565306222222532	5.4581810416666983	5.4598245277778092	5.4614737250000314	5.4631241444444765	5.4647665916666988	5.4664110666666987	5.4680409416666986	5.4696760888889209	5.4713075861111431	5.4729378666666983	5.4745754472222536	5.476211811111142	5.4778530416666973	5.4794942722222526	5.4811265805555864	5.4827540250000313	5.4843879555555874	5.4860202638889204	5.487672313888921	5.4893162083333653	5.4909552083333653	5.4925962472222531	5.4942405500000318	5.495882997222254	5.4975295000000317	5.4991670805555879	5.5008062833333646	5.5024430527778101	5.5040704972222549	5.5057007777778102	5.5073387638889209	5.5089751277778092	5.5106110861111421	5.5122454222222537	5.5138939500000319	5.5155497777778093	5.517196280555587	5.5188456194444768	5.5204840111111428	5.522133208333365	5.5237868916666981	5.5254287472222536	5.5270832444444764	5.5287406944444761	5.5303847638889208	5.5320130166666992	5.5336526250000322	5.5352837166666999	5.5369099416666998	5.5385487388889212	5.540177397222255	5.5418088944444772	5.5434359305555878	5.5450593194444773	5.5466802750000319	5.5482943361111436	5.5499148861111429	5.5515520611111437	5.5531961305555875	5.5548445111111437	5.5564961527778101	5.55813332777781	5.55977415277781	5.5614263305555882	5.563074047222254	5.5647120333333655	5.5663540750000315	5.5679965222222547	5.5696316694444761	5.5712668166666983	5.5729072361111429	5.5745448166666991	5.5761864527778098	5.5778232222222544	5.5794616138889213	5.5810996000000319	5.5827254222222544	5.5843552972222543	5.5859867944444765	5.5876215361111434	5.5892523611111429	5.5908795583333655	5.5925095777778093	5.5941508083333655	5.5957883888889208	5.5974279972222547	5.5990631444444769	5.6006958583333653	5.6023273555555875	5.6039677750000321	5.6056041388889204	5.6072380694444766	5.6088801111111426	5.6105217472222533	5.6121718972222538	5.6138159666666976	5.6154616555555874	5.6171053194444758	5.6187397722222538	5.6203649527778099	5.6219887472222538	5.6236149750000317	5.6252347138889212	5.626857291666699	5.628493250000032	5.6301255583333649	5.6317554333333648	5.6333820666666981	5.6350087000000304	5.636641819444475	5.6382753444444758	5.6398991388889197	5.641535502777808	5.6431702444444749	5.6448163416666972	5.6464486500000302	5.6480677861111417	5.6497025277778086	5.6513255111111418	5.6529513333333643	5.6545824250000312	5.6562127055555864	5.6578437972222533	5.6594752944444755	5.6611092250000317	5.6627423444444753	5.6643758694444761	5.6660053388889207	5.6676376472222536	5.6692699555555865	5.6709022638889204	5.6725309222222533	5.6741599861111425	5.6757914833333647	5.6774246027778092	5.6790532611111422	5.6806916527778091	5.6823219333333643	5.6839538361111419	5.6855833055555864	5.6872160194444747	5.68885360000003	5.6904859083333639	5.6921137555555861	5.6937416027778092	5.6953601250000307	5.6969737805555862	5.6985910861111417	5.7002083916666972	5.7018350250000305	5.7034573861111415	5.7050833750000303	5.7067049277778077	5.7083160000000293	5.7099190111111406	5.7115397583333634	5.713172877777807	5.7148015361111408	5.7164326277778077	5.7180641250000299	5.7196952166666968	5.7213271194444753	5.7229565888889189	5.7245779500000298	5.726200933333363	5.7278389194444745	5.7294749861111409	5.7311050055555857	5.7327386527778081	5.7343585944444753	5.7359813583333645	5.7375968666666974	5.7392192277778085	5.7408307027778083	5.742448627777808	5.7440653444444747	5.7456844805555862	5.7472991805555864	5.7489278388889193	5.750567041666697	5.7522038111111415	5.7538405805555861	5.7554649555555866	5.757085300000031	5.7587052416666982	5.7603271972222529	5.7619507666666978	5.7635727222222535	5.7651886305555866	5.7668069583333645	5.7684192388889199	5.7700258777778082	5.7716538805555855	5.7732914611111408	5.7749164722222526	5.7765386444444751	5.778170952777808	5.7797852500000308	5.7814043861111424	5.7830198944444753	5.7846341916666972	5.7862476833333645	5.7878631916666974	5.7894839388889201	5.7911010583333642	5.7927153555555861	5.7943260250000304	5.795938711111142	5.7975702083333642	5.7991907583333644	5.8008113083333646	5.8024346972222531	5.8040655222222526	5.8056935250000299	5.8073166916666974	5.8089322000000303	5.8105606055555867	5.8121874000000311	5.813805727777809	5.8154220416666975	5.8170476277778089	5.8186808722222523	5.8203024250000306	5.8219259944444746	5.8235511777778086	5.82518997500003	5.8268155611111414	5.8284346972222529	5.8300542361111418	5.8316721611111424	5.8333025833333645	5.8349313944444754	5.8365763305555873	5.8382297305555868	5.8398835333333645	5.8415361277778084	5.8431826750000306	5.8448163222222531	5.8464527916666977	5.8480739416666978	5.849685819444475	5.8512976972222521	5.8529095750000293	5.8545162138889184	5.8561264805555844	5.8577419888889182	5.8593562861111401	5.8609629250000284	5.8625683527778065	5.864175394444473	5.865784450000028	5.8673935055555839	5.8689993361111394	5.8706087972222507	5.8722243055555836	5.8738339166666949	5.8754482138889177	5.8770693638889178	5.8786852722222509	5.8803007777778058	5.881915477777806	5.8835301777778062	5.885150925000028	5.8867724777778063	5.8883863722222509	5.890003491666695	5.891613758333361	5.893236119444472	5.8948540444444726	5.8964628527778062	5.8980696583333625	5.8996728555555835	5.9012756527778061	5.902867230555584	5.9044716305555829	5.9060760305555826	5.9076836361111384	5.9092983361111386	5.9109057805555834	5.9125148388889173	5.9141295388889175	5.915740611111139	5.9173516833333615	5.9189456638889171	5.9205448555555833	5.9221440472222495	5.9237364250000279	5.9253376194444716	5.9269356083333609	5.9285380055555823	5.9301416055555816	5.9317460055555813	5.933366752777804	5.9349923388889145	5.9366151027778038	5.9382269805555818	5.9398428916666921	5.9414488944444708	5.9430625138889148	5.9446713222222485	5.9462789305555823	5.9478829305555818	5.9494897361111381	5.951103355555583	5.9527193777778047	5.9543470222222501	5.9559690555555829	5.9575950972222493	5.9592091166666936	5.9608258333333604	5.9624250250000266	5.9640362388889159	5.9656478527778045	5.9672570638889164	5.9688674750000272	5.9704778861111389	5.9720882972222507	5.9736898916666945	5.9753007055555836	5.9769083138889174	5.9785195277778067	5.9801275361111399	5.9817323388889188	5.9833288388889185	5.9849253388889183	5.9865186527778071	5.988108780555585	5.9897083722222515	5.9913251972222517	5.9929400166666964	5.9945520305555853	5.9961676527778076	5.9977916916666958	5.9994109194444736	6.0010313500000292	6.0026517805555848	6.0042642166666953	6.0058591250000282	6.0074540333333619	6.0090668500000284	6.0106800666666951	6.0123000972222505	6.0139177222222511	6.0155285361111401	6.0171253222222507	6.0187237111111394	6.0203277111111388	6.0219397250000286	6.0235445916666945	6.0251510527778063	6.0267575138889171	6.0283448527778063	6.0299460472222499	6.0315504472222496	6.0331656694444717	6.034776883333361	6.0363836888889173	6.0379916972222505	6.0396029111111398	6.0412189333333624	6.0428161222222512	6.0444082416666953	6.0460091250000287	6.0476056250000285	6.0491909722222506	6.0507767166666957	6.052373102777806	6.0539694888889173	6.0555678777778059	6.0571510388889163	6.0587518333333605	6.0603526277778048	6.0619491277778046	6.0635324833333604	6.0651257972222492	6.0667258833333602	6.0683215888889155	6.0699244638889152	6.0715233555555823	6.0731314083333601	6.0747482333333602	6.076367461111138	6.0779858888889153	6.0795955000000275	6.08118682222225	6.0827809333333605	6.0843730527778046	6.0859707500000271	6.0875680472222493	6.0891613611111381	6.0907606500000275	6.0923687027778053	6.0939759611111386	6.0955652916666949	6.0971530277778054	6.0987495277778061	6.1003539277778058	6.1019540138889168	6.1035485222222503	6.1051474138889175	6.1067510861111387	6.1083511722222505	6.1099544472222505	6.1115585166666948	6.1131657750000281	6.1147646666666953	6.116372719444473	6.1179664500000284	6.119557011111139	6.1211455916666946	6.1227464500000286	6.1243385972222502	6.1259410722222505	6.1275359805555834	6.1291400500000277	6.1307337611111388	6.1323398222222494	6.1339502666666945	6.1355603111111394	6.1371607722222503	6.1387525222222505	6.1403395194444723	6.1419166166666948	6.1435079694444719	6.1450941750000281	6.1466863222222505	6.1482903472222503	6.149899994444473	6.1515028694444727	6.1530997694444727	6.1546780555555838	6.1562630750000285	6.1578445277778062	6.1594366750000287	6.1610331777778065	6.1626280972222505	6.1642210361111394	6.1658104111111394	6.167404933333362	6.1690014361111398	6.1706094222222507	6.1722003000000285	6.17377071111114	6.1753395472222508	6.1769099583333613	6.1784949750000289	6.1800736583333622	6.1816681805555849	6.183274583333362	6.1848710861111398	6.1864565000000296	6.1880407250000289	6.1896229444444737	6.1912153972222512	6.1928035194444746	6.1943984388889186	6.1959897944444737	6.1975827333333626	6.1991776527778066	6.200775341666696	6.2023773888889187	6.2039853750000296	6.2055801888889182	6.2071675250000293	6.2087521055555852	6.2103402277778077	6.211921263888919	6.2134963972222526	6.2150754666666961	6.2166545361111405	6.2182308500000296	6.2198083444444734	6.2213897750000289	6.222951116666696	6.2245124583333622	6.2260856222222518	6.2276473722222514	6.2292189638889175	6.2308015750000294	6.2323818250000294	6.2339518416666966	6.2355214638889187	6.2370997472222518	6.2386843277778077	6.2402547361111411	6.2418302638889198	6.2434093333333633	6.2449915527778082	6.2465623555555867	6.2481406388889207	6.2497185277778096	6.2512905111111428	6.2528518666666981	6.2544187333333641	6.2559887500000313	6.2575603416666974	6.2591264222222538	6.2607039166666985	6.2622794444444763	6.2638656000000319	6.2654446694444754	6.2670249194444763	6.2685972972222537	6.2701677083333651	6.2717321805555875	6.2733077083333653	6.274887566666699	6.2764587638889209	6.2780240555555871	6.2795917111111432	6.2811621222222547	6.2827325333333661	6.2843163277778098	6.2858922472222538	6.2874708027778086	6.2890497500000313	6.2906343305555863	6.2922153666666976	6.2937936500000315	6.2953636666666979	6.2969435222222536	6.2985143250000322	6.3000859166666983	6.301670102777809	6.3032412250000318	6.3048033472222542	6.3063658611111428	6.3079248527778091	6.3094721083333649	6.3110209277778093	6.3125771805555875	6.3141346083333652	6.3157069861111426	6.3172789694444758	6.3188399194444758	6.3204063472222538	6.3219794250000305	6.3235611111111423	6.3251314500000309	6.3267154833333645	6.3282999083333644	6.3298896055555867	6.3314793027778089	6.3330674250000314	6.3346323222222543	6.3361960111111433	6.3377624388889204	6.3393413861111432	6.3409262027778093	6.3425055416666982	6.3440840972222539	6.3456595222222534	6.3472492194444756	6.3488278944444758	6.3504080166666981	6.3519748361111423	6.3535522194444756	6.3551252972222532	6.3566889861111422	6.3582526750000312	6.3598198861111426	6.3613906166666991	6.3629562611111439	6.3645187750000325	6.3660702638889211	6.367620197222255	6.3691658527778108	6.3707153972222548	6.3722790861111438	6.3738392527778114	6.3753935500000329	6.376949413888922	6.3785044944444778	6.3800642694444782	6.381616536111145	6.3831774861111441	6.3847364777778104	6.386296644444478	6.3878564194444776	6.3894060222222562	6.3909611027778119	6.3925240083333676	6.3940904361111448	6.3956345361111451	6.3971805805555899	6.3987390694444795	6.4002866694444798	6.4018397944444798	6.4033987861111461	6.4049624750000351	6.4065163805555905	6.4080616805555906	6.4096093277778134	6.4111456500000363	6.4126916944444812	6.4142319055555923	6.4157858111111477	6.4173412833333696	6.4188955805555921	6.4204530083333688	6.4220151305555921	6.4235815583333693	6.4251409416667027	6.4266912638889258	6.4282295305555914	6.4297666305555916	6.4313083972222591	6.4328649416667032	6.4344345000000356	6.4359844944444804	6.4375399666667024	6.4390903527778125	6.4406481722222573	6.4421922722222575	6.4437336500000351	6.4452824166667018	6.4468323500000357	6.4483976027778134	6.4499569861111468	6.4515195000000354	6.4530784916667017	6.4546367027778127	6.4561855222222571	6.4577304000000346	6.4592791666667013	6.4608217111111461	6.4623728777778133	6.463919741666702	6.465467388888924	6.4670209055555903	6.4685748111111456	6.4701302833333676	6.4716771472222563	6.4732357500000344	6.4747782944444792	6.4763157833333684	6.4778747750000347	6.4794263333333673	6.4809778916667007	6.482531797222256	6.4840868777778118	6.4856470444444785	6.4872021250000351	6.4887572055555909	6.490321286111147	6.4918867750000357	6.4934460416667026	6.4950076416667031	6.4965641861111472	6.4981204388889253	6.499680605555592	6.5012376416667026	6.5027978083333702	6.5043434972222594	6.5058880138889252	6.5074344472222583	6.5089993083333697	6.510571605555592	6.5121525083333696	6.5137322388889256	6.5153010138889256	6.5168725277778137	6.5184428666667031	6.5200053805555918	6.5215852361111475	6.5231559666667032	6.5247266972222588	6.5262970361111474	6.5278579861111474	6.5294099361111471	6.5309618861111467	6.5325126611111468	6.5340493527778136	6.5356138583333694	6.5371799388889249	6.538749561111147	6.5403132777778135	6.5418714888889253	6.5434355694444815	6.5449902583333701	6.5465598166667034	6.5481383722222581	6.5497118416667028	6.5512850055555916	6.5528471472222583	6.5544018111111475	6.5559651361111477	6.5575303888889254	6.5591140305555928	6.5606796750000376	6.5622394500000381	6.5638004000000372	6.5653696277778151	6.5669392500000372	6.5685132027778144	6.570097388888926	6.5716803944444813	6.5732554305555926	6.5748402472222596	6.5764336722222589	6.5780298361111482	6.5796080000000376	6.5811763833333714	6.582746794444482	6.58432074722226	6.5859049361111488	6.5874859750000372	6.5890662250000371	6.5906342166667038	6.5922072944444814	6.5937901555555918	6.5953671472222588	6.5969296611111474	6.5985051888889252	6.6000661500000364	6.6016251444444807	6.6031857138889256	6.6047525805555924	6.6063315277778143	6.6079081277778133	6.6094772944444804	6.6110225944444805	6.6125898027778138	6.6141542722222582	6.6157117000000358	6.6172872277778145	6.6188556694444811	6.6204280472222594	6.6220011250000361	6.6235761611111474	6.6251484583333697	6.626725841666703	6.628300094444481	6.6298653472222586	6.6314298166667029	6.6329966361111472	6.6345614972222586	6.6361307250000356	6.6376999527778136	6.6392550333333693	6.6408214611111474	6.6423957138889254	6.64397700833337	6.6455571305555923	6.6471356861111479	6.6487079833333702	6.6502748027778145	6.6518660750000365	6.653452063888925	6.6550349250000362	6.6566119166667024	6.6581783444444804	6.6597439888889252	6.6613104166667023	6.6628721472222585	6.6644461000000357	6.6660110000000357	6.6675684194444802	6.6691242833333693	6.6706867972222579	6.6722414861111465	6.6738016527778141	6.6753563416667028	6.6769153333333691	6.6784747166667024	6.6800356666667025	6.6815966166667025	6.6831638250000358	6.6847400333333695	6.6863142861111475	6.6878795388889252	6.6894385305555915	6.690993219444481	6.6925549500000363	6.6941088555555925	6.6956635444444812	6.6972147111111484	6.6987545333333705	6.700292800000037	6.7018396222222592	6.7033857027778154	6.7049388277778155	6.7064974305555936	6.708062291666705	6.7096287194444821	6.7111924083333712	6.7127756611111495	6.7143420888889267	6.7158955222222598	6.7174575111111485	6.7190218333333718	6.7205896555555933	6.7221662555555932	6.7237350305555932	6.7253038055555932	6.7268725805555931	6.7284546583333711	6.7300249972222597	6.7315889305555929	6.733155975000038	6.7347306194444831	6.7363013500000388	6.7378669944444836	6.739431855555595	6.7409971083333726	6.7425666666667059	6.7441283972222612	6.7457038222222616	6.747280977777816	6.7488499666667048	6.7504232333333718	6.7520076583333717	6.7535913000000383	6.755167508333372	6.7567476305555951	6.758332055555595	6.7599039611111502	6.7614573944444833	6.7630053833333719	6.7645483166667058	6.7661053527778163	6.7676612166667045	6.769213166666705	6.7707670722222604	6.772329586111149	6.7738815361111486	6.7754120250000378	6.7769405694444815	6.778478447222259	6.7800264361111475	6.7815798694444807	6.7831251361111473	6.7846782611111474	6.786230211111147	6.7877864638889251	6.7893278416667027	6.7908664972222583	6.7924253750000361	6.793995141666703	6.79556490833337	6.797124175000036	6.7986996000000364	6.8002762000000354	6.8018504527778134	6.80342118333337	6.8049777277778141	6.8065323277778145	6.8080931500000368	6.8096473611111481	6.8112058500000368	6.8127573388889262	6.8143088277778157	6.8158603166667042	6.8174310472222599	6.8189840916667048	6.8205441361111498	6.8221162361111496	6.8236817250000392	6.8252402138889288	6.8268053138889284	6.8283762472222618	6.8299378472222623	6.8315207083333735	6.8330900861111514	6.8346396305555954	6.8361841194444848	6.8377254972222623	6.8392618194444852	6.8407969750000399	6.8423332972222628	6.8438680638889302	6.8454020527778185	6.8469414833333735	6.8484719722222627	6.8500114055555956	6.8515698944444852	6.8531365500000403	6.8547020388889299	6.8562640277778186	6.8578267944444855	6.859398116666708	6.8609747166667079	6.8625402055555966	6.8641091944444854	6.8656809055555961	6.8672467833333739	6.8688076055555962	6.8703707611111513	6.8719168055555961	6.8734733500000402	6.8750335166667069	6.8765974500000411	6.8781497166667069	6.8797124833333738	6.8812876944444854	6.8828636833333743	6.8844229500000411	6.8859639388889295	6.8875119777778178	6.8890584500000394	6.8906013833333732	6.8921458722222626	6.893689972222262	6.8952434055555951	6.8967851722222626	6.8983277166667065	6.8998788166667069	6.9014396388889283	6.9030070722222616	6.9045690611111503	6.9061364944444836	6.9076942055555941	6.9092585277778165	6.9108197388889279	6.9123755055555955	6.9139425500000398	6.915513094444484	6.9170723611111509	6.9186467944444843	6.9202068388889284	6.9217668833333734	6.9233137055555956	6.9248597500000404	6.926405016666707	6.92794795000004	6.9294974944444849	6.931030633333374	6.9325556555555954	6.9340915888889292	6.9356111888889291	6.9371261222222627	6.9386554444444855	6.9401913777778192	6.9417315888889304	6.9432675222222642	6.9448010472222643	6.946336891666709	6.9478895472222648	6.9494550361111536	6.9510170250000423	6.952579013888931	6.954135947222265	6.9556889916667091	6.9572408694444867	6.9587863750000425	6.9603338138889308	6.9618835722222636	6.9634412833333741	6.9649931611111517	6.9665259833333737	6.9680591944444847	6.9695939611111521	6.9711353388889297	6.9726777527778188	6.974238333333374	6.9758097361111524	6.9773714777778189	6.9789361888889303	6.9805036222222627	6.9820714444444851	6.9836209888889291	6.9851545138889293	6.9866748972222625	6.9881910277778188	6.9897187555555966	6.9912453250000413	6.9927890361111524	6.9943257472222626	6.9958640138889292	6.9974075888889296	6.9989577333333735	7.0004958972222626	7.0020479750000399	7.0036004388889292	7.005156205555596	7.0067088611111519	7.0082514055555958	7.0097903416667071	7.0113281194444852	7.0128720805555966	7.0144075388889302	7.0159542055555963	7.0175012583333745	7.0190483111111526	7.0205972972222632	7.0221608416667074	7.0237067361111523	7.0252487638889294	7.0267958166667075	7.0283339805555967	7.0298794861111524	7.0314230611111519	7.0329766861111525	7.0345353361111522	7.0361128805555966	7.0376773277778195	7.0392363638889304	7.0407876694444855	7.0423331750000404	7.043882161111152	7.0454292138889301	7.0469731750000415	7.0485012888889296	7.0500442222222635	7.0515847055555971	7.0531309861111531	7.0546602611111524	7.0561798722222635	7.0577122388889304	7.0592619972222632	7.0608218055555971	7.0623881861111526	7.0639318944444858	7.0654839722222631	7.0670321861111525	7.0685904500000412	7.0701456194444861	7.0716903527778188	7.0732451361111526	7.0747792416667075	7.0763164194444856	7.077861666666708	7.0794191555555974	7.0809751000000416	7.0825337500000414	7.0840873750000419	7.0856514361111529	7.0872023555555979	7.0887364611111527	7.0902759444444863	7.0918133333333753	7.0933534277778199	7.0949008666667082	7.0964475333333752	7.0979988388889304	7.0995485972222632	7.1010903861111521	7.1026337111111522	7.1041758833333741	7.1057257388889301	7.1072859333333742	7.108839944444485	7.1103893166667076	7.1119383027778191	7.1134930861111521	7.1150218138889301	7.1165551500000408	7.118091944444485	7.1196295055555971	7.1211536222222627	7.1226715916667072	7.124217872222264	7.1257513972222641	7.127279355555598	7.1288261388889307	7.130364086111153	7.1319001111111531	7.1334376750000423	7.1349683222222646	7.1365008916667092	7.1380361500000422	7.139570255555598	7.1411074333333753	7.142655369444487	7.1442033055555978	7.1457520083333756	7.1473010944444875	7.1488432666667094	7.1503869750000426	7.1519349111111543	7.153467563888932	7.1550028888889319	7.1565508222222656	7.1580999083333774	7.1596332444444881	7.1611627388889332	7.1626787888889325	7.1642025222222667	7.1657130305555992	7.1672136138889329	7.168704652777822	7.1702103305555998	7.1716975694444898	7.1731932583333782	7.1747150694444901	7.1762468694444905	7.1777554694444907	7.1792751416667127	7.1807951944444905	7.182307611111157	7.1838165916667123	7.1853286277778228	7.1868523611111561	7.188380702777823	7.1898873944444901	7.1914120305556004	7.1929504111111564	7.1944811555556001	7.1960096083333784	7.1975285166667113	7.1990714583333775	7.2006170888889329	7.2021512694444887	7.2036724694444887	7.2052077944444894	7.2067354833333788	7.2082601194444891	7.2097881916667106	7.2113249861111548	7.2128561111111553	7.2143853277778218	7.2159111083333771	7.2174345972222662	7.2189653416667108	7.2204979944444885	7.2220386638889327	7.2235950500000436	7.2251284666667104	7.2266595916667109	7.2281972083333779	7.2297298611111556	7.2312644222222673	7.2327974555556001	7.2343255277778216	7.235871158333377	7.2374267750000438	7.2389590444444885	7.2404768083333773	7.2420052611111556	7.2435463138889329	7.2450713305556	7.2465963472222663	7.2481236555555997	7.2496475277778218	7.2511790361111546	7.2527051972222658	7.254229069444488	7.2557514138889321	7.2572855944444878	7.2588178638889316	7.2603478444444871	7.2618618722222648	7.2633784916667095	7.264907708333376	7.266444941666709	7.2679753027778204	7.2695091000000422	7.2710470972222643	7.2725785777778196	7.2741039861111538	7.2756263611111534	7.2771551861111536	7.2786798361111531	7.2801874138889309	7.2817139611111532	7.2832515777778202	7.2847750916667087	10 LPM, 6kW	23.2	23.2	23.3	23.3	23.3	23.3	23.4	23.4	23.5	23.5	23.5	23.5	23.5	23.6	23.6	23.6	23.6	23.7	23.7	23.8	23.8	23.8	23.8	23.8	23.9	23.9	23.9	23.9	24	24	24	24.1	24.1	24.2	24.2	24.2	24.2	24.2	24.3	24.3	24.4	24.4	24.4	24.4	24.5	24.5	24.5	24.6	24.6	24.6	24.7	24.7	24.7	24.7	24.8	24.8	24.8	24.9	24.9	24.9	25	25	25	25	25	25.1	25.1	25.1	25.2	25.2	25.3	25.3	25.4	25.4	25.4	25.4	25.5	25.5	25.5	25.5	25.6	25.6	25.6	25.6	25.7	25.7	25.7	25.8	25.8	25.8	25.8	25.9	25.9	25.9	26	26	26	26.1	26.1	26.1	26.1	26.2	26.2	26.2	26.3	26.3	26.3	26.3	26.4	26.4	26.4	26.5	26.5	26.5	26.5	26.6	26.6	26.6	26.7	26.7	26.7	26.7	26.8	26.8	26.8	26.8	26.9	26.9	26.9	27	27	27	27.1	27.1	27.1	27.2	27.2	27.2	27.2	27.3	27.3	27.3	27.4	27.4	27.4	27.5	27.5	27.5	27.5	27.6	27.6	27.6	27.6	27.7	27.7	27.7	27.8	27.8	27.8	27.8	27.9	27.9	27.9	28	28	28	28	28.1	28.1	28.1	28.2	28.2	28.2	28.2	28.3	28.3	28.3	28.4	28.4	28.4	28.5	28.5	28.5	28.5	28.5	28.6	28.6	28.6	28.7	28.7	28.7	28.7	28.8	28.8	28.8	28.9	28.9	28.9	28.9	29	29	29	29.1	29.1	29.1	29.1	29.2	29.2	29.2	29.2	29.2	29.3	29.3	29.3	29.4	29.4	29.4	29.4	29.5	29.5	29.5	29.6	29.6	29.6	29.7	29.7	29.7	29.7	29.8	29.8	29.8	29.9	29.9	29.9	29.9	30	30	30	30	30.1	30.1	30.1	30.2	30.2	30.2	30.3	30.3	30.3	30.3	30.4	30.4	30.4	30.4	30.5	30.5	30.5	30.5	30.6	30.6	30.6	30.7	30.7	30.7	30.8	30.8	30.8	30.8	30.8	30.9	30.9	30.9	31	31	31	31.1	31.1	31.1	31.1	31.2	31.2	31.2	31.2	31.3	31.3	31.3	31.4	31.4	31.4	31.4	31.5	31.5	31.5	31.6	31.6	31.6	31.6	31.7	31.7	31.7	31.8	31.8	31.8	31.8	31.8	31.9	31.9	31.9	32	32	32	32	32	32.1	32.1	32.200000000000003	32.200000000000003	32.200000000000003	32.200000000000003	32.299999999999997	32.299999999999997	32.299999999999997	32.299999999999997	32.4	32.4	32.4	32.5	32.5	32.5	32.5	32.6	32.6	32.6	32.700000000000003	32.700000000000003	32.700000000000003	32.700000000000003	32.700000000000003	32.799999999999997	32.799999999999997	32.799999999999997	32.9	32.9	32.9	32.9	33	33	33	33	33.1	33.1	33.1	33.200000000000003	33.200000000000003	33.200000000000003	33.299999999999997	33.299999999999997	33.299999999999997	33.299999999999997	33.4	33.4	33.4	33.5	33.5	33.5	33.5	33.5	33.6	33.6	33.6	33.700000000000003	33.700000000000003	33.700000000000003	33.700000000000003	33.799999999999997	33.799999999999997	33.799999999999997	33.9	33.9	33.9	33.9	34	34	34	34	34.1	34.1	34.1	34.200000000000003	34.200000000000003	34.200000000000003	34.200000000000003	34.299999999999997	34.299999999999997	34.299999999999997	34.4	34.4	34.4	34.4	34.5	34.5	34.5	34.5	34.6	34.6	34.6	34.700000000000003	34.700000000000003	34.700000000000003	34.799999999999997	34.799999999999997	34.799999999999997	34.799999999999997	34.9	34.9	34.9	34.9	35	35	35	35	35.1	35.1	35.1	35.1	35.200000000000003	35.200000000000003	35.200000000000003	35.200000000000003	35.299999999999997	35.299999999999997	35.299999999999997	35.4	35.4	35.4	35.5	35.5	35.5	35.5	35.6	35.6	35.6	35.6	35.700000000000003	35.700000000000003	35.700000000000003	35.700000000000003	35.799999999999997	35.799999999999997	35.799999999999997	35.799999999999997	35.9	35.9	35.9	36	36	36	36	36	36.1	36.1	36.1	36.200000000000003	36.200000000000003	36.200000000000003	36.200000000000003	36.299999999999997	36.299999999999997	36.299999999999997	36.4	36.4	36.4	36.4	36.5	36.5	36.5	36.6	36.6	36.6	36.6	36.700000000000003	36.700000000000003	36.700000000000003	36.700000000000003	36.700000000000003	36.799999999999997	36.799999999999997	36.9	36.9	36.9	36.9	36.9	36.9	37	37	37	37	37.1	37.1	37.1	37.1	37.200000000000003	37.200000000000003	37.299999999999997	37.299999999999997	37.299999999999997	37.299999999999997	37.299999999999997	37.4	37.4	37.5	37.5	37.5	37.5	37.5	37.6	37.6	37.6	37.6	37.700000000000003	37.700000000000003	37.700000000000003	37.700000000000003	37.799999999999997	37.799999999999997	37.799999999999997	37.799999999999997	37.9	37.9	37.9	37.9	38	38	38	38.1	38.1	38.1	38.1	38.1	38.200000000000003	38.200000000000003	38.200000000000003	38.200000000000003	38.299999999999997	38.299999999999997	38.299999999999997	38.299999999999997	38.4	38.4	38.4	38.4	38.5	38.5	38.5	38.5	38.6	38.6	38.6	38.6	38.700000000000003	38.700000000000003	38.700000000000003	38.799999999999997	38.799999999999997	38.799999999999997	38.799999999999997	38.799999999999997	38.9	38.9	38.9	38.9	39	39	39	39	39.1	39.1	39.1	39.1	39.200000000000003	39.200000000000003	39.200000000000003	39.200000000000003	39.299999999999997	39.299999999999997	39.299999999999997	39.4	39.4	39.4	39.4	39.5	39.5	39.5	39.5	39.6	39.6	39.6	39.700000000000003	39.700000000000003	39.700000000000003	39.700000000000003	39.700000000000003	39.799999999999997	39.799999999999997	39.799999999999997	39.799999999999997	39.9	39.9	39.9	39.9	39.9	40	40	40	40.1	40.1	40.1	40.1	40.1	40.200000000000003	40.200000000000003	40.200000000000003	40.200000000000003	40.299999999999997	40.299999999999997	40.299999999999997	40.299999999999997	40.4	40.4	40.4	40.4	40.5	40.5	40.5	40.5	40.6	40.6	40.6	40.6	40.700000000000003	40.700000000000003	40.700000000000003	40.799999999999997	40.799999999999997	40.799999999999997	40.799999999999997	40.799999999999997	40.9	40.9	40.9	40.9	41	41	41	41	41.1	41.1	41.1	41.1	41.1	41.2	41.2	41.2	41.2	41.3	41.3	41.3	41.3	41.4	41.4	41.4	41.4	41.5	41.5	41.5	41.5	41.5	41.6	41.6	41.6	41.6	41.7	41.7	41.7	41.7	41.8	41.8	41.8	41.8	41.9	41.9	41.9	41.9	41.9	41.9	42	42	42	42	42.1	42.1	42.1	42.1	42.1	42.2	42.2	42.2	42.2	42.2	42.3	42.3	42.4	42.4	42.4	42.4	42.4	42.5	42.5	42.5	42.5	42.6	42.6	42.6	42.6	42.6	42.7	42.7	42.7	42.7	42.7	42.8	42.8	42.8	42.8	42.8	42.9	42.9	42.9	42.9	43	43	43	43	43.1	43.1	43.1	43.1	43.2	43.2	43.2	43.2	43.2	43.3	43.3	43.3	43.3	43.4	43.4	43.4	43.4	43.5	43.5	43.5	43.5	43.5	43.6	43.6	43.6	43.6	43.7	43.7	43.7	43.7	43.7	43.8	43.8	43.8	43.8	43.9	43.9	43.9	43.9	43.9	44	44	44	44	44	44.1	44.1	44.1	44.1	44.2	44.2	44.2	44.2	44.2	44.3	44.3	44.3	44.3	44.3	44.4	44.4	44.4	44.4	44.5	44.5	44.5	44.5	44.6	44.6	44.6	44.6	44.6	44.6	44.7	44.7	44.7	44.7	44.7	44.8	44.8	44.8	44.8	44.9	44.9	44.9	44.9	45	45	45	45	45	45.1	45.1	45.1	45.1	45.1	45.2	45.2	45.2	45.2	45.2	45.3	45.3	45.3	45.3	45.4	45.4	45.4	45.4	45.4	45.4	45.5	45.5	45.5	45.5	45.5	45.6	45.6	45.6	45.6	45.6	45.7	45.7	45.7	45.7	45.7	45.8	45.8	45.8	45.8	45.8	45.9	45.9	45.9	45.9	45.9	46	46	46	46	46.1	46.1	46.1	46.1	46.1	46.2	46.2	46.2	46.2	46.2	46.3	46.3	46.3	46.3	46.3	46.4	46.4	46.4	46.4	46.4	46.4	46.5	46.5	46.5	46.5	46.5	46.6	46.6	46.6	46.6	46.7	46.7	46.7	46.7	46.7	46.7	46.8	46.8	46.8	46.8	46.8	46.9	46.9	46.9	46.9	46.9	47	47	47	47	47	47.1	47.1	47.1	47.1	47.1	47.2	47.2	47.2	47.2	47.2	47.2	47.3	47.3	47.3	47.3	47.3	47.4	47.4	47.4	47.4	47.4	47.4	47.5	47.5	47.5	47.5	47.5	47.6	47.6	47.6	47.6	47.6	47.6	47.7	47.7	47.7	47.7	47.7	47.8	47.8	47.8	47.8	47.8	47.8	47.9	47.9	47.9	47.9	47.9	47.9	48	48	48	48	48	48	48.1	48.1	48.1	48.1	48.2	48.2	48.2	48.2	48.2	48.2	48.3	48.3	48.3	48.3	48.3	48.3	48.4	48.4	48.4	48.4	48.4	48.4	48.5	48.5	48.5	48.5	48.5	48.5	48.6	48.6	48.6	48.6	48.6	48.6	48.7	48.7	48.7	48.7	48.7	48.7	48.7	48.8	48.8	48.8	48.8	48.8	48.9	48.9	48.9	48.9	48.9	48.9	48.9	49	49	49	49	49	49.1	49.1	49.1	49.1	49.1	49.1	49.2	49.2	49.2	49.2	49.2	49.2	49.2	49.3	49.3	49.3	49.3	49.3	49.3	49.4	49.4	49.4	49.4	49.4	49.4	49.5	49.5	49.5	49.5	49.5	49.5	49.5	49.6	49.6	49.6	49.6	49.6	49.6	49.7	49.7	49.7	49.7	49.7	49.7	49.7	49.7	49.8	49.8	49.8	49.8	49.8	49.8	49.9	49.9	49.9	49.9	49.9	49.9	50	50	50	50	50	50	50	50.1	50.1	50.1	50.1	50.1	50.1	50.2	50.2	50.2	50.2	50.2	50.2	50.2	50.2	50.3	50.3	50.3	50.3	50.3	50.3	50.3	50.3	50.4	50.4	50.4	50.4	50.4	50.4	50.5	50.5	50.5	50.5	50.5	50.5	50.5	50.6	50.6	50.6	50.6	50.6	50.6	50.6	50.6	50.6	50.7	50.7	50.7	50.7	50.7	50.7	50.8	50.8	50.8	50.8	50.8	50.8	50.8	50.9	50.9	50.9	50.9	50.9	50.9	50.9	50.9	50.9	51	51	51	51	51	51	51	51	51.1	51.1	51.1	51.1	51.1	51.1	51.2	51.2	51.2	51.2	51.2	51.2	51.2	51.3	51.3	51.3	51.3	51.3	51.3	51.3	51.3	51.3	51.3	51.4	51.4	51.4	51.4	51.4	51.4	51.5	51.5	51.5	51.5	51.5	51.5	51.5	51.5	51.5	51.5	51.6	51.6	51.6	51.6	51.6	51.6	51.6	51.6	51.7	51.7	51.7	51.7	51.7	51.7	51.7	51.8	51.8	51.8	51.8	51.8	51.8	51.8	51.8	51.8	51.8	51.9	51.9	51.9	51.9	51.9	51.9	51.9	52	52	52	52	52	52	52	52	52	52.1	52.1	52.1	52.1	52.1	52.1	52.1	52.1	52.1	52.2	52.2	52.2	52.2	52.2	52.2	52.2	52.2	52.2	52.2	52.3	52.3	52.3	52.3	52.3	52.3	52.3	52.3	52.3	52.4	52.4	52.4	52.4	52.4	52.4	52.4	52.4	52.4	52.4	52.5	52.5	52.5	52.5	52.5	52.5	52.5	52.5	52.5	52.5	52.6	52.6	52.6	52.6	52.6	52.6	52.6	52.6	52.6	52.7	52.7	52.7	52.7	52.7	52.7	52.7	52.7	52.7	52.7	52.7	52.8	52.8	52.8	52.8	52.8	52.8	52.8	52.8	52.8	52.8	52.9	52.9	52.9	52.9	52.9	52.9	52.9	52.9	52.9	52.9	52.9	53	53	53	53	53	53	53	53	53	53	53	53	53.1	53.1	53.1	53.1	53.1	53.1	53.1	53.1	53.1	53.1	53.1	53.2	53.2	53.2	53.2	53.2	53.2	53.2	53.2	53.2	53.2	53.2	53.3	53.3	53.3	53.3	53.3	53.3	53.3	53.3	53.3	53.3	53.3	53.3	53.4	53.4	53.4	53.4	53.4	53.4	53.4	53.4	53.4	53.4	53.4	53.4	53.5	53.5	53.5	53.5	53.5	53.5	53.5	53.5	53.5	53.5	53.5	53.5	53.6	53.6	53.6	53.6	53.6	53.6	53.6	53.6	53.6	53.6	53.6	53.6	53.6	53.7	53.7	53.7	53.7	53.7	53.7	53.7	53.7	53.7	53.7	53.7	53.7	53.7	53.8	53.8	53.8	53.8	53.8	53.8	53.8	53.8	53.8	53.8	53.8	53.8	53.8	53.8	53.8	53.8	53.9	53.9	53.9	53.9	53.9	53.9	53.9	53.9	53.9	53.9	53.9	53.9	53.9	53.9	54	54	54	54	54	54	54	54	54	54	54	54	54.1	54.1	54.1	54.1	54.1	54.1	54.1	54.1	54.1	54.1	54.1	54.1	54.1	54.1	54.1	54.2	54.2	54.2	54.2	54.2	54.2	54.2	54.2	54.2	54.2	54.2	54.2	54.2	54.2	54.3	54.3	54.3	54.3	54.3	54.3	54.3	54.3	54.3	54.3	54.3	54.3	54.3	54.3	54.3	54.3	54.3	54.4	54.4	54.4	54.4	54.4	54.4	54.4	54.4	54.4	54.4	54.4	54.4	54.4	54.4	54.4	54.4	54.5	54.5	54.4	54.5	54.5	54.5	54.5	54.5	54.5	54.5	54.5	54.5	54.5	54.5	54.5	54.5	54.5	54.5	54.5	54.5	54.6	54.6	54.6	54.6	54.6	54.6	54.6	54.6	54.6	54.6	54.6	54.6	54.6	54.6	54.7	54.7	54.7	54.7	54.7	54.7	54.7	54.7	54.7	54.7	54.7	54.7	54.7	54.7	54.7	54.7	54.7	54.7	54.7	54.8	54.8	54.8	54.7	54.8	54.8	54.8	54.8	54.8	54.8	54.8	54.8	54.8	54.8	54.8	54.8	54.8	54.8	54.8	54.9	54.9	54.9	54.8	54.9	54.9	54.9	54.9	54.9	54.9	54.9	54.9	54.9	54.9	54.9	54.9	54.9	54.9	54.9	55	55	55	55	55	55	55	55	55	55	55	55	55	55	55	55	55	55	55	55	55	55	55	55	55	55.1	55.1	55.1	55.1	55.1	55.1	55.1	55.1	55.1	55.1	55.1	55.1	55.1	55.1	55.1	55.1	55.1	55.1	55.1	55.1	55.1	55.1	55.2	55.2	55.2	55.2	55.2	55.2	55.2	55.2	55.2	55.2	55.2	55.2	55.2	55.2	55.2	55.2	55.2	55.2	55.3	55.3	55.3	55.3	55.2	55.3	55.3	55.3	55.3	55.3	55.3	55.3	55.3	55.3	55.3	55.3	55.3	55.3	55.3	55.3	55.3	55.3	55.3	55.4	55.4	55.3	55.3	55.3	55.4	55.4	55.4	55.4	55.4	55.4	55.4	55.4	55.4	55.4	55.4	55.4	55.4	55.4	55.4	55.4	55.4	55.4	55.4	55.4	55.4	55.4	55.4	55.4	55.4	55.5	55.5	55.5	55.5	55.5	55.5	55.5	55.5	55.5	55.5	55.5	55.5	55.5	55.5	55.5	55.5	55.5	55.5	55.5	55.5	55.6	55.6	55.6	55.6	55.5	55.6	55.6	55.6	55.6	55.6	55.6	55.6	55.6	55.6	55.6	55.6	55.6	55.6	55.6	55.6	55.6	55.6	55.6	55.6	55.6	55.6	55.6	55.6	55.6	55.6	55.6	55.6	55.7	55.7	55.7	55.7	55.7	55.7	55.7	55.7	55.7	55.7	55.7	55.7	55.7	55.7	55.7	55.7	55.7	55.7	55.7	55.7	55.7	55.7	55.7	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.9	55.9	55.9	55.8	55.8	55.8	55.8	55.9	55.9	55.9	55.9	55.9	55.9	55.9	55.9	55.9	55.9	55.9	55.9	55.9	55.9	55.9	55.9	55.9	55.9	55.9	55.9	55.9	55.9	55.9	55.9	56	56	56	56	56	56	56	56	56	56	56	56	56	56	56	56	56	56	56	56	56	56	56	56	56	56	56	56	56	56	56	56	56.1	56.1	56.1	56	56	56	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.6	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.8	56.7	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.9	56.9	56.9	56.9	56.8	56.8	56.8	56.8	56.8	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.3	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.6	57.6	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	58	58	58	58	58	58	58	58	58	58	58	58	58	58	58	58	58	58	58	58	58	58	58	58	58	58	58	58	58	58.1	58.1	58.1	58.1	58	58	58	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.2	58.1	58.1	58.1	58.1	58.1	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.3	58.3	58.3	58.3	58.3	58.3	58.3	58.3	58.3	58.3	58.3	58.3	58.3	58.3	58.3	58.3	58.3	58.3	58.3	58.3	58.3	58.3	58.3	58.3	58.3	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.5	58.5	58.5	58.5	58.5	58.5	58.5	58.5	58.5	58.5	58.5	58.5	58.5	58.5	58.5	58.5	58.5	58.5	58.5	58.5	58.5	58.5	58.5	58.5	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.7	58.7	58.7	58.7	58.7	58.7	58.7	58.7	58.7	58.7	58.7	58.7	58.7	58.7	58.7	58.7	58.7	58.7	58.7	58.7	58.7	58.7	58.7	58.7	58.7	58.7	58.8	58.8	58.8	58.8	58.8	58.8	58.8	58.8	58.8	58.8	58.8	58.8	58.8	58.8	58.8	58.8	58.8	58.8	58.8	58.8	58.8	58.8	58.8	58.8	58.8	58.8	58.8	58.9	58.9	58.9	58.9	58.9	58.9	58.9	58.9	58.9	58.9	58.9	58.9	58.9	58.9	58.9	58.9	58.9	58.9	58.9	58.9	58.9	58.9	58.9	58.9	58.9	59	59	59	59	59	59	59	59	59	59	59	59	59	59	59	59	59	59	59	59	59	59	59	59	59.1	59.1	59.1	59.1	59.1	59.1	59.1	59.1	59.1	59.1	59.1	59.1	59.1	59.1	59.1	59.1	59.1	59.1	59.1	59.1	59.1	59.1	59.1	59.1	59.1	59.2	59.2	59.2	59.2	59.2	59.2	59.2	59.2	59.2	59.2	59.2	59.2	59.2	59.2	59.2	59.2	59.2	59.2	59.2	59.2	59.2	59.3	59.3	59.3	59.3	59.3	59.3	59.3	59.3	59.3	59.3	59.3	59.3	59.3	59.3	59.3	59.3	59.3	59.3	59.3	59.3	59.3	59.3	59.4	59.4	59.4	59.4	59.4	59.4	59.4	59.4	59.4	59.4	59.4	59.4	59.4	59.4	59.4	59.4	59.4	59.4	59.4	59.4	59.4	59.4	59.5	59.5	59.5	59.5	59.5	59.5	59.5	59.5	59.5	59.5	59.5	59.5	59.5	59.5	59.5	59.6	59.5	59.5	59.5	59.6	59.6	59.6	59.6	59.6	59.6	59.6	59.6	59.6	59.6	59.6	59.6	59.6	59.6	59.6	59.6	59.6	59.6	59.6	59.7	59.7	59.7	59.7	59.7	59.7	59.7	59.7	59.7	59.7	59.7	59.7	59.7	59.7	59.7	59.7	59.7	59.7	59.7	59.8	59.8	59.8	59.8	59.8	59.8	59.8	59.8	59.8	59.8	59.8	59.8	59.8	59.8	59.8	59.8	59.9	59.9	59.9	59.9	59.9	59.9	59.9	59.9	59.9	59.9	59.9	59.9	59.9	59.9	59.9	59.9	59.9	59.9	59.9	59.9	59.9	59.9	60	60	60	60	60	60	60	60	60	60	60	60	60	60	60	60	60	60	60	60.1	60.1	60.1	60.1	60.1	60.1	60.1	60.1	60.1	60.1	60.1	60.1	60.1	60.1	60.1	60.1	60.1	60.2	60.2	60.2	60.2	60.2	60.2	60.2	60.2	60.2	60.2	60.2	60.2	60.2	60.2	60.2	60.2	60.2	60.3	60.3	60.3	60.3	60.3	60.3	60.3	60.3	60.3	60.3	60.3	60.3	60.3	60.3	60.3	60.3	60.4	60.4	60.4	60.4	60.4	60.4	60.4	60.4	60.4	60.4	60.4	60.4	60.4	60.4	60.4	60.4	60.5	60.5	60.5	60.5	60.5	60.5	60.5	60.5	60.5	60.5	60.5	60.5	60.5	60.5	60.5	60.5	60.6	60.6	60.6	60.6	60.6	60.6	60.6	60.6	60.6	60.6	60.6	60.6	60.6	60.6	60.6	60.7	60.7	60.7	60.7	60.7	60.7	60.7	60.7	60.7	60.7	60.7	60.7	60.7	60.8	60.8	60.8	60.8	60.8	60.8	60.8	60.8	60.8	60.8	60.8	60.8	60.8	60.8	60.8	60.8	60.9	60.9	60.9	60.9	60.9	60.9	60.9	60.9	60.9	60.9	60.9	60.9	60.9	60.9	61	61	61	61	61	61	61	61	61	61	61	61	61	61	61	61.1	61.1	61.1	61.1	61.1	61.1	61.1	61.1	61.1	61.1	61.1	61.1	61.1	61.1	61.2	61.2	61.2	61.2	61.2	61.2	61.2	61.2	61.2	61.2	61.2	61.2	61.2	61.2	61.3	61.3	61.3	61.3	61.3	61.3	61.3	61.3	61.3	61.3	61.3	61.3	61.3	61.4	61.4	61.4	61.4	61.4	61.4	61.4	61.4	61.4	61.4	61.4	61.4	61.4	61.5	61.5	61.5	61.5	61.5	61.5	61.5	61.5	61.5	61.5	61.5	61.5	61.6	61.6	61.6	61.6	61.6	61.6	61.6	61.6	61.6	61.6	61.7	61.7	61.7	61.7	61.7	61.7	61.7	61.7	61.7	61.7	61.7	61.7	61.7	61.7	61.7	61.8	61.8	61.8	61.8	61.8	61.8	61.8	61.8	61.8	61.8	61.8	61.8	61.9	61.9	61.9	61.9	61.9	61.9	61.9	61.9	61.9	61.9	61.9	62	62	62	62	62	62	62	62	62	62	62	62	62	62.1	62.1	62.1	62.1	62.1	62.1	62.1	62.1	62.1	62.1	62.1	62.1	62.2	62.2	62.2	62.2	62.2	62.2	62.2	62.2	62.2	62.2	62.2	62.2	62.3	62.3	62.3	62.3	62.3	62.3	62.3	62.3	62.3	62.3	62.3	62.3	62.3	62.4	62.4	62.4	62.4	62.4	62.4	62.4	62.4	62.4	62.4	62.4	62.4	62.5	62.5	62.5	62.5	62.5	62.5	62.5	62.5	62.5	62.5	62.5	62.5	62.5	62.6	62.6	62.6	62.6	62.6	62.6	62.6	62.6	62.6	62.6	62.6	62.6	62.6	62.7	62.7	62.7	62.7	62.7	62.7	62.7	62.7	62.7	62.7	62.7	62.7	62.7	62.8	62.8	62.8	62.8	62.8	62.8	62.8	62.8	62.8	62.9	62.9	62.9	62.9	62.9	62.9	62.9	62.9	62.9	62.9	62.9	62.9	62.9	62.9	63	63	63	63	63	63	63	63	63	63	63	63	63	63.1	63.1	63.1	63.1	63.1	63.1	63.1	63.1	63.1	63.1	63.1	63.1	63.2	63.2	63.2	63.2	63.2	63.2	63.2	63.2	63.2	63.3	63.3	63.3	63.3	63.3	63.3	63.3	63.3	63.3	63.3	63.3	63.3	63.3	63.3	63.3	63.4	63.4	63.4	63.4	63.4	63.4	63.4	63.4	63.4	63.4	63.4	63.4	63.5	63.5	63.5	63.5	63.5	63.5	63.5	63.5	63.5	63.5	63.5	63.5	63.5	63.6	63.6	63.6	63.6	63.6	63.6	63.6	63.6	63.6	63.6	63.6	63.6	63.7	63.7	63.7	63.7	63.7	63.7	63.7	63.7	63.7	63.7	63.7	63.7	63.8	63.8	63.8	63.8	63.8	63.8	63.8	63.8	63.8	63.8	63.8	63.9	63.9	63.9	63.9	63.9	63.9	63.9	63.9	63.9	63.9	63.9	64	64	64	64	64	64	64	64	64	64	64	64.099999999999994	64.099999999999994	64.099999999999994	64.099999999999994	64.099999999999994	64.099999999999994	64.099999999999994	64.099999999999994	64.099999999999994	64.099999999999994	64.099999999999994	64.099999999999994	64.2	64.2	64.2	64.2	64.2	64.2	64.2	64.2	64.2	64.2	64.2	64.3	64.3	64.3	64.3	64.3	64.3	64.3	64.3	64.3	64.3	64.3	64.400000000000006	64.400000000000006	64.400000000000006	64.400000000000006	64.400000000000006	64.400000000000006	64.400000000000006	64.400000000000006	64.400000000000006	64.400000000000006	64.5	64.5	64.5	64.5	64.5	64.5	64.5	64.5	64.599999999999994	64.599999999999994	64.599999999999994	64.599999999999994	64.599999999999994	64.599999999999994	64.599999999999994	64.599999999999994	64.599999999999994	64.599999999999994	64.599999999999994	64.7	64.7	64.7	64.7	64.7	64.7	64.7	64.7	64.7	64.7	64.7	64.7	64.8	64.8	64.8	64.8	64.8	64.8	64.8	64.8	64.900000000000006	64.900000000000006	64.900000000000006	64.900000000000006	64.900000000000006	64.900000000000006	64.900000000000006	64.900000000000006	64.900000000000006	64.900000000000006	64.900000000000006	64.900000000000006	64.900000000000006	65	65	65	65	65	65	65	65	65.099999999999994	65.099999999999994	65.099999999999994	65.099999999999994	65.099999999999994	65.099999999999994	65.099999999999994	65.099999999999994	65.099999999999994	65.099999999999994	65.099999999999994	65.099999999999994	65.2	65.2	65.2	65.2	65.2	65.2	65.2	65.2	65.2	65.2	65.3	65.3	65.3	65.3	65.3	65.3	65.3	65.3	65.400000000000006	65.400000000000006	65.400000000000006	65.400000000000006	65.400000000000006	65.400000000000006	65.400000000000006	65.400000000000006	65.400000000000006	65.400000000000006	65.400000000000006	65.400000000000006	65.5	65.5	65.5	65.5	65.5	65.5	65.5	65.5	65.5	65.5	65.599999999999994	65.599999999999994	65.599999999999994	65.599999999999994	65.599999999999994	65.599999999999994	65.599999999999994	65.599999999999994	65.7	65.7	65.7	65.7	65.7	65.7	65.7	65.7	65.7	65.7	65.8	65.8	65.8	65.8	65.8	65.8	65.8	65.8	65.8	65.8	65.900000000000006	65.900000000000006	65.900000000000006	65.900000000000006	65.900000000000006	65.900000000000006	65.900000000000006	66	66	66	66	66	66	66	66	66	66	66	66	66.099999999999994	66.099999999999994	66.099999999999994	66.099999999999994	66.099999999999994	66.099999999999994	66.099999999999994	66.099999999999994	66.099999999999994	66.2	66.2	66.2	66.2	66.2	66.2	66.2	66.2	66.2	66.2	66.3	66.3	66.3	66.3	66.3	66.3	66.3	66.3	66.400000000000006	66.400000000000006	66.400000000000006	66.400000000000006	66.400000000000006	66.400000000000006	66.400000000000006	66.400000000000006	66.400000000000006	66.5	66.5	66.5	66.5	66.5	66.5	66.5	66.5	66.5	66.5	66.599999999999994	66.599999999999994	66.599999999999994	66.599999999999994	66.599999999999994	66.599999999999994	66.599999999999994	66.599999999999994	66.7	66.7	66.7	66.7	66.7	66.7	66.7	66.7	66.7	66.8	66.7	66.8	66.8	66.8	66.8	66.8	66.8	66.8	66.8	66.8	66.900000000000006	66.900000000000006	66.900000000000006	66.900000000000006	66.900000000000006	66.900000000000006	66.900000000000006	66.900000000000006	66.900000000000006	67	67	67	67	67	67	67	67	67	67.099999999999994	67.099999999999994	67.099999999999994	67.099999999999994	67.099999999999994	67.099999999999994	67.099999999999994	67.099999999999994	67.099999999999994	67.2	67.2	67.2	67.2	67.2	67.2	67.2	67.2	67.2	67.3	67.3	67.3	67.3	67.3	67.3	67.3	67.3	67.3	67.3	67.400000000000006	67.400000000000006	67.400000000000006	67.400000000000006	67.400000000000006	67.400000000000006	67.400000000000006	67.400000000000006	67.400000000000006	67.5	67.5	67.5	67.5	67.5	67.5	67.5	67.5	67.5	67.599999999999994	67.599999999999994	67.599999999999994	67.599999999999994	67.599999999999994	67.599999999999994	67.599999999999994	67.599999999999994	67.599999999999994	67.599999999999994	67.7	67.7	67.7	67.7	67.7	67.7	67.7	67.7	67.7	67.8	67.8	67.8	67.8	67.8	67.8	67.8	67.8	67.8	67.900000000000006	67.900000000000006	67.900000000000006	67.900000000000006	67.900000000000006	67.900000000000006	67.900000000000006	67.900000000000006	67.900000000000006	67.900000000000006	68	68	68	68	68	68	68	68	68.099999999999994	68.099999999999994	68.099999999999994	68.099999999999994	68.099999999999994	68.099999999999994	68.099999999999994	68.099999999999994	68.099999999999994	68.099999999999994	68.099999999999994	68.2	68.2	68.2	68.2	68.2	68.2	68.2	68.2	68.2	68.2	68.3	68.3	68.3	68.3	68.3	68.3	68.3	68.3	68.3	68.400000000000006	68.400000000000006	68.400000000000006	68.400000000000006	68.400000000000006	68.400000000000006	68.400000000000006	68.400000000000006	68.400000000000006	68.400000000000006	68.5	68.5	68.5	68.5	68.5	68.5	68.5	68.5	68.5	68.5	68.599999999999994	68.599999999999994	68.599999999999994	68.599999999999994	68.599999999999994	68.599999999999994	68.599999999999994	68.599999999999994	68.599999999999994	68.7	68.7	68.7	68.7	68.7	68.7	68.7	68.7	68.7	68.7	68.8	68.8	68.8	68.8	68.8	68.8	68.8	68.8	68.8	68.8	68.900000000000006	68.900000000000006	68.900000000000006	68.900000000000006	68.900000000000006	68.900000000000006	68.900000000000006	68.900000000000006	68.900000000000006	69	69	69	69	69	69	69	69	69	69	69.099999999999994	69.099999999999994	69.099999999999994	69.099999999999994	69.099999999999994	69.099999999999994	69.099999999999994	69.099999999999994	69.099999999999994	69.099999999999994	69.2	69.2	69.2	69.2	69.2	69.2	69.2	69.2	69.2	69.2	69.3	69.3	69.3	69.3	69.3	69.3	69.3	69.3	69.3	69.3	69.3	69.400000000000006	69.400000000000006	69.400000000000006	69.400000000000006	69.400000000000006	69.400000000000006	69.400000000000006	69.400000000000006	69.5	69.5	69.5	69.5	69.5	69.5	69.5	69.5	69.5	69.5	69.599999999999994	69.599999999999994	69.599999999999994	69.599999999999994	69.599999999999994	69.599999999999994	69.599999999999994	69.599999999999994	69.599999999999994	69.599999999999994	69.599999999999994	69.7	69.7	69.7	69.7	69.7	69.7	69.7	69.7	69.7	69.7	69.7	69.7	69.8	69.8	69.8	69.8	69.8	69.8	69.8	69.8	69.8	69.8	69.8	69.900000000000006	69.900000000000006	69.900000000000006	69.900000000000006	69.900000000000006	69.900000000000006	69.900000000000006	69.900000000000006	69.900000000000006	69.900000000000006	69.900000000000006	70	70	70	70	70	70	70	70	70	70	70	70.099999999999994	70.099999999999994	70.099999999999994	70.099999999999994	70.099999999999994	70.099999999999994	70.099999999999994	70.099999999999994	70.099999999999994	70.099999999999994	70.099999999999994	70.2	70.2	70.2	70.2	70.2	70.2	70.2	70.2	70.2	70.2	70.2	70.2	70.3	70.3	70.3	70.3	70.3	70.3	70.3	70.3	70.3	70.3	70.400000000000006	70.400000000000006	70.400000000000006	70.400000000000006	70.400000000000006	70.400000000000006	70.400000000000006	70.400000000000006	70.400000000000006	70.400000000000006	70.400000000000006	70.400000000000006	70.400000000000006	70.400000000000006	70.5	70.5	70.5	70.5	70.5	70.5	70.5	70.5	70.5	70.5	70.5	70.599999999999994	70.599999999999994	70.599999999999994	70.599999999999994	70.599999999999994	70.599999999999994	70.599999999999994	70.599999999999994	70.599999999999994	70.599999999999994	70.599999999999994	70.599999999999994	70.599999999999994	70.7	70.7	70.7	70.7	70.7	70.7	70.7	70.7	70.7	70.7	70.7	70.7	70.8	70.8	70.8	70.8	70.8	70.8	70.8	70.8	70.8	70.8	70.8	70.900000000000006	70.900000000000006	70.900000000000006	70.900000000000006	70.900000000000006	70.900000000000006	70.900000000000006	70.900000000000006	70.900000000000006	70.900000000000006	70.900000000000006	70.900000000000006	70.900000000000006	71	71	71	71	71	71	71	71	71	71	71.099999999999994	71.099999999999994	71.099999999999994	71.099999999999994	71.099999999999994	71.099999999999994	71.099999999999994	71.099999999999994	71.099999999999994	71.099999999999994	71.099999999999994	71.099999999999994	71.099999999999994	71.099999999999994	71.099999999999994	71.2	71.2	71.2	71.2	71.2	71.2	71.2	71.2	71.2	71.2	71.2	71.2	71.2	71.3	71.3	71.3	71.3	71.3	71.3	71.3	71.3	71.3	71.3	71.400000000000006	71.400000000000006	71.400000000000006	71.400000000000006	71.400000000000006	71.400000000000006	71.400000000000006	71.400000000000006	71.400000000000006	71.400000000000006	71.400000000000006	71.400000000000006	71.400000000000006	71.400000000000006	71.400000000000006	71.400000000000006	71.400000000000006	71.400000000000006	71.5	71.5	71.5	71.5	71.5	71.5	71.5	71.5	71.5	71.5	71.5	71.5	71.5	71.5	71.599999999999994	71.599999999999994	71.599999999999994	71.599999999999994	71.599999999999994	71.599999999999994	71.599999999999994	71.599999999999994	71.599999999999994	71.599999999999994	71.599999999999994	71.599999999999994	71.599999999999994	71.599999999999994	71.599999999999994	71.7	71.7	71.7	71.7	71.7	71.7	71.7	71.7	71.7	71.7	71.7	71.7	71.7	71.7	71.8	71.8	71.8	71.8	71.8	71.8	71.8	71.8	71.8	71.8	71.8	71.8	71.8	71.8	71.8	71.8	71.8	71.8	71.8	71.8	71.900000000000006	71.900000000000006	71.900000000000006	71.900000000000006	71.900000000000006	71.900000000000006	71.900000000000006	71.900000000000006	71.900000000000006	71.900000000000006	71.900000000000006	71.900000000000006	71.900000000000006	71.900000000000006	71.900000000000006	71.900000000000006	71.900000000000006	71.900000000000006	72	72	72	72	72	72	72	72	72	72	72	72	72	72	72	72	72	72	72	72	72	72.099999999999994	72.099999999999994	72.099999999999994	72.099999999999994	72.099999999999994	72.099999999999994	72.099999999999994	72.099999999999994	72.099999999999994	72.099999999999994	72.099999999999994	72.099999999999994	72.099999999999994	72.099999999999994	72.099999999999994	72.099999999999994	72.099999999999994	72.099999999999994	72.099999999999994	72.099999999999994	72.2	72.2	72.2	72.2	72.2	72.2	72.2	72.2	72.2	72.2	72.2	72.2	72.2	72.2	72.2	72.2	72.2	72.2	72.2	72.2	72.2	72.2	72.3	72.3	72.3	72.3	72.3	72.3	72.3	72.3	72.3	72.3	72.3	72.3	72.3	72.3	72.3	72.3	72.3	72.3	72.3	72.3	72.3	72.3	72.400000000000006	72.400000000000006	72.400000000000006	0.22	0.22152076666666667	0.22302102500000001	0.22452559166666666	0.22602997222222224	0.22753041944444444	0.22901298333333334	0.23049943055555555	0.23196335277777777	0.23345016944444444	0.23493698611111111	0.23642213888888888	0.23790414722222222	0.23936971111111111	0.2408385611111111	0.24232001388888888	0.24380128055555556	0.24526684444444444	0.24672839166666666	0.24818975555555556	0.24965111944444446	0.2511143111111111	0.25259298888888887	0.25407277777777776	0.25553706388888886	0.25701555833333334	0.25849738055555554	0.25997920277777775	0.26146195	0.26294044444444442	0.26444014166666668	0.26592492499999998	0.26740434444444444	0.2688883861111111	0.27037242777777776	0.27185536111111108	0.27335899166666666	0.27486262222222224	0.27634703333333333	0.27784579444444446	0.27933020833333333	0.28082859444444441	0.28232698055555555	0.28382349166666665	0.28530568333333334	0.28680819166666666	0.28830601666666666	0.28978821111111108	0.29129240277777779	0.292792475	0.29427374166666664	0.29575852499999999	0.29725765833333334	0.29875679166666669	0.30023972500000001	0.30174260555555554	0.30324043055555555	0.30474293611111114	0.30624544166666667	0.30774457500000002	0.30922121944444447	0.31072204166666667	0.31222080277777775	0.31371956388888889	0.31522300833333333	0.31672794999999998	0.31822820833333332	0.31973015277777778	0.32121419444444443	0.32271258055555557	0.32419662222222223	0.32568066388888889	0.32717886111111111	0.32867705833333333	0.33018162500000003	0.33168619166666669	0.33316635	0.33464650833333337	0.3361493888888889	0.33764889722222224	0.33912720555555559	0.34061050833333339	0.34211282777777779	0.34360896388888895	0.34508708888888895	0.3465894083333334	0.34808948055555561	0.34957130277777781	0.35107530833333339	0.35257613055555559	0.3540750777777778	0.3555785222222223	0.3570827138888889	0.35858353333333337	0.36006480000000007	0.36156880555555559	0.36306719166666673	0.3645458694444445	0.36604762777777788	0.36754770000000009	0.36904421111111119	0.37052363055555559	0.37202370277777785	0.37351721666666676	0.37499386111111122	0.37649430833333342	0.37799138333333338	0.37948639722222233	0.38096692500000007	0.38246849444444453	0.38396556944444449	0.38544739166666675	0.38695027222222228	0.38844790833333342	0.38994329722222232	0.39142456666666675	0.39292238888888897	0.39441515555555562	0.39589161388888894	0.39738943611111122	0.39888107777777787	0.40037346666666673	0.40187185277777787	0.40336799166666676	0.40486150555555567	0.40638018611111126	0.40787894722222234	0.40937489722222231	0.41089243888888904	0.41239400833333345	0.41389051944444455	0.41540502500000009	0.41690378611111123	0.41839955000000012	0.41989343888888903	0.4213698972222224	0.42286921944444456	0.42436591944444457	0.42586299444444453	0.42736418888888905	0.42886463611111125	0.43036227222222234	0.43186271944444454	0.43336391388888901	0.43485873888888904	0.43635450277777788	0.43785495000000013	0.43935165000000009	0.44084647777777791	0.44234392777777787	0.44384250000000014	0.44533582777777792	0.44684976388888897	0.44835058333333344	0.44984878055555566	0.45134154444444458	0.45283768333333352	0.45433513333333347	0.45582715000000013	0.45733805277777795	0.45883437777777791	0.46032882777777789	0.46181990833333342	0.46331436111111124	0.46480975000000013	0.4663002666666668	0.46780984166666684	0.46930485555555568	0.47079762222222243	0.47230814444444458	0.47380390555555574	0.47530060555555564	0.47681245555555574	0.47832734166666679	0.47982647777777787	0.48132261666666676	0.48283446666666685	0.48433191666666686	0.48583273611111122	0.48734743333333352	0.48884488333333342	0.49034439166666677	0.49183978055555566	0.49335144166666678	0.49486651666666681	0.49636209166666678	0.49787299444444455	0.49938882777777793	0.50088852500000014	0.5023856000000001	0.50389801944444457	0.50541366388888898	0.50691073888888893	0.50842429722222238	0.50993823611111122	0.51143755833333349	0.51293481944444463	0.51444818888888899	0.515965352777778	0.51746505000000009	0.51898012500000013	0.52049463055555567	0.52199339166666681	0.52348915555555564	0.52499948888888903	0.52651342500000009	0.52800881388888898	0.52950420277777788	0.53101169166666673	0.53252392222222233	0.53403766944444453	0.53553080833333344	0.53704285000000007	0.5385579250000001	0.54005293888888894	0.5415634611111112	0.54307398333333334	0.54458943888888889	0.54608314166666672	0.547592525	0.54910646388888895	0.55060016666666667	0.55210841388888887	0.55361836666666664	0.55511150555555555	0.55660239722222227	0.55811159166666668	0.5596223027777778	0.56111431944444445	0.56262199722222228	0.56413005277777784	0.56562188055555562	0.56710977500000004	0.56861460833333344	0.57012342500000013	0.57161356944444452	0.57310071388888906	0.57461028888888899	0.57612156944444459	0.57761115000000007	0.57912110277777784	0.58063541944444452	0.58213249444444459	0.58362563333333339	0.58513938055555559	0.58663683055555571	0.58812959722222236	0.58963936111111115	0.59115273055555562	0.59264643333333344	0.59413713888888897	0.59564880000000009	0.59716330833333342	0.59865682222222238	0.60016905277777788	0.60168128333333348	0.60319560000000016	0.60468518055555576	0.6061966527777779	0.60770812500000015	0.60919957777777789	0.61070839444444458	0.61221721111111127	0.61370491944444461	0.61519262777777795	0.61668258333333348	0.61819557222222232	0.61970343888888901	0.62119189444444456	0.62268447222222234	0.62419708333333346	0.62568703888888899	0.62717886666666678	0.6286905277777779	0.63017917222222242	0.63166781666666683	0.63316058333333347	0.63467053611111124	0.63615768055555566	0.6376476361111113	0.6391589166666668	0.640666213888889	0.6421535472222224	0.64366501944444454	0.64517250833333351	0.64665815555555572	0.64814661111111127	0.64963525555555568	0.65114217500000016	0.65262875833333345	0.65411946388888897	0.65562638333333345	0.65711165555555562	0.65860161111111126	0.66009250277777787	0.66159733333333348	0.66308223055555571	0.66457143611111125	0.66605895555555572	0.66754516388888896	0.66903399444444456	0.67052470000000008	0.67202972222222224	0.67353208888888894	0.67501773611111116	0.67650225833333344	0.67800083055555571	0.679487413888889	0.68097474722222229	0.68247597500000012	0.68397587500000012	0.68548089722222227	0.68696448333333338	0.68846324444444451	0.68994683055555561	0.69143303888888885	0.69291475000000002	0.69441635555555559	0.69590556111111113	0.69739551666666666	0.69889845277777785	0.70040575000000005	0.70189570555555558	0.70338060277777781	0.70488240000000002	0.70637235555555555	0.70786043888888883	0.70936223611111104	0.71086498055555547	0.71235081388888877	0.71383364999999988	0.71533506666666657	0.71682202499999981	0.71830710833333311	0.71978544722222204	0.72128686388888874	0.72279169444444424	0.72427246944444423	0.72577616388888866	0.72728099444444427	0.7287658916666665	0.73026749722222206	0.73176910277777762	0.73327583055555545	0.73476409999999992	0.73626949999999991	0.73778040277777768	0.73928769999999988	0.74079139444444431	0.74229508888888873	0.74380181666666645	0.74528783888888872	0.7467701138888887	0.74827627499999982	0.7497585499999998	0.75124082499999978	0.75274243055555545	0.75424821111111096	0.75573254444444427	0.75721463055555538	0.7586989638888888	0.76018536111111101	0.76166557499999987	0.76314803611111093	0.76463574444444427	0.76614095555555539	0.76762360555555542	0.76910943888888872	0.77061408055555536	0.77209729166666641	0.77358274999999976	0.77507101944444423	0.77657528333333314	0.77805643333333308	0.77954114444444422	0.78104654444444421	0.78252919444444413	0.78401203055555524	0.78551610277777739	0.78701922777777744	0.78850150277777742	0.78998921111111076	0.7914963194444441	0.79299868611111068	0.79448189722222184	0.79596998055555523	0.7974744333333329	0.79895764444444406	0.80044385277777741	0.80195114999999961	0.80345294722222182	0.80493484722222175	0.80641768333333286	0.80791909999999956	0.80939912499999955	0.81088271111111054	0.8123687333333327	0.81386901111111054	0.81535203611111051	0.81683805833333267	0.81834251111111045	0.81984373888888817	0.82133051111111033	0.82283667222222145	0.82433771111111032	0.82582129722222142	0.82732821666666589	0.82883228888888816	0.830314002777777	0.83179740277777703	0.83330223333333264	0.83480251111111037	0.8362836611111103	0.83776762222222145	0.83926846944444367	0.84076609166666583	0.84224743055555473	0.84373382777777695	0.84523581388888802	0.84673305833333246	0.84821458333333244	0.84969648333333248	0.85119239999999907	0.85269229999999918	0.85417888333333247	0.85568200833333252	0.85718152777777701	0.85868579166666603	0.86016937777777702	0.86166699999999929	0.86316727777777702	0.86465386111111042	0.86613594722222143	0.86763565833333256	0.86912280277777698	0.87060938611111038	0.87211004444444362	0.87361203055555481	0.87509823888888816	0.87658407222222157	0.87808776666666599	0.87959316666666609	0.88107787777777713	0.88255996388888824	0.88406081111111046	0.88556488333333261	0.88704734444444366	0.88855028055555485	0.89005568055555484	0.89156108055555483	0.89304298055555487	0.89454743333333264	0.89605454166666587	0.89753850277777703	0.89903897222222151	0.900539441666666	0.90204256666666593	0.90354569166666598	0.90502421944444389	0.90652449722222161	0.9080268638888882	0.90950726388888825	0.91098672777777712	0.91248928333333268	0.91399108055555489	0.91547223055555493	0.9169738361111105	0.91847525277777708	0.91995434166666601	0.92145594722222157	0.92295755277777713	0.92445745277777713	0.92593598055555504	0.92741675555555503	0.92892025833333269	0.9303987861111106	0.93187731388888839	0.93336052499999944	0.93486042499999944	0.9363436361111106	0.93782684722222165	0.93931136944444382	0.94081164722222155	0.94231268611111052	0.94379945833333267	0.94530428888888829	0.94678881111111046	0.94827333333333252	0.94975598333333255	0.95123863333333258	0.95274384444444371	0.95424905555555484	0.95573526388888819	0.95723516388888819	0.95873506388888818	0.96023875833333272	0.96172196944444377	0.96322262777777712	0.96472878888888824	0.9662338111111104	0.96771402499999926	0.96921847777777703	0.97069925277777702	0.97218002777777701	0.97366024166666598	0.97516298611111041	0.97666383333333262	0.97814236111111041	0.97962519722222152	0.98110784722222155	0.98259049722222158	0.98407164722222151	0.98557609999999929	0.9870803638888882	0.98856432499999924	0.99007029444444383	0.99157626388888831	0.99307824999999939	0.99456221111111043	0.99604617222222158	0.99754683055555482	0.99904616111111044	1.0005273111111104	1.0020101472222216	1.0035108055555548	1.0050114638888881	1.0064926138888881	1.0079881499999992	1.0094836861111103	1.0109830166666658	1.0124626694444436	1.0139566888888882	1.0154533638888881	1.0169361999999993	1.0184353416666658	1.0199344833333326	1.0214368499999993	1.0229397861111102	1.0244190638888881	1.0259176361111104	1.0274163972222214	1.0289130722222215	1.0303871055555549	1.031885677777777	1.0333842499999992	1.0348814944444438	1.0363787388888881	1.0378786388888881	1.0393779694444438	1.0408772999999993	1.0423789055555548	1.043878616666666	1.0453735833333326	1.0468679805555547	1.0483652249999993	1.0498596222222214	1.0513532611111105	1.0528489861111103	1.0543467999999994	1.055841766666666	1.057337302777777	1.058817891666666	1.0603158944444437	1.061812377777777	1.0633130361111105	1.0648150222222215	1.0663147333333327	1.0678140638888882	1.0693130138888882	1.0708076027777771	1.0722987749999993	1.0737952583333328	1.0752921222222216	1.0767848138888882	1.0782786416666661	1.0797747472222217	1.0812668694444438	1.0827774499999994	1.0842705194444437	1.085759605555555	1.0872462249999995	1.0887552694444438	1.0902483388888884	1.0917406499999995	1.0932299249999995	1.0947229944444439	1.0962160638888885	1.097704769444444	1.0991944249999994	1.1006890138888885	1.1021836027777774	1.1036757249999996	1.1051699333333329	1.1066660388888885	1.1081570222222219	1.1096504722222218	1.1111460083333329	1.1126415444444442	1.1141338555555551	1.1156257861111107	1.1171346388888885	1.118624294444444	1.1201141388888884	1.1216043638888884	1.1231099499999997	1.1245956222222218	1.126081294444444	1.127573605555555	1.1290805361111107	1.1305891972222217	1.1320839749999996	1.1335947472222216	1.1351078249999995	1.1366046888888883	1.1381015527777774	1.1396111749999995	1.1411207972222217	1.1426329166666662	1.1441235194444439	1.1456302583333329	1.1471419916666661	1.1486539166666661	1.1501448999999995	1.151657594444444	1.1531724027777772	1.1546858638888884	1.1561804527777775	1.1576769361111108	1.1591896305555554	1.1606988666666664	1.1621904194444441	1.1636834888888885	1.1651940694444443	1.1667023444444442	1.1681946555555554	1.169689433333333	1.1712027027777776	1.172715972222222	1.174214922222222	1.1757318416666664	1.1772487611111109	1.1787486611111109	1.1802485611111109	1.1817446666666664	1.1832612027777776	1.1847790833333331	1.1862767055555554	1.1877870944444442	1.1892969055555553	1.1908103666666665	1.1923024888888887	1.1937976444444443	1.1953134111111108	1.1968241833333331	1.1983136499999998	1.1998061499999997	1.2013153861111108	1.2028246222222219	1.2043350111111109	1.2058280805555552	1.2073390444444441	1.2088471277777775	1.210359244444444	1.2118562972222218	1.2133503166666662	1.2148614749999995	1.2163762833333329	1.217872008333333	1.2193667861111106	1.2208785194444438	1.2223892916666661	1.2238778083333326	1.2253693611111105	1.2268866638888882	1.2283976277777771	1.2299087861111102	1.2314045111111103	1.2329177805555549	1.2344283611111104	1.2359404805555549	1.2374350694444438	1.2389464194444439	1.2404537361111105	1.2419673888888882	1.2434617861111104	1.2449760166666661	1.2464881361111106	1.2480015972222216	1.2494914416666663	1.2509983722222218	1.2525102972222217	1.2540222222222219	1.2555328027777775	1.2570374277777774	1.2585464722222219	1.2600539805555553	1.2615584138888885	1.2630839499999997	1.2645918416666664	1.2660962777777773	1.2676049388888886	1.2691341694444442	1.2706633999999999	1.2721687944444442	1.273673997222222	1.2752016722222219	1.276724097222222	1.2782449666666664	1.2797524749999998	1.2812597916666664	1.2827611527777776	1.2842655861111107	1.2857667555555552	1.2872679249999996	1.2887862666666665	1.2902935833333331	1.2917953277777776	1.2932970722222221	1.2948179416666665	1.296320647222222	1.2978233527777776	1.299326058333333	1.3008519833333332	1.3023759638888888	1.3038815499999998	1.3053871361111109	1.3069148111111109	1.3084380138888887	1.3099641333333329	1.3114741388888886	1.3129953972222219	1.3145129611111108	1.3160357749999996	1.317559172222222	1.3190817916666662	1.3206059666666663	1.3221346138888885	1.3236615111111107	1.3251862694444441	1.3267160833333329	1.328245119444444	1.3297706555555551	1.3312800833333329	1.332809119444444	1.3343375722222219	1.3358644694444441	1.3373765861111107	1.338903872222222	1.3404257138888886	1.3419491111111108	1.3434748416666664	1.344997072222222	1.3465196916666664	1.3480473666666664	1.3495764027777775	1.351085447222222	1.3526113722222219	1.3541390472222219	1.3556647777777775	1.3571674833333331	1.358694769444444	1.3602224444444442	1.361747397222222	1.3632742944444443	1.3647852611111109	1.3663121583333333	1.3678400277777776	1.3693739249999999	1.3708875777777778	1.3724185583333333	1.373948761111111	1.3754793527777776	1.377007805555555	1.3785164666666661	1.3800468638888883	1.3815772611111106	1.3831045472222216	1.3846153194444442	1.3861478555555553	1.3876755305555553	1.3892047611111107	1.3907376861111109	1.3922671111111109	1.3937918694444442	1.3953189611111108	1.3968452749999998	1.3983715888888888	1.3998994583333333	1.4014288833333333	1.4029542249999998	1.4044770388888888	1.4060019916666666	1.4075234444444447	1.4090454805555557	1.410571016666667	1.4121157472222223	1.4136397277777779	1.4151602083333334	1.4166837999999999	1.4182265611111109	1.4197649916666664	1.4212872222222219	1.4228110083333332	1.424332461111111	1.4258726638888886	1.427397811111111	1.4289227638888888	1.430442661111111	1.4319785333333332	1.4334955138888885	1.4350171611111109	1.4365376416666662	1.4380602611111106	1.4396055833333328	1.4411475583333329	1.4426746499999994	1.4442009638888884	1.4457247499999997	1.4472661333333328	1.4488071222222216	1.4503297416666661	1.4518498333333327	1.4533718694444437	1.4549134499999994	1.4564384027777773	1.4579631611111106	1.4595063166666662	1.4610490777777771	1.4625703361111106	1.4640933444444439	1.4656159638888882	1.4671579388888882	1.4686983388888883	1.4702215416666662	1.4717474666666663	1.473290033333333	1.4748290555555552	1.4763737861111106	1.4778979611111107	1.4794168861111108	1.4809348388888885	1.4824697277777774	1.484001272222222	1.4855159194444443	1.4870358166666664	1.4885714916666666	1.4901063805555554	1.4916239444444443	1.4931391749999998	1.4946524583333334	1.4961883305555554	1.4977301083333332	1.4992720833333333	1.5007937305555554	1.5023182944444444	1.5038608583333335	1.5054000777777778	1.506938902777778	1.508458605555556	1.5099785027777781	1.5115155583333337	1.5130563527777783	1.514595769444445	1.5161108055555561	1.5176476638888896	1.519186883333334	1.5207229527777784	1.5222588250000004	1.5237795000000005	1.5253167500000004	1.5268555750000006	1.5283985333333339	1.5299414916666672	1.5314795305555562	1.5330144194444451	1.5345542277777784	1.5360958083333338	1.5376344361111116	1.5391738527777783	1.5407150388888895	1.5422560277777784	1.5437954444444451	1.5453174805555563	1.5468547305555562	1.5483919805555562	1.5499341527777784	1.5514745527777782	1.5530102277777784	1.5545457083333338	1.5560859111111116	1.5576227694444449	1.5591578555555561	1.5606760027777782	1.5622144333333339	1.5637493222222227	1.5652855888888892	1.5668263833333338	1.5683665861111116	1.5699032472222225	1.5714442361111114	1.5729848333333338	1.5745224777777782	1.576079844444445	1.5776224083333341	1.5791612333333342	1.5806978944444452	1.5822327833333341	1.5837831777777787	1.5853145250000009	1.5868480361111119	1.5883809583333339	1.5899119111111117	1.5914430611111117	1.5929744083333339	1.5945028027777783	1.5960325750000004	1.5975672666666672	1.5991246333333338	1.6006599166666673	1.6021926416666674	1.603729694444445	1.6052862638888894	1.6068378527777785	1.6083737250000005	1.6099125500000007	1.6114490138888895	1.6130029916666675	1.6145601583333342	1.6160980000000007	1.6176338722222228	1.6191683666666674	1.6207245361111118	1.622279711111112	1.6238181444444453	1.6253567750000006	1.6268940250000006	1.6284273416666672	1.6299827166666674	1.6315217388888896	1.6330601694444451	1.6345978138888897	1.6361350638888896	1.6376948194444452	1.6392535777777786	1.6407892527777788	1.6423333916666676	1.6438941444444453	1.6454507138888896	1.6470090750000008	1.6485500638888897	1.6500947944444453	1.6516367694444454	1.6531965250000009	1.6547536916666676	1.6563060777777789	1.6578378166666679	1.659372902777779	1.6609254888888902	1.6624780750000012	1.6640340472222235	1.6655650000000011	1.6670920166666678	1.6686430083333343	1.6701965888888899	1.6717469833333345	1.6732927972222233	1.6748251277777788	1.6763771138888899	1.6779263111111122	1.6794782972222235	1.6810322750000013	1.6825614555555568	1.6841078666666678	1.6856582611111124	1.6872078583333348	1.6887600444444459	1.690315219444446	1.6918522722222236	1.6934042583333349	1.6949536555555571	1.6965052444444459	1.6980526500000017	1.699617269444446	1.7011648750000017	1.7027142722222239	1.7042614805555574	1.7058084888888907	1.7073610750000019	1.7089333527777797	1.7104849416666685	1.7120397194444466	1.7135954916666687	1.7151488750000019	1.7167028527777797	1.7182602194444465	1.7198173861111132	1.7213711666666687	1.7229261416666688	1.7245002333333355	1.7260552083333356	1.7276097861111135	1.7291641638888913	1.7307171472222245	1.7322853944444467	1.7338546472222245	1.7354239000000022	1.7369742944444468	1.7385246888888912	1.7400752805555579	1.7416258722222244	1.7431947222222246	1.7447461138888911	1.746300291666669	1.7478508861111135	1.7493988888888912	1.7509663277777801	1.7525337666666692	1.7540835638888914	1.7556391361111134	1.7571982944444469	1.7587582500000025	1.7603174083333359	1.7618908944444471	1.7634480611111139	1.7650028361111139	1.7665536277777805	1.7681030250000029	1.7696749000000027	1.7712443555555584	1.7728111916666696	1.7743631805555584	1.775913972222225	1.7774621750000028	1.7790267944444473	1.7805938305555584	1.7821424305555584	1.7836878444444473	1.7852394333333361	1.7868090916666695	1.7883775388888918	1.7899471972222252	1.7915214916666695	1.7930750722222251	1.7946262638888917	1.7961947111111141	1.7977655777777808	1.7993364444444475	1.8008912222222253	1.8024499833333365	1.8040248805555588	1.8055955444444476	1.8071718527777809	1.8087507833333365	1.8103045638888919	1.8118603361111143	1.8134326138888921	1.8150016666666697	1.8165717277777809	1.8181436027777806	1.8197162833333362	1.8212688694444474	1.8228413472222253	1.8244136250000031	1.825982677777781	1.8275527388888919	1.8291256222222252	1.8306780083333365	1.8322462555555588	1.833811477777781	1.8353845611111141	1.8369530083333365	1.8385208527777808	1.8400682583333365	1.8416334805555588	1.843201325000003	1.8447772305555585	1.8463497083333362	1.8479199694444475	1.8495121722222252	1.8510902944444474	1.8526609583333362	1.8542336388888916	1.8558055138888916	1.8573773888888914	1.8589614333333357	1.8605240361111135	1.862085630555558	1.8636490388888913	1.8652138583333358	1.8667823055555579	1.8683505527777804	1.8699372500000027	1.8715282277777805	1.8730988916666693	1.8746713694444472	1.8762426388888918	1.8778348416666695	1.8794073194444472	1.8809985027777805	1.8825734000000029	1.8841444694444474	1.8857109027777805	1.8872805611111141	1.8888678694444474	1.8904519138888918	1.8920225777777806	1.8935948555555584	1.895163908333336	1.8967499916666695	1.8983395416666695	1.8999303166666694	1.9015149722222249	1.9030840250000025	1.904658519444447	1.9062444000000025	1.9078317083333358	1.9094224833333358	1.9110106083333358	1.9125756305555579	1.9141394416666691	1.9157206305555579	1.9172991694444468	1.9188836222222245	1.9204690944444469	1.9220576250000023	1.9236467694444468	1.9252180388888913	1.9268071833333356	1.928395716666669	1.9299793555555578	1.9315670722222247	1.9331554000000026	1.9347420972222249	1.936334708333336	1.9379303777777805	1.9395221722222249	1.9411155972222249	1.9427110638888914	1.9443046944444469	1.9458938388888913	1.9474653111111135	1.9490367833333357	1.950623480555558	1.9522126250000025	1.9538003416666692	1.9553862222222247	1.9569680250000026	1.9585374805555582	1.9601278472222248	1.9617151555555581	1.9633024638888916	1.964892422222225	1.966479933333336	1.9680694861111139	1.9696797888888917	1.9712853472222251	1.9728653138888919	1.9744448722222252	1.9760258583333363	1.9776066388888918	1.9792072472222253	1.9808095055555588	1.9823888611111142	1.9839678083333365	1.9855455333333363	1.9871259083333364	1.9887232138888917	1.9903211388888917	1.9919221583333362	1.9935019194444472	1.9950814777777808	1.9966616472222252	1.998248750000003	1.999853688888892	2.0014596583333364	2.0030681055555588	2.0046755194444477	2.0062804583333365	2.0078653194444476	2.0094526277777809	2.0110600444444477	2.0126699361111142	2.0142816833333366	2.0158878611111142	2.0174930083333362	2.019101250000003	2.0206910055555585	2.0222940888888918	2.0238951083333361	2.0255027305555586	2.0271060194444472	2.0287062138888921	2.0302910750000032	2.0318777722222254	2.0334829194444475	2.0350886833333361	2.0366971305555586	2.0383028944444472	2.0399074222222251	2.0414967694444477	2.0430828555555585	2.0446620055555584	2.0462626138888917	2.0478692055555587	2.049473113888892	2.0510714527777809	2.0526695833333366	2.0542681277777812	2.0558666722222254	2.0574664527777808	2.0590645833333365	2.0606647777777809	2.0622662111111145	2.0638707388888924	2.0654789777777811	2.067060780555559	2.0686433972222256	2.0702495750000032	2.0718534833333369	2.0734555361111147	2.0750588250000037	2.0766631472222259	2.0782660250000036	2.079871583333337	2.0814814750000039	2.0830888916666703	2.084689911111115	2.0862946444444481	2.0879012361111151	2.0895070000000038	2.091108433333337	2.0927133722222262	2.0943195500000038	2.0959099166666704	2.097516094444448	2.0991208277777811	2.1007245305555591	2.1023269944444478	2.1039304916666701	2.1055333694444478	2.1071204750000034	2.1087285083333369	2.1103398444444479	2.1119487055555588	2.1135590083333367	2.1151684861111142	2.1167713638888923	2.1183775416666699	2.1199847500000035	2.1216100166666698	2.1232143361111144	2.1248201000000035	2.1264252444444476	2.1280258527777813	2.1296295555555589	2.131235319444448	2.1328379888888924	2.1344418972222257	2.1360458055555593	2.1376519833333369	2.1392523861111146	2.1408560888888926	2.1424626805555591	2.1440624638888925	2.1456816777777812	2.1473059000000037	2.1489135222222258	2.1505197000000034	2.1521291777777809	2.1537409250000032	2.1553506111111145	2.1569580277777809	2.1585640000000033	2.1601683222222254	2.1617841972222251	2.1633876944444475	2.1649905722222251	2.1665926250000029	2.1681948833333364	2.1697963166666696	2.1713956861111141	2.1729894861111143	2.1745874111111143	2.1762047472222252	2.1778225000000031	2.1794243444444477	2.1810317611111141	2.1826389694444477	2.1842439083333365	2.1858509111111144	2.1874745083333362	2.1890908000000033	2.1907093888888922	2.1923321500000035	2.1939313138888923	2.1955292388888923	2.197126338888892	2.198726738888892	2.2003430305555591	2.2019601583333368	2.2035810416666699	2.2052013000000033	2.2068221833333364	2.2084459888888919	2.2100476277777812	2.2116418388888923	2.2132348138888922	2.2148492277777811	2.2164663555555588	2.2180853611111142	2.2197097916666699	2.2213325527777812	2.2229496805555589	2.2245720250000032	2.2261777888888918	2.2277816972222255	2.2294044583333368	2.2310284722222256	2.2326524861111143	2.2342779611111143	2.2359007222222256	2.2375243194444479	2.2391424916666698	2.240741655555559	2.2423437083333364	2.2439447277777811	2.2455438916666699	2.2471461500000034	2.2487655722222257	2.2503841611111146	2.2520046277777812	2.2536261361111145	2.2552466027777811	2.2568685305555589	2.2584784222222254	2.2601064000000033	2.2617331250000032	2.2633604777777809	2.2649836555555587	2.2666049555555587	2.2682243777777811	2.2698456777777811	2.2714728222222256	2.2731138138888922	2.2747374111111145	2.2763564166666699	2.2779720833333363	2.2795875416666695	2.2812061305555589	2.2828253444444475	2.2844412194444477	2.2860602250000031	2.2877022694444475	2.2893434722222255	2.2909829861111142	2.2926065833333364	2.2942287194444475	2.2958491861111141	2.2974696527777807	2.2990953361111139	2.300717472222225	2.3023525527777808	2.3039886888888916	2.3056193388888917	2.3072510444444476	2.3088850722222252	2.3105191000000027	2.3121347666666692	2.3137512694444471	2.3153717361111137	2.3169938722222247	2.318617469444447	2.3202546611111137	2.3218943861111137	2.3235317888888916	2.3251687694444474	2.3268099722222249	2.3284490638888919	2.3300707833333365	2.331694588888892	2.3333183944444476	2.3349617055555587	2.3365980527777808	2.3382386222222249	2.3398779250000028	2.3415206027777806	2.3431645472222251	2.3448110250000029	2.346451172222225	2.3480620388888918	2.3496760361111138	2.351309430555558	2.3529411361111134	2.354574108333336	2.3562094000000027	2.3578495472222247	2.3594835750000027	2.3611190777777802	2.3627518388888915	2.3643841777777803	2.3660167277777804	2.3676503305555583	2.3692833000000024	2.3709135277777804	2.3725498750000025	2.3741881222222245	2.3758213027777804	2.3774576500000024	2.3790980083333357	2.3807387888888911	2.3823774583333357	2.384015916666669	2.385657541666669	2.3872790500000023	2.3889215194444464	2.3905650444444464	2.3922001250000022	2.3938330972222244	2.3954681777777802	2.3971076916666689	2.398747838888891	2.4003873527777801	2.4020348861111134	2.4036798861111133	2.4053200333333353	2.4069622916666686	2.4086049722222245	2.4102394222222245	2.4118759805555579	2.4135188722222245	2.4151602861111132	2.4168021222222245	2.4184418472222244	2.4200847388888911	2.4217255194444469	2.423367566666669	2.4250306250000024	2.4266934694444471	2.42833192777778	2.4299720750000025	2.4316113777777799	2.4332473027777803	2.434884494444447	2.4365210527777803	2.4381550777777803	2.4397884694444469	2.4414427750000023	2.4430985750000023	2.444749680555558	2.4464063361111132	2.4480664055555579	2.4497042305555579	2.4513426888888912	2.4529838916666691	2.4546240388888911	2.4562624972222245	2.4579066555555573	2.4595463805555577	2.4611837833333352	2.4628254083333352	2.4644884666666687	2.466146613888891	2.4678024138888905	2.4694601361111133	2.471115725000002	2.4727672583333353	2.4744213527777799	2.4760564333333352	2.4776900361111132	2.4793219527777799	2.4809585111111132	2.4825957027777799	2.484230572222224	2.4858654416666686	2.487496725000002	2.4891250527777795	2.4907731694444464	2.4924279027777794	2.4940811416666682	2.4957348083333351	2.497394025000002	2.4990345944444461	2.5006715750000019	2.5023104555555578	2.5039501805555577	2.5056061944444461	2.5072564472222241	2.5089137416666683	2.5105710361111124	2.5122225694444453	2.51388263888889	2.5155465500000007	2.5172089666666677	2.5188533333333343	2.5205025555555567	2.5221498777777791	2.5237921361111124	2.5254537000000012	2.5271171833333348	2.5287772527777794	2.5304354000000013	2.5320965361111121	2.5337578861111121	2.5354141138888897	2.5370703416666678	2.5387218750000007	2.5403704194444452	2.5420193916666673	2.5436538388888894	2.5453079333333335	2.5469607472222222	2.5486193222222222	2.5502804583333329	2.5519396749999999	2.5536008111111106	2.5552604527777776	2.5569190277777771	2.5585746166666663	2.5602348999999998	2.5618945416666663	2.5635518361111105	2.5652104111111105	2.5668541472222217	2.5684938722222217	2.5701274777777772	2.5717864805555553	2.5734414277777771	2.5750991499999998	2.5767558055555551	2.5784098999999991	2.580065913888888	2.5817247027777768	2.5833834916666656	2.5850367305555544	2.5866874083333324	2.5883404361111104	2.5899958111111099	2.5916492638888875	2.5933037833333321	2.59494308611111	2.5966001666666658	2.5982572472222216	2.5999151833333327	2.6015746111111104	2.6032299861111103	2.6048819444444438	2.606536891666666	2.6081918388888883	2.6098448666666658	2.6114989611111104	2.6131536944444433	2.6148065083333321	2.6164650833333316	2.6181485611111097	2.6198307444444433	2.6214903861111098	2.6231500277777768	2.62482811111111	2.6264830583333323	2.6281407805555546	2.6297993555555546	2.6314508888888875	2.6331041277777767	2.6347562999999989	2.6364099666666654	2.6380768277777769	2.6397518888888878	2.6414275972222212	2.6430979111111101	2.64476563611111	2.6464398333333325	2.6481168361111105	2.6497925444444439	2.6514676055555548	2.6531454722222216	2.6548027666666658	2.6564534444444439	2.6581049777777768	2.6597612055555548	2.6614131638888883	2.6630655499999993	2.6647226305555551	2.666374163888888	2.6680274027777773	2.6696806416666665	2.6713518194444443	2.6730234277777778	2.6746954694444445	2.676372475	2.6780291305555552	2.679683436111111	2.6813353944444445	2.6829837249999997	2.6846324833333335	2.6862878583333329	2.6879436583333334	2.6896024472222222	2.6912603833333328	2.6929163972222216	2.6945704916666657	2.6962228777777768	2.6978744111111101	2.6995440777777766	2.7012139611111103	2.7028909638888883	2.7045716361111101	2.7062512305555546	2.7079275861111096	2.709585733333332	2.7112425999999985	2.7128994666666655	2.714573663888888	2.7162296777777764	2.7178795027777767	2.7195250583333324	2.7211742416666658	2.7228411027777768	2.7245105555555544	2.7261836749999993	2.7278628361111106	2.7295441555555553	2.7312261222222216	2.7329095999999997	2.7345889777777779	2.7362698666666669	2.7379533444444446	2.7396305638888894	2.7412861527777781	2.7429434472222223	2.7446005277777781	2.7462732166666668	2.7479245361111118	2.7495794833333336	2.7512365638888894	2.7529064472222231	2.7545743888888898	2.7562462138888897	2.75791803888889	2.7595894333333342	2.7612597472222227	2.7629354555555561	2.7646081444444448	2.7662827750000005	2.7679548166666672	2.7696247000000005	2.7712930722222229	2.7729422555555563	2.7746071750000008	2.7762716638888896	2.7779404666666676	2.7796025805555562	2.7812640472222228	2.7829285361111116	2.784595397222223	2.7862594527777782	2.7879269611111113	2.7895961972222225	2.7912656472222221	2.7929325083333336	2.7946051972222223	2.7962727055555558	2.797936761111111	2.7996042694444441	2.8012765249999996	2.8029695583333329	2.8046614999999995	2.8063536583333333	2.8080449444444442	2.809731213888889	2.8114139916666669	2.8130967694444449	2.8147632000000002	2.8164335138888892	2.8181068499999999	2.8197791055555554	2.8214407888888888	2.8231033361111111	2.8247714916666662	2.8264418055555551	2.8281097472222219	2.8297815722222217	2.8314546916666665	2.8331260861111107	2.8347989888888887	2.8364740499999996	2.8381471694444445	2.8398230944444447	2.8415022555555556	2.8431981250000002	2.8448874500000003	2.8465748111111115	2.8482654444444448	2.849957169444445	2.8516309361111114	2.8533083722222226	2.8549817083333333	2.8566524555555555	2.8583244972222221	2.8599952444444443	2.8616618916666665	2.8633296166666669	2.8649990694444445	2.8666689527777778	2.8683351666666663	2.8700022444444446	2.8716710500000002	2.8733366166666667	2.8750049888888887	2.8766714194444445	2.878361833333333	2.8800502861111106	2.8817275055555553	2.8834001944444441	2.8850735305555553	2.8867472972222217	2.8884346583333329	2.8900991472222217	2.8917705416666664	2.8934460361111105	2.8951202361111106	2.8967935722222213	2.8984660444444437	2.900135927777777	2.9018066749999991	2.9034817361111105	2.9051630555555552	2.9068404916666659	2.9085179277777771	2.91019773611111	2.9118766833333325	2.9135712444444439	2.915269077777777	2.9169653833333324	2.9186568888888882	2.9203338916666661	2.9220108944444441	2.9237076361111107	2.925404158333333	2.9271006805555557	2.928775311111111	2.9304467055555552	2.9321170194444441	2.9337901388888885	2.9354589416666665	2.937123861111111	2.9388107861111115	2.9404981472222227	2.9421863805555559	2.9438741777777779	2.9455648111111108	2.9472589333333334	2.9489554555555557	2.9506517611111112	2.9523419583333332	2.9540219000000003	2.9557033694444446	2.9573885472222221	2.959071325	2.9607556305555556	2.9624460444444445	2.9641373305555554	2.9658168361111112	2.9675002694444443	2.9691841388888887	2.9708440944444443	2.972504697222222	2.9741670277777774	2.9758282777777771	2.9774919027777775	2.979157469444444	2.9808404666666659	2.9825243361111102	2.9842184583333329	2.9859114916666658	2.9876021249999991	2.9892927583333324	2.9909836083333325	2.9926718416666658	2.9943594194444429	2.996047869444443	2.9977369749999987	2.9994236805555543	3.0011130027777768	3.0028055999999985	3.0044793666666654	3.0061568027777761	3.0078372583333315	3.0095118888888872	3.0112040472222206	3.0128981722222208	3.0145883694444429	3.0162790027777757	3.017969636111109	3.0196576527777754	3.0213437055555534	3.0230306305555534	3.0247227916666648	3.0264149527777757	3.0281023138888874	3.0297879305555537	3.0314735472222201	3.0331569805555532	3.0348412888888867	3.0365277777777755	3.0382144861111087	3.0398977027777754	3.0415833194444417	3.0432654444444416	3.0449453888888862	3.0466292611111085	3.0483179305555526	3.0500209861111083	3.0517176472222194	3.0534167333333304	3.0551186861111082	3.0568149055555529	3.0584944111111088	3.0601782805555531	3.0618606222222198	3.0635481999999974	3.0652407972222195	3.0669338305555525	3.0686253361111082	3.0703190222222192	3.0720100916666637	3.0737005055555526	3.0753935388888856	3.0770913722222191	3.0787933499999967	3.0804900916666633	3.0822043944444411	3.0839164916666633	3.0856241777777744	3.0873347305555523	3.0890419749999967	3.0907514249999966	3.0924595527777745	3.0941674583333301	3.0958724972222189	3.0975544027777744	3.0992376194444411	3.1009232361111074	3.1026081972222186	3.1042837777777743	3.1059667749999962	3.1076543527777738	3.1093395333333298	3.1110266749999966	3.1127151277777743	3.114399869444441	3.1160865749999966	3.1177734999999966	3.1194588972222186	3.1211464749999962	3.1228482055555515	3.1245512611111068	3.1262534333333289	3.1279615611111069	3.1296685861111069	3.1313767138888848	3.1330832972222185	3.1347898805555521	3.1364999916666627	3.1382083388888851	3.1399140416666631	3.1416190805555519	3.1433267666666631	3.1450344527777743	3.1467231222222187	3.1484126638888852	3.1501019861111077	3.1518037166666635	3.1535069916666632	3.1552100472222184	3.1569133222222185	3.1585963194444404	3.160283897222218	3.1619710388888849	3.163654472222218	3.1653466305555513	3.1670370444444402	3.1687209138888845	3.1704036916666625	3.1721074083333289	3.1738117861111066	3.1755196916666621	3.1772306861111068	3.1789418999999954	3.1806458361111063	3.1823462444444397	3.1840481972222174	3.185749266666662	3.187450777777773	3.1891536111111063	3.1908537972222173	3.1925568527777726	3.1942663027777725	3.1959795027777731	3.1976869666666619	3.1993730166666619	3.2010632138888839	3.2027501388888839	3.2044377166666616	3.2061300944444389	3.2078211638888834	3.2095109249999947	3.211193049999995	3.2128985305555506	3.2146011444444391	3.216300449999995	3.2180037249999947	3.2197074416666611	3.2214085111111057	3.2231122277777722	3.224816166666661	3.2265247361111054	3.2282286749999938	3.2299352583333274	3.231641841666661	3.2333471027777723	3.2350523638888835	3.2367618138888834	3.2384699416666614	3.2401716749999947	3.2418712027777725	3.2435755805555497	3.2452795194444386	3.2469849999999942	3.2486904805555499	3.2503917722222169	3.2520895361111055	3.2537725333333278	3.2554566222222165	3.2571404944444384	3.2588634222222166	3.2605910305555499	3.2623175249999941	3.2640241083333277	3.2657306916666613	3.2674383777777725	3.2691469472222168	3.270859044444439	3.2725713611111051	3.2742799305555499	3.275983427777772	3.2776864833333272	3.2793913027777717	3.2810943583333274	3.2827947666666608	3.2844936333333274	3.2861958055555496	3.2878953333333274	3.2895986083333271	3.2913043111111051	3.2930075861111048	3.294711744444438	3.2964209749999935	3.2981288833333271	3.2998367916666602	3.3015411694444379	3.303249077777771	3.3049536777777715	3.3066609249999939	3.3083710388888825	3.3100824749999935	3.3117936916666597	3.3134906527777712	3.3152075999999933	3.3169181527777711	3.3186282638888822	3.3203443305555491	3.3220586333333268	3.3237700694444379	3.3254819444444377	3.3271920555555488	3.3288975361111044	3.3306052222222156	3.3323135694444379	3.33401574166666	3.335715930555549	3.3374161194444381	3.3391220416666605	3.3408266416666605	3.3425312416666606	3.3442398111111054	3.3459501444444384	3.3476580499999939	3.3493672805555494	3.3510791555555497	3.3527910305555495	3.3544962916666607	3.3562048611111051	3.3579169583333273	3.3596264083333272	3.3613354166666607	3.3630419999999939	3.3647492444444387	3.3664551666666611	3.3681776472222169	3.3698820249999941	3.371584638888883	3.3732874722222164	3.374990747222216	3.3766938027777718	3.3783961972222158	3.3801007972222159	3.3818100277777714	3.3835174944444382	3.3852265027777717	3.3869339694444385	3.3886394499999941	3.3903422833333274	3.3920468833333275	3.393751483333328	3.3954536555555501	3.3971571527777722	3.3988657222222165	3.4005707611111053	3.4022727138888826	3.4039786361111051	3.4056861027777718	3.4073926861111055	3.4090957416666607	3.4108018833333276	3.4125073638888836	3.414212402777772	3.4159176638888833	3.417645719444439	3.4193715444444388	3.4210920194444387	3.4228138333333278	3.4245343083333277	3.4262496555555497	3.4279647805555498	3.4296832499999943	3.4313968166666613	3.4331123888888833	3.4348290749999943	3.4365435333333276	3.4382448222222166	3.4399463333333276	3.4416487249999941	3.4433484722222163	3.445050424999994	3.4467521555555498	3.4484483722222161	3.4501487805555495	3.4518531583333272	3.4535590805555492	3.4552645611111052	3.4569693805555497	3.4586753027777721	3.4603832083333277	3.4620895694444394	3.4638001222222168	3.465510894444439	3.4672143888888836	3.4689203111111055	3.4706284388888835	3.4723359027777727	3.4740407222222172	3.4757508333333282	3.477462708333328	3.479170613888884	3.4808805055555503	3.4825873083333283	3.4842927888888844	3.4859967249999952	3.4877022055555509	3.4894083472222177	3.4911116222222174	3.4928146777777731	3.4945411722222173	3.4962681111111058	3.4979934916666617	3.4997224388888841	3.5014449222222175	3.5031638388888839	3.5048843138888839	3.5066052361111066	3.508322591666662	3.5100450749999954	3.5117708999999957	3.5134913749999952	3.51519751944444	3.5169085138888843	3.5186157611111066	3.5203212416666623	3.5220273861111067	3.5237388222222177	3.5254502583333287	3.5271561805555511	3.5288643083333291	3.5305704527777735	3.5322754944444403	3.5339805361111072	3.5356866805555516	3.5373897361111073	3.5390899249999959	3.5407925388888848	3.5424927277777738	3.5441913722222185	3.5458924416666626	3.5475970416666631	3.549298774999996	3.550998963888885	3.5527189944444406	3.5544367944444408	3.5561514749999965	3.5578719499999965	3.5595982222222187	3.5613211499999964	3.5630449694444408	3.5647703499999968	3.5664972888888853	3.5682217777777741	3.5699449277777742	3.5716714222222183	3.5733932361111074	3.5751141583333297	3.5768431055555521	3.5785722749999964	3.5802792999999964	3.5819810333333297	3.5836812222222187	3.5853829555555521	3.5870840249999962	3.5887848749999964	3.5904890333333292	3.5921905444444406	3.5938885277777741	3.5955882749999963	3.5972922138888848	3.59899526944444	3.6007011916666625	3.6024086583333292	3.6041132583333297	3.6058182999999966	3.6075255472222185	3.6092272805555519	3.6109298944444408	3.6126349361111076	3.6143441666666631	3.6160686555555519	3.6177886861111075	3.6195104999999965	3.621229416666663	3.6229458805555521	3.6246645722222186	3.6263868305555516	3.6281066388888852	3.6298222111111071	3.6315435777777738	3.6332587055555519	3.6349740555555519	3.6366902972222186	3.6383929111111075	3.6400933194444409	3.6417913027777744	3.643494799999996	3.645202705555552	3.6469075249999965	3.6486149916666633	3.6503248833333299	3.65204825833333	3.6537510916666629	3.6554521611111075	3.6571499222222186	3.6588472444444413	3.6605439027777744	3.6622454138888854	3.6639489111111074	3.6656466722222185	3.667351272222219	3.6690560916666635	3.6707560583333301	3.6724599944444414	3.6758678666666631	3.6775700388888852	3.6792739749999961	3.6809814416666629	3.6826822916666626	3.6843840222222184	3.6860899444444408	3.687796527777774	3.6895000249999961	3.6912070499999965	3.6929176027777739	3.6946222027777744	3.6963307722222187	3.698041766666663	3.6997481305555522	3.7014650388888852	3.7031843999999969	3.7049035388888854	3.7066224527777742	3.7083221999999965	3.7100420055555521	3.7117421944444411	3.7134421611111077	3.7151467611111082	3.7168546666666638	3.7185616916666637	3.7202678333333306	3.7219788277777748	3.7236847499999972	3.7253829527777751	3.7270793916666642	3.7287760499999973	3.7304716055555529	3.7321691472222196	3.7338704388888861	3.7355701861111084	3.7372677277777755	3.7389683555555533	3.7406705277777754	3.7423740249999975	3.7440764194444416	3.7457827833333308	3.7474882638888865	3.7491937444444421	3.7509131055555534	3.7526351416666643	3.7543589611111088	3.7560830027777756	3.7578063749999977	3.7595297472222198	3.7612513361111088	3.7629733722222198	3.7646974138888867	3.7664212333333311	3.7681397027777752	3.7698601777777752	3.7715831055555533	3.7733024666666646	3.7750202666666648	3.7767391805555537	3.7784587638888869	3.7801816916666646	3.7819050638888871	3.7836224194444426	3.7853370999999982	3.787037949999998	3.7887407833333313	3.7904438388888866	3.7921460111111087	3.7938669333333315	3.7955898611111092	3.7973092222222204	3.7990305888888871	3.800749502777776	3.8024485888888875	3.8041531861111091	3.8058586666666652	3.8075634861111096	3.8092665416666653	3.810969816666665	3.812675516666665	3.8143776888888872	3.8160791999999986	3.8177835777777758	3.8194872944444422	3.8211885833333312	3.8229090583333312	3.8246377833333312	3.8263656138888869	3.828090324999998	3.8298206083333315	3.8315515611111093	3.8332738194444422	3.8349891694444422	3.8367091999999978	3.8384296749999978	3.840149258333331	3.8418659444444421	3.8435804027777754	3.8452915166666641	3.8470064194444418	3.8487282333333308	3.8504489333333307	3.8521665111111085	3.8538858722222198	3.8556052333333311	3.8573243722222199	3.859042619444442	3.8607622027777753	3.8624793361111087	3.8641960222222198	3.8659144916666643	3.8676345222222199	3.8693509861111086	3.8710649972222195	3.8727856972222194	3.8745050583333307	3.8762008361111087	3.8779005833333309	3.8796058444444421	3.8813104444444422	3.8830146027777754	3.8847238333333309	3.8864255666666643	3.8881281805555532	3.8898318972222197	3.8915329666666643	3.8932364638888863	3.8949390777777753	3.8966445583333309	3.8983699388888864	3.9000904138888863	3.9018104444444419	3.9035324805555529	3.9052534027777752	3.9069754388888862	3.9086983666666639	3.9104212944444416	3.9121464527777752	3.9138698277777753	3.9155938694444421	3.9173147916666644	3.9190305861111088	3.9207448222222201	3.9224646305555533	3.9241855527777756	3.9259024638888866	3.927618258333331	3.929338511111109	3.9310569805555535	3.9327747805555537	3.9344939194444426	3.9362150638888869	3.9379304138888869	3.9396482138888871	3.9413698055555537	3.9430920638888871	3.9448074138888871	3.9465238777777758	3.948241677777776	3.9499592555555538	3.9516757194444425	3.9533796583333314	3.9550820527777759	3.956785327777776	3.9584901472222205	3.9601967305555537	3.961899566666665	3.9636048277777762	3.9653069999999984	3.9670047638888875	3.9687047333333321	3.970407347222221	3.9721106222222211	3.9738147805555544	3.9755162916666653	3.9772219944444429	3.9789431388888872	3.9806609388888874	3.9823780722222208	3.9841003305555542	3.9858192472222207	3.9875377166666652	3.9892608666666654	3.9909813416666653	3.9926989194444431	3.9944171666666652	3.9961389805555543	3.9978574499999988	3.9995743611111099	4.0012959527777765	4.0030177666666651	4.0047366833333315	4.0064549305555541	4.0081762972222208	4.0098998944444428	4.0116179194444426	4.0133372805555538	4.0150624388888874	4.0167824694444434	4.0185036138888872	4.0202260972222206	4.021948355555554	4.0236677166666652	4.0253895305555547	4.0271137972222215	4.0288376166666655	4.0305618833333323	4.0322823583333323	4.033978577777777	4.0356763388888881	4.0373776305555547	4.0390791416666652	4.0407786694444434	4.0424786361111096	4.0441843388888872	4.0458884972222204	4.0475882444444427	4.0492864472222205	4.0509897222222211	4.0526892499999985	4.0543863499999988	4.0560803638888876	4.0577785666666655	4.0594767694444434	4.0611718861111097	4.0628667805555541	4.0645638805555544	4.0662596583333324	4.0679565388888879	4.0696756777777763	4.0713905805555539	4.0731034777777761	4.0748246222222209	4.0765455444444427	4.0782651277777759	4.0799869416666654	4.0817063027777767	4.0834191999999989	4.085136108333332	4.086855913888888	4.0885770583333318	4.0902944138888877	4.0920124388888874	4.093730908333332	4.0954498222222213	4.0971689611111097	4.0988700305555543	4.1005929583333325	4.1023172222222213	4.1040432694444435	4.1057682027777762	4.1074909083333324	4.1092122749999991	4.1109345333333325	4.1126538944444437	4.1143538611111099	4.11605846111111	4.11776306111111	4.1194623666666654	4.1211603499999994	4.1228611999999991	4.124559402777777	4.126254958333333	4.1279461055555551	4.1296368111111104	4.1313275166666665	4.1330188833333326	4.1347139999999998	4.1364062499999994	4.1381013666666666	4.139800672222222	4.1415012999999998	4.1431997249999997	4.1448974861111108	4.1465970138888881	4.1482967611111103	4.1499989333333325	4.1517011055555546	4.1534017333333324	4.1550994944444435	4.156817963888888	4.1585330888888885	4.1602504444444435	4.1619709194444434	4.1636913944444434	4.1654109777777766	4.167126324999999	4.168843233333333	4.1705674972222218	4.1722877499999997	4.1740111222222218	4.1757356111111106	4.1774580916666659	4.1791794583333326	4.1809037222222214	4.1826262027777767	4.184342666666665	4.1860633638888878	4.1877825027777762	4.1895003027777769	4.1912011527777766	4.1929053083333327	4.1946043944444433	4.1963034805555548	4.1980087388888876	4.1997137777777764	4.2014166111111102	4.2031220916666658	4.2048280138888883	4.2065321694444435	4.208231255555555	4.2099334277777771	4.2116393499999996	4.2133395361111106	4.2150410472222211	4.2167403527777765	4.2184389972222212	4.2201391833333322	4.2218426777777767	4.2235485999999991	4.2252666249999988	4.2269846499999986	4.2287026749999983	4.2304244888888869	4.2321442972222201	4.2338632138888865	4.2355801249999976	4.2372992638888869	4.2390175111111095	4.240732861111109	4.2424517777777755	4.2441682416666646	4.2458891638888865	4.2476127611111085	4.2493325694444417	4.2510521527777749	4.2527746361111083	4.254499347222219	4.2562182638888855	4.2579380722222187	4.2596612222222188	4.2613819222222187	4.2631039583333301	4.264827999999997	4.2665295111111083	4.2682285972222198	4.269928566666664	4.2716291972222198	4.2733280638888864	4.2750289138888862	4.2767332916666643	4.2784367888888868	4.2801396249999977	4.2818409166666642	4.2835433111111083	4.2852446027777749	4.2869458944444414	4.2886549055555525	4.2903639166666636	4.292069838888886	4.2937722333333301	4.2954766111111082	4.2971759166666637	4.2988738999999967	4.3005751916666632	4.3022703083333296	4.3039700555555518	4.3056871888888848	4.307406997222218	4.3091247972222178	4.3108396999999954	4.312554602777773	4.3142715138888841	4.3159895388888838	4.317709122222217	4.3194304888888837	4.3211502972222169	4.3228678749999947	4.3245879055555498	4.326307936111105	4.3280096694444383	4.3297147111111052	4.3314396444444387	4.3331616805555502	4.3348850555555503	4.3366048638888834	4.3383280138888836	4.3400518333333284	4.3417738694444399	4.3434773666666624	4.3451797611111065	4.3468784055555512	4.3485788138888841	4.3502781194444395	4.3519743388888843	4.3536734249999958	4.3553700861111073	4.3570652027777736	4.3587609805555516	4.360462713888885	4.3621648861111071	4.3638679416666628	4.3655683499999958	4.3672687583333287	4.3689636555555511	4.3706594333333291	4.3723534472222179	4.3740452555555516	4.3757397111111072	4.3774543916666628	4.3791733083333293	4.3808937833333292	4.3826167111111074	4.3843387472222188	4.3860545416666632	4.3877663249999967	4.389479222222219	4.3911905583333297	4.3929050166666634	4.3946243777777747	4.3963424027777744	4.3980419305555518	4.3997436611111072	4.4014480388888853	4.4031493305555518	4.4048503999999964	4.4065503666666634	4.4082501138888857	4.4099503027777747	4.41165203333333	4.4133553083333297	4.4150605694444405	4.4167634027777742	4.4184699861111074	4.4201734833333299	4.4218732305555521	4.4235747416666635	4.4252777972222193	4.4269793083333306	4.4286781722222193	4.4303821083333306	4.4321030305555524	4.4338275194444412	4.43555200833333	4.4372740444444414	4.4389949666666633	4.4407152194444413	4.4424385916666633	4.4441583972222185	4.4458755305555515	4.4475948916666628	4.449314252777774	4.4510324999999966	4.4527500777777744	4.4544674333333303	4.4561867944444415	4.4579041499999974	4.4596241805555525	4.4613453249999973	4.4630691444444421	4.4647920722222203	4.4665125472222202	4.4682352527777756	4.4699550583333307	4.4716692916666645	4.4733841944444421	4.4750990972222198	4.476812216666664	4.4785275638888864	4.4802453638888862	4.4819649472222194	4.4836854222222193	4.4853893583333306	4.4870921916666644	4.4887903944444423	4.4904896999999977	4.4921905499999975	4.4938891944444421	4.49558739722222	4.4972858222222198	4.4989815999999978	4.5006793611111089	4.5023804305555535	4.5041026888888869	4.5058200444444427	4.5075402972222207	4.5092667916666649	4.5109881583333316	4.5127059583333313	4.514427324999998	4.5161482472222199	4.5178673861111092	4.519584963888887	4.5213025416666648	4.523021902777776	4.5247394805555539	4.526455944444443	4.5281770888888877	4.5299004611111098	4.5316227194444432	4.5333478749999987	4.53506723611111	4.5367836999999991	4.5385026138888875	4.5402206388888873	4.5419364333333316	4.5436515583333312	4.5453704722222197	4.5470717611111082	4.5487695222222193	4.550472577777775	4.5521771749999971	4.5538769222222193	4.555573361111108	4.5572733277777751	4.5589726333333305	4.5606651027777749	4.5623641888888864	4.5640628333333311	4.5657601527777754	4.5674572527777757	4.5691719333333314	4.5708703555555532	4.5725926138888866	4.5743155416666648	4.576041813888887	4.5777651888888871	4.5794852194444422	4.5812034666666648	4.5829179249999985	4.5846305999999988	4.5863455027777764	4.5880621888888875	4.5897782083333318	4.5914960083333316	4.5932187138888869	4.5949389666666649	4.5966569916666646	4.5983770222222198	4.6000981666666645	4.6018188666666644	4.6035366666666642	4.6052560277777754	4.6069785111111088	4.6086965361111085	4.6104174583333304	4.6121383805555523	4.6138577416666635	4.6155552833333298	4.6172548111111071	4.6189565444444405	4.6206547472222184	4.6223560388888849	4.6240615194444405	4.6257665611111074	4.6274671916666632	4.6291717916666633	4.6308752888888858	4.6325785638888854	4.6342805166666636	4.6359857777777744	4.6376877305555526	4.6393899027777747	4.641094061111108	4.6427984388888861	4.6445162388888859	4.6462275749999966	4.6479435944444409	4.6496571611111079	4.6513736249999971	4.653094099999997	4.6548123472222196	4.6565254666666638	4.6582434916666635	4.6599619611111081	4.6616782027777743	4.6633991249999962	4.6651032833333295	4.6668047944444409	4.6685021166666631	4.6702018638888854	4.6719247916666635	4.6736408111111079	4.6753561611111074	4.6770596583333299	4.6787624944444408	4.6804609194444406	4.6821575805555522	4.6838542416666638	4.6855506805555525	4.6872468999999972	4.6889470888888862	4.6906474972222192	4.6923485666666638	4.6940520638888863	4.695755119444442	4.697455308333331	4.6991539527777757	4.7008570083333314	4.7025591805555536	4.7042602499999981	4.7059613194444427	4.7076623888888873	4.7093594888888877	4.7110759527777768	4.7127919722222211	4.7145070999999987	4.7162235638888879	4.7179382444444435	4.7196524805555544	4.7213633722222212	4.7230593694444432	4.7247818527777765	4.7264998777777762	4.7282183472222208	4.7299388222222207	4.7316613055555541	4.7333650222222206	4.7350696222222206	4.7367751027777762	4.7384772749999984	4.7401801083333321	4.7418855888888878	4.7435882027777767	4.7452912583333324	4.7469936527777765	4.7486984722222205	4.750401969444443	4.7521059055555543	4.7538124888888875	4.7555164249999988	4.757216172222221	4.7589223138888874	4.7606308833333317	4.7623363638888874	4.7640411833333314	4.7657437972222203	4.7674464111111092	4.7691459388888866	4.7708467888888864	4.7725496222222201	4.7742458416666649	4.7759442666666647	4.7776420277777758	4.7793397888888869	4.781056252777776	4.7827736083333319	4.7844896249999982	4.7862034138888871	4.7879192083333315	4.7896200583333313	4.7913167166666648	4.7930122722222199	4.794707827777775	4.7963994138888859	4.7980932055555527	4.7997887611111079	4.8014869638888857	4.8031851666666636	4.8048893249999969	4.8065959083333301	4.8082994055555526	4.8100020194444415	4.8117017666666637	4.8134019555555527	4.8150997166666638	4.8167992444444412	4.8185018583333301	4.8201996194444412	4.8219022333333301	4.823607272222219	4.8253114305555522	4.827016691666663	4.828723716666663	4.8304287555555518	4.8321126249999962	4.833795622222218	4.8354823277777736	4.8371716499999957	4.8388749249999954	4.8405762138888839	4.8422823555555503	4.8439873944444392	4.8456900083333281	4.8473954888888837	4.8490965583333283	4.8507960833333286	4.8524956083333288	4.8541966777777734	4.8558928944444402	4.8575880083333294	4.8592873138888848	4.8609844138888851	4.8626819555555514	4.8643803777777732	4.8660829916666621	4.8677825166666624	4.8694820416666627	4.871183772222218	4.8728877083333293	4.8745916444444406	4.8762933749999959	4.8779984138888848	4.8796990416666626	4.8814009944444408	4.8831029472222189	4.8847971805555526	4.8864949416666636	4.8881909388888856	4.8898906861111078	4.8915955055555518	4.8932976777777739	4.8950170388888852	4.8967404138888853	4.8984414833333298	4.9001385833333302	4.9018442861111078	4.903550869444441	4.905255469444441	4.9069620527777742	4.9086681972222186	4.9103712527777743	4.9120736472222184	4.9137778055555517	4.915481744444441	4.9171852416666635	4.9188863111111081	4.920588924999997	4.9222919805555527	4.9239932722222193	4.9256958861111082	4.9273962944444412	4.9290982472222193	4.9308052722222193	4.9325167083333303	4.9342261583333302	4.9359294333333299	4.9376344749999967	4.9393179083333303	4.9410035249999966	4.942709669444441	4.944414488888885	4.9461140166666624	4.9478131027777739	4.9495141722222185	4.9512119361111075	4.9529101388888854	4.954611430555552	4.9563109583333294	4.958009602777774	4.9597089083333294	4.9614090972222185	4.963103552777774	4.9647982277777745	4.9664953277777748	4.9681924277777751	4.9698848972222196	4.9715833222222194	4.9732835111111084	4.9749843611111082	4.976685211111108	4.9783893694444412	4.9800928666666637	4.9817928361111079	4.9834958916666636	4.9851982861111077	4.9869028861111078	4.9886010888888856	4.9903211194444408	4.9920395888888853	4.9937435249999966	4.9954479027777747	4.9971566916666639	4.9988621722222195	5.0005663305555528	5.0022702666666641	5.0039744249999973	5.005677699999997	5.0073814166666635	5.0090866777777743	5.0107870861111072	5.0124872749999962	5.0141896694444403	5.0158913999999957	5.0175889416666619	5.0192922166666616	5.0209952722222173	5.0226965638888839	5.0243976333333285	5.0260984833333282	5.0278024194444395	5.0295037111111061	5.0311992666666612	5.0329163999999942	5.0346324166666605	5.0363468749999942	5.038047502777772	5.0397443833333275	5.0414414833333279	5.0431410111111052	5.0448396555555499	5.046537638888883	5.0482334166666609	5.049931399999994	5.051629161111105	5.0533282472222165	5.0550293166666611	5.0567299444444389	5.0584296916666611	5.0601285555555497	5.061821244444439	5.0635137138888835	5.0652000083333277	5.0668911555555498	5.0685834055555494	5.070280063888883	5.0719778249999941	5.0736760277777719	5.0753720249999938	5.077067580555549	5.0787690916666604	5.0804692805555494	5.0821650583333273	5.0838439111111047	5.0855240722222161	5.0872042333333276	5.0888978055555496	5.0905955666666607	5.0922935472222166	5.0939871194444386	5.0956833361111054	5.0973828611111056	5.0990819472222171	5.1007843388888841	5.1024918027777728	5.1041946361111066	5.1058976916666623	5.1076000833333293	5.1093024749999962	5.1110037638888848	5.1127043916666626	5.114410313888885	5.1161157944444406	5.1178148805555521	5.1195137444444407	5.121213491666663	5.12291345833333	5.124615849999997	5.1263032111111082	5.1279875166666642	5.1296733499999974	5.1313591833333305	5.1330415249999968	5.134722122222219	5.1364048999999969	5.1381103805555526	5.1397935944444413	5.1414926805555528	5.1431888999999975	5.1448822527777756	5.1465793527777759	5.1482810861111092	5.1499836999999982	5.1516860944444423	5.1533856222222196	5.1550847083333311	5.156780705555553	5.1584767027777749	5.1601755694444416	5.1618704666666639	5.1635611722222192	5.1652529805555529	5.1669329249999976	5.1686135249999978	5.1702956499999981	5.1719817027777761	5.173667972222221	5.1753514055555545	5.1770352777777768	5.1787163138888879	5.1803986583333321	5.1820827472222213	5.1837703277777765	5.185457252777776	5.1871413416666652	5.1888254305555543	5.190512138888888	5.1921940472222214	5.1938768277777774	5.1955609166666665	5.1972386777777775	5.1989170944444441	5.200593111111111	5.2022747999999996	5.2039582333333332	5.2056392694444442	5.2073407805555556	5.2090215972222227	5.2106991416666668	5.2123760305555553	5.2140566277777776	5.2157372249999998	5.2174156416666664	5.2190979833333326	5.2207787999999997	5.2224596166666668	5.2241432694444443	5.2258293222222223	5.2275149388888886	5.2291981555555553	5.2308804972222216	5.232565894444444	5.2342432194444442	5.2359231638888888	5.2376277638888888	5.2393239833333336	5.2410215249999998	5.2427188472222221	5.2444011888888884	5.2460785138888886	5.2477595472222216	5.2494423277777775	5.2511181249999996	5.2527915222222221	5.2544734277777776	5.2561557694444438	5.2578361499999993	5.2595167472222215	5.2611951638888881	5.2628764166666659	5.2645559222222218	5.2662387027777777	5.267921044444444	5.2696031694444443	5.2712848583333329	5.2729704749999993	5.2746528166666655	5.2763336333333326	5.2780344833333324	5.2797395222222212	5.2814225194444431	5.2831035527777761	5.2847850222222208	5.2864697638888876	5.2881481805555541	5.2898274694444432	5.2915050111111102	5.2931851722222216	5.294870569444444	5.2965590194444436	5.2982459444444432	5.2999291583333319	5.3016136833333318	5.3033008249999982	5.3049842583333318	5.3066663833333321	5.308350908333332	5.3100371777777768	5.3117184305555547	5.3133998999999994	5.3151029555555551	5.316805569444444	5.3184881305555551	5.320171127777777	5.3218523805555549	5.3235338499999996	5.3252137916666662	5.3268976611111105	5.3285780388888879	5.3302595083333326	5.3319422861111105	5.333624191666666	5.3353045694444434	5.3369836388888876	5.3386664166666655	5.3403478861111102	5.3420287027777773	5.3436959944444435	5.3453807361111103	5.3470659138888879	5.3487508749999986	5.3504173055555544	5.3520815777777768	5.3537654499999991	5.3554499749999991	5.3571375555555543	5.3588268805555543	5.3605131499999992	5.3621965833333327	5.3638813277777775	5.3655623638888885	5.3672477611111109	5.368932069444444	5.3706100499999998	5.3722897749999996	5.3739721194444439	5.3756529361111109	5.3773289527777779	5.379004752777778	5.380685788888889	5.3823444499999997	5.3840026805555556	5.3856654416666672	5.3873303611111112	5.388990102777778	5.3906530805555555	5.3923147638888889	5.3939768777777779	5.3956583472222226	5.3973430888888894	5.3990258694444453	5.4007117027777785	5.4024003722222229	5.4040842416666672	5.4057685472222232	5.407448272222223	5.4091264694444456	5.4108040138888898	5.4124835194444456	5.4141462805555571	5.4158131416666686	5.4174789250000019	5.4191427666666687	5.4208081194444464	5.4224758444444463	5.4241431388888905	5.4258080583333346	5.4274912750000013	5.4291736166666675	5.4308574861111119	5.4325413555555562	5.434220861111112	5.435900150000001	5.437584455555557	5.439268761111113	5.4409319555555573	5.4425955805555573	5.4442624416666687	5.4459245555555578	5.4475836500000021	5.4492414472222244	5.4508992444444466	5.4525574750000025	5.4542191583333359	5.4558845083333356	5.4575502916666689	5.4592119750000023	5.4608725777777805	5.4625538305555583	5.4642333361111142	5.4659093527777811	5.4675879861111145	5.4692718555555588	5.4709483083333366	5.4726267250000031	5.4743110305555591	5.4759983916666704	5.4776626638888928	5.4793275833333368	5.4809916388888924	5.4826548333333367	5.4843197527777807	5.4859838083333363	5.487642469444447	5.4893011305555577	5.4909641083333351	5.4926242805555576	5.4942777638888911	5.4959509444444468	5.4976300138888909	5.4993069027777794	5.5009844444444465	5.5026622055555574	5.5043438944444461	5.5060218750000018	5.5076989805555572	5.5093567777777794	5.5110186750000016	5.5126831638888909	5.5143530472222242	5.5160224972222238	5.5176869861111131	5.5193519055555571	5.5210183361111129	5.5226808833333347	5.5243494722222239	5.5260178444444463	5.527684488888891	5.5293509194444468	5.531018211111113	5.5327025194444461	5.5343892277777798	5.5360707000000016	5.5377345416666683	5.5393940666666683	5.5410518666666686	5.5427103138888905	5.5443676805555571	5.5460239694444455	5.5476796111111124	5.5493397833333349	5.5510012500000014	5.5526625027777792	5.55432763888889	5.5559955805555568	5.5576613638888901	5.5593461055555569	5.5610308472222236	5.5627173361111124	5.5644005527777791	5.5660672000000018	5.567731905555557	5.5693920777777794	5.5710544083333353	5.5727147972222246	5.5743782083333357	5.5760416194444469	5.5777056750000025	5.5793680055555583	5.5810299055555586	5.5826954722222251	5.5843621194444477	5.586026608333337	5.5876932555555596	5.5893607638888927	5.5910233111111145	5.5926671611111143	5.5943307861111142	5.5959944111111142	5.5976532888888917	5.5993128138888917	5.600976008333336	5.6026351027777803	5.604293763888891	5.6059545833333351	5.6076158333333348	5.6092775166666682	5.6109424361111122	5.6126105916666678	5.6142789638888901	5.6159438833333342	5.6176118250000009	5.6192663444444451	5.620915527777778	5.6225834694444448	5.6242518416666671	5.6259215083333336	5.6275877222222226	5.6292554472222225	5.6309244666666673	5.6325893861111114	5.6342530111111113	5.6359153416666672	5.6375774555555562	5.6392380583333344	5.6408993083333341	5.6425637972222233	5.6442248333333342	5.6458695361111122	5.6475176527777791	5.649162355555557	5.6508047111111122	5.652469847222223	5.6541371388888892	5.6558016277777785	5.6574648222222228	5.6591265055555562	5.6607897000000005	5.662449872222223	5.664111986111112	5.6657736694444454	5.6674347055555563	5.6690963888888897	5.6707402388888895	5.6723828083333343	5.6740266583333341	5.675673708333334	5.6773218250000008	5.6789705833333342	5.6806210472222229	5.6822883416666672	5.6839515361111115	5.6856190444444445	5.6872874166666669	5.6889538472222227	5.6906181194444452	5.6922634638888896	5.6939081666666675	5.6955505222222227	5.6971973611111117	5.698848466666667	5.700497652777778	5.7021393694444447	5.7037830055555556	5.7054253611111108	5.7070707055555552	5.7087175444444442	5.7103660888888887	5.7120340305555555	5.7137004611111113	5.7153643027777781	5.7170238277777781	5.7186653305555559	5.7203083250000004	5.7219496138888895	5.7235900500000003	5.7252345388888894	5.7268856444444447	5.7285318416666673	5.7301741972222224	5.731818261111111	5.7334610444444447	5.7351038277777784	5.7367696111111117	5.7384377666666673	5.7401039805555563	5.7417520972222231	5.7434032027777784	5.7450487583333336	5.7466898333333338	5.7483315472222225	5.749974541666667	5.7516164694444445	5.7532588249999996	5.7549063027777771	5.7565563416666663	5.7582044583333332	5.759852575	5.7615045333333335	5.7631535055555556	5.7648201500000003	5.7664691222222224	5.7681187333333339	5.7697677055555561	5.7714149694444448	5.7730645805555563	5.7747112055555565	5.7763578305555567	5.7780121361111121	5.7796660166666678	5.7813156277777793	5.7829667333333346	5.7846197611111121	5.7862717194444455	5.7879215444444458	5.7895726500000011	5.7912246083333345	5.792872086111112	5.7945204166666677	5.7961661861111118	5.7978143027777787	5.7994553777777789	5.8011002944444456	5.8027426500000008	5.8043847916666671	5.8060230916666669	5.8076631000000001	5.809302252777778	5.8109439666666667	5.8125884583333329	5.8142350833333332	5.8158802138888888	5.8175236361111109	5.8191679138888883	5.8208098444444438	5.8224515611111105	5.8240988249999992	5.8257456638888883	5.8273892999999992	5.8290314416666655	5.8306737972222207	5.8323123111111093	5.8339340972222207	5.8355768805555543	5.8372164611111099	5.8388571083333325	5.8404979694444439	5.8421394722222217	5.8437820416666666	5.8454216222222222	5.8470607777777781	5.8487027055555556	5.8503418611111115	5.851983788888889	5.8536308388888889	5.8552553694444445	5.8568985777777778	5.8585469083333335	5.8601982277777775	5.8618454916666662	5.863490408333333	5.8651370333333332	5.8667823777777777	5.8684283611111114	5.8700764777777783	5.8717267305555563	5.8733767694444454	5.8750084750000013	5.8766408138888906	5.8782706194444465	5.8798953611111129	5.8815141916666684	5.8831355555555573	5.8847744972222236	5.8864168527777787	5.8880621972222231	5.8897049805555568	5.8913303527777794	5.8929546694444461	5.8945813083333354	5.8962060472222246	5.8978301527777806	5.8994597472222248	5.9010916638888915	5.9027199916666691	5.9043451527777799	5.9059722138888908	5.9076169166666688	5.9092618333333355	5.9109069638888911	5.9125578555555576	5.9142053333333351	5.9158338722222243	5.9174668416666689	5.9191025555555576	5.920737636111113	5.9223718722222243	5.9240090638888914	5.9256441444444468	5.9272798583333355	5.9289170500000026	5.9305694361111136	5.9322218222222247	5.9338744222222246	5.9355099250000025	5.9371437416666692	5.9387735472222252	5.9404029305555586	5.9420327361111145	5.943662963888892	5.945296569444448	5.9469308083333372	5.9485593472222265	5.950205544444449	5.9518543027777824	5.9534845305555599	5.9551107472222267	5.9567378083333375	5.9583686694444484	5.9599921444444481	5.9616164638888929	5.9632445805555596	5.9648703777777818	5.9664951194444482	5.9681207055555596	5.969745447222226	5.9713871611111147	5.9730252472222256	5.9746542083333365	5.9762835916666699	5.9779121305555591	5.9795404583333367	5.9811679416666701	5.9827920500000031	5.9844129916666695	5.9860362555555584	5.9876762638888916	5.9893184055555579	5.9909675888888909	5.9926163472222242	5.994246363888891	5.9958740583333352	5.9974996416666686	5.9991275472222245	6.0007495444444467	6.0023702750000023	6.0039948027777799	6.0056214416666691	6.00724660277778	6.0088713416666693	6.0104960805555585	6.0121220861111144	6.013749358333337	6.0153768416666704	6.0170066472222263	6.0186315972222264	6.020256125000004	6.0218850861111148	6.0235142583333374	6.0251413194444483	6.0267711250000042	6.0284007194444484	6.0300263027777818	6.0316514638888927	6.0332914722222259	6.034916425000004	6.0365407444444488	6.0381661194444485	6.0397933916666711	6.0414217194444486	6.04304730555556	6.0446752111111159	6.0463054388888935	6.0479325000000044	6.0495593500000044	6.051185777777782	6.052831547222226	6.0544590305555595	6.0560865138888929	6.0577127305555596	6.0593378944444485	6.0609639027777815	6.0625905416666708	6.0642207694444483	6.0658512083333376	6.0674822805555602	6.069111241666671	6.0707372500000041	6.0723800333333378	6.0740249500000045	6.0756520111111154	6.0772748527777818	6.0788998055555599	6.0805262333333374	6.0821541388888933	6.0837803555555601	6.0854110055555601	6.0870393333333377	6.0886851027777817	6.0903359944444482	6.0919851777777811	6.0936294555555586	6.0952705305555588	6.096899069444448	6.098528875000004	6.1001584694444482	6.1017901750000041	6.103423777777782	6.10507168055556	6.1067180916666715	6.1083685555555602	6.1100141111111155	6.1116609472222265	6.1133090638888934	6.114954194444449	6.116599963888893	6.1182287138888931	6.119853875000004	6.1214796694444482	6.1231044083333375	6.1247323138888934	6.1263583194444493	6.1280030222222273	6.1296473000000047	6.1312926444444491	6.1329190722222267	6.1345455000000042	6.1361696083333372	6.1377951944444487	6.1394197250000042	6.1410467861111151	6.1426763805555593	6.1443009111111149	6.1459260750000038	6.1475703527777812	6.1492188972222257	6.1508640277777813	6.1525059555555588	6.1541502333333362	6.1557772944444471	6.1574041444444472	6.1590312055555581	6.1606614333333356	6.162290816666669	6.1639180888888916	6.1655447277777808	6.1671703138888923	6.1687942111111145	6.1704404083333371	6.1720838305555592	6.1737274666666702	6.1753736638888928	6.1770049472222261	6.1786364416666704	6.1802700472222263	6.1819021750000038	6.1835311361111147	6.1851558777777811	6.1867795638888925	6.1884104250000034	6.190037697222226	6.1916634944444482	6.1933086250000038	6.1949550361111152	6.1965867416666711	6.1982163361111153	6.1998452972222262	6.2014742583333371	6.203102163888893	6.2047294361111156	6.2063541750000049	6.2079782805555608	6.2096007000000055	6.2112050972222281	6.2128330027777841	6.21445900833334	6.2160833250000067	6.2177105972222293	6.2193340694444519	6.2209581750000078	6.2225829138888971	6.224207019444453	6.2258323916666756	6.2274550222222311	6.2290846166666753	6.2307135777777862	6.232339794444453	6.2339719222222305	6.2355840416666748	6.2372119472222307	6.23884048611112	6.24047303611112	6.2421038972222309	6.243734547222231	6.2453656194444536	6.2470000694444536	6.2486296638888978	6.2502586250000087	6.2518875861111196	6.2535157027777863	6.2551265694444531	6.2567345166666755	6.2583405833333421	6.2599606805555643	6.2615835222222307	6.2632101611111199	6.2648399666666759	6.2664661833333426	6.2681002111111201	6.2697352916666755	6.2713674194444531	6.273001025000009	6.2746342083333424	6.2762667583333425	6.2778919222222314	6.2795156083333428	6.2811454138888987	6.2827747972222321	6.2844024916666763	6.2860365194444539	6.2876659027777873	6.2892965527777873	6.2909257250000099	6.2925546861111208	6.2942023777777871	6.295830283333343	6.2974628333333431	6.2990913722222324	6.3007188555555658	6.3023497166666766	6.3039786777777875	6.3056065833333435	6.3072309000000102	6.3088556388888994	6.3104850222222328	6.3121141944444554	6.3137440000000113	6.3153725388889006	6.316998122222234	6.3186256055555674	6.3202535111111233	6.3218801500000126	6.3235072111111235	6.3251368055555677	6.3267661888889011	6.328395994444457	6.3300253777777904	6.3316585583333458	6.3332923750000125	6.3349217583333459	6.3365526194444568	6.3381853805555677	6.3398179305555677	6.341447525000012	6.3430790194444562	6.3447050277777892	6.3463337777777893	6.3479833888889008	6.349634494444456	6.351262400000012	6.3528905166666787	6.3545224333333454	6.3561509722222347	6.3577742361111236	6.3594006638889011	6.36102582777779	6.3626461361111231	6.3642725638889006	6.365903847222234	6.3675363972222341	6.3691674694444567	6.3708002305555675	6.3724327805555676	6.3740651194444569	6.3756896500000124	6.3773150250000121	6.3789393444444569	6.3805647194444566	6.3821917805555675	6.3838154666666789	6.3854414750000119	6.3870876722222345	6.3887202222222346	6.390345808333346	6.3919747694444569	6.3936077416666794	6.395242611111124	6.3968755833333466	6.3985064444444575	6.4001377277777909	6.4017669000000135	6.4033943833333469	6.4050246111111244	6.4066567361111249	6.4082882277777919	6.4099159222222362	6.4115408722222362	6.4131658222222363	6.4147943611111256	6.4164222666666815	6.418050594444459	6.4196789222222366	6.42130830555557	6.4229366333333475	6.4245458305555694	6.4261705722222358	6.4277961583333472	6.4294221666666802	6.4310490166666803	6.4326754444444578	6.4342963861111242	6.4359219722222356	6.4375528333333465	6.4391771527777912	6.4407803000000134	6.4423830277777911	6.4439857555555689	6.4456085972222352	6.4472377694444578	6.4488686305555687	6.4504948472222354	6.4521200111111243	6.4537292083333462	6.4553407027777903	6.4569488583333454	6.4585607694444569	6.4601893083333461	6.4618189027777904	6.4634480750000129	6.4650759805555689	6.4666986111111244	6.4683294722222353	6.4699622333333462	6.4715703888889013	6.4731749972222348	6.4747823166666789	6.476393811111123	6.478006138888901	6.4796342555555677	6.4812642722222344	6.4828921777777904	6.4845240944444571	6.486153900000013	6.4877815944444572	6.4894090777777906	6.4910207777777904	6.492631016666679	6.4942435527777898	6.4958521222222343	6.4974590222222339	6.4990659222222336	6.5006944611111228	6.5023166666666787	6.5039229416666791	6.5055329722222348	6.5071375777777902	6.5087451055555681	6.5103534666666789	6.5119626638889008	6.513573113888901	6.5151812666666791	6.5167892111111234	6.5184177500000127	6.5200422805555682	6.5216708194444575	6.5233014694444575	6.5249092055555691	6.526514230555569	6.5281186277777916	6.5297249055555691	6.5313332694444579	6.5329435111111245	6.5345760611111245	6.5362054444444579	6.5378136000000131	6.5394261361111239	6.5410386722222347	6.5426418194444569	6.5442526861111237	6.545859797222235	6.5474662833333461	6.5490918694444575	6.5507212527777909	6.5523548583333469	6.5539865638889028	6.555618902777792	6.5572324833333475	6.558846063888903	6.560459227777792	6.5620721833333473	6.5636799194444588	6.5653055055555702	6.5669300361111258	6.5685526666666814	6.5701759305555703	6.5717968722222366	6.5733981388889031	6.5750025361111257	6.5766098555555699	6.578217175000014	6.5798276250000143	6.5814382833333473	6.5830514444444583	6.5846831472222362	6.5862992305555697	6.5879073833333477	6.5895159527777922	6.5911251500000141	6.5927368500000139	6.594349802777792	6.5959600416666806	6.5975715333333476	6.5991821916666806	6.6007947277777914	6.6024106027777911	6.6040314861111247	6.6056306500000135	6.607230019444458	6.6088291833333468	6.6104277277777914	6.6120188444444583	6.6136267916666807	6.6152393277777914	6.6168522833333467	6.6184587694444579	6.6200646277777908	6.6216551277777906	6.6232410888889017	6.6248272555555685	6.6264194055555681	6.628011969444457	6.6295997861111235	6.6311896666666792	6.6327822305555681	6.6343560805555679	6.6359309500000121	6.6375058194444563	6.6391039527777895	6.6406981666666782	6.6422956805555673	6.6438954638889003	6.6454911222222339	6.6470824472222336	6.648676866666678	6.6502519388888999	6.6518255833333439	6.6533971888888992	6.6549687944444544	6.6565436611111215	6.6581356027777883	6.6597283694444549	6.661324438888899	6.6629213333333439	6.6645132750000107	6.6660842694444549	6.6676560777777878	6.6692248277777875	6.6707937805555648	6.6723613055555644	6.6739495333333423	6.6755357000000091	6.6771060805555642	6.6786838027777868	6.6802574472222309	6.6818296638888972	6.6834039194444523	6.6849732805555631	6.6865416222222294	6.688111594444452	6.6896844222222294	6.6912550083333402	6.6928278361111175	6.6944080055555624	6.6959689944444509	6.6975295805555621	6.6990843222222285	6.7006591888888956	6.702228755555562	6.7038009722222283	6.7053731888888946	6.7069480555555616	6.7085225166666724	6.7100754444444499	6.7116283722222274	6.7131815027777826	6.7147384611111161	6.7162932027777824	6.7178550000000046	6.7194151833333375	6.7209743583333372	6.7225345416666702	6.7240975472222262	6.725640769444448	6.7271804055555595	6.7287204416666704	6.7302600777777819	6.7317947333333379	6.7333268000000048	6.7348592666666711	6.7363913333333381	6.7379045722222273	6.7394247000000052	6.740944827777783	6.742466333333339	6.7439846888888946	6.7455046194444499	6.7470225805555613	6.748541330555561	6.7500600805555608	6.7515650055555607	6.7530679833333389	6.7545696027777833	6.7560745277777832	6.7575778972222276	6.7590960583333386	6.7606191388888943	6.7621443833333386	6.7636692361111166	6.7651940888888946	6.7667052361111164	6.7682123000000054	6.7697123638888943	6.7712097055555613	6.7727064638888947	6.7742049722222282	6.7756984250000061	6.7771946000000058	6.7786756027777839	6.780156605555562	6.7816353027777838	6.783117072222228	6.7845986500000057	6.786081188888895	6.7875635361111168	6.7890437694444499	6.7905249638888945	6.7919859750000056	6.7934662083333386	6.7949283555555606	6.7964103166666714	6.79787265555556	6.7993544250000042	6.8008327361111149	6.8023049000000038	6.8037772583333371	6.8052501916666701	6.8067256222222259	6.8081818888888925	6.8096419500000041	6.8110987861111152	6.8125561916666708	6.8140153055555599	6.8154793500000039	6.8169481388888924	6.8184150305555589	6.8198817305555588	6.8213336583333364	6.8227816500000031	6.8242475916666701	6.8257160000000034	6.8271844083333368	6.828645038888892	6.8301054805555586	6.8315657305555586	6.8330290166666696	6.8344743861111139	6.8359240638888918	6.8373664361111137	6.8388058111111141	6.8402504305555585	6.8416907416666692	6.8431502333333363	6.8446127611111143	6.8460747194444478	6.8475214000000033	6.8489660194444477	6.8504168222222255	6.8518668750000034	6.8533137444444474	6.8547608000000029	6.8562106666666693	6.8576580972222247	6.8591023444444472	6.8605283083333362	6.8619566777777807	6.8633850472222253	6.8648089750000034	6.8662299444444477	6.8676516527777807	6.8690739166666699	6.8704950722222256	6.871919555555559	6.8733458888888928	6.8747510138888925	6.8761554083333367	6.8775654638888923	6.8789769805555592	6.8803863055555592	6.8817936222222258	6.8832066000000038	6.8846188472222263	6.8860307277777819	6.8874246333333371	6.8888147555555594	6.8902028944444487	6.8915919361111158	6.8929844000000049	6.8943915333333381	6.8957999472222271	6.8972065333333381	6.8986116583333379	6.8999997972222271	6.9013864944444494	6.9027753555555602	6.9041660166666716	6.9055568583333384	6.9069433750000053	6.9083347583333383	6.9097221777777831	6.9111110388888939	6.9125051250000054	6.9138817583333383	6.9152543000000053	6.9166264861111166	6.9179984944444497	6.9193667694444496	6.9207314861111167	6.9220986916666725	6.923466788888895	6.9248380861111176	6.9261893444444507	6.927538497222228	6.928892036111117	6.9302431194444507	6.9315956055555619	6.9329477416666734	6.9343233083333402	6.935698341666674	6.9370746194444521	6.9384309666666741	6.9397780138888967	6.9411278694444523	6.9424763194444523	6.9438256472222299	6.9451788361111184	6.9465292166666739	6.9478773166666743	6.9492220833333409	6.9505717638888962	6.9519071861111188	6.9532424361111191	6.9545587111111189	6.9558922305555635	6.9572283444444523	6.958562555555563	6.9598901888888962	6.9612185138888965	6.962532569444452	6.9638461138888967	6.9651623888888965	6.9664793472222302	6.9677956222222299	6.9691151416666743	6.9704355138888969	6.9717552055555636	6.9730731888888968	6.974392538888897	6.9757129111111196	6.977013430555564	6.9783161388888972	6.979620025000008	6.98092172222223	6.9822161805555636	6.9835269916666745	6.9848413888888965	6.9861549333333413	6.9874724027777857	6.9887898722222301	6.990090727777786	6.9913920888888974	6.992694291666675	6.9939971666666754	6.9953007166666756	6.9965983722222314	6.9979022583333421	6.9992027777777865	7.0005007694444537	7.0017814777777874	7.0030628500000098	7.0043432250000102	7.0056211111111208	7.0068956777777878	7.0081742277777881	7.0094521138888988	7.0107318250000095	7.0120117027777873	7.0132902527777876	7.0145490638888983	7.0158057500000091	7.0170624361111198	7.018323866666675	7.0195838250000087	7.02084231111112	7.0220999777777866	7.0233591166666756	7.0246355083333425	7.025910572222231	7.0271501722222309	7.028410458333342	7.0296713972222307	7.0309290638888973	7.0321885305555636	7.0334458694444528	7.0347068083333415	7.0359659472222305	7.0372232861111197	7.0384630500000087	7.0397029750000089	7.0409438666666757	7.0421833055555645	7.0434259694444536	7.0446733111111204	7.0459175888888979	7.047160252777787	7.0484040472222311	7.0496452611111202	7.0508653611111205	7.0520883194444535	7.053314138888898	7.0545378944444534	7.0557605361111202	7.0569838138888983	7.058206455555565	7.0594254444444537	7.0606517416666756	7.061878991666676	7.0630860472222317	7.0642913805555647	7.0655006250000092	7.0667081500000091	7.0679186472222311	7.0691300833333424	7.0703419888888979	7.0715542083333425	7.0727656444444538	7.073960575000009	7.0751561222222312	7.0763472000000087	7.077537044444453	7.0787275055555643	7.0799179666666756	7.0811096611111202	7.0823012027777867	7.0835123250000089	7.0847215694444534	7.0859140361111201	7.0871057305555647	7.0882918750000092	7.0894800250000092	7.0906681750000091	7.0918581750000094	7.093044783333343	7.0942347833333432	7.0954238583333433	7.0966072305555654	7.097773155555565	7.0989405972222315	7.1001072805555649	7.1012748750000094	7.1024458083333428	7.1036153750000093	7.1047840305555647	7.1059534472222312	7.1071260500000086	7.108298044444453	7.10944903611112	7.1105964444444529	7.1117454944444534	7.1128900638888979	7.1140346333333424	7.1151781555555642	7.1163427138888977	7.1174907194444534	7.1186575527777869	7.1198275750000093	7.1209776722222315	7.1221052500000095	7.1232331222222314	7.1243602583333425	7.1254837194444534	7.1266121805555649	7.1277406416666764	7.1288676305555656	7.1299955027777875	7.1311073527777875	7.1322194916666763	7.1333296055555655	7.1344440583333437	7.1355554750000101	7.1366681916666765	7.1377804750000102	7.1389087888888989	7.1400306333333434	7.141156888888899	7.1422639666666772	7.1433735027777887	7.1444860750000112	7.1456032777777887	7.1467178750000109	7.1478301583333446	7.148942875000011	7.1500551583333447	7.1511638250000118	7.1522769777777899	7.1533869472222342	7.1544812805555678	7.1555814472222341	7.1566791972222337	7.1577753805555666	7.1588718500000112	7.1599697416666777	7.1610640750000112	7.1621569861111221	7.1632511777777887	7.1643455111111223	7.1654378527777887	7.1665316194444557	7.1676051944444561	7.1686733138889007	7.1697428333333448	7.1708192083333451	7.1718943250000118	7.1729677611111233	7.1740409166666792	7.1751207888889015	7.1762034583333456	7.1772841694444569	7.1783676777777901	7.1794332361111231	7.1804975555555677	7.1815602250000126	7.1826245444444572	7.1836866638889019	7.1847472694444576	7.1858093888889023	7.1868724722222357	7.18793706666668	7.1889967111111241	7.1900530527777908	7.1910899666666799	7.1921289083333466	7.1931687972222358	7.1942119277777916	7.1952551944444583	7.196295352777792	7.1973356472222365	7.1983770222222363	7.1994185333333478	7.2004601777777921	7.2015019583333473	7.2025214777777915	7.2035447166666806	7.2045675555555695	7.2055905277777921	7.2066084527777923	7.2076238555555703	7.2086387277777924	7.2096532000000142	7.2106700638889034	7.2116910444444589	7.2127133527777918	7.2137155805555695	7.2147206777777919	7.215747636111125	7.2167737972222366	7.2177992944444584	7.2188267833333475	7.2198534750000141	7.2208753861111248	7.2218982277777917	7.2229210694444586	7.2239419194444583	7.224961705555569	7.2259615861111248	7.2269635527777911	7.2279679972222359	7.2289733555555689	7.2299770166666804	7.23097976666668	7.231981863888902	7.2329823944444573	7.2339783611111237	7.2349774583333462	7.2359615916666797	7.236947902777791	7.2379348527777907	7.2389218027777904	7.2399052944444566	7.2408872500000125	7.2418725361111234	7.2428582055555681	7.2438465638889014	7.2448374833333462	7.2458249444444576	7.2468093333333465	7.2477942361111243	7.2487814416666803	7.2497508694444583	7.2507161500000139	7.2516853250000137	7.2526529944444578	7.2536191555555689	7.2545844361111245	7.2555479555555689	7.2565134861111247	7.2574806527777911	7.2584450527777911	7.2594108361111243	7.2603593833333466	7.2613085472222352	7.2622551222222356	7.2632040388889019	7.2641535722222352	7.2651021194444576	7.2660514055555687	7.267000322222235	7.2679507194444568	7.2689022250000122	7.2698528694444562	7.270803266666678	7.2717552666666778	7.2726872666666775	7.2736173305555667	7.2745467916666779	7.2754787916666777	7.2764120000000112	7.2773440000000109	7.2782751527777885	7.2792078777777887	7.2801409666666776	7.2810752638888996	7.2820070222222331	7.2829376916666773	7.2838509416666772	7.2847639555555661	7.2856788638888998	7.2865923500000109	7.2875061916666777	7.2884202722222335	7.2893309138889002	7.2902401333333451	7.2911504194444561	7.2920607055555671	7.2929705166666778	7.2938620166666777	7.2947539805555666	7.2956483833333445	7.2965438333333443	7.2974380055555663	7.2983341527777883	7.2992322750000103	7.3001313277777884	7.3010275916666769	7.3019193222222327	7.302810705555566	7.3037039472222327	7.3045981194444547	7.3054725638888991	7.306347122222232	7.307220769444454	7.3080940750000094	7.3089687472222318	7.3098446694444537	7.31072116111112	7.3115962888888975	7.3124684555555639	7.3133433555555643	7.3142039277777862	7.3150631638888974	7.3159219527777859	7.3167789583333418	7.317633625000008	7.3184877333333418	7.3193434027777862	7.3201953944444531	7.3210497250000088	7.3219053944444532	7.3227603944444528	7.3236143916666752	7.3244703944444529	7.3253261750000087	7.3261825138888979	7.3270208500000091	7.3278588583333422	7.3286967583333418	7.3295379305555644	7.3303787750000087	7.3312186388888971	7.3320595944444529	7.3329019666666753	7.333742922222231	7.3345840944444536	7.3354259222222318	7.3362665500000093	7.3371035777777873	7.3379247555555649	7.3387439055555648	7.3395635888888977	7.3403846611111199	7.3412070138888978	7.3420274444444535	7.3428479833333427	7.3436698027777867	7.344491727777787	7.345312477777787	7.3461146777777868	7.3469192777777872	7.3477246083333432	7.3485272250000095	7.3493296333333431	7.3501337111111207	7.3509389361111204	7.3517465611111206	7.3525532472222315	7.3533603500000089	7.3541642194444536	7.3549681916666758	7.355771330555565	7.3565546861111208	7.3573362055555656	7.358118233333343	7.358901894444454	7.3596854527777875	7.3604534777777877	7.3612247888888991	7.3619948055555655	7.3627641250000098	7.3635300583333434	7.3642983833333435	7.3650659111111212	7.3658355305555654	7.3666038555555655	7.3673718805555657	7.368140602777788	7.3689092250000101	7.3696767527777878	7.3704432833333433	7.3711733138888986	7.3719066638888986	7.3726386861111211	7.3733713722222323	7.3741059555555655	7.374836461111121	7.3755662083333435	7.3762961444444546	7.3770263638888993	7.3777531694444551	7.3784783638888998	7.3792046000000111	7.3799304583333445	7.3806568861111224	7.3813845444444555	7.382096047222233	7.3828098611111219	7.3835210861111218	7.3842327750000107	7.3849462194444548	7.3856569833333436	7.3863681166666773	7.3870762888888999	7.3877857583333446	7.3884972611111221	7.3891939444444557	7.3898906277777892	7.3905851500000113	7.3912784083333447	7.3919536861111226	7.392627033333345	7.3932984500000121	7.3939728500000124	7.3946487416666793	7.3953234055555681	7.3959984194444566	7.396673433333345	7.3973471305555671	7.3980213555555672	7.3986954055555669	7.3993686666666783	7.4000415750000119	7.4007150972222338	7.4013915166666786	7.4020660916666783	7.4027418972222341	7.4034161222222341	7.4040912250000117	7.4047499611111229	7.405389069444456	7.4060280944444559	7.4066667055555673	7.4073043194444566	7.407942930555568	7.4085813750000122	7.4092178277777903	7.4098547777777899	7.4104917277777895	7.411127683333345	7.4117617305555674	7.412395030555567	7.4130307361111223	7.4136675222222337	7.4143054694444563	7.414943416666679	7.4155808666666791	7.4162175694444565	7.4168356777777902	7.4174562861111237	7.4180772972222346	7.4186972583333457	7.4193191555555682	7.4199408916666796	7.4205615805555682	7.4211808972222348	7.4217990055555685	7.4224171138889021	7.423035463888902	7.4236541361111241	7.4242728083333462	7.424890997222235	7.4255074916666794	7.4261248750000126	7.4267427416666791	7.4273610111111239	7.4279800055555683	7.4286006138889018	7.4292190444444577	7.4298188166666801	7.4304188222222356	7.4310207055555688	7.431622588888902	7.4322231444444578	7.4328211944444575	7.43342096666668	7.4340203472222353	7.4346201194444577	7.4352202833333463	7.4358198194444576	7.436419436111124	7.437023588888902	7.437627430555569	7.4382312722222359	7.4388332361111251	7.439436763888903	7.4400410750000141	7.4406451500000141	7.441248600000014	7.4418354333333472	7.4424222666666804	7.4430084916666805	7.4435925916666807	7.4441766916666809	7.4447592750000142	7.4453422388889035	7.4459223194444588	7.4465028555555701	7.4470850611111254	7.4476687083333477	7.448253341666681	7.4488390361111252	7.4494233638889034	7.4500078444444586	7.4505904277777919	7.4511716444444582	7.4517543027777915	7.4523353694444578	7.4529164361111242	7.4534800805555683	7.4540436500000125	7.4545896805555678	7.4551357111111232	7.4556826638889007	7.4562293333333454	7.4567755750000124	7.4573200388889012	7.4578672055555675	7.458432169444456	7.4589971333333445	7.4595632000000114	7.4601283861111227	7.4606929833333453	7.4612587555555674	7.461827836111123	7.4623965500000118	7.4629623972222339	7.4635303750000119	7.46409835277779	7.4646670666666788	7.4652355611111236	7.4658023638889013	7.4663697555555677	7.4669189861111231	7.4674682166666786	7.4680160250000123	10 LPM, 12kW	23.2	23.2	23.3	23.3	23.3	23.4	23.4	23.5	23.5	23.6	23.6	23.7	23.7	23.7	23.8	23.9	23.9	23.9	24	24	24.1	24.2	24.2	24.3	24.3	24.4	24.4	24.5	24.5	24.6	24.6	24.7	24.7	24.8	24.9	24.9	25	25.1	25.1	25.1	25.2	25.2	25.3	25.3	25.4	25.5	25.5	25.6	25.6	25.7	25.7	25.8	25.8	25.9	25.9	26	26.1	26.1	26.2	26.2	26.3	26.3	26.4	26.5	26.5	26.5	26.6	26.6	26.7	26.8	26.8	26.9	26.9	27	27.1	27.1	27.1	27.2	27.2	27.3	27.4	27.5	27.5	27.5	27.6	27.6	27.7	27.7	27.8	27.8	28	28	28	28.1	28.1	28.2	28.2	28.3	28.3	28.4	28.5	28.5	28.5	28.6	28.6	28.7	28.8	28.8	28.8	28.9	29	29	29.1	29.1	29.2	29.2	29.3	29.3	29.4	29.4	29.5	29.6	29.6	29.7	29.7	29.8	29.8	29.9	29.9	30	30	30.1	30.1	30.2	30.2	30.3	30.4	30.4	30.5	30.5	30.6	30.6	30.7	30.8	30.8	30.9	30.9	31	31	31.1	31.1	31.2	31.2	31.3	31.3	31.4	31.4	31.5	31.6	31.6	31.6	31.7	31.7	31.9	31.9	31.9	31.9	32	32	32.1	32.1	32.200000000000003	32.200000000000003	32.299999999999997	32.299999999999997	32.4	32.4	32.5	32.5	32.6	32.700000000000003	32.700000000000003	32.700000000000003	32.799999999999997	32.9	32.9	33	33	33.1	33.1	33.200000000000003	33.200000000000003	33.299999999999997	33.299999999999997	33.4	33.4	33.5	33.5	33.6	33.6	33.700000000000003	33.799999999999997	33.799999999999997	33.9	33.9	34	34	34.1	34.200000000000003	34.200000000000003	34.200000000000003	34.299999999999997	34.299999999999997	34.4	34.4	34.5	34.5	34.6	34.6	34.700000000000003	34.700000000000003	34.799999999999997	34.799999999999997	34.9	34.9	35	35	35.1	35.1	35.200000000000003	35.200000000000003	35.299999999999997	35.299999999999997	35.4	35.4	35.5	35.5	35.6	35.6	35.700000000000003	35.700000000000003	35.799999999999997	35.799999999999997	35.9	35.9	36	36	36.1	36.1	36.200000000000003	36.200000000000003	36.299999999999997	36.299999999999997	36.4	36.5	36.5	36.6	36.6	36.6	36.700000000000003	36.700000000000003	36.799999999999997	36.799999999999997	36.9	36.9	37	37	37.1	37.1	37.200000000000003	37.200000000000003	37.299999999999997	37.299999999999997	37.4	37.4	37.5	37.5	37.6	37.6	37.700000000000003	37.700000000000003	37.799999999999997	37.799999999999997	37.9	37.9	38	38	38.1	38.1	38.1	38.200000000000003	38.200000000000003	38.299999999999997	38.299999999999997	38.4	38.4	38.5	38.6	38.6	38.6	38.700000000000003	38.700000000000003	38.799999999999997	38.799999999999997	38.9	38.9	39	39	39.1	39.1	39.200000000000003	39.200000000000003	39.299999999999997	39.4	39.4	39.4	39.5	39.5	39.5	39.6	39.6	39.700000000000003	39.700000000000003	39.799999999999997	39.799999999999997	39.9	39.9	40	40.1	40.1	40.1	40.1	40.200000000000003	40.200000000000003	40.299999999999997	40.299999999999997	40.4	40.4	40.5	40.5	40.6	40.6	40.6	40.700000000000003	40.700000000000003	40.799999999999997	40.799999999999997	40.9	41	41	41	41.1	41.1	41.2	41.2	41.2	41.3	41.3	41.4	41.5	41.5	41.5	41.6	41.6	41.6	41.7	41.7	41.8	41.8	41.9	41.9	41.9	42	42	42.1	42.1	42.2	42.2	42.3	42.3	42.3	42.4	42.4	42.5	42.5	42.6	42.6	42.6	42.7	42.7	42.8	42.8	42.8	42.9	43	43	43	43.1	43.1	43.1	43.2	43.2	43.3	43.3	43.3	43.4	43.4	43.5	43.5	43.6	43.6	43.7	43.7	43.7	43.8	43.8	43.8	43.9	43.9	44	44	44	44.1	44.1	44.2	44.2	44.3	44.3	44.3	44.4	44.4	44.4	44.5	44.5	44.6	44.6	44.6	44.7	44.7	44.8	44.8	44.8	44.9	44.9	44.9	45	45	45.1	45.1	45.1	45.2	45.2	45.2	45.3	45.3	45.3	45.4	45.4	45.5	45.5	45.5	45.6	45.6	45.6	45.7	45.7	45.7	45.8	45.8	45.9	45.9	45.9	46	46	46	46.1	46.1	46.1	46.2	46.2	46.3	46.3	46.3	46.4	46.4	46.4	46.5	46.5	46.5	46.6	46.6	46.6	46.6	46.7	46.7	46.7	46.8	46.8	46.8	46.9	46.9	47	47	47	47.1	47.1	47.1	47.2	47.2	47.2	47.3	47.3	47.3	47.4	47.4	47.4	47.4	47.5	47.5	47.6	47.6	47.6	47.6	47.7	47.7	47.7	47.8	47.8	47.8	47.9	47.9	47.9	48	48	48	48.1	48.1	48.1	48.1	48.2	48.2	48.3	48.3	48.3	48.3	48.4	48.4	48.4	48.4	48.5	48.5	48.5	48.6	48.6	48.6	48.6	48.7	48.7	48.7	48.8	48.8	48.8	48.8	48.9	48.9	48.9	49	49	49	49.1	49.1	49.1	49.1	49.2	49.2	49.2	49.2	49.3	49.3	49.3	49.4	49.4	49.4	49.4	49.5	49.5	49.5	49.5	49.6	49.6	49.6	49.6	49.7	49.7	49.7	49.7	49.8	49.8	49.8	49.9	49.9	49.9	49.9	50	50	50	50	50.1	50.1	50.1	50.1	50.1	50.2	50.2	50.2	50.2	50.3	50.3	50.3	50.3	50.4	50.4	50.4	50.4	50.5	50.5	50.5	50.5	50.6	50.6	50.6	50.6	50.7	50.7	50.7	50.7	50.7	50.8	50.8	50.8	50.8	50.8	50.9	50.9	50.9	51	51	51	51	51	51.1	51.1	51.1	51.1	51.1	51.2	51.2	51.2	51.2	51.2	51.3	51.3	51.3	51.3	51.4	51.4	51.4	51.4	51.4	51.5	51.5	51.5	51.5	51.5	51.6	51.6	51.6	51.6	51.6	51.7	51.7	51.7	51.7	51.7	51.8	51.8	51.8	51.8	51.8	51.9	51.9	51.9	51.9	51.9	52	52	52	52	52	52.1	52.1	52.1	52.1	52.1	52.1	52.2	52.2	52.2	52.2	52.2	52.2	52.3	52.3	52.3	52.3	52.3	52.4	52.4	52.4	52.4	52.4	52.5	52.5	52.5	52.5	52.5	52.5	52.6	52.6	52.6	52.6	52.6	52.6	52.7	52.7	52.7	52.7	52.7	52.7	52.8	52.8	52.8	52.8	52.8	52.8	52.9	52.9	52.9	52.9	52.9	52.9	53	53	53	53	53	53	53	53.1	53.1	53.1	53.1	53.1	53.1	53.1	53.2	53.2	53.2	53.2	53.2	53.2	53.3	53.3	53.3	53.3	53.3	53.3	53.3	53.4	53.4	53.4	53.4	53.4	53.4	53.4	53.5	53.5	53.5	53.5	53.5	53.5	53.5	53.5	53.6	53.6	53.6	53.6	53.6	53.6	53.7	53.7	53.7	53.7	53.7	53.7	53.7	53.7	53.8	53.8	53.8	53.8	53.8	53.8	53.8	53.8	53.9	53.9	53.9	53.9	53.9	53.9	53.9	53.9	54	54	54	54	54	54	54	54	54.1	54.1	54.1	54.1	54.1	54.1	54.1	54.1	54.2	54.2	54.2	54.2	54.2	54.2	54.2	54.2	54.2	54.2	54.3	54.3	54.3	54.3	54.3	54.4	54.4	54.4	54.4	54.4	54.4	54.4	54.4	54.4	54.4	54.5	54.5	54.5	54.5	54.5	54.5	54.5	54.5	54.5	54.6	54.6	54.6	54.6	54.6	54.6	54.6	54.6	54.6	54.7	54.7	54.7	54.7	54.7	54.7	54.7	54.7	54.8	54.8	54.8	54.8	54.8	54.8	54.8	54.8	54.8	54.8	54.9	54.9	54.9	54.9	54.9	54.9	54.9	54.9	54.9	54.9	55	55	55	55	55	55	55	55	55	55.1	55.1	55.1	55.1	55.1	55.1	55.1	55.1	55.1	55.1	55.1	55.2	55.2	55.2	55.2	55.2	55.2	55.2	55.2	55.2	55.3	55.3	55.3	55.3	55.3	55.3	55.3	55.3	55.3	55.3	55.3	55.3	55.4	55.4	55.4	55.4	55.4	55.4	55.4	55.4	55.4	55.4	55.5	55.5	55.5	55.5	55.5	55.5	55.5	55.5	55.5	55.5	55.5	55.5	55.6	55.6	55.6	55.6	55.6	55.6	55.6	55.6	55.6	55.6	55.7	55.7	55.7	55.7	55.7	55.7	55.7	55.7	55.7	55.7	55.7	55.7	55.7	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.8	55.9	55.9	55.9	55.9	55.9	55.9	55.9	55.9	55.9	55.9	55.9	55.9	56	56	56	56	56	56	56	56	56	56	56	56	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.1	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.2	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.3	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.4	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.5	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.6	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.7	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.8	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	56.9	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.1	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.2	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.3	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.4	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.5	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.6	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.7	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.8	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	57.9	58	58	58	58	58	58	58	58	58	58	58	58	58	58	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.1	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.2	58.3	58.3	58.3	58.3	58.3	58.3	58.3	58.3	58.3	58.3	58.3	58.3	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.4	58.5	58.5	58.5	58.5	58.5	58.5	58.5	58.5	58.5	58.5	58.5	58.5	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.6	58.7	58.7	58.7	58.7	58.7	58.7	58.7	58.7	58.7	58.7	58.7	58.7	58.8	58.8	58.8	58.8	58.8	58.8	58.8	58.8	58.8	58.8	58.8	58.8	58.9	58.9	58.9	58.9	58.9	58.9	58.9	58.9	58.9	58.9	58.9	59	59	59	59	59	59	59	59	59	59	59.1	59.1	59.1	59.1	59.1	59.1	59.1	59.1	59.1	59.1	59.1	59.1	59.2	59.2	59.2	59.2	59.2	59.2	59.2	59.2	59.2	59.2	59.3	59.3	59.3	59.3	59.3	59.3	59.3	59.3	59.3	59.3	59.4	59.4	59.4	59.4	59.4	59.4	59.4	59.4	59.4	59.4	59.5	59.5	59.5	59.5	59.5	59.5	59.5	59.5	59.5	59.6	59.6	59.6	59.6	59.6	59.6	59.6	59.6	59.6	59.6	59.7	59.7	59.7	59.7	59.7	59.7	59.7	59.7	59.7	59.7	59.8	59.8	59.8	59.8	59.8	59.8	59.8	59.8	59.8	59.9	59.9	59.9	59.9	59.9	59.9	59.9	59.9	60	60	60	60	60	60	60	60	60	60.1	60.1	60.1	60.1	60.1	60.1	60.1	60.1	60.1	60.2	60.2	60.2	60.2	60.2	60.2	60.2	60.2	60.3	60.3	60.3	60.3	60.3	60.3	60.3	60.3	60.4	60.4	60.4	60.4	60.4	60.4	60.4	60.4	60.4	60.5	60.5	60.5	60.5	60.5	60.5	60.5	60.5	60.6	60.6	60.6	60.6	60.6	60.6	60.6	60.7	60.7	60.7	60.7	60.7	60.7	60.7	60.7	60.8	60.8	60.8	60.8	60.8	60.8	60.8	60.8	60.9	60.9	60.9	60.9	60.9	60.9	60.9	60.9	61	61	61	61	61	61	61	61.1	61.1	61.1	61.1	61.1	61.1	61.1	61.1	61.2	61.2	61.2	61.2	61.2	61.2	61.2	61.3	61.3	61.3	61.3	61.3	61.3	61.3	61.3	61.4	61.4	61.4	61.4	61.4	61.4	61.4	61.5	61.5	61.5	61.5	61.5	61.5	61.6	61.6	61.6	61.6	61.6	61.6	61.6	61.6	61.7	61.7	61.7	61.7	61.7	61.7	61.7	61.8	61.8	61.8	61.8	61.8	61.8	61.9	61.9	61.9	61.9	61.9	61.9	61.9	62	62	62	62	62	62.1	62.1	62.1	62.1	62.1	62.1	62.1	62.2	62.2	62.2	62.2	62.2	62.3	62.3	62.3	62.3	62.3	62.3	62.3	62.4	62.4	62.4	62.4	62.4	62.4	62.5	62.5	62.5	62.5	62.5	62.5	62.5	62.6	62.6	62.6	62.6	62.6	62.6	62.7	62.7	62.7	62.7	62.7	62.7	62.8	62.8	62.8	62.8	62.8	62.8	62.9	62.9	62.9	62.9	62.9	63	63	63	63	63	63	63.1	63.1	63.1	63.1	63.1	63.1	63.2	63.2	63.2	63.2	63.2	63.3	63.3	63.3	63.3	63.3	63.3	63.4	63.4	63.4	63.4	63.4	63.5	63.5	63.5	63.5	63.5	63.6	63.6	63.6	63.6	63.6	63.6	63.7	63.7	63.7	63.7	63.7	63.8	63.8	63.8	63.8	63.8	63.9	63.9	63.9	63.9	63.9	64	64	64	64	64	64	64.099999999999994	64.099999999999994	64.099999999999994	64.099999999999994	64.099999999999994	64.2	64.2	64.2	64.2	64.2	64.3	64.3	64.3	64.3	64.3	64.400000000000006	64.400000000000006	64.400000000000006	64.400000000000006	64.5	64.5	64.5	64.5	64.5	64.599999999999994	64.599999999999994	64.599999999999994	64.599999999999994	64.599999999999994	64.7	64.7	64.7	64.7	64.8	64.8	64.8	64.8	64.8	64.900000000000006	64.900000000000006	64.900000000000006	64.900000000000006	65	65	65	65	65	65.099999999999994	65.099999999999994	65.099999999999994	65.099999999999994	65.2	65.2	65.2	65.2	65.3	65.3	65.3	65.3	65.3	65.400000000000006	65.400000000000006	65.400000000000006	65.400000000000006	65.5	65.5	65.5	65.5	65.599999999999994	65.599999999999994	65.599999999999994	65.599999999999994	65.7	65.7	65.7	65.7	65.7	65.7	65.8	65.8	65.8	65.8	65.900000000000006	65.900000000000006	65.900000000000006	65.900000000000006	65.900000000000006	66	66	66	66	66	66.099999999999994	66.099999999999994	66.099999999999994	66.099999999999994	66.2	66.2	66.2	66.2	66.2	66.3	66.3	66.3	66.3	66.400000000000006	66.400000000000006	66.400000000000006	66.400000000000006	66.400000000000006	66.400000000000006	66.5	66.5	66.5	66.5	66.599999999999994	66.599999999999994	66.599999999999994	66.599999999999994	66.599999999999994	66.599999999999994	66.7	66.7	66.7	66.7	66.7	66.7	66.8	66.8	66.8	66.8	66.8	66.900000000000006	66.900000000000006	66.900000000000006	66.900000000000006	66.900000000000006	67	67	67	67	67	67.099999999999994	67.099999999999994	67.099999999999994	67.099999999999994	67.099999999999994	67.2	67.2	67.2	67.2	67.2	67.3	67.3	67.3	67.3	67.3	67.400000000000006	67.400000000000006	67.400000000000006	67.400000000000006	67.5	67.5	67.5	67.5	67.5	67.599999999999994	67.599999999999994	67.599999999999994	67.599999999999994	67.599999999999994	67.7	67.7	67.7	67.8	67.8	67.8	67.8	67.8	67.8	67.8	67.900000000000006	67.900000000000006	67.900000000000006	67.900000000000006	67.900000000000006	68	68	68	68.099999999999994	68.099999999999994	68.099999999999994	68.099999999999994	68.099999999999994	68.2	68.2	68.2	68.2	68.3	68.3	68.3	68.3	68.400000000000006	68.400000000000006	68.400000000000006	68.400000000000006	68.400000000000006	68.5	68.5	68.5	68.5	68.599999999999994	68.599999999999994	68.599999999999994	68.599999999999994	68.599999999999994	68.7	68.7	68.7	68.7	68.8	68.8	68.8	68.8	68.900000000000006	68.900000000000006	68.900000000000006	68.900000000000006	68.900000000000006	69	69	69	69	69.099999999999994	69.099999999999994	69.099999999999994	69.099999999999994	69.2	69.2	69.2	69.2	69.2	69.3	69.3	69.3	69.3	69.400000000000006	69.400000000000006	69.400000000000006	69.400000000000006	69.5	69.5	69.5	69.5	69.599999999999994	69.599999999999994	69.599999999999994	69.599999999999994	69.7	69.7	69.7	69.7	69.8	69.8	69.8	69.8	69.900000000000006	69.900000000000006	69.900000000000006	69.900000000000006	69.900000000000006	70	70	70	70.099999999999994	70.099999999999994	70.099999999999994	70.099999999999994	70.2	70.2	70.2	70.3	70.3	70.3	70.3	70.400000000000006	70.400000000000006	70.400000000000006	70.400000000000006	70.400000000000006	70.5	70.5	70.599999999999994	70.599999999999994	70.599999999999994	70.599999999999994	70.599999999999994	70.7	70.7	70.7	70.7	70.8	70.8	70.8	70.8	70.8	70.900000000000006	70.900000000000006	70.900000000000006	71	71	71	71	71.099999999999994	71.099999999999994	71.2	71.2	71.2	71.2	71.2	71.3	71.3	71.3	71.400000000000006	71.400000000000006	71.400000000000006	71.5	71.5	71.5	71.5	71.5	71.599999999999994	71.599999999999994	71.599999999999994	71.7	71.7	71.7	71.7	71.8	71.8	71.8	71.8	71.900000000000006	71.900000000000006	71.900000000000006	72	72	72	72	0.36	0.36257343333333331	0.36516604722222223	0.36777751944444442	0.3704464833333333	0.37315177222222223	0.37585706111111111	0.37857981944444441	0.38133339444444442	0.38410839444444445	0.38692597777777776	0.3897810333333333	0.3926360888888889	0.3954890611111111	0.39840308888888887	0.40132175555555555	0.40424042222222223	0.40717889444444444	0.41011881111111109	0.41307567222222219	0.41604908888888886	0.41902286666666666	0.42201608888888886	0.42500931111111112	0.42799850555555552	0.43098697777777778	0.43399595000000002	0.43700639444444445	0.44003736666666665	0.44306647777777775	0.44609856111111112	0.44913250555555556	0.45218439444444447	0.45523703333333332	0.45827578333333335	0.46133586666666671	0.4643757277777778	0.46743208888888887	0.47048995000000005	0.47354781111111111	0.47660267222222225	0.47965867222222225	0.48271392222222226	0.48577064444444451	0.4888255055555556	0.49185945000000003	0.49491431111111117	0.49795120000000004	0.5010057	0.50404333888888897	0.50709933888888892	0.51013586666666666	0.51319333888888896	0.51622728333333334	0.51926270000000008	0.5222981166666667	0.52533464444444444	0.52836597777777783	0.53137825555555551	0.53441181111111113	0.53742261666666669	0.54045394999999996	0.54346511666666664	0.54647775555555556	0.54949114444444447	0.55250561666666664	0.55552083888888881	0.55853606111111109	0.56154981111111102	0.56454483888888884	0.56755711666666664	0.57056572777777781	0.57357433888888887	0.57656133888888883	0.57952714444444442	0.58250867222222225	0.58548908888888884	0.58847756111111116	0.59146383888888887	0.59444864444444445	0.59741445000000004	0.60037950555555564	0.60334456111111123	0.6063268111111112	0.60928717222222228	0.61226650555555562	0.61522794999999997	0.61818867222222229	0.62115011666666664	0.6241170055555556	0.62706125555555559	0.63000550555555557	0.63296586666666665	0.63590361666666673	0.6388628666666667	0.64180422777777779	0.64476347777777776	0.64770411666666661	0.6506604777777778	0.65362336666666665	0.65656978333333327	0.65951619999999989	0.66248308888888885	0.66545069999999995	0.66842192222222219	0.67139533888888892	0.67434678333333331	0.67732056111111105	0.68029142222222216	0.68325903333333327	0.68623061666666652	0.68920219999999988	0.69215114444444437	0.69512347777777772	0.698077811111111	0.70105231111111099	0.70400592222222214	0.70697933888888875	0.70993222777777776	0.712904561111111	0.71587761666666661	0.718829061111111	0.72178050555555551	0.72472439444444436	0.72767044999999986	0.7306186722222221	0.73356256111111096	0.73651006111111106	0.73945719999999993	0.74240036666666653	0.74533811666666661	0.74827875555555545	0.7512179499999998	0.75416003333333315	0.75709994999999985	0.76003986666666656	0.76298411666666643	0.76593161666666654	0.76887731111111091	0.77182228333333314	0.77476906111111088	0.77771800555555537	0.78066189444444423	0.78358031111111093	0.78651878333333314	0.78944042222222199	0.79237817222222207	0.7953155611111109	0.7982522277777776	0.80116958888888878	0.80411131111111089	0.80703367222222211	0.80997358888888871	0.812906311111111	0.81583831111111094	0.81877389444444426	0.82171019999999984	0.82464686666666642	0.82756600555555537	0.8304887277777776	0.8334300888888887	0.83637000555555541	0.83931028333333313	0.84223517222222211	0.84516006111111097	0.84810106111111094	0.85104206111111091	0.85395619999999983	0.85689467222222215	0.85981633888888886	0.86275950555555547	0.86568294999999984	0.86861817222222215	0.8715312277777777	0.87446214444444437	0.87737592222222216	0.88030972777777772	0.8832270888888889	0.88616556111111111	0.8890814777777778	0.89199417222222221	0.89490614444444438	0.89783669999999993	0.90074761666666658	0.9036563666666666	0.90656692222222224	0.90947675555555552	0.9123887277777778	0.91529928333333332	0.91820983888888896	0.92112181111111113	0.92405703333333333	0.92697008888888888	0.92989703333333329	0.93280831111111107	0.93573994999999988	0.9386487	0.94157492222222217	0.94449156111111099	0.9474314777777777	0.9503456166666665	0.95328011666666645	0.95619353333333312	0.95911017222222195	0.96202931111111079	0.96494739444444411	0.96788261666666631	0.97079925555555513	0.97371017222222178	0.97662108888888854	0.97955381111111073	0.98246758888888852	0.98540317222222185	0.98831908888888842	0.9912364499999996	0.99414986666666627	0.99706078333333292	0.99996489444444403	1.0028936444444441	1.0058176999999997	1.0087417555555551	1.0116401444444443	1.0145656444444442	1.0174697555555552	1.020393811111111	1.0232968388888888	1.0262180055555552	1.0291416999999998	1.0320671999999997	1.0349894499999999	1.0379117	1.040828561111111	1.0437497277777776	1.0466701722222223	1.0495916999999999	1.0525193666666666	1.0554484777777779	1.0583804777777779	1.0613099500000001	1.0642365333333332	1.0671598666666666	1.070083922222222	1.0730235888888888	1.0759476444444445	1.0788789222222221	1.0818109222222221	1.084736061111111	1.087652922222222	1.0905864222222221	1.0935148388888889	1.0964432555555554	1.0993575888888887	1.1022976166666667	1.1052238388888886	1.1081547555555553	1.1110816999999997	1.1140050333333331	1.1169290888888888	1.1198756444444442	1.1228051166666666	1.1257513111111108	1.1286717555555554	1.1316107	1.1345304222222219	1.1374751722222221	1.1404181166666665	1.1433610611111109	1.1462908944444441	1.1492450888888885	1.1521738388888885	1.1551145888888885	1.1580343111111109	1.1609714499999997	1.1638854222222219	1.1668149222222219	1.1697484222222219	1.172682644444444	1.1756175888888887	1.1785550888888885	1.1814741166666662	1.1844163388888884	1.187358172222222	1.1902989222222218	1.1932393111111106	1.1961804222222217	1.1991131999999995	1.2020499777777773	1.2049881999999996	1.2079304222222218	1.2108918666666662	1.2138286444444439	1.2167860611111108	1.2197304499999997	1.2226864222222218	1.2256217277777774	1.2285776999999998	1.2315133666666664	1.234449783333333	1.2373847277777776	1.2403388666666664	1.2432658388888886	1.2462166999999997	1.2491788666666663	1.2521410333333329	1.2550806999999997	1.2580399499999997	1.2609796166666662	1.2639410611111108	1.2668854499999997	1.2698479777777774	1.2727905611111108	1.2757486999999998	1.2787064777777775	1.2816461444444442	1.284585811111111	1.2875472555555554	1.2904876444444442	1.2934436166666665	1.2963966444444444	1.2993496722222222	1.3023136722222222	1.3052761999999998	1.308230338888889	1.3111811999999998	1.3141346166666668	1.3170920333333331	1.320050172222222	1.3230061444444443	1.3259653944444443	1.3289246444444442	1.3318879222222222	1.3348733666666668	1.3378501444444444	1.3408240055555556	1.3437938388888888	1.3467737833333333	1.3497264499999999	1.3526835055555555	1.3556449500000001	1.3585961722222222	1.3615477555555557	1.3645077277777777	1.3674758944444445	1.3704234500000001	1.3733886722222222	1.3763362277777778	1.3792974222222223	1.3822482833333334	1.3852002277777777	1.3881735333333332	1.3911468388888886	1.3941060888888885	1.3970664222222222	1.4000386444444444	1.4029931444444443	1.4059650055555553	1.4089147555555552	1.4118876999999999	1.4148370888888886	1.4177897555555554	1.4207424222222222	1.423713172222222	1.4266683944444445	1.4296457555555553	1.4326257	1.4355820333333331	1.4385619777777778	1.4415375055555555	1.4445174499999998	1.4474803388888891	1.4504643111111108	1.4534482833333331	1.4564285888888886	1.4594030055555556	1.4623744777777774	1.4653452277777776	1.4683203944444441	1.4712970333333333	1.4742692555555554	1.4772484499999998	1.4802446444444444	1.4832216444444444	1.4861964222222221	1.4891734222222222	1.4921478388888887	1.4951270333333331	1.4981069777777773	1.5011094777777778	1.5040912555555552	1.5070878388888889	1.5100677833333331	1.5130602833333331	1.5160572277777775	1.519062311111111	1.5220655333333331	1.5250687555555551	1.5280693944444441	1.5310438111111111	1.5340307555555555	1.5370213944444444	1.5400150055555555	1.5430049222222224	1.5460040888888886	1.5490102000000001	1.5520163111111112	1.5550099222222222	1.5580087000000002	1.5609986166666667	1.5639822277777777	1.5669632555555557	1.5699465055555559	1.5729338388888889	1.5759196722222222	1.5789220611111112	1.5819145611111112	1.5849288388888891	1.5879431166666667	1.5909363666666669	1.593940616666667	1.5969312555555559	1.5999503944444449	1.6029680333333336	1.6059782277777783	1.608981727777778	1.6119904222222226	1.6149957833333337	1.617998533333334	1.6209938388888894	1.6239910055555558	1.6269751444444447	1.6299592833333336	1.6329583111111114	1.6359424500000004	1.6389515888888897	1.6419390611111115	1.6449500611111119	1.6479637000000009	1.6509709500000009	1.6539617277777787	1.6569358111111119	1.6599265888888897	1.6629203666666679	1.6659235055555568	1.6689266444444457	1.6719264222222234	1.6749269500000015	1.6779434500000017	1.6809499777777792	1.6839743944444461	1.6870025888888902	1.6900132277777793	1.6930482000000016	1.6960831722222238	1.699122283333335	1.7021546166666686	1.7051880888888906	1.7082192833333352	1.7112535055555576	1.7142801722222241	1.7173030888888907	1.7203503111111127	1.7233837833333352	1.7264385888888909	1.7294933944444462	1.7325260888888909	1.7355793944444464	1.7386250888888908	1.7416654777777794	1.7447051166666685	1.7477428666666683	1.7507874500000016	1.7538571444444462	1.7569093111111127	1.7599641166666684	1.7630407000000017	1.7660894500000017	1.7691610611111126	1.7722322833333353	1.7753031444444463	1.7783804777777794	1.7814292277777795	1.7845012277777794	1.7875724500000016	1.7906448388888903	1.7937275333333349	1.7968014500000016	1.7998780333333348	1.802944311111113	1.8060257833333351	1.8090867000000017	1.8121460888888903	1.8152054777777793	1.8182915611111126	1.8213543944444459	1.8244370333333348	1.8275135055555571	1.8305838388888906	1.8336637833333351	1.8367494777777797	1.8398424777777795	1.8429385611111129	1.8460330888888907	1.8491253111111128	1.8522133111111128	1.855306311111113	1.8583993111111128	1.8614911722222236	1.8645799500000018	1.8676951444444461	1.8708103388888908	1.8739087277777795	1.8770101722222243	1.8801292277777799	1.8832283666666685	1.8863190611111134	1.8894253666666687	1.8925281722222245	1.8956371722222243	1.8987481166666691	1.9018509222222248	1.9049475611111135	1.9080442000000022	1.9111435333333358	1.9142571722222246	1.9173665611111135	1.9204732555555579	1.9235745333333356	1.9266762000000024	1.9297980611111134	1.9328989500000024	1.9360091166666691	1.9391410888888911	1.9422620611111134	1.9453760888888914	1.9485154500000026	1.9516341166666691	1.9547462000000024	1.9578773944444468	1.9610152000000021	1.9641354222222245	1.9672743944444466	1.9703764500000021	1.9735014222222245	1.9766263944444464	1.9797575888888908	1.9828646444444464	1.9859833944444465	1.9891095333333353	1.9922337277777795	1.9953513111111127	1.9984782277777797	2.0016121444444464	2.0047468388888907	2.0078885333333352	2.0110466444444461	2.0142047555555576	2.0173378944444464	2.0204897277777798	2.023647061111113	2.0267860333333352	2.0299398388888905	2.0330916722222239	2.0362532833333349	2.0394223388888904	2.0425984500000016	2.0457686722222239	2.0489322555555574	2.0520907555555574	2.0552512000000016	2.0584140055555573	2.0615772000000017	2.064747422222224	2.0679293944444459	2.0710867277777791	2.0742475611111124	2.0774212555555569	2.0806020333333346	2.0837655055555571	2.0869289777777791	2.090094005555557	2.0932458388888904	2.0964152000000014	2.0995818111111126	2.1027303111111126	2.1058945611111128	2.1090544777777791	2.1122222833333346	2.1154099500000014	2.1185678944444457	2.1217246722222236	2.1248814500000015	2.128064755555557	2.1312309777777791	2.1344058666666683	2.1375895888888907	2.1407907277777793	2.1439848944444462	2.1471927555555572	2.1504053666666683	2.1535928388888905	2.1567876444444463	2.1599800611111126	2.1631724777777794	2.1663585611111129	2.1695410888888906	2.1727196444444461	2.1759232277777794	2.1791140611111128	2.1823279777777791	2.1855418944444458	2.1887566166666681	2.1919713388888904	2.1951590055555572	2.1983669500000018	2.201584061111113	2.2048011722222243	2.2080167000000017	2.2112298388888907	2.2144382000000018	2.2176473388888907	2.2208457277777796	2.2240488944444459	2.2272592277777794	2.2304894777777795	2.2336926444444458	2.2369000611111125	2.2401074777777792	2.2433180888888904	2.2465120888888905	2.2497363388888907	2.2529657833333352	2.2561848111111127	2.2594118666666683	2.2626381166666683	2.2658675611111128	2.2691193388888906	2.2723711166666685	2.2756097833333349	2.2788508666666685	2.282099422222224	2.2853423388888907	2.2885707555555572	2.2917873944444462	2.2950234500000017	2.2982627277777796	2.3014869777777793	2.3047112277777795	2.3079638111111129	2.3112123666666684	2.3144484222222239	2.3176897277777795	2.3209338666666683	2.3241888666666686	2.3274426722222241	2.3307188666666683	2.3339613944444464	2.3372010888888908	2.3404748388888907	2.3437408944444464	2.3470069500000021	2.350251088888891	2.3534960333333355	2.3567665333333352	2.360038672222224	2.363292061111113	2.3665654222222239	2.3698379500000017	2.3730910333333353	2.3763441166666688	2.3796044777777801	2.3828786444444465	2.3861536166666686	2.3894285888888911	2.3927043666666687	2.3959817833333354	2.3992672833333355	2.4025568388888914	2.4058591166666692	2.4091597555555579	2.412451755555558	2.4157392833333358	2.4190362555555582	2.4223438388888914	2.4256497833333355	2.4289328666666687	2.4322229222222247	2.4355186722222246	2.4388270611111138	2.4421338388888914	2.4454279500000027	2.4487220611111136	2.4520112833333361	2.4552988666666691	2.4586158388888912	2.4619140333333358	2.4652105888888913	2.468502255555558	2.4718159500000021	2.4751243111111134	2.4784123111111134	2.4817003111111133	2.4850242555555577	2.4883412277777799	2.4916487555555578	2.4949509500000024	2.4982458944444468	2.5015542555555577	2.5048638388888911	2.5081758944444466	2.5115025333333354	2.5148254777777801	2.5181346444444466	2.5214637555555575	2.5247928666666688	2.5281166166666691	2.5314263388888909	2.5347260611111131	2.5380356444444465	2.5413730333333358	2.544700505555558	2.5480271444444469	2.5513546166666692	2.5546820888888915	2.5580235888888914	2.5613655055555582	2.564697116666669	2.5680258388888912	2.571354144444447	2.5746845055555583	2.5780177555555581	2.5813576166666694	2.584707533333336	2.5880674222222249	2.5914089222222247	2.594743422222225	2.5980857555555583	2.6014427277777807	2.6047984500000028	2.6081749222222252	2.6115193111111141	2.6148762833333361	2.6182241166666698	2.6215673944444471	2.6249227000000026	2.6282734500000027	2.6316258666666696	2.6349782833333362	2.6383427277777804	2.6417071722222247	2.6450929222222248	2.6484870333333359	2.6518564500000026	2.6552258666666693	2.6585849222222246	2.6619593944444473	2.6653297000000022	2.6686979222222247	2.6720552833333353	2.6753948388888911	2.6787618111111131	2.6821321166666685	2.6855091166666685	2.6888848666666685	2.6922593388888911	2.695645450000002	2.698989894444447	2.7023280611111136	2.7056829222222247	2.7090413111111138	2.7123997000000029	2.7157602000000027	2.7191180055555586	2.7224737000000028	2.7258377555555584	2.7292108388888914	2.7325826722222248	2.735939811111114	2.7393099777777805	2.7426556722222251	2.7460097000000032	2.749371450000003	2.752724811111114	2.7560811166666701	2.7594567277777813	2.7628632277777809	2.7662409500000034	2.7696186722222254	2.7730014222222255	2.7763762000000032	2.7797509777777809	2.7831324777777806	2.7865372833333359	2.7899403944444474	2.793322727777781	2.7967109222222253	2.8001079500000032	2.8035190888888923	2.8069133388888923	2.8103075888888926	2.8137065055555595	2.8170888388888926	2.8204736722222261	2.8238835611111153	2.8272879500000045	2.830681783333338	2.8340823666666708	2.837478727777782	2.8408877555555594	2.844299311111115	2.8477108666666706	2.8511266444444487	2.8545339777777818	2.8579582000000041	2.8613982833333376	2.8648332555555598	2.8682460888888932	2.8716416166666714	2.875043894444449	2.8784478666666713	2.8818790333333379	2.8853063666666716	2.888732422222227	2.8921695333333384	2.895575200000005	2.8989804222222268	2.9024103111111157	2.9058575888888933	2.9093018944444489	2.9127368666666711	2.9161680333333377	2.9195932555555602	2.9230295055555602	2.9264657555555607	2.9299003111111159	2.9333310333333382	2.936750311111116	2.9401662000000051	2.9435897277777827	2.9470408944444491	2.9504644222222267	2.9538883666666713	2.9573072000000047	2.9607260333333381	2.9641576166666712	2.9676036722222272	2.9710416166666715	2.974476144444449	2.9779136722222264	2.9813533388888929	2.9847802555555596	2.9882050333333376	2.991620061111115	2.9950482000000038	2.9984784777777818	3.0018935055555596	3.0053085333333369	3.0087320611111146	3.0121466722222259	3.0155680611111144	3.0190158388888921	3.0224717000000032	3.0259194777777814	3.0293680888888925	3.0328269500000036	3.0362674500000035	3.0397041166666701	3.0431200055555592	3.0465358944444483	3.0499742555555596	3.0534254222222259	3.0568919777777817	3.0603533944444488	3.0638088388888929	3.0672510333333376	3.070692366666671	3.0741434777777825	3.0776223944444494	3.0810919222222268	3.0845584777777826	3.0879968388888934	3.0914352000000047	3.0948825333333381	3.0983145333333382	3.1017495055555608	3.1051827833333383	3.1086386444444494	3.1120842833333384	3.1155346166666722	3.1189819500000056	3.1224207555555608	3.1258421444444497	3.1292635333333383	3.1326963944444493	3.1361450055555609	3.1396000333333385	3.1430435333333384	3.1464964222222269	3.1499484500000046	3.1533872555555602	3.1568230611111154	3.1602640055555598	3.1637079222222266	3.1671518388888931	3.1705983111111156	3.1740294222222269	3.1774677833333382	3.1809147000000051	3.1843560611111159	3.1878021166666715	3.1912728944444497	3.1947262000000052	3.1981846444444493	3.2016396722222269	3.2051070611111157	3.2085565333333381	3.2120081444444493	3.2154597555555609	3.2189240888888944	3.2223897277777835	3.2258302277777835	3.2292745888888943	3.2327121166666721	3.236150477777783	3.2395786166666718	3.2430169777777831	3.2464641444444498	3.2499190333333381	3.2533739222222269	3.2568313944444496	3.2603038944444496	3.2637593388888937	3.2672169222222269	3.2706732277777828	3.2741337833333382	3.2776071444444494	3.2810852277777829	3.284559450000005	3.2880336722222272	3.2915203388888936	3.2949843111111163	3.2984482833333386	3.3019024500000054	3.3053425333333384	3.3088068666666719	3.3122759222222276	3.3157325333333385	3.3192007277777833	3.3226843944444497	3.3261744777777831	3.3296624222222277	3.333150366666672	3.3366340333333384	3.3401116722222275	3.3436039222222274	3.3470820055555608	3.3505626444444498	3.3540463111111163	3.3575265333333384	3.3609960333333384	3.3644565055555611	3.367936977777783	3.3714082000000052	3.374884977777783	3.3783600611111164	3.381839866666672	3.385314950000005	3.3887865888888942	3.3922449222222277	3.3957092555555612	3.3992035333333392	3.4026874500000059	3.4061726722222283	3.4096548666666728	3.4131295055555619	3.4166105888888954	3.4200998388888952	3.4235890888888947	3.4270731722222281	3.4305443944444503	3.4340304777777839	3.4375165611111171	3.4410008944444508	3.4444778944444505	3.4479491166666727	3.4514203388888953	3.4548821166666732	3.4583567555555619	3.4618298944444508	3.4653068944444509	3.4687852000000063	3.4722518388888957	3.4757249777777846	3.4792050055555621	3.4826850333333397	3.4861676444444507	3.4896524222222287	3.4931193388888953	3.4966019500000063	3.500098366666673	3.5035947833333401	3.5070769777777846	3.5105617555555626	3.5140413666666732	3.5175200888888956	3.5209988111111179	3.5244988388888956	3.5279971166666737	3.5315001722222292	3.5350022000000068	3.5384986166666739	3.5419950333333405	3.5454841166666742	3.5489831444444517	3.5524687833333406	3.5559634777777855	3.5594663944444522	3.5629723111111189	3.5665005333333415	3.5700244222222302	3.5735426722222301	3.5770464500000081	3.5805502277777861	3.5840540055555641	3.5875530333333416	3.5910429777777861	3.594526450000008	3.5979995611111186	3.6014735611111188	3.6049557555555634	3.6084306166666749	3.6119219500000077	3.6154115611111188	3.6188790888888964	3.6223582555555627	3.6258374222222294	3.6293183111111182	3.6328009222222293	3.6362714500000068	3.6397502000000066	3.6432237555555624	3.6466830611111178	3.6501670333333398	3.6536510055555618	3.6571323666666729	3.6606176444444509	3.6641137555555616	3.6676067277777835	3.6710997000000058	3.6745961166666725	3.6780895333333392	3.6815738666666729	3.6850517277777839	3.6885465333333398	3.6920539222222284	3.6955604500000061	3.6990825888888952	3.7026147277777843	3.7061468666666735	3.7096777000000065	3.7132093944444509	3.7167131722222284	3.7202065888888955	3.7236991444444514	3.7271917000000068	3.7307017000000071	3.7342168944444514	3.7377282000000069	3.7412290888888955	3.7447295333333401	3.7482356166666735	3.7517369500000064	3.7552382833333398	3.7587543666666727	3.7622838944444505	3.7657773111111177	3.7692616444444509	3.7727551444444511	3.7762577555555623	3.7797807833333397	3.7833063944444509	3.7868389500000061	3.7903628388888948	3.7939006166666731	3.7974392555555618	3.8009457833333395	3.8044549222222286	3.8079849777777839	3.8115002000000064	3.815003255555562	3.8185137000000067	3.8220267277777844	3.8255254500000064	3.8290372000000064	3.8325489500000063	3.8360680611111171	3.8395837000000062	3.8430928388888952	3.8465998111111173	3.8501020055555619	3.8536137277777844	3.857135477777784	3.8606655333333397	3.8641729222222283	3.8676790055555617	3.8711863944444502	3.8747142000000059	3.8782441722222281	3.8817723944444502	3.8852915055555615	3.8888080055555614	3.8923075888888947	3.8958385055555618	3.8993751166666728	3.902916950000006	3.9064535611111166	3.9099713666666722	3.9134891722222278	3.9170082833333391	3.9205373666666721	3.9240534500000055	3.9275612833333389	3.9310691166666718	3.934566977777783	3.9380896166666721	3.9416083111111164	3.9451322555555608	3.9486562000000052	3.9521884222222274	3.9557110611111166	3.9592071722222277	3.9627080611111163	3.9662037277777831	3.9696972277777829	3.9731877000000049	3.9766751444444495	3.9801690888888936	3.9836678111111161	3.9871948111111162	3.9907379500000055	3.9942872000000054	3.9978364500000052	4.0013996722222283	4.0049611444444499	4.0084916444444501	4.011999477777783	4.015504283333339	4.0189956166666718	4.0225025888888934	4.0260156166666716	4.0295269222222272	4.0330347555555601	4.0365425888888931	4.0400673944444492	4.0435861166666713	4.0471048388888935	4.0506318388888936	4.0541562277777823	4.0576819222222262	4.0611819500000044	4.0646828388888929	4.0681889222222267	4.0717054222222266	4.0752288666666709	4.0787523111111152	4.0822718666666713	4.0857927277777826	4.0892962277777825	4.0927988388888936	4.0963201166666714	4.0998593388888942	4.1033889500000047	4.10691725555556	4.1104564777777828	4.1139795055555606	4.1175025333333384	4.1210264222222266	4.1245368666666717	4.1280429500000047	4.1315490333333384	4.1350364777777822	4.1385295611111159	4.1420091722222265	4.1454987833333377	4.1489918666666714	4.1524996722222269	4.1560074777777825	4.1595187555555597	4.1630544777777825	4.1665818388888933	4.1701170055555599	4.1736356722222272	4.1771543388888936	4.1806617277777827	4.1841660888888939	4.1876739222222268	4.191176533333338	4.1946926166666705	4.1982156444444483	4.20172825555556	4.2052334777777816	4.2087356722222262	4.2122587555555597	4.2157696166666714	4.2192952277777822	4.2228186722222265	4.2263542833333378	4.2298898944444483	4.2334207277777818	4.2369446166666709	4.2404763111111148	4.2440114777777813	4.2475427277777813	4.2510774500000039	4.2546004777777817	4.2581392555555597	4.2616588388888923	4.2651784222222258	4.268704977777781	4.2722253944444484	4.2757445055555596	4.2792688111111152	4.2827918388888921	4.2863274500000035	4.2898491722222261	4.2933695888888925	4.2968808944444481	4.3003865611111145	4.3039108666666701	4.3074505055555594	4.3109818666666708	4.314496644444449	4.3180136166666703	4.3215305888888924	4.3250258388888927	4.3285336722222256	4.3320501722222255	4.3355714500000042	4.339092727777782	4.3426101166666706	4.3461092555555592	4.3496201166666708	4.3531305611111151	4.3566388388888928	4.3601592555555602	4.363698477777783	4.3672582000000046	4.3708122555555606	4.3743274500000044	4.377847422222227	4.3813665333333374	4.3848856444444486	4.3884203666666712	4.391956838888893	4.3954876722222265	4.3990046166666703	4.4025189500000037	4.4060224500000036	4.4095359222222257	4.4130524222222256	4.4165698111111151	4.4200728666666702	4.4235754777777814	4.4270780888888925	4.430592422222225	4.4341080611111146	4.4376193666666701	4.4411423944444479	4.4446610611111144	4.4481697555555586	4.4516706444444472	4.4551706722222253	4.4586763388888917	4.4621820055555581	4.465695922222225	4.4692241444444472	4.4727515055555589	4.4762845055555589	4.4798131722222259	4.4833353111111149	4.4868413944444479	4.4903505333333369	4.4938548944444481	4.4973566444444479	4.5008583944444478	4.504367088888892	4.5078914222222251	4.5114105333333363	4.5149331166666693	4.5184465888888914	4.5219482000000024	4.5254586444444467	4.5289738388888914	4.5324951166666692	4.5360194222222248	4.5395337555555582	4.5430528666666685	4.5465711166666685	4.5500885055555571	4.5536050055555579	4.5571249777777796	4.5606380055555569	4.5641354222222237	4.5676215055555573	4.5711367000000021	4.5746679777777794	4.5781862277777794	4.5817027277777793	4.5852075333333353	4.5887123388888904	4.5922362277777795	4.5957601166666686	4.5993026722222234	4.6028434777777791	4.6063799500000009	4.6099151166666683	4.613432505555557	4.6169392833333349	4.6204640333333344	4.6239909500000014	4.6275265611111127	4.6310573944444453	4.6345882277777788	4.6381090888888901	4.6416078111111121	4.6451277833333346	4.6486412555555567	4.6521577555555567	4.6556651444444448	4.659178172222223	4.6626851444444446	4.6661921166666671	4.6696969222222222	4.673204755555556	4.6767082555555559	4.6802082833333332	4.6837187277777774	4.6872213388888886	4.6907326444444442	4.6942500333333328	4.6977674222222223	4.701287394444444	4.7047969499999995	4.7083004499999994	4.7118095888888885	4.7153187277777775	4.7188339222222222	4.7223552	4.7258652000000003	4.729361311111111	4.7328574222222217	4.736363088888889	4.7398665888888889	4.743371394444444	4.7468714222222221	4.7503682833333327	4.7538834777777774	4.7573951999999995	4.7609121444444442	4.7644399222222225	4.7679672833333333	4.7714907277777776	4.7750163388888884	4.7785376166666671	4.7820519499999996	4.78557845	4.7891023388888891	4.792591005555555	4.7960796722222216	4.7995601444444436	4.8030636444444443	4.8065710333333325	4.8100814777777776	4.8135966722222214	4.8171157833333327	4.8206318666666661	4.8241301444444433	4.8276323388888889	4.8311380055555553	4.8346193388888885	4.8381118944444443	4.8416197277777773	4.8451275611111102	4.8486301722222214	4.8521549222222218	4.8556796722222213	4.8591922833333321	4.8626961999999994	4.8662040333333323	4.8697140333333326	4.8732275055555547	4.8767321444444436	4.8802436722222211	4.8837551999999986	4.8872619777777766	4.890759283333332	4.8942492277777765	4.8977696444444438	4.9012822555555546	4.9047974499999984	4.9083221999999989	4.9118213388888874	4.9153204777777768	4.9188160333333322	4.9223055611111102	4.9258054499999995	4.929299727777777	4.9327883944444437	4.9362662555555543	4.9397762555555538	4.9432836444444428	4.9467971166666649	4.9503244777777757	4.9538518388888866	4.9573757277777757	4.9608682833333306	4.9643470055555525	4.9678352277777753	4.9713234499999972	4.9748254777777747	4.9783171722222193	4.9817997833333312	4.9853145611111085	4.9888293388888867	4.9923319499999979	4.9958206722222203	4.9993076166666643	5.0027941166666645	5.0062806166666647	5.009764088888887	5.0132635333333315	5.0167694499999982	5.0202883111111092	5.0238058944444424	5.0273061999999982	5.0307996166666644	5.0342776999999987	5.0377557833333322	5.0412274222222209	5.0447061722222211	5.0481970055555534	5.0516925611111088	5.0551881166666641	5.0586871444444421	5.0621947833333305	5.0656873388888854	5.0691859222222195	5.0726771722222193	5.0761757555555524	5.0796605333333309	5.0831345333333307	5.0866085333333295	5.0900958944444401	5.0935832555555516	5.0970801166666622	5.1005838944444406	5.1040950055555516	5.1076229499999961	5.1111340888888845	5.1146641722222173	5.1181951166666622	5.1216980333333284	5.1251905888888833	5.1286831444444392	5.1321851722222167	5.1356764222222173	5.1391668111111057	5.1426589222222168	5.1461494499999949	5.1496283944444396	5.1531094777777735	5.1565978666666616	5.1600913944444402	5.163603783333329	5.1671191999999957	5.1706294499999963	5.174137949999996	5.1776477555555518	5.181133116666663	5.1846107555555516	5.1880866999999959	5.1915557555555516	5.1950252555555512	5.1985003388888851	5.2019792833333298	5.2054590888888859	5.2089410333333301	5.2124255611111083	5.215903199999997	5.2193825611111073	5.2228666444444416	5.226340005555552	5.2298176444444406	5.233293588888885	5.2367703666666623	5.2402641999999959	5.2437580333333287	5.2472408388888852	5.2507184777777729	5.2541832555555512	5.2576493111111064	5.2611025055555514	5.2645573944444397	5.2680320333333288	5.2715178388888848	5.2750139499999955	5.2785241999999961	5.2820160055555521	5.2855121166666628	5.2890082277777735	5.2924867277777734	5.2959605055555521	5.2994270055555521	5.3028767555555518	5.306326088888885	5.3097805611111069	5.3132406999999962	5.3166957277777733	5.3201460611111067	5.3235963944444409	5.3270448666666628	5.3304933388888847	5.3339512555555508	5.337408422222218	5.3408617277777735	5.3443099222222177	5.3477619499999953	5.3512156999999947	5.3546783944444396	5.3581381166666624	5.3615850333333279	5.3650390611111058	5.3685003944444398	5.3719464499999949	5.3753967833333283	5.3788505333333285	5.3823076999999957	5.3857558944444399	5.3892045055555506	5.3926458666666628	5.3960872277777741	5.3995324222222179	5.4029874499999959	5.4064335055555519	5.409891949999996	5.4133529499999957	5.4168135055555515	5.4202633944444401	5.4237141444444399	5.4271683111111066	5.4306088111111075	5.4340484499999953	5.4374953111111068	5.4409481166666627	5.4444214777777731	5.4478944222222179	5.4513626722222179	5.4548223944444407	5.4582730888888848	5.4617152833333291	5.4651472833333301	5.4685792833333302	5.4720176444444419	5.4754722277777752	5.4789379222222196	5.4824023388888863	5.485888505555554	5.4893417277777754	5.4927724499999986	5.4961968111111101	5.4996173666666648	5.5030672555555542	5.5065154499999984	5.5099743111111099	5.5134250611111097	5.5168481444444435	5.5202708111111098	5.5237023944444426	5.5271407555555543	5.5305770055555543	5.5340175055555543	5.5374482277777775	5.5408900055555552	5.544331783333333	5.547783311111111	5.5512208388888888	5.5546422277777774	5.5580742277777784	5.5615019777777777	5.5649225333333332	5.5683265055555555	5.5717300611111105	5.5751268666666665	5.5785376444444443	5.5819543666666673	5.5853833944444444	5.5888247277777783	5.59226308888889	5.5956717000000005	5.5990798944444453	5.6024880888888893	5.6059131722222224	5.6093335888888891	5.6127643111111123	5.6162009777777788	5.6196427555555566	5.6230724777777787	5.6265051444444456	5.6299247277777784	5.6333248944444456	5.6367348388888896	5.6401553944444451	5.6435755055555559	5.6469845333333337	5.6503969500000002	5.6538063944444454	5.6572158388888898	5.6606252833333341	5.6640410611111127	5.6674568388888904	5.6708734777777794	5.6742833666666685	5.6776987277777806	5.6811162000000017	5.6845269222222248	5.6879376444444469	5.691339088888892	5.6947396722222257	5.6981318111111143	5.7015311444444476	5.704930477777781	5.7083390888888923	5.7117464222222258	5.715161783333337	5.7185805333333368	5.7219912555555599	5.7253727555555596	5.7287521444444485	5.7321675055555597	5.7355828666666717	5.7389893666666714	5.7423929222222263	5.7457973111111151	5.749177533333337	5.7525665611111148	5.7559409222222264	5.7593056166666701	5.7627024222222261	5.76611061666667	5.7694963111111148	5.7728820055555596	5.7762643388888932	5.7796634500000037	5.7830646722222259	5.786465894444448	5.7898821166666696	5.7933063388888923	5.796722255555558	5.8001348111111133	5.803535172222225	5.8069242277777802	5.8103132833333362	5.813706116666669	5.817118950000002	5.8205080055555571	5.8239041722222247	5.8272940611111137	5.8306831166666688	5.8340750888888913	5.8374950888888923	5.8409038666666699	5.8443092833333363	5.8477163666666705	5.8511247277777816	5.8545402000000033	5.8579561166666698	5.8613552277777803	5.8647375611111139	5.8681207277777805	5.871503894444448	5.8748916722222253	5.8782887000000033	5.8816469222222247	5.8850051444444471	5.8883815888888922	5.8917677000000026	5.8951496166666697	5.8985306722222255	5.901929783333336	5.9053201166666698	5.9087079500000028	5.912089950000003	5.9154911722222252	5.9188831444444476	5.9222609777777802	5.9256388111111136	5.9290283111111135	5.9324224222222242	5.9358044222222244	5.9391918388888909	5.9425905333333358	5.9459541722222244	5.9493161444444471	5.9526802000000023	5.9560580333333357	5.959432505555557	5.9628078388888905	5.9661743666666691	5.9695480055555583	5.9729262555555582	5.9763099222222245	5.9796931722222251	5.9830776722222243	5.9864671722222242	5.9898337000000028	5.9931952277777807	5.9965709777777798	5.9999554777777799	6.0033399777777801	6.006717394444447	6.0100685611111135	6.0134172277777802	6.0167729500000027	6.0201595333333353	6.0235473666666683	6.0269318666666685	6.0302896722222243	6.0336433388888908	6.0369953388888913	6.0403752555555581	6.0437572555555583	6.0471417555555584	6.0505070333333366	6.0538752000000038	6.057244200000004	6.060618200000004	6.0640189777777822	6.0673834222222265	6.0707499500000051	6.0741293388888931	6.0775153666666712	6.0808926722222258	6.0842592000000044	6.087614088888893	6.0909552833333382	6.0943010611111159	6.097632727777782	6.1009693666666713	6.1043122277777826	6.1076472000000042	6.1109821722222266	6.114324200000004	6.1176691444444486	6.1210198944444478	6.1243523111111147	6.1276987555555591	6.1310377833333369	6.1343955888888928	6.1377459222222255	6.1411149222222265	6.144459311111115	6.1477987555555593	6.1511532277777814	6.15450811666667	6.1578630055555594	6.1612012000000043	6.1645414777777825	6.1678912277777824	6.1712347833333379	6.174600894444449	6.177948588888893	6.1812975333333373	6.1846407000000045	6.1879867555555599	6.1913063944444486	6.1946260333333383	6.1979592833333381	6.2012925333333389	6.2046357000000052	6.2079846166666721	6.211324477777783	6.2146488388888947	6.2179526722222285	6.2212822000000063	6.2246265888888948	6.2279528388888954	6.2312550333333396	6.2345555888888962	6.2378598388888955	6.2411567000000066	6.2444804500000064	6.247781005555562	6.2510700888888957	6.2543743388888959	6.2576830888888955	6.260991838888895	6.2643222000000067	6.2676178388888957	6.2709315333333402	6.2742452277777838	6.2775564500000058	6.2808557833333394	6.2841674222222288	6.2874790611111182	6.2907947833333404	6.2941084777777849	6.2974152000000077	6.3007011722222295	6.3040010055555635	6.3073253666666744	6.3106542277777855	6.3139818666666745	6.3172943388888978	6.3206060055555637	6.3239447000000082	6.3272928388888969	6.3306040888888973	6.3339235055555632	6.3372278111111191	6.3405402833333415	6.3438397000000082	6.3471411722222308	6.3504450888888977	6.3537490055555645	6.3570480333333421	6.3603376722222311	6.3636244500000085	6.3669230611111205	6.3702224777777863	6.3735100611111193	6.3768172277777868	6.3801112555555637	6.3834200611111198	6.3867158111111193	6.3900058666666748	6.3932735333333408	6.3965590333333404	6.3998588666666745	6.40314892222223	6.4064234777777855	6.4096968388888964	6.4129803111111192	6.4162804222222301	6.4195965611111188	6.4228589500000082	6.4261185055555643	6.4293780611111204	6.4326420888888975	6.43591056111112	6.4391843111111209	6.4424600888888977	6.4457403388888981	6.4490070333333422	6.4522840333333429	6.4555679222222313	6.4588603388888979	6.4621559777777868	6.4654234777777866	6.4687073666666759	6.471977477777787	6.4752386722222326	6.4784892555555649	6.4817406444444545	6.4849932277777871	6.4882714500000098	6.491552894444454	6.4948195888888982	6.4980915333333424	6.501366700000009	6.5046333944444532	6.507900894444453	6.5111683944444527	6.5144306722222307	6.5177034222222314	6.5209866444444531	6.5242650333333421	6.5275422277777864	6.5308157833333427	6.5340913666666758	6.537359283333342	6.5406247833333424	6.5438874500000086	6.5471517277777869	6.5504260888888979	6.5536751722222313	6.5569214500000088	6.5601945888888977	6.5634604777777872	6.5667279777777869	6.5699654500000095	6.5732317555555646	6.5765020888888976	6.5797724222222307	6.5830303388888973	6.5862706166666758	6.5895369222222309	6.5927935333333423	6.5960420888888978	6.5992663388888975	6.6024929777777865	6.6057407277777873	6.6090054222222312	6.6122380888888976	6.6154707555555641	6.6186893944444529	6.6219403666666752	6.6251978111111196	6.6284463666666751	6.631678616666675	6.6349188944444535	6.6381682555555646	6.6414196444444542	6.6446447000000095	6.6478697555555648	6.6511179222222312	6.6543721166666758	6.6576339777777873	6.6608817277777872	6.664113588888898	6.6673454500000089	6.6706081166666751	6.6738570888888971	6.6771245888888968	6.6803868666666748	6.6836426722222306	6.6869009222222306	6.6901591722222307	6.6934202277777857	6.6967138388888969	6.6999737000000081	6.7032339500000075	6.7064849222222298	6.7097431722222298	6.7130250333333406	6.7162985888888969	6.7195802000000073	6.7228638388888973	6.7261469222222301	6.7294113388888972	6.7326562833333412	6.7359100888888968	6.7391493666666742	6.7424121722222301	6.7456765888888963	6.7489187000000079	6.7521672555555643	6.7554357277777868	6.7587009777777869	6.7619674222222308	6.7652232277777866	6.7684697833333427	6.7717219777777879	6.7749997833333433	6.7782905611111204	6.7815467833333427	6.784811061111121	6.7880797833333428	6.791368144444454	6.7946239500000098	6.7978874222222325	6.8011448666666769	6.8044023111111214	6.8076714222222332	6.8109586722222337	6.8142285888889003	6.8174852000000117	6.8207551166666782	6.8240250333333456	6.8272860888889007	6.830554394444456	6.8338065888889004	6.8370460611111232	6.8402994500000123	6.8435528388889022	6.8468026166666798	6.8500499777777906	6.8532965333333467	6.8565475055555689	6.8597725611111242	6.8630118388889025	6.8662612000000136	6.869522672222236	6.8727833388889019	6.8760488388889023	6.8793098944444573	6.8825737833333465	6.885820061111124	6.8890783666666797	6.8923519222222351	6.8956194222222349	6.8988768666666793	6.9021075333333455	6.9053430055555687	6.9086085055555682	6.9118760055555679	6.9151178944444567	6.9183577555555678	6.9215944222222339	6.9248542833333442	6.9280976166666779	6.9313138388888991	6.9345380888888997	6.9377643388888997	6.9410108944444548	6.944241561111121	6.9474734222222319	6.9507052833333427	6.9539429500000089	6.9571748111111198	6.9604050611111195	6.963638116666675	6.9668735888888973	6.9701245611111196	6.9733483944444536	6.9765610055555642	6.9797932555555642	6.9830255055555641	6.9862397277777859	6.9894631722222309	6.9926745888888968	6.9958940333333413	6.9990940055555635	7.0023222555555629	7.0055577277777861	7.0088120333333412	7.0120719500000082	7.0153154222222307	7.0185588944444532	7.0217895611111194	7.0250097833333411	7.0282209222222294	7.0314271444444518	7.0346337555555625	7.0378407555555622	7.0410427277777847	7.0442447000000064	7.0474669500000067	7.0506980055555619	7.0539250611111175	7.0571314222222288	7.0603420333333391	7.0635462277777838	7.0667632555555624	7.0699656444444514	7.0731664222222292	7.0763723944444514	7.0796030611111176	7.0828213666666722	7.0860603944444502	7.0893198944444507	7.0925793944444502	7.0958172277777836	7.0990335611111171	7.102249477777784	7.1054881444444504	7.1086948944444508	7.1119032555555615	7.1150956722222283	7.1182880888888942	7.1214852833333389	7.1246980055555609	7.1278955888888937	7.1310816444444498	7.13425150555556	7.137439533333338	7.1406339500000042	7.1438303388888942	7.1470207555555598	7.1501818944444491	7.1533727277777821	7.156583477777783	7.1597679777777827	7.1629707000000042	7.1661943944444486	7.1694334222222276	7.1726341722222271	7.1758297555555606	7.179056033333338	7.1822567833333384	7.1854575333333388	7.1886531166666723	7.1918475055555611	7.1950260611111174	7.1982046166666729	7.2013899222222291	7.2045748111111179	7.2077664500000065	7.2109470055555622	7.2141271444444506	7.2172890333333397	7.220450922222228	7.2235939222222285	7.226760616666672	7.2299320611111169	7.2330797833333387	7.2362357833333393	7.2394139500000056	7.242606783333339	7.2457928666666724	7.2489789500000059	7.2521654222222285	7.2553487277777844	7.2585158111111179	7.261664700000007	7.2648531722222289	7.2680483666666742	7.2712307277777848	7.2744028388888964	7.2775824500000077	7.2807859500000065	7.283959644444451	7.2871160333333407	7.2902862000000068	7.2934520333333408	7.2966178666666739	7.2997840888888961	7.3029510888888955	7.3060896166666733	7.3092715888888957	7.3124535611111172	7.315612838888895	7.3187873388888951	7.3219642000000054	7.3251246444444496	7.3282850888888946	7.3314545333333383	7.3346290333333384	7.3377972277777825	7.3409447555555607	7.3441062555555598	7.3472890055555604	7.3504588388888941	7.3536192833333383	7.3567754222222268	7.3599530611111161	7.363123283333338	7.3662943111111154	7.3694727555555604	7.3726558944444491	7.3758284777777829	7.3789912833333382	7.3821411722222265	7.3852758666666709	7.3884218388888927	7.3915705611111147	7.3947251444444486	210i Curve Fit	20	20.100000000000001	20.2	20.3	20.399999999999999	20.5	20.6	20.7	20.8	20.9	21	21.1	21.2	21.3	21.4	21.5	21.6	21.7	21.8	21.9	22	22.1	22.2	22.3	22.4	22.5	22.6	22.7	22.8	22.9	23	23.1	23.2	23.3000000000001	23.4	23.5	23.600000000000101	23.7	23.8000000000001	23.900000000000102	24.000000000000099	24.100000000000101	24.200000000000099	24.3000000000001	24.400000000000102	24.500000000000099	24.600000000000101	24.700000000000099	24.8000000000001	24.900000000000102	25.000000000000099	25.100000000000101	25.200000000000099	25.3000000000001	25.400000000000102	25.500000000000099	25.600000000000101	25.700000000000099	25.8000000000001	25.900000000000102	26.000000000000099	26.100000000000101	26.200000000000099	26.3000000000001	26.400000000000102	26.500000000000099	26.600000000000101	26.700000000000099	26.8000000000001	26.900000000000102	27.000000000000099	27.100000000000101	27.200000000000099	27.3000000000001	27.400000000000102	27.500000000000099	27.600000000000101	27.700000000000099	27.8000000000001	27.900000000000102	28.000000000000099	28.100000000000101	28.200000000000099	28.3000000000001	28.400000000000102	28.500000000000099	28.600000000000101	28.700000000000099	28.8000000000001	28.900000000000102	29.000000000000099	29.100000000000101	29.200000000000099	29.3000000000001	29.400000000000102	29.500000000000099	29.600000000000101	29.700000000000099	29.8000000000001	29.900000000000102	30.000000000000099	30.100000000000101	30.200000000000099	30.3000000000001	30.400000000000102	30.500000000000099	30.6000000000002	30.700000000000198	30.8000000000002	30.900000000000201	31.000000000000199	31.1000000000002	31.200000000000198	31.3000000000002	31.400000000000201	31.500000000000199	31.6000000000002	31.700000000000198	31.8000000000002	31.900000000000201	32.000000000000199	32.1000000000002	32.200000000000202	32.300000000000203	32.400000000000198	32.500000000000199	32.6000000000002	32.700000000000202	32.800000000000203	32.900000000000198	33.000000000000199	33.1000000000002	33.200000000000202	33.300000000000203	33.400000000000198	33.500000000000199	33.6000000000002	33.700000000000202	33.800000000000203	33.900000000000198	34.000000000000199	34.1000000000002	34.200000000000202	34.300000000000203	34.400000000000198	34.500000000000199	34.6000000000002	34.700000000000202	34.800000000000203	34.900000000000198	35.000000000000199	35.1000000000002	35.200000000000202	35.300000000000203	35.400000000000198	35.500000000000199	35.6000000000002	35.700000000000202	35.800000000000203	35.900000000000198	36.000000000000199	36.1000000000002	36.200000000000202	36.300000000000203	36.400000000000198	36.500000000000199	36.6000000000002	36.700000000000202	36.800000000000203	36.900000000000198	37.000000000000199	37.1000000000002	37.200000000000202	37.300000000000203	37.400000000000198	37.500000000000199	37.6000000000003	37.700000000000301	37.800000000000303	37.900000000000297	38.000000000000298	38.1000000000003	38.200000000000301	38.300000000000303	38.400000000000297	38.500000000000298	38.6000000000003	38.700000000000301	38.800000000000303	38.900000000000297	39.000000000000298	39.1000000000003	39.200000000000301	39.300000000000303	39.400000000000297	39.500000000000298	39.6000000000003	39.700000000000301	39.800000000000303	39.900000000000297	40.000000000000298	40.1000000000003	40.200000000000301	40.300000000000303	40.400000000000297	40.500000000000298	40.6000000000003	40.700000000000301	40.800000000000303	40.900000000000297	41.000000000000298	41.1000000000003	41.200000000000301	41.300000000000303	41.400000000000297	41.500000000000298	41.6000000000003	41.700000000000301	41.800000000000303	41.900000000000297	42.000000000000298	42.1000000000003	42.200000000000301	42.300000000000303	42.400000000000297	42.500000000000298	42.6000000000003	42.700000000000301	42.800000000000303	42.900000000000297	43.000000000000298	43.1000000000003	43.200000000000301	43.300000000000303	43.400000000000297	43.500000000000298	43.6000000000003	43.700000000000301	43.800000000000303	43.900000000000297	44.000000000000298	44.1000000000003	44.200000000000301	44.300000000000303	44.400000000000297	44.500000000000298	44.6000000000003	44.700000000000401	44.800000000000402	44.900000000000396	45.000000000000398	45.100000000000399	45.200000000000401	45.300000000000402	45.400000000000396	45.500000000000398	45.600000000000399	45.700000000000401	45.800000000000402	45.900000000000396	46.000000000000398	46.100000000000399	46.200000000000401	46.300000000000402	46.400000000000396	46.500000000000398	46.600000000000399	46.700000000000401	46.800000000000402	46.900000000000396	47.000000000000398	47.100000000000399	47.200000000000401	47.300000000000402	47.400000000000396	47.500000000000398	47.600000000000399	47.700000000000401	47.800000000000402	47.900000000000396	48.000000000000398	48.100000000000399	48.200000000000401	48.300000000000402	48.400000000000396	48.500000000000398	48.600000000000399	48.700000000000401	48.800000000000402	48.900000000000396	49.000000000000398	49.100000000000399	49.200000000000401	49.300000000000402	49.400000000000396	49.500000000000398	49.600000000000399	49.700000000000401	49.800000000000402	49.900000000000396	50.000000000000398	50.100000000000399	50.200000000000401	50.300000000000402	50.400000000000396	50.500000000000398	50.600000000000399	50.700000000000401	50.800000000000402	50.900000000000396	51.000000000000398	51.100000000000399	51.200000000000401	51.300000000000402	51.400000000000396	51.500000000000398	51.600000000000399	51.7000000000005	51.800000000000502	51.900000000000503	52.000000000000497	52.100000000000499	52.2000000000005	52.300000000000502	52.400000000000503	52.500000000000497	52.600000000000499	52.7000000000005	52.800000000000502	52.900000000000503	53.000000000000497	53.100000000000499	53.2000000000005	53.300000000000502	53.400000000000503	53.500000000000497	53.600000000000499	53.7000000000005	53.800000000000502	53.900000000000503	54.000000000000497	54.100000000000499	54.2000000000005	54.300000000000502	54.400000000000503	54.500000000000497	54.600000000000499	54.7000000000005	54.800000000000502	54.900000000000503	55.000000000000497	55.100000000000499	55.2000000000005	55.300000000000502	55.400000000000503	55.500000000000497	55.600000000000499	55.7000000000005	55.800000000000502	55.900000000000503	56.000000000000497	56.100000000000499	56.2000000000005	56.300000000000502	56.400000000000503	56.500000000000497	56.600000000000499	56.7000000000005	56.800000000000502	56.900000000000503	57.000000000000497	57.100000000000499	57.2000000000005	57.300000000000502	57.400000000000503	57.500000000000497	57.600000000000499	57.7000000000005	57.800000000000502	57.900000000000503	58.000000000000497	58.100000000000499	58.2000000000005	58.300000000000502	58.400000000000503	58.500000000000497	58.600000000000499	58.7000000000005	58.800000000000601	58.900000000000603	59.000000000000597	59.100000000000598	59.2000000000006	59.300000000000601	59.400000000000603	59.500000000000597	59.600000000000598	59.7000000000006	59.800000000000601	59.900000000000603	60.000000000000597	60.100000000000598	60.2000000000006	60.300000000000601	60.400000000000603	60.500000000000597	60.600000000000598	60.7000000000006	60.800000000000601	60.900000000000603	61.000000000000597	61.100000000000598	61.2000000000006	61.300000000000601	61.400000000000603	61.500000000000597	61.600000000000598	61.7000000000006	61.800000000000601	61.900000000000603	62.000000000000597	62.100000000000598	62.2000000000006	62.300000000000601	62.400000000000603	62.500000000000597	62.600000000000598	62.7000000000006	62.800000000000601	62.900000000000603	63.000000000000597	63.100000000000598	63.2000000000006	63.300000000000601	63.400000000000603	63.500000000000597	63.600000000000598	63.7000000000006	63.800000000000601	63.900000000000603	64.000000000000597	64.100000000000605	64.2000000000006	64.300000000000594	64.400000000000603	64.500000000000597	64.600000000000605	64.7000000000006	64.800000000000594	64.900000000000603	65.000000000000597	65.100000000000605	65.2000000000006	65.300000000000594	65.400000000000603	65.500000000000597	65.600000000000605	65.7000000000006	65.800000000000693	65.900000000000702	66.000000000000696	66.100000000000705	66.200000000000699	66.300000000000693	66.400000000000702	66.500000000000696	66.600000000000705	66.700000000000699	66.800000000000693	66.900000000000702	67.000000000000696	67.100000000000705	67.200000000000699	67.300000000000693	67.400000000000702	67.500000000000696	67.600000000000705	67.700000000000699	67.800000000000693	67.900000000000702	68.000000000000696	68.100000000000705	68.200000000000699	68.300000000000693	68.400000000000702	68.500000000000696	68.600000000000705	68.700000000000699	68.800000000000693	68.900000000000702	69.000000000000696	69.100000000000705	69.200000000000699	69.300000000000693	69.400000000000702	69.500000000000696	69.600000000000705	69.700000000000699	69.800000000000693	69.900000000000702	70.000000000000696	70.100000000000705	70.200000000000699	70.300000000000693	70.400000000000702	70.500000000000696	70.600000000000705	70.700000000000699	70.800000000000693	70.900000000000702	71.000000000000696	71.100000000000705	71.200000000000699	71.300000000000693	71.400000000000702	71.500000000000696	71.600000000000705	71.700000000000699	71.800000000000693	71.900000000000702	72.000000000000696	72.100000000000705	72.200000000000699	72.300000000000693	72.400000000000702	72.500000000000696	72.600000000000705	72.700000000000699	72.800000000000793	72.900000000000801	73.000000000000796	7.3056992900400214E-2	8.3339611119570778E-2	9.3622229338745186E-2	0.10390484755792519	0.11418746577711035	0.12447008399630205	0.1347527022155004	0.14503532043470596	0.15531793865391938	0.1656005568731409	0.1758831750923722	0.18616579331161359	0.19644841153086559	0.20673102975013044	0.21701364796940747	0.22729626618869914	0.23757888440800629	0.24786150262732978	0.25814412084667204	0.2684267390660342	0.27870935728541801	0.28899197550482542	0.29927459372425808	0.30955721194371905	0.31983983016320999	0.33012244838273491	0.34040506660229536	0.35068768482189455	0.36097030304153677	0.37125292126122494	0.38153553948096397	0.39181815770075795	0.40210077592061172	0.4123833941405407	0.42266601236051959	0.43294863058058619	0.44323124880074677	0.45351386702097812	0.4637964852413291	0.4740791034617779	0.48436172168234376	0.49464433990303797	0.50492695812387089	0.51520957634485565	0.52549219456600571	0.53577481278733419	0.54605743100885829	0.55634004923059432	0.56662266745256185	0.57690528567478094	0.5871879038972736	0.59747052212006413	0.60775314034317829	0.6180357585666455	0.62831837679049651	0.63860099501476464	0.64888361323948818	0.65916623146470532	0.66944884969046115	0.6797314679168025	0.69001408614378068	0.70029670437145286	0.71057932259987966	0.7208619408291278	0.73114455905926945	0.74142717729038321	0.75170979552255568	0.76199241375587934	0.77227503199045711	0.78255765022639812	0.79284026846382272	0.8031228867028628	0.81340550494365971	0.82368812318636941	0.83397074143116023	0.84425335967821569	0.8545359779277355	0.86481859617993673	0.87510121443505662	0.88538383269335219	0.89566645095510367	0.9059490692206158	0.91623168749021988	0.92651430576427773	0.93679692404318171	0.94707954232735891	0.9573621606172753	0.9676447789134367	0.97792739721639399	0.98821001552674648	0.99849263384514608	1.0087752521723035	1.0190578705089908	1.0293404888560487	1.0396231072143916	1.0499057255850146	1.0601883439690021	1.0704709623675317	1.0807535807818871	1.0910361992134641	1.1013188176637805	1.1116014361344906	1.1218840546273923	1.1321666731444442	1.1424492916877755	1.1527319102597047	1.1630145288627642	1.1732971474996783	1.1835797661734451	1.1938623848873149	1.2041450036448242	1.2144276224498241	1.2247102413065016	1.234992860219416	1.2452754791935279	1.2555580982342343	1.2658407173474102	1.2761233365394478	1.2864059558173027	1.2966885751885446	1.3069711946614107	1.3172538142448655	1.3275364339486631	1.3378190537834183	1.3481016737606821	1.3583842938930257	1.3686669141941274	1.3789495346788727	1.3892321553634599	1.3995147762655162	1.4097973974042244	1.4200800188004579	1.4303626404769323	1.4406452624583663	1.4509278847716587	1.4612105074460831	1.471493130513492	1.4817757540085494	1.4920583779689767	1.5023410024358208	1.5126236274537532	1.5229062530713817	1.5331888793416037	1.5434715063219817	1.5537541340751544	1.5640367626692888	1.5743193921785623	1.5846020226836952	1.5948846542725286	1.6051672870406506	1.6154499210920827	1.62573255654002	1.6360151935076426	1.6462978321289961	1.6565804725499484	1.6668631149292366	1.6771457594395967	1.6874284062690019	1.6977110556220061	1.7079937077212048	1.7182763628088313	1.7285590211484807	1.7388416830270015	1.7491243487565429	1.7594070186767874	1.7696896931573818	1.7799723726005749	1.7902550574440985	1.8005377481642924	1.8108204452795138	1.8211031493538439	1.8313858610011164	1.8416685808893101	1.8519513097453226	1.8622340483601687	1.8725167975946357	1.8827995583854471	1.8930823317519188	1.9033651188033096	1.9136479207467092	1.9239307388956814	1.9342135746796516	1.9444964296541303	1.9547793055118317	1.9650622040947772	1.9753451274074658	1.9856280776312036	1.9959110571397001	2.0061940685160389	2.0164771145711446	2.0267601983638843	2.0370433232229299	2.0473264927705594	2.057609710948558	2.0678929820463927	2.0781763107318865	2.0884597020845872	2.0987431616320813	2.1090266953895185	2.1193103099026089	2.1295940122944277	2.1398778103163374	2.1501617124034009	2.1604457277346927	2.1707298662989136	2.1810141389658146	2.1912985575638904	2.2015831349649519	2.2118678851761491	2.2221528234400987	2.2324379663438632	2.2427233319375195	2.2530089398632036	2.2632948114955185	2.2735809700943403	2.2838674409710884	2.2941542516696609	2.3044414321633342	2.3147290150690085	2.3250170358803652	2.3353055332215695	2.3455945491233452	2.355884129323401	2.3661743235933326	2.376465186094356	2.3867567757644013	2.3970491567393246	2.4073423988112674	2.4176365779274023	2.4279317767326583	2.4382280851602696	2.4485256010743788	2.4588244309692655	2.4691246907302	2.4794265064613343	2.4897300153865345	2.5000353668295752	2.5103427232806732	2.5206522615569673	2.5309641740651845	2.5412786701754966	2.5515959777163291	2.5619163446007422	2.5722400405959642	2.5825673592486087	2.5928986199792772	2.6032341703613735	2.6135743886003051	2.6239196862305731	2.6342705110499769	2.6446273503114845	2.6549907341954562	2.6653612395866704	2.6757394941827566	2.6861261809629777	2.6965220430487382	2.7069278889899429	2.7173445985142379	2.7277731287793205	2.7382145211719751	2.748669908701153	2.7591405240364759	2.7696277082478518	2.7801329203065954	2.7906577474134973	2.8012039162247389	2.8117733050524487	2.8223679571229972	2.8329900949829758	2.8436421361500717	2.8543267101139476	2.8650466768005916	2.8758051466226355	2.8866055022477193	2.8974514222271863	2.9083469066383145	2.9192963049047593	2.9303043459720972	2.9413761710282009	2.9525173689716078	2.9637340148451705	2.9750327114668438	2.9864206345046038	2.9979055812579749	3.0094960234243242	3.0212011641439527	3.0330309996335862	3.0449963857331763	3.0571091097053191	3.0693819676398868	3.0818288478280467	3.0944648204789749	3.1073062341587767	3.1203708193331154	3.1336777993921112	3.1472480095266642	3.161104023808023	3.175270290795555	3.1897732779588606	3.204641625147624	3.2199063072727676	3.2356008062726525	3.2517612923245363	3.2684268141201169	3.2856394978503305	3.303444754333384	3.3218914934658059	3.3410323448730317	3.360923883277104	3.3816268566778991	3.4032064149537224	3.425732335920479	3.4492792452394063	3.4739268258258682	3.4997600115818801	3.5268691593505457	3.5553501919724004	3.5853047042166759	3.6168400221746295	3.650069205455559	3.6851109802420252	3.7220895899788267	3.7611345492350865	3.8023802851555089	3.8459656499829706	3.8920332874864951	3.940728835880448	3.9921999501040428	4.0465951272927221	4.10406232107362	4.1647473331208769	4.2287919743734257	4.2963319935910143	4.3674947776137287	4.4423968358517207	4.521141091145652	4.6038140100841973	4.690482617898823	4.7811914557913875	4.8759595514428113	4.9747774858006713	5.0776046502050782	5.1843667965297477	5.2949539882776397	5.4092190614848006	5.5269766999752701	5.6480032193168173	5.7720371374239186	5.898780587239548	6.0279015988919147	6.1590372462818213	6.291797617818828	6.4257705350072314	6.5605269080671702	6.6956265871134093	6.8306245428116679	6.9650771937284652	7.098548690066961	7.2306169657238506	7.3608793824350549	7.4889578102859762	7.6145030164876211	7.7371982670297452	7.8567620813164671	7.9729501158214946	8.0855561869888923	8.1944124742050608	8.299388969288362	8.4003922587094504	8.4973637383066389	8.5902773677045996	8.6791370734717734	8.7639739070335558	8.844843056437476	8.9218208012547322	8.9950014881941946	9.0644945923106626	9.1304219157906061	9.1929149638260768	9.2521125255112722	9.3081584773365549	9.3611998178959492	9.411384934937475	9.4588620998537927	9.5037781800501122	9.5462775562098443	9.586501229153388	9.6245860995878303	9.6606644034123477	9.6948632852206149	9.7273044930885177	9.7581041785258762	9.7873727865033811	9.8152150216483491	9.8417298779664719	9.8670107207351769	9.891145410484496	9.9142164602031038	9.9363012180586132	9.957472068988535	9.9777966494940689	10.000923073314572	10.023325151660361	10.045057629346951	10.066171409492538	10.086713776940645	10.106728616240302	10.126256622872615	10.145335506745152	10.164000187255812	10.182282979461579	10.200213771080945	10.217820190217141	10.235127763817456	10.25216006698607	10.268938863348181	10.285484236724825	10.301814714423868	10.317947382485688	10.333897993244431	10.349681065579075	10.365309978235064	10.380797056597507	10.396153653293164	10.411390222990669	10.426516391758101	10.441541021324655	10.456472268579191	10.471317640623754	10.4860840456845	10.500777840166856	10.515404872125906	10.529970521407314	10.544479736698865	10.558937069717746	10.573346706744315	10.58771249769932	10.602037982948374	10.616326418004871	10.630580796290751	10.644803870103207	10.658998169924899	10.673166022205304	10.687309565731494	10.701430766697911	10.715531432576586	10.729613224881655	10.743677670914845	10.757726174572225	10.771760026286108	10.785780412170615	10.79978842243389	10.81378505911519	10.827771243200557	10.841747821166505	10.855715570997393	10.869675207718476	10.883627388483356	10.897572717251549	10.911511749088907	10.92544499412131	10.939372921169298	10.953295961089323	10.967214509845292	10.981128931331975	10.995039559970333	11.00894670309312	11.022850643137614	11.036751639661134	11.050649931193497	11.064545736939694	11.078439258344797	11.092330680532269	11.106220173625886	11.120107893964645	11.133993985219371	11.147878579418911	11.16176179789325	11.175643752140275	11.189524544622341	11.203404269498327	11.217283013296434	11.231160855532449	11.245037869277958	11.258914121682523	11.272789674453565	11.286664584297366	11.300538903324334	11.31441267942146	11.32828595659457	11.342158775282863	11.356031172647961	11.369903182839524	11.383774837239367	11.397646164685776	11.411517191679646	11.425387942573922	11.439258439747691	11.453128703766152	11.466998753527649	11.480868606398735	11.494738278338358	11.508607784011925	11.522477136896166	11.536346349375462	11.550215432830377	11.564084397719048	11.577953253651915	11.591822009460458	11.605690673260316	11.619559252509317	11.633427754060797	11.647296184212587	11.661164548752051	11.675032852997456	11.688901101835988	11.70276929975871	11.716637450892645	11.730505559030309	11.744373627656815	11.758241659974777	11.772109658927226	11.785977627218639	11.79984556733428	11.813713481557972	11.827581371988414	11.841449240554196	11.855317089027585	11.86918491903721	11.883052732079644	11.896920529530199	150i Curve Fit	20	20.100000000000001	20.2	20.3	20.399999999999999	20.5	20.6	20.7	20.8	20.9	21	21.1	21.2	21.3	21.4	21.5	21.6	21.7	21.8	21.9	22	22.1	22.2	22.3	22.4	22.5	22.6	22.7	22.8	22.9	23	23.1	23.2	23.3000000000001	23.4	23.5	23.600000000000101	23.7	23.8000000000001	23.900000000000102	24.000000000000099	24.100000000000101	24.200000000000099	24.3000000000001	24.400000000000102	24.500000000000099	24.600000000000101	24.700000000000099	24.8000000000001	24.900000000000102	25.000000000000099	25.100000000000101	25.200000000000099	25.3000000000001	25.400000000000102	25.500000000000099	25.600000000000101	25.700000000000099	25.8000000000001	25.900000000000102	26.000000000000099	26.100000000000101	26.200000000000099	26.3000000000001	26.400000000000102	26.500000000000099	26.600000000000101	26.700000000000099	26.8000000000001	26.900000000000102	27.000000000000099	27.100000000000101	27.200000000000099	27.3000000000001	27.400000000000102	27.500000000000099	27.600000000000101	27.700000000000099	27.8000000000001	27.900000000000102	28.000000000000099	28.100000000000101	28.200000000000099	28.3000000000001	28.400000000000102	28.500000000000099	28.600000000000101	28.700000000000099	28.8000000000001	28.900000000000102	29.000000000000099	29.100000000000101	29.200000000000099	29.3000000000001	29.400000000000102	29.500000000000099	29.600000000000101	29.700000000000099	29.8000000000001	29.900000000000102	30.000000000000099	30.100000000000101	30.200000000000099	30.3000000000001	30.400000000000102	30.500000000000099	30.6000000000002	30.700000000000198	30.8000000000002	30.900000000000201	31.000000000000199	31.1000000000002	31.200000000000198	31.3000000000002	31.400000000000201	31.500000000000199	31.6000000000002	31.700000000000198	31.8000000000002	31.900000000000201	32.000000000000199	32.1000000000002	32.200000000000202	32.300000000000203	32.400000000000198	32.500000000000199	32.6000000000002	32.700000000000202	32.800000000000203	32.900000000000198	33.000000000000199	33.1000000000002	33.200000000000202	33.300000000000203	33.400000000000198	33.500000000000199	33.6000000000002	33.700000000000202	33.800000000000203	33.900000000000198	34.000000000000199	34.1000000000002	34.200000000000202	34.300000000000203	34.400000000000198	34.500000000000199	34.6000000000002	34.700000000000202	34.800000000000203	34.900000000000198	35.000000000000199	35.1000000000002	35.200000000000202	35.300000000000203	35.400000000000198	35.500000000000199	35.6000000000002	35.700000000000202	35.800000000000203	35.900000000000198	36.000000000000199	36.1000000000002	36.200000000000202	36.300000000000203	36.400000000000198	36.500000000000199	36.6000000000002	36.700000000000202	36.800000000000203	36.900000000000198	37.000000000000199	37.1000000000002	37.200000000000202	37.300000000000203	37.400000000000198	37.500000000000199	37.6000000000003	37.700000000000301	37.800000000000303	37.900000000000297	38.000000000000298	38.1000000000003	38.200000000000301	38.300000000000303	38.400000000000297	38.500000000000298	38.6000000000003	38.700000000000301	38.800000000000303	38.900000000000297	39.000000000000298	39.1000000000003	39.200000000000301	39.300000000000303	39.400000000000297	39.500000000000298	39.6000000000003	39.700000000000301	39.800000000000303	39.900000000000297	40.000000000000298	40.1000000000003	40.200000000000301	40.300000000000303	40.400000000000297	40.500000000000298	40.6000000000003	40.700000000000301	40.800000000000303	40.900000000000297	41.000000000000298	41.1000000000003	41.200000000000301	41.300000000000303	41.400000000000297	41.500000000000298	41.6000000000003	41.700000000000301	41.800000000000303	41.900000000000297	42.000000000000298	42.1000000000003	42.200000000000301	42.300000000000303	42.400000000000297	42.500000000000298	42.6000000000003	42.700000000000301	42.800000000000303	42.900000000000297	43.000000000000298	43.1000000000003	43.200000000000301	43.300000000000303	43.400000000000297	43.500000000000298	43.6000000000003	43.700000000000301	43.800000000000303	43.900000000000297	44.000000000000298	44.1000000000003	44.200000000000301	44.300000000000303	44.400000000000297	44.500000000000298	44.6000000000003	44.700000000000401	44.800000000000402	44.900000000000396	45.000000000000398	45.100000000000399	45.200000000000401	45.300000000000402	45.400000000000396	45.500000000000398	45.600000000000399	45.700000000000401	45.800000000000402	45.900000000000396	46.000000000000398	46.100000000000399	46.200000000000401	46.300000000000402	46.400000000000396	46.500000000000398	46.600000000000399	46.700000000000401	46.800000000000402	46.900000000000396	47.000000000000398	47.100000000000399	47.200000000000401	47.300000000000402	47.400000000000396	47.500000000000398	47.600000000000399	47.700000000000401	47.800000000000402	47.900000000000396	48.000000000000398	48.100000000000399	48.200000000000401	48.300000000000402	48.400000000000396	48.500000000000398	48.600000000000399	48.700000000000401	48.800000000000402	48.900000000000396	49.000000000000398	49.100000000000399	49.200000000000401	49.300000000000402	49.400000000000396	49.500000000000398	49.600000000000399	49.700000000000401	49.800000000000402	49.900000000000396	50.000000000000398	50.100000000000399	50.200000000000401	50.300000000000402	50.400000000000396	50.500000000000398	50.600000000000399	50.700000000000401	50.800000000000402	50.900000000000396	51.000000000000398	51.100000000000399	51.200000000000401	51.300000000000402	51.400000000000396	51.500000000000398	51.600000000000399	51.7000000000005	51.800000000000502	51.900000000000503	52.000000000000497	52.100000000000499	52.2000000000005	52.300000000000502	52.400000000000503	52.500000000000497	52.600000000000499	52.7000000000005	52.800000000000502	52.900000000000503	53.000000000000497	53.100000000000499	53.2000000000005	53.300000000000502	53.400000000000503	53.500000000000497	53.600000000000499	53.7000000000005	53.800000000000502	53.900000000000503	54.000000000000497	54.100000000000499	54.2000000000005	54.300000000000502	54.400000000000503	54.500000000000497	54.600000000000499	54.7000000000005	54.800000000000502	54.900000000000503	55.000000000000497	55.100000000000499	55.2000000000005	55.300000000000502	55.400000000000503	55.500000000000497	55.600000000000499	55.7000000000005	55.800000000000502	55.900000000000503	56.000000000000497	56.100000000000499	56.2000000000005	56.300000000000502	56.400000000000503	56.500000000000497	56.600000000000499	56.7000000000005	56.800000000000502	56.900000000000503	57.000000000000497	57.100000000000499	57.2000000000005	57.300000000000502	57.400000000000503	57.500000000000497	57.600000000000499	57.7000000000005	57.800000000000502	57.900000000000503	58.000000000000497	58.100000000000499	58.2000000000005	58.300000000000502	58.400000000000503	58.500000000000497	58.600000000000499	58.7000000000005	58.800000000000601	58.900000000000603	59.000000000000597	59.100000000000598	59.2000000000006	59.300000000000601	59.400000000000603	59.500000000000597	59.600000000000598	59.7000000000006	59.800000000000601	59.900000000000603	60.000000000000597	60.100000000000598	60.2000000000006	60.300000000000601	60.400000000000603	60.500000000000597	60.600000000000598	60.7000000000006	60.800000000000601	60.900000000000603	61.000000000000597	61.100000000000598	61.2000000000006	61.300000000000601	61.400000000000603	61.500000000000597	61.600000000000598	61.7000000000006	61.800000000000601	61.900000000000603	62.000000000000597	62.100000000000598	62.2000000000006	62.300000000000601	62.400000000000603	62.500000000000597	62.600000000000598	62.7000000000006	62.800000000000601	62.900000000000603	63.000000000000597	63.100000000000598	63.2000000000006	63.300000000000601	63.400000000000603	63.500000000000597	63.600000000000598	63.7000000000006	63.800000000000601	63.900000000000603	64.000000000000597	64.100000000000605	64.2000000000006	64.300000000000594	64.400000000000603	64.500000000000597	64.600000000000605	64.7000000000006	64.800000000000594	64.900000000000603	65.000000000000597	65.100000000000605	65.2000000000006	65.300000000000594	65.400000000000603	65.500000000000597	65.600000000000605	65.7000000000006	65.800000000000693	65.900000000000702	66.000000000000696	66.100000000000705	66.200000000000699	66.300000000000693	66.400000000000702	66.500000000000696	66.600000000000705	66.700000000000699	66.800000000000693	66.900000000000702	67.000000000000696	67.100000000000705	67.200000000000699	67.300000000000693	67.400000000000702	67.500000000000696	67.600000000000705	67.700000000000699	67.800000000000693	67.900000000000702	68.000000000000696	68.100000000000705	68.200000000000699	68.300000000000693	68.400000000000702	68.500000000000696	68.600000000000705	68.700000000000699	68.800000000000693	68.900000000000702	69.000000000000696	69.100000000000705	69.200000000000699	69.300000000000693	69.400000000000702	69.500000000000696	69.600000000000705	69.700000000000699	69.800000000000693	69.900000000000702	70.000000000000696	70.100000000000705	70.200000000000699	70.300000000000693	70.400000000000702	70.500000000000696	70.600000000000705	70.700000000000699	70.800000000000693	70.900000000000702	71.000000000000696	71.100000000000705	71.200000000000699	71.300000000000693	71.400000000000702	71.500000000000696	71.600000000000705	71.700000000000699	71.800000000000693	71.900000000000702	72.000000000000696	72.100000000000705	72.200000000000699	72.300000000000693	72.400000000000702	72.500000000000696	72.600000000000705	72.700000000000699	72.800000000000793	72.900000000000801	73.000000000000796	-2.5658703828060632E-2	-1.8967219970867026E-2	-1.2275736110390482E-2	-5.5842522464278604E-3	1.1072316212356048E-3	7.7987154928288527E-3	1.4490199368594265E-2	2.1181683248789197E-2	2.7873167133687583E-2	3.4564651023579342E-2	4.125613491877321E-2	4.794761881959652E-2	5.463910272639614E-2	6.1330586639541725E-2	6.8022070559424608E-2	7.4713554486461192E-2	8.1405038421092896E-2	8.8096522363788413E-2	9.4788006315046039E-2	0.10147949027539391	0.10817097424539371	0.11486245822564109	0.12155394221676849	0.12824542621944809	0.13493691023439264	0.14162839426235979	0.14831987830415352	0.15501136236062679	0.16170284643268656	0.16839433052129466	0.17508581462747322	0.18177729875230675	0.18846878289694677	0.19516026706262316	0.20185175125061386	0.20854323546231776	0.21523471969919819	0.22192620396278892	0.22861768825476692	0.23530917257686365	0.2420006569309455	0.24869214131898781	0.25538362574308632	0.26207511020546781	0.26876659470849545	0.27545807925467847	0.28214956384668172	0.2888410484873335	0.29553253317963779	0.30222401792678322	0.30891550273215534	0.31560698759934946	0.32229847253218191	0.32898995753470539	0.3356814426112224	0.34237292776630102	0.34906441300479152	0.3557558983318434	0.36244738375292468	0.36913886927384032	0.37583035490075362	0.38252184064020917	0.38921332649915458	0.39590481248496739	0.40259629860547991	0.40928778486900802	0.41597927128438161	0.42267075786097486	0.42936224460874162	0.43605373153824978	0.44274521866071892	0.44943670598806285	0.45612819353292955	0.46281968130874901	0.46951116932977943	0.47620265761115943	0.48289414616896292	0.48958563502025532	0.49627712418315634	0.50296861367690393	0.50966010352192359	0.51635159373990269	0.52304308435386637	0.52973457538826241	0.53642606686904737	0.54311755882377977	0.54980905128172086	0.55650054427393714	0.56319203783341409	0.56988353199517316	0.57657502679639749	0.58326652227656706	0.58995801847759788	0.59664951544399503	0.60334101322301015	0.61003251186481267	0.61672401142266953	0.6234155119531356	0.6301070135162582	0.63679851617579142	0.64349001999942435	0.65018152505902727	0.65687303143090603	0.6635645391960775	0.67025604844056086	0.67694755925568517	0.68363907173842664	0.69033058599172481	0.69702210212489846	0.70371362025400686	0.71040514050227455	0.71709666300053421	0.72378818788769494	0.73047971531124345	0.73717124542777035	0.74386277840353443	0.75055431441505882	0.7572458536497646	0.76393739630664492	0.7706289425969769	0.77732049274508219	0.78401204698913129	0.79070360558199893	0.79739516879217176	0.80408673690471166	0.81077831022228097	0.81746988906622653	0.82416147377773452	0.8308530647190554	0.83754466227480351	0.84423626685333986	0.85092787888823529	0.85761949883982869	0.86431112719687919	0.87100276447832026	0.87769441123512437	0.88438606805227882	0.89107773555088565	0.89776941439039337	0.90446110527096246	0.91115280893598072	0.91784452617472945	0.92453625782521842	0.93122800477719392	0.93791976797533239	0.94461154842263317	0.95130334718401666	0.95799516539014884	0.96468700424149956	0.9713788650126518	0.97807074905687874	0.98476265781099925	0.99145459280053694	0.99814655564519661	1.004838548064678	1.0115305718848502	1.0182226290443039	1.0249147216013128	1.0316068517412196	1.0382990217842822	1.0449912341940042	1.0516834915859739	1.058375796737256	1.0650681525963603	1.071760562293824	1.0784530291534513	1.085145556704241	1.091838148693056	1.098530809098073	1.1052235421430598	1.1119163523125393	1.1186092443678826	1.1253022233644012	1.1319952946694922	1.1386884639819022	1.1453817373521828	1.1520751212044129	1.1587686223592284	1.1654622480583432	1.1721560059905127	1.1788499043191363	1.1855439517115527	1.1922381573701486	1.1989325310653822	1.2056270831708467	1.2123218247005001	1.2190167673481853	1.2257119235295966	1.2324073064268297	1.2391029300356848	1.245798809215886	1.2524949597443977	1.2591913983720335	1.2658881428835553	1.2725852121614776	1.2792826262538168	1.2859804064460036	1.2926785753372458	1.2993771569215928	1.3060761766740001	1.3127756616417041	1.3194756405412262	1.326176143861362	1.3328772039725183	1.3395788552427896	1.3462811341611922	1.3529840794684886	1.3596877322960796	1.366392136313451	1.3730973378847084	1.3798033862347527	1.3865103336256925	1.3932182355441205	1.3999271508999247	1.4066371422373374	1.4133482759589793	1.4200606225636891	1.4267742568989914	1.4334892584290959	1.440205711519382	1.4469237057383793	1.4536433361783103	1.4603647037953398	1.4670879157707291	1.4738130858941791	1.4805403349707142	1.4872697912525419	1.4940015908974211	1.5007358784551472	1.5074728073838692	1.5142125405980604	1.5209552510500559	1.5277011223472106	1.5344503494068316	1.5412031391511762	1.5479597112449484	1.5547202988778546	1.5614851495949538	1.5682545261776761	1.5750287075785683	1.5818079899129978	1.5885926875112311	1.5953831340345175	1.6021796836589979	1.6089827123314935	1.6157926191014635	1.6226098275336511	1.6294347872062205	1.636267975299398	1.6431098982800614	1.6499610936877858	1.6568221320283949	1.6636936187812708	1.6705761965270403	1.6774705472026372	1.6843773944910885	1.6912975063537781	1.6982316977133489	1.7051808332958205	1.7121458306409432	1.7191276632902668	1.7261273641628654	1.7331460291291576	1.7401848207937505	1.7472449724987509	1.754327792559522	1.7614346687453779	1.768567073018275	1.7757265665430875	1.7829148049836143	1.7901335440990127	1.7973846456558877	1.8046700836718161	1.8119919510065814	1.8193524663178977	1.8267539813988629	1.8341989889147912	1.84169013055746	1.8492302056350978	1.8568221801166789	1.8644691961492281	1.8721745820668592	1.8799418629101796	1.8877747714744426	1.8956772599043803	1.9036535118530447	1.9117079552210803	1.9198452754917423	1.92807042967549	1.9363886608761942	1.9448055134887836	1.9533268490354767	1.9619588626445834	1.9707081001720892	1.9795814759618302	1.9885862912349495	1.9977302530933752	2.0070214941152549	2.0164685925124526	2.0260805928113212	2.035867027007864	2.0458379361369969	2.0560038921828059	2.0663760202423167	2.0769660208392682	2.0877861922665741	2.0988494528164097	2.1101693627351641	2.1217601457165967	2.1336367097204834	2.1458146668756761	2.1583103521957976	2.171140840802765	2.1843239633179801	2.1978783190434323	2.2118232865152767	2.226179030970886	2.2409665082272672	2.2562074644243437	2.2719244310419864	2.2881407145543169	2.3048803800413129	2.3221682280352898	2.3400297638408838	2.3584911585324799	2.3775792008044432	2.397321238828805	2.4177451112642285	2.4388790665615612	2.4607516697273364	2.4833916957401017	2.5068280088680859	2.5310894272133981	2.5562045719106603	2.5822017005393638	2.6091085244720862	2.6369520100771844	2.6657581639264025	2.6955518024262535	2.7263563065969425	2.7581933630633229	2.7910826926965169	2.8250417687485632	2.8600855267505052	2.8962260688889416	2.9334723660282664	2.971829960994008	3.011300677163617	3.0518823368098245	3.0935684939915089	3.1363481870706371	3.1802057161330675	3.2251204506881295	3.2710666730004618	3.3180134622526407	3.3659246244373424	3.4147586724253585	3.4644688600478228	3.5150032732707324	3.5663049806359144	3.6183122441111717	3.6709587903553969	3.7241741411904519	3.7778840008146597	3.8320106960305242	3.8864736645330975	3.9411899851568801	3.9960749429492255	4.0510426210651262	4.1060065107946517	4.1608801305670333	4.2155776445424786	4.2700144714134334	4.3241078742910748	4.3777775230398186	4.4309460211239182	4.4835393899185734	4.5354875044796898	4.5867244759235541	4.6371889767986474	4.6868245070951309	4.7355795997923487	4.7834079660530531	4.8302685813019668	4.8761257144472765	4.9209489033955176	4.9647128807576522	5.0073974542383457	5.0489873466395618	5.0894720006959133	5.1288453541028769	5.167105590107977	5.204254868929727	5.2402990450609614	5.2752473752233051	5.309112221384698	5.3419087528497187	5.3736546509993328	5.4043698198077577	5.4340761048121058	5.4627970227669866	5.4970121837399617	5.5302930073025811	5.5626665333504546	5.5941605287476808	5.6248032899397584	5.6546234617136237	5.6836498720048674	5.7119113824586929	5.7394367542912033	5.7662545288688118	5.7923929223232857	5.8178797334453227	5.8427422640479012	5.8670072509586593	5.8907008087859509	5.9138483826029073	5.9364747097055677	5.9586037896226953	5.9802588615840113	6.0014623886887248	6.0222360480556079	6.0426007262782129	6.0625765195529526	6.0821827378926487	6.1014379128830427	6.1203598084839781	6.1389654344199363	6.1572710617460649	6.175292240215315	6.1930438171096833	6.2105399572337765	6.227794163801665	6.2448192999785439	6.2616276108668414	6.278230745752313	6.2946397804493319	6.3108652396060894	6.3269171188500914	6.342804906671847	6.3585376059606169	6.37412375512032	6.3895714487062927	6.4048883575350466	6.4200817482289683	6.4351585021668551	6.4501251338188341	6.4649878084509522	6.4797523591906252	6.4944243034491533	6.5090088587018586	6.5235109576301822	6.5379352626330522	6.5522861797176564	6.5665678717817437	6.5807842713014972	6.5949390924403506	6.6090358425952873	6.6230778333980318	6.6370681911889955	6.6510098669826343	6.6649056459425662	6.6787581563853777	6.6925698783317653	6.7063431516235186	6.7200801836247015	6.7337830565250103	6.7474537342629164	6.7610940690858339	6.7747058077639819	6.7882905974742478	6.8018499913697363	6.8153854538501841	6.8288983655479365	6.8423900280435195	6.8558616683243887	6.8693144429998689	6.8827494422846947	6.8961676937631209	6.9095701659449871	6.9229577716246036	6.9363313710528924	6.9496917749326412	6.9630397472463468	6.9763760079255892	6.9897012353705215	7.003016068827562	7.0163211106330126	7.0296169283299585	7.0429040566653534	7.0561829994739096	7.0694542314550759	7.0827181998489497	7.0959753260168386	7.1092260069317001	7.1224706165835423	7.1357095073045453	7.148943011018388	7.1621714404180654	7.1753950900762273	7.1886142374918247	7.2018291440767062	7.215040056085523	7.2282472054922104	7.2414508108160351	7.2546510779000997	7.2678482006450302	7.2810423617003588	7.2942337331160783	7.3074224769565879	7.3206087458792188	7.3337926836793583	7.3469744258040866	7.3601540998361301	7.3733318259498644	7.3865077173409022	7.3996818806308848	7.4128544162488188	7.4260254187903554	7.4391949773562693	7.4523631758713265	7.4655300933847037	7.4786958043529754	7.4918603789067353	7.5050238831017335	7.5181863791554706	7.5313479256700857	7.5445085778422811	7.5576683876611357	7.5708274040943362	7.583985673263749	1.56 x 150i	20	20.100000000000001	20.2	20.3	20.399999999999999	20.5	20.6	20.7	20.8	20.9	21	21.1	21.2	21.3	21.4	21.5	21.6	21.7	21.8	21.9	22	22.1	22.2	22.3	22.4	22.5	22.6	22.7	22.8	22.9	23	23.1	23.2	23.3000000000001	23.4	23.5	23.600000000000101	23.7	23.8000000000001	23.900000000000102	24.000000000000099	24.100000000000101	24.200000000000099	24.3000000000001	24.400000000000102	24.500000000000099	24.600000000000101	24.700000000000099	24.8000000000001	24.900000000000102	25.000000000000099	25.100000000000101	25.200000000000099	25.3000000000001	25.400000000000102	25.500000000000099	25.600000000000101	25.700000000000099	25.8000000000001	25.900000000000102	26.000000000000099	26.100000000000101	26.200000000000099	26.3000000000001	26.400000000000102	26.500000000000099	26.600000000000101	26.700000000000099	26.8000000000001	26.900000000000102	27.000000000000099	27.100000000000101	27.200000000000099	27.3000000000001	27.400000000000102	27.500000000000099	27.600000000000101	27.700000000000099	27.8000000000001	27.900000000000102	28.000000000000099	28.100000000000101	28.200000000000099	28.3000000000001	28.400000000000102	28.500000000000099	28.600000000000101	28.700000000000099	28.8000000000001	28.900000000000102	29.000000000000099	29.100000000000101	29.200000000000099	29.3000000000001	29.400000000000102	29.500000000000099	29.600000000000101	29.700000000000099	29.8000000000001	29.900000000000102	30.000000000000099	30.100000000000101	30.200000000000099	30.3000000000001	30.400000000000102	30.500000000000099	30.6000000000002	30.700000000000198	30.8000000000002	30.900000000000201	31.000000000000199	31.1000000000002	31.200000000000198	31.3000000000002	31.400000000000201	31.500000000000199	31.6000000000002	31.700000000000198	31.8000000000002	31.900000000000201	32.000000000000199	32.1000000000002	32.200000000000202	32.300000000000203	32.400000000000198	32.500000000000199	32.6000000000002	32.700000000000202	32.800000000000203	32.900000000000198	33.000000000000199	33.1000000000002	33.200000000000202	33.300000000000203	33.400000000000198	33.500000000000199	33.6000000000002	33.700000000000202	33.800000000000203	33.900000000000198	34.000000000000199	34.1000000000002	34.200000000000202	34.300000000000203	34.400000000000198	34.500000000000199	34.6000000000002	34.700000000000202	34.800000000000203	34.900000000000198	35.000000000000199	35.1000000000002	35.200000000000202	35.300000000000203	35.400000000000198	35.500000000000199	35.6000000000002	35.700000000000202	35.800000000000203	35.900000000000198	36.000000000000199	36.1000000000002	36.200000000000202	36.300000000000203	36.400000000000198	36.500000000000199	36.6000000000002	36.700000000000202	36.800000000000203	36.900000000000198	37.000000000000199	37.1000000000002	37.200000000000202	37.300000000000203	37.400000000000198	37.500000000000199	37.6000000000003	37.700000000000301	37.800000000000303	37.900000000000297	38.000000000000298	38.1000000000003	38.200000000000301	38.300000000000303	38.400000000000297	38.500000000000298	38.6000000000003	38.700000000000301	38.800000000000303	38.900000000000297	39.000000000000298	39.1000000000003	39.200000000000301	39.300000000000303	39.400000000000297	39.500000000000298	39.6000000000003	39.700000000000301	39.800000000000303	39.900000000000297	40.000000000000298	40.1000000000003	40.200000000000301	40.300000000000303	40.400000000000297	40.500000000000298	40.6000000000003	40.700000000000301	40.800000000000303	40.900000000000297	41.000000000000298	41.1000000000003	41.200000000000301	41.300000000000303	41.400000000000297	41.500000000000298	41.6000000000003	41.700000000000301	41.800000000000303	41.900000000000297	42.000000000000298	42.1000000000003	42.200000000000301	42.300000000000303	42.400000000000297	42.500000000000298	42.6000000000003	42.700000000000301	42.800000000000303	42.900000000000297	43.000000000000298	43.1000000000003	43.200000000000301	43.300000000000303	43.400000000000297	43.500000000000298	43.6000000000003	43.700000000000301	43.800000000000303	43.900000000000297	44.000000000000298	44.1000000000003	44.200000000000301	44.300000000000303	44.400000000000297	44.500000000000298	44.6000000000003	44.700000000000401	44.800000000000402	44.900000000000396	45.000000000000398	45.100000000000399	45.200000000000401	45.300000000000402	45.400000000000396	45.500000000000398	45.600000000000399	45.700000000000401	45.800000000000402	45.900000000000396	46.000000000000398	46.100000000000399	46.200000000000401	46.300000000000402	46.400000000000396	46.500000000000398	46.600000000000399	46.700000000000401	46.800000000000402	46.900000000000396	47.000000000000398	47.100000000000399	47.200000000000401	47.300000000000402	47.400000000000396	47.500000000000398	47.600000000000399	47.700000000000401	47.800000000000402	47.900000000000396	48.000000000000398	48.100000000000399	48.200000000000401	48.300000000000402	48.400000000000396	48.500000000000398	48.600000000000399	48.700000000000401	48.800000000000402	48.900000000000396	49.000000000000398	49.100000000000399	49.200000000000401	49.300000000000402	49.400000000000396	49.500000000000398	49.600000000000399	49.700000000000401	49.800000000000402	49.900000000000396	50.000000000000398	50.100000000000399	50.200000000000401	50.300000000000402	50.400000000000396	50.500000000000398	50.600000000000399	50.700000000000401	50.800000000000402	50.900000000000396	51.000000000000398	51.100000000000399	51.200000000000401	51.300000000000402	51.400000000000396	51.500000000000398	51.600000000000399	51.7000000000005	51.800000000000502	51.900000000000503	52.000000000000497	52.100000000000499	52.2000000000005	52.300000000000502	52.400000000000503	52.500000000000497	52.600000000000499	52.7000000000005	52.800000000000502	52.900000000000503	53.000000000000497	53.100000000000499	53.2000000000005	53.300000000000502	53.400000000000503	53.500000000000497	53.600000000000499	53.7000000000005	53.800000000000502	53.900000000000503	54.000000000000497	54.100000000000499	54.2000000000005	54.300000000000502	54.400000000000503	54.500000000000497	54.600000000000499	54.7000000000005	54.800000000000502	54.900000000000503	55.000000000000497	55.100000000000499	55.2000000000005	55.300000000000502	55.400000000000503	55.500000000000497	55.600000000000499	55.7000000000005	55.800000000000502	55.900000000000503	56.000000000000497	56.100000000000499	56.2000000000005	56.300000000000502	56.400000000000503	56.500000000000497	56.600000000000499	56.7000000000005	56.800000000000502	56.900000000000503	57.000000000000497	57.100000000000499	57.2000000000005	57.300000000000502	57.400000000000503	57.500000000000497	57.600000000000499	57.7000000000005	57.800000000000502	57.900000000000503	58.000000000000497	58.100000000000499	58.2000000000005	58.300000000000502	58.400000000000503	58.500000000000497	58.600000000000499	58.7000000000005	58.800000000000601	58.900000000000603	59.000000000000597	59.100000000000598	59.2000000000006	59.300000000000601	59.400000000000603	59.500000000000597	59.600000000000598	59.7000000000006	59.800000000000601	59.900000000000603	60.000000000000597	60.100000000000598	60.2000000000006	60.300000000000601	60.400000000000603	60.500000000000597	60.600000000000598	60.7000000000006	60.800000000000601	60.900000000000603	61.000000000000597	61.100000000000598	61.2000000000006	61.300000000000601	61.400000000000603	61.500000000000597	61.600000000000598	61.7000000000006	61.800000000000601	61.900000000000603	62.000000000000597	62.100000000000598	62.2000000000006	62.300000000000601	62.400000000000603	62.500000000000597	62.600000000000598	62.7000000000006	62.800000000000601	62.900000000000603	63.000000000000597	63.100000000000598	63.2000000000006	63.300000000000601	63.400000000000603	63.500000000000597	63.600000000000598	63.7000000000006	63.800000000000601	63.900000000000603	64.000000000000597	64.100000000000605	64.2000000000006	64.300000000000594	64.400000000000603	64.500000000000597	64.600000000000605	64.7000000000006	64.800000000000594	64.900000000000603	65.000000000000597	65.100000000000605	65.2000000000006	65.300000000000594	65.400000000000603	65.500000000000597	65.600000000000605	65.7000000000006	65.800000000000693	65.900000000000702	66.000000000000696	66.100000000000705	66.200000000000699	66.300000000000693	66.400000000000702	66.500000000000696	66.600000000000705	66.700000000000699	66.800000000000693	66.900000000000702	67.000000000000696	67.100000000000705	67.200000000000699	67.300000000000693	67.400000000000702	67.500000000000696	67.600000000000705	67.700000000000699	67.800000000000693	67.900000000000702	68.000000000000696	68.100000000000705	68.200000000000699	68.300000000000693	68.400000000000702	68.500000000000696	68.600000000000705	68.700000000000699	68.800000000000693	68.900000000000702	69.000000000000696	69.100000000000705	69.200000000000699	69.300000000000693	69.400000000000702	69.500000000000696	69.600000000000705	69.700000000000699	69.800000000000693	69.900000000000702	70.000000000000696	70.100000000000705	70.200000000000699	70.300000000000693	70.400000000000702	70.500000000000696	70.600000000000705	70.700000000000699	70.800000000000693	70.900000000000702	71.000000000000696	71.100000000000705	71.200000000000699	71.300000000000693	71.400000000000702	71.500000000000696	71.600000000000705	71.700000000000699	71.800000000000693	71.900000000000702	72.000000000000696	72.100000000000705	72.200000000000699	72.300000000000693	72.400000000000702	72.500000000000696	72.600000000000705	72.700000000000699	72.800000000000793	72.900000000000801	73.000000000000796	-4.0250545489469783E-2	-2.9753683403573015E-2	-1.9256821312526332E-2	-8.7599592160110765E-3	1.7369028863096544E-3	1.2233764994794996E-2	2.2730627109825166E-2	3.3227489231803881E-2	4.372435136116086E-2	5.4221213498350886E-2	6.4718075643858272E-2	7.5214937798196518E-2	8.5711799961909738E-2	9.6208662135577799E-2	0.10670552431981459	0.11720238651527333	0.12769924872264646	0.13819611094266918	0.14869297317612323	0.15918983542383702	0.16968669768669173	0.18018355996562169	0.19068042226161902	0.20117728457573819	0.21167414690909722	0.22217100926288472	0.23266787163836181	0.24316473403686653	0.25366159645982167	0.26415845890873596	0.27465532138521287	0.28515218389095365	0.29564904642776468	0.30614590899757521	0.31664277160239002	0.32713963424440345	0.33763649692591102	0.3481333596493188	0.35863022241725739	0.36912708523244292	0.3796239480978032	0.39012081101643686	0.40061767399163156	0.41111453702688033	0.42161140012589032	0.43210826329259772	0.44260512653118284	0.45310198984608241	0.46359885324200878	0.47409571672396383	0.48459258029725849	0.49508944396753274	0.50558630774077307	0.51608317162333706	0.52658003562197397	0.53707689974384965	0.54757376399657276	0.55807062838822108	0.56856749292737241	0.57906435762313291	0.58956122248517073	0.60005808752375256	0.61055495274977678	0.62105181817481669	0.63154868381115858	0.64204554967184768	0.65254241577073513	0.66303928212252627	0.67353614874283541	0.68403301564824059	0.69452988285634154	0.70502675038582752	0.71552361825653932	0.7260204864895442	0.73651735510720906	0.74701422413328167	0.75751109359297697	0.76800796351306522	0.77850483392197078	0.78900170484987198	0.79949857632881005	0.80999544839280579	0.82049232107797854	0.83098919442267905	0.84148606846762541	0.85198294325604829	0.86247981883384939	0.87297669524976251	0.88347357255553161	0.8939704508060945	0.90446733005978008	0.91496421037851994	0.92546109182806757	0.93595797447823748	0.9464548584031528	0.95695174368151392	0.96744863039688012	0.9779455186379683	0.98844240849897436	0.99893930007990839	1.0094361934869536	1.0199330888328524	1.030429986237305	1.0409268858274012	1.051423787738079	1.0619206921126052	1.0724175991031053	1.0829145088710594	1.0934114215879551	1.1039083374358529	1.1144052566080545	1.1249021793097951	1.1353991057589803	1.1458960361869712	1.1563929708394096	1.166889909977104	1.1773868538769645	1.1878838028329965	1.1983807571573586	1.2088777171814791	1.2193746832572492	1.2298716557582841	1.2403686350812662	1.2508656216473673	1.2613626159037616	1.271859618325232	1.2823566294158721	1.2928536497108973	1.3033506797785661	1.313847720222219	1.3243447716824479	1.3348418348393907	1.3453389104151763	1.3558359991765163	1.3663331019374563	1.376830219562301	1.3873273529687142	1.3978245031310121	1.4083216710836648	1.4188188579250072	1.4293160648211836	1.439813293010332	1.4503105438070292	1.4608078186070117	1.4713051188921831	1.4818024462359387	1.4922998023088077	1.5027971888844547	1.5132946078460443	1.5237920611930016	1.5342895510481924	1.5447870796655399	1.5552846494381172	1.5657822629067384	1.5762799227690794	1.5867776318893616	1.597275393308633	1.6077732102556859	1.6182710861586453	1.6287690246572761	1.6392670296160505	1.6497651051380158	1.6602632555795245	1.6707614855658734	1.6812598000079046	1.6917582041196357	1.7022567034369704	1.7127553038375745	1.723254011561973	1.7337528332359469	1.7442517758943212	1.7547508470062101	1.765250054501829	1.7757494068009585	1.7862489128431638	1.7967485821198836	1.8072484247085039	1.8177484513084869	1.8282486732798344	1.8387491026838187	1.8492497523262801	1.8597506358035842	1.8702517675514208	1.880753162896607	1.8912548381120924	1.9017568104753597	1.9122590983304206	1.9227617211536472	1.9332646996236578	1.9437680556955206	1.9542718126795324	1.9647759953248554	1.9752806299083192	1.985785744328697	1.996291368206796	2.0067975329917336	2.0173042720737469	2.0278116209039809	2.0383196171216551	2.0488283006890708	2.05933771403495	2.0698479022066061	2.0803589130314988	2.0908707972887544	2.1013836088912492	2.1118974050789294	2.1224122466240316	2.1329281980489618	2.1434453278575956	2.1539637087808283	2.1644834180372583	2.1750045376099187	2.1855271545400581	2.196051361239014	2.2065772558192815	2.2171049424459714	2.2276345317098878	2.2381661410235751	2.2486998950417245	2.2592359261074404	2.2697743747259564	2.2803153900674675	2.2908591305008725	2.3014057641603176	2.3119554695465392	2.3225084361651391	2.3330648652040402	2.343624970252522	2.3541889780643661	2.3647571293677965	2.375329679725076	2.3859069004447591	2.396489079549819	2.407076522805037	2.4176695548072353	2.428268520142181	2.4388737846121753	2.4494857365386129	2.4601047881440272	2.4707313770184167	2.4813659676749213	2.4920090532002055	2.5026611570052482	2.5133228346825289	2.523994675975969	2.5346773068703623	2.5453713918073761	2.5560776360356652	2.5667967881029559	2.5775296424986429	2.5882770424555446	2.5990398829202945	2.609819113702188	2.620615742810863	2.6314308399937922	2.6422655404851163	2.6531210489779808	2.6639986438331764	2.6748996815375388	2.6858256014262634	2.6967779306839921	2.7077582896402812	2.7187683973758148	2.7298100776565137	2.7408852652134899	2.7519960123876328	2.7631444961584299	2.7743330255775027	2.7855640496281753	2.7968401655332649	2.8081641275341513	2.8195388561650101	2.8309674480469642	2.8424531862276878	2.853999551092778	2.8656102318759431	2.8772891387956916	2.8890404158468166	2.9008684542754208	2.9127779067666095	2.9247737023741891	2.936861062221741	2.9490455160043072	2.9613329193195099	2.9737294718562506	2.9862417364681551	2.9988766591575442	3.0116415899939364	3.0245443049887908	3.0375930289453654	3.0507964592991113	3.0641637909598054	3.0777047421616781	3.0914295813218664	3.1053491549006198	3.1194749162486497	3.133818955417691	3.1483940298996611	3.1632135962475161	3.1782918425169675	3.1936437214523665	3.2092849843221858	3.225232215289414	3.2415028661796348	3.258115291484414	3.2750887834096902	3.2924436067478831	3.3102010333184038	3.3283833756837464	3.3470140198074865	3.3661174562760054	3.3857193096576093	3.4058463655208948	3.426526594578748	3.4477891733654102	3.4696645007917635	3.4921842098588205	3.5153811737417562	3.5392895053871984	3.563944549696493	3.5893828672965187	3.6156422088313778	3.6427614786417108	3.670780686637269	3.6997408871139785	3.7296841032218926	3.7606532357579407	3.7926919549404006	3.8258445738243454	3.8601559020425058	3.8956710786085567	3.9324353826039813	3.9704940206899435	4.0098918905467302	4.0506733195494249	4.0928817782439282	4.1365595684956631	4.1817474865469482	4.2284844616401172	4.2768071713417246	4.3267496352377162	4.378342789256326	4.4316140435087892	4.486586827209444	4.543280124934264	4.6017080091862033	4.6618791749388082	4.7237964825055823	4.7874565157080982	4.85284916286464	4.9199572285660684	4.98875608451812	5.0592133678817062	5.131288735509175	5.2049336822314194	5.280091430880427	5.3566969010221799	5.4346767624210992	5.5139495780645742	5.5944260401581705	5.6760093008840844	5.7585953979319502	5.8420737729066836	5.9263278787463172	6.0112358703027047	6.0966713703144784	6.1825043011999217	6.2686017714818174	6.3548290042867341	6.4410502942888055	6.5271299787350898	6.6129334078242028	6.6983278997266167	6.7831836659335449	6.8673746933853179	6.9507795709302407	7.0332822490584581	7.114772723489506	7.1951476350073884	7.2743107798680011	7.3521735270854851	7.4286551408724817	7.5036830084048312	7.5771927748521213	7.6491283892171547	7.7194420659263896	7.788094168285836	7.8550530208489322	7.9202946584318319	7.9838025199606193	8.045567095560374	8.1055855353101229	8.1638612279224905	8.2204033572803308	8.2752264443079007	8.3283498810975019	8.3797974635816175	8.4295969283611942	8.4777794985964139	8.5243794431572564	8.5694336525354409	8.623106624576458	8.675313911106235	8.7260979293316385	8.775502236847549	8.82357122199776	8.870349819565698	8.9158832516382116	8.9602167931820667	9.0033955616219359	9.0454643295065367	9.08646735919233	9.1264482583571276	9.1654498550748862	9.2035140911328561	9.2406819322492826	9.2769932938493689	9.3124869810756614	9.3472006417427433	9.3811707309918919	9.4144324864564126	9.4470199128101573	9.4789657746381799	9.5103015966376461	9.5410576702275911	9.5712630657164688	9.6009456492458654	9.6301321037960879	9.6588479536044414	9.687117591408871	9.7149643079883425	9.7424103235265402	9.7694768203768607	9.7961839768545964	9.8225510017263158	9.8485961691070862	9.8743368535133023	9.8997895648526164	9.9249699831633649	9.949892992943278	9.9745727169323839	9.9990225492373277	10.023255187704031	10.047282665463666	10.071116381592233	10.094767130838063	10.118245132383617	10.1415600576185	10.164721056909855	10.187736785364191	10.210615427581523	10.233364721408631	10.255991980702884	10.278504117122564	10.300907660962666	10.32320878105824	10.345413303779361	10.367526731143704	10.38955425807398	10.411500788828324	10.433370952632842	10.455169118545131	10.47689940957846	10.498565716115854	10.520171708643128	10.541720849829646	10.563216405985024	10.584661457919397	10.606058911234285	10.62741150607021	10.64872182633666	10.669992308448975	10.691225249596005	10.712422815561546	10.733587048121615	10.754719872038851	10.775823101674435	10.796898447237039	10.817947520687541	10.838971841317393	10.859972841017665	10.880951869255156	10.901910197771011	10.922849025016736	10.943769480341617	10.964672627945012	10.985559470606225	11.006430953204028	11.027287966037441	11.048131347958526	11.068961889327623	11.089780334800892	11.110587385959287	11.131383703787963	11.152169911014331	11.17294659431268	11.193714306382887	11.21447356791022	11.235224869412974	11.255968672984242	11.276705413933785	11.297435502335684	11.318159324487088	11.338877244283127	11.359589604512735	11.380296728079875	11.400998919154469	11.421696464256966	11.442389633280424	11.463078680453604	11.483763845248495	11.504445353235447	11.525123416888903	11.545798236346581	11.566470000124786	11.587138885792319	11.607805060605454	11.628468682106144	11.649129898685613	11.669788850115337	11.690445668047232	11.711100476484932	11.731753392227702	11.752404525288686	11.773053979288859	11.793701851828176	11.814348234835215	11.834993214896473	11.855636873566686	11.876279287660962	11.896920529530199	Outlet Temperature (°C)


Energy Stored (kWh)



Test 1 (6 kW, 5 LPM)	38.658999999999999	39.027099999999997	39.936999999999998	41.4	43.3	45.5	47.6	49.6	51.7	53.6	55.5	57.1	58.7	60.3	61.5	62.8	63.9	65	66	66.8	67.5	68.099999999999994	68.7	69.099999999999994	69.599999999999994	69.900000000000006	70.400000000000006	70.7	71	71.3	71.5	71.599999999999994	71.7	72	72.2	72.400000000000006	72.5	72.5	72.7	72.8	72.900000000000006	73.099999999999994	73.400000000000006	73.599999999999994	73.8	74	74.3	74.599999999999994	74.900000000000006	75.3	75.7	76.099999999999994	76.7	77.400000000000006	78.3	79.5	80.8	82	0	0.21013966666666589	0.41144233333334795	0.6059423333333479	0.79669233333334788	0.98674788888890341	1.1747201111111256	1.3614145555555701	1.5486367777777923	1.7356645555555701	1.9247201111111258	2.1145534444444589	2.3032478888889036	2.4942478888889035	2.6844145555555703	2.8762201111111261	3.0684701111111261	3.2627756666666814	3.4579145555555706	3.6554701111111263	3.8499423333333485	4.047859000000015	4.2433312222222375	4.4414701111111263	4.6405534444444596	4.8405812222222364	5.0396923333333481	5.2404145555555699	5.4402756666666807	5.6399145555555696	5.8394423333333476	6.0398312222222366	6.2404701111111249	6.4429701111111255	6.6449145555555695	6.846192333333347	7.0478034444444582	7.2474423333333471	7.4466645555555697	7.6446645555555692	7.8422756666666809	8.0384701111111259	8.2362756666666801	8.4323867777777917	8.6301367777777909	8.8278867777777918	9.0228590000000146	9.2184423333333481	9.4136090000000152	9.6079145555555705	9.8020534444444589	9.9956923333333485	10.187442333333349	10.37630344444446	10.564081222222239	10.748275666666682	10.929636777777795	11.10855344444446	Test 2 (6 kW, 10 LPM)	33	35.299999999999997	37.700000000000003	39.9	42.1	44.2	46.1	47.9	49.7	51.4	52.9	54.4	55.7	56.8	57.9	58.8	59.6	60.4	61	61.5	61.9	62.3	62.7	63	63.2	63.5	63.7	63.8	64.099999999999994	64.2	64.3	64.5	64.599999999999994	64.7	64.900000000000006	65	65.099999999999994	65.2	65.400000000000006	65.5	65.7	65.900000000000006	66.2	66.5	66.900000000000006	67.3	67.900000000000006	68.7	69.599999999999994	70.5	71.5	72.599999999999994	73.7	74.900000000000006	76	76.8	0.8	0.98888533333333273	1.1775199999999986	1.3663153333333313	1.5554806666666641	1.74429233333333	1.9316999999999966	2.1196603333333299	2.3069509999999966	2.4958606666666761	2.6848720000000084	2.8746096666666743	3.0636893333333406	3.2548793333333403	3.4477640000000056	3.6401373333333389	3.8345510000000047	4.0297923333333383	4.2259653333333382	4.4216900000000052	4.6189146666666714	4.8164106666666715	5.0159220000000042	5.2145043333333376	5.4133126666666742	5.61306333333334	5.8130626666666725	6.0143790000000061	6.2150986666666723	6.4165413333333383	6.6183703333333375	6.8199016666666701	7.0211473333333361	7.2214363333333349	7.4213923333333343	7.6214976666666665	7.8211959999999987	8.0211786666666658	8.2210389999999975	8.4211836666666802	8.619890000000014	8.8169410000000124	9.0138113333333454	9.2092863333333455	9.403559000000012	9.5957493333333446	9.7850710000000092	9.9723373333333427	10.156495666666677	10.340788000000009	10.522201666666673	10.700448333333339	10.877768666666672	11.055868666666671	11.231266000000003	11.395241333333335	Test 3 (3 kW, 10 LPM)	25.6	26.5	35.4	36.5	37.4	38.4	39.4	40.299999999999997	41.2	42.1	43	43.8	44.7	45.4	46.2	47	47.7	48.5	49.2	49.8	50.4	51	51.7	52.2	52.8	53.3	53.8	54.2	54.7	55.1	55.4	55.8	56.1	56.4	56.7	57	57.4	57.8	58.9	59.1	59.3	59.4	59.5	59.6	59.9	60.1	60.2	60.3	60.5	60.6	60.8	61.5	62	62.9	64.099999999999994	65.599999999999994	66.5	67.400000000000006	69.2	70.099999999999994	71	72	72.900000000000006	74	75.3	77.2	79	0	9.5538666666666328E-2	0.82851433333333768	0.91853366666667069	1.008250333333337	1.0978233333333367	1.1860806666666697	1.2754683333333361	1.3632840000000024	1.450569000000002	1.5389110000000015	1.6259083333333344	1.7126146666666675	1.7994103333333338	1.8862520000000003	1.9728283333333332	2.0594460000000065	2.145445666666673	2.2313853333333391	2.317201333333339	2.4030276666666719	2.4886613333333383	2.5745080000000047	2.6598326666666714	2.7462583333333375	2.8325116666666705	2.9184850000000035	3.0057543333333365	3.0927183333333366	3.1795956666666694	3.2651360000000023	3.3516990000000018	3.4387366666666681	3.5254320000000012	3.6121880000000011	3.6988463333333343	3.8725239999999999	4.0456276666666664	4.7444436666666698	4.919952000000003	5.0953516666666685	5.2696963333333349	5.4451356666666673	5.620245999999999	5.9709403333333313	6.3215896666666707	6.6740003333333355	6.8507713333333351	7.2000479999999998	7.5502859999999972	7.8992943333333301	8.8569709999999997	9.2001106666666654	9.5361369999999983	9.8660186666666725	10.186830333333337	10.344485666666667	10.501561333333335	10.810382333333333	10.961247	11.110391666666668	11.258233000000001	11.404459999999998	11.549178999999997	11.763596333333338	12.04181866666667	12.314067666666668	Test 4 (3 kW, 5 LPM)	29.1	29.4	29.8	30.6	31.5	32.700000000000003	33.799999999999997	34.9	36	37	38.1	39.1	40	41	42	43	43.8	44.7	45.5	46.4	47.3	48	48.8	49.5	50.2	50.9	55.6	56.1	56.5	57	57.7	58.4	59	59.5	59.7	59.9	60.2	60.4	60.9	61.3	61.7	62	62.3	62.5	62.7	62.9	63.3	63.5	63.6	63.8	64	64.3	64.599999999999994	64.900000000000006	65.3	65.900000000000006	66.400000000000006	66.7	67.3	68.099999999999994	69	69.8	70.2	70.7	71.599999999999994	72.5	72.900000000000006	73.400000000000006	73.900000000000006	74.400000000000006	74.8	75.3	75.8	76.2	76.599999999999994	77.099999999999994	77.5	78	78.400000000000006	78.8	79.099999999999994	0	0.10260233333333298	0.20112999999999931	0.29551566666667312	0.38785000000000613	0.47924866666667248	0.57002366666667226	0.65958400000000528	0.75027100000000502	0.84049200000000468	0.93056700000000447	1.0199333333333374	1.1084050000000036	1.1965040000000033	1.2844516666666699	1.3729123333333362	1.4597500000000025	1.5465310000000023	1.6327336666666687	1.719300333333335	1.8056503333333345	1.8918003333333342	1.9770263333333338	2.0618799999999999	2.147237333333333	2.2321699999999995	2.996194000000004	3.0805893333333372	3.1655810000000035	3.249999000000003	3.4191316666666691	3.5893603333333357	3.7606113333333346	3.9309333333333334	4.0158566666666662	4.1012789999999999	4.1867123333333396	4.2706970000000055	4.525708666666671	4.7810996666666696	5.0401683333333365	5.2987003333333362	5.5570913333333349	5.815050666666667	6.0723126666666731	6.4149666666666718	6.9257833333333361	7.3488783333333414	7.6032063333333335	7.8569743333333388	8.1103903333333314	8.530929666666669	8.7813430000000015	9.1136273333333335	9.3592999999999993	9.6005393333333302	9.7599343333333284	9.9160983333333288	10.069315333333329	10.221111999999996	10.37132033333333	10.445938000000002	10.520226999999995	10.593200666666666	10.740276333333334	10.811828999999994	10.884000333333333	10.955962000000005	11.028365000000001	11.099843000000007	11.241756000000008	11.311887	11.382202666666672	11.451787333333332	11.521158333333339	11.590046666666666	11.658379000000004	11.725536666666665	11.79221166666667	11.85920733333333	11.924631000000003	Curve Fit	20	21	22	23	24	25	26	27	28	29	30	31	32	33	34	35	36	37	38	39	40	41	42	43	44	45	46	47	48	49	50	51	52	53	54	55	56	57	58	59	60	61	62	63	64	65	66	67	68	69	70	71	72	73	-0.40142770490712981	-0.28215898502791642	-0.16289026514869678	-4.3621545269461187E-2	7.564717460981786E-2	0.19491589448920954	0.31418461436889622	0.43345333424935567	0.5527220541318395	0.6719907740196257	0.79125949392130301	0.91052821385936744	1.029796933892748	1.1490656541758109	1.2683343751129195	1.3876030977633114	1.5068718249016715	1.6261405637963255	1.745409333486754	1.864678183847134	1.9839472455235401	2.1032168607450226	2.2224879259843151	2.3417627895573623	2.4610476028639048	2.5803584792629928	2.6997376257430545	2.8192955891500882	2.9393218459663943	3.0605739809158261	3.1850316826233405	3.3178478810938836	3.472297685566597	3.6816708857268945	4.0237549712783567	4.6493056218378133	5.726700440221709	7.1601625973550949	8.4646828704170485	9.311262588134932	9.7769723482153275	10.069319760785664	10.274035072842061	10.443536866403864	10.5993275671524	10.749844263001618	10.898341768282217	11.046067594125072	11.193498706735168	11.340817294359905	11.488092922901233	11.635352151417109	11.782605119163282	11.929855696850975	Inlet Temperature (°C)


Energy Stored (kWh)




Correction Temp	y = 0.2191x
R² = 0.9999

73.424434019987757	36.504514514539125	16.01379650160138	31.135318244466216	15.490000000000009	7.6899999999999977	3.3900000000000006	6.3900000000000006	Power / Flow Rate (kJ kg-1)


Correction Temperature (°C)



Correction Temp	
154.19666767326285	148.62782642484717	155.20850023220584	151.23739610199635	125.36886813341673	173.85171790235083	183.1349163011495	55.335704757670058	0	33.843099999999993	33.709999999999994	34.11	33.209999999999994	29.409999999999997	40.709999999999994	41.11	10.909999999999997	0	Power / Flow Rate (kJ kg-1)


Correction Temperature (°C)



Test 1 (6 kW, 5 LPM)	23.16899999999999	23.537099999999988	24.446999999999989	25.909999999999989	27.809999999999988	30.009999999999991	32.109999999999992	34.109999999999992	36.209999999999994	38.109999999999992	40.009999999999991	41.609999999999992	43.209999999999994	44.809999999999988	46.009999999999991	47.309999999999988	48.409999999999989	49.509999999999991	50.509999999999991	51.309999999999988	52.009999999999991	52.609999999999985	53.209999999999994	53.609999999999985	54.109999999999985	54.41	54.91	55.209999999999994	55.509999999999991	55.809999999999988	56.009999999999991	56.109999999999985	56.209999999999994	56.509999999999991	56.709999999999994	56.91	57.009999999999991	57.009999999999991	57.209999999999994	57.309999999999988	57.41	57.609999999999985	57.91	58.109999999999985	58.309999999999988	58.509999999999991	58.809999999999988	59.109999999999985	59.41	59.809999999999988	60.209999999999994	60.609999999999985	61.209999999999994	61.91	62.809999999999988	64.009999999999991	65.309999999999988	66.509999999999991	0	0.21013966666666589	0.41144233333334795	0.6059423333333479	0.79669233333334788	0.98674788888890341	1.1747201111111256	1.3614145555555701	1.5486367777777923	1.7356645555555701	1.9247201111111258	2.1145534444444589	2.3032478888889036	2.4942478888889035	2.6844145555555703	2.8762201111111261	3.0684701111111261	3.2627756666666814	3.4579145555555706	3.6554701111111263	3.8499423333333485	4.047859000000015	4.2433312222222375	4.4414701111111263	4.6405534444444596	4.8405812222222364	5.0396923333333481	5.2404145555555699	5.4402756666666807	5.6399145555555696	5.8394423333333476	6.0398312222222366	6.2404701111111249	6.4429701111111255	6.6449145555555695	6.846192333333347	7.0478034444444582	7.2474423333333471	7.4466645555555697	7.6446645555555692	7.8422756666666809	8.0384701111111259	8.2362756666666801	8.4323867777777917	8.6301367777777909	8.8278867777777918	9.0228590000000146	9.2184423333333481	9.4136090000000152	9.6079145555555705	9.8020534444444589	9.9956923333333485	10.187442333333349	10.37630344444446	10.564081222222239	10.748275666666682	10.929636777777795	11.10855344444446	Test 2 (6 kW, 10 LPM)	25.310000000000002	27.61	30.010000000000005	32.21	34.410000000000004	36.510000000000005	38.410000000000004	40.21	42.010000000000005	43.71	45.21	46.71	48.010000000000005	49.11	50.21	51.11	51.910000000000004	52.71	53.31	53.81	54.21	54.61	55.010000000000005	55.31	55.510000000000005	55.81	56.010000000000005	56.11	56.41	56.510000000000005	56.61	56.81	56.91	57.010000000000005	57.210000000000008	57.31	57.41	57.510000000000005	57.710000000000008	57.81	58.010000000000005	58.210000000000008	58.510000000000005	58.81	59.210000000000008	59.61	60.210000000000008	61.010000000000005	61.91	62.81	63.81	64.91	66.010000000000005	67.210000000000008	68.31	69.11	0.8	0.98888533333333273	1.1775199999999986	1.3663153333333313	1.5554806666666641	1.74429233333333	1.9316999999999966	2.1196603333333299	2.3069509999999966	2.4958606666666761	2.6848720000000084	2.8746096666666743	3.0636893333333406	3.2548793333333403	3.4477640000000056	3.6401373333333389	3.8345510000000047	4.0297923333333383	4.2259653333333382	4.4216900000000052	4.6189146666666714	4.8164106666666715	5.0159220000000042	5.2145043333333376	5.4133126666666742	5.61306333333334	5.8130626666666725	6.0143790000000061	6.2150986666666723	6.4165413333333383	6.6183703333333375	6.8199016666666701	7.0211473333333361	7.2214363333333349	7.4213923333333343	7.6214976666666665	7.8211959999999987	8.0211786666666658	8.2210389999999975	8.4211836666666802	8.619890000000014	8.8169410000000124	9.0138113333333454	9.2092863333333455	9.403559000000012	9.5957493333333446	9.7850710000000092	9.9723373333333427	10.156495666666677	10.340788000000009	10.522201666666673	10.700448333333339	10.877768666666672	11.055868666666671	11.231266000000003	11.395241333333335	Test 3 (3 kW, 10 LPM)	22.21	23.11	32.01	33.11	34.01	35.01	36.01	36.909999999999997	37.81	38.71	39.61	40.409999999999997	41.31	42.01	42.81	43.61	44.31	45.11	45.81	46.41	47.01	47.61	48.31	48.81	49.41	49.91	50.41	50.81	51.31	51.71	52.01	52.41	52.71	53.01	53.31	53.61	54.01	54.41	55.51	55.71	55.91	56.01	56.11	56.21	56.51	56.71	56.81	56.91	57.11	57.21	57.41	58.11	58.61	59.51	60.709999999999994	62.209999999999994	63.11	64.010000000000005	65.81	66.709999999999994	67.61	68.61	69.510000000000005	70.61	71.91	73.81	75.61	0	9.5538666666666328E-2	0.82851433333333768	0.91853366666667069	1.008250333333337	1.0978233333333367	1.1860806666666697	1.2754683333333361	1.3632840000000024	1.450569000000002	1.5389110000000015	1.6259083333333344	1.7126146666666675	1.7994103333333338	1.8862520000000003	1.9728283333333332	2.0594460000000065	2.145445666666673	2.2313853333333391	2.317201333333339	2.4030276666666719	2.4886613333333383	2.5745080000000047	2.6598326666666714	2.7462583333333375	2.8325116666666705	2.9184850000000035	3.0057543333333365	3.0927183333333366	3.1795956666666694	3.2651360000000023	3.3516990000000018	3.4387366666666681	3.5254320000000012	3.6121880000000011	3.6988463333333343	3.8725239999999999	4.0456276666666664	4.7444436666666698	4.919952000000003	5.0953516666666685	5.2696963333333349	5.4451356666666673	5.620245999999999	5.9709403333333313	6.3215896666666707	6.6740003333333355	6.8507713333333351	7.2000479999999998	7.5502859999999972	7.8992943333333301	8.8569709999999997	9.2001106666666654	9.5361369999999983	9.8660186666666725	10.186830333333337	10.344485666666667	10.501561333333335	10.810382333333333	10.961247	11.110391666666668	11.258233000000001	11.404459999999998	11.549178999999997	11.763596333333338	12.04181866666667	12.314067666666668	Test 4 (3 kW, 5 LPM)	22.71	23.009999999999998	23.41	24.21	25.11	26.310000000000002	27.409999999999997	28.509999999999998	29.61	30.61	31.71	32.71	33.61	34.61	35.61	36.61	37.409999999999997	38.31	39.11	40.01	40.909999999999997	41.61	42.41	43.11	43.81	44.51	49.21	49.71	50.11	50.61	51.31	52.01	52.61	53.11	53.31	53.51	53.81	54.01	54.51	54.91	55.31	55.61	55.91	56.11	56.31	56.51	56.91	57.11	57.21	57.41	57.61	57.91	58.209999999999994	58.510000000000005	58.91	59.510000000000005	60.010000000000005	60.31	60.91	61.709999999999994	62.61	63.41	63.81	64.31	65.209999999999994	66.11	66.510000000000005	67.010000000000005	67.510000000000005	68.010000000000005	68.41	68.91	69.41	69.81	70.209999999999994	70.709999999999994	71.11	71.61	72.010000000000005	72.41	72.709999999999994	0	0.10260233333333298	0.20112999999999931	0.29551566666667312	0.38785000000000613	0.47924866666667248	0.57002366666667226	0.65958400000000528	0.75027100000000502	0.84049200000000468	0.93056700000000447	1.0199333333333374	1.1084050000000036	1.1965040000000033	1.2844516666666699	1.3729123333333362	1.4597500000000025	1.5465310000000023	1.6327336666666687	1.719300333333335	1.8056503333333345	1.8918003333333342	1.9770263333333338	2.0618799999999999	2.147237333333333	2.2321699999999995	2.996194000000004	3.0805893333333372	3.1655810000000035	3.249999000000003	3.4191316666666691	3.5893603333333357	3.7606113333333346	3.9309333333333334	4.0158566666666662	4.1012789999999999	4.1867123333333396	4.2706970000000055	4.525708666666671	4.7810996666666696	5.0401683333333365	5.2987003333333362	5.5570913333333349	5.815050666666667	6.0723126666666731	6.4149666666666718	6.9257833333333361	7.3488783333333414	7.6032063333333335	7.8569743333333388	8.1103903333333314	8.530929666666669	8.7813430000000015	9.1136273333333335	9.3592999999999993	9.6005393333333302	9.7599343333333284	9.9160983333333288	10.069315333333329	10.221111999999996	10.37132033333333	10.445938000000002	10.520226999999995	10.593200666666666	10.740276333333334	10.811828999999994	10.884000333333333	10.955962000000005	11.028365000000001	11.099843000000007	11.241756000000008	11.311887	11.382202666666672	11.451787333333332	11.521158333333339	11.590046666666666	11.658379000000004	11.725536666666665	11.79221166666667	11.85920733333333	11.924631000000003	Curve Fit	20	21	22	23	24	25	26	27	28	29	30	31	32	33	34	35	36	37	38	39	40	41	42	43	44	45	46	47	48	49	50	51	52	53	54	55	56	57	58	59	60	61	62	63	64	65	66	67	68	69	70	71	72	73	-0.40142770490712981	-0.28215898502791642	-0.16289026514869678	-4.3621545269461187E-2	7.564717460981786E-2	0.19491589448920954	0.31418461436889622	0.43345333424935567	0.5527220541318395	0.6719907740196257	0.79125949392130301	0.91052821385936744	1.029796933892748	1.1490656541758109	1.2683343751129195	1.3876030977633114	1.5068718249016715	1.6261405637963255	1.745409333486754	1.864678183847134	1.9839472455235401	2.1032168607450226	2.2224879259843151	2.3417627895573623	2.4610476028639048	2.5803584792629928	2.6997376257430545	2.8192955891500882	2.9393218459663943	3.0605739809158261	3.1850316826233405	3.3178478810938836	3.472297685566597	3.6816708857268945	4.0237549712783567	4.6493056218378133	5.726700440221709	7.1601625973550949	8.4646828704170485	9.311262588134932	9.7769723482153275	10.069319760785664	10.274035072842061	10.443536866403864	10.5993275671524	10.749844263001618	10.898341768282217	11.046067594125072	11.193498706735168	11.340817294359905	11.488092922901233	11.635352151417109	11.782605119163282	11.929855696850975	Effective Temperature T* (°C)


Energy Stored (kWh)




T outlet (predicted)	
20.2	21.9	23.8	26	28.1	30.2	32.200000000000003	34	35.799999999999997	37.5	39	40.5	41.8	43	44.1	45.1	46	46.9	47.7	48.4	49.1	49.7	50.2	50.7	51.2	51.6	51.9	52.3	52.6	52.9	53.2	53.8	54	54.2	54.5	54.7	54.9	55	55.2	55.4	55.6	55.4	55.9	55.7	55.9	56.4	56.2	56.4	56.5	56.7	56.9	57	57.2	57.4	57.6	57.7	58	58.2	58.4	58.7	59	59.3	59.6	60	60.4	61	61.5	62.2	62.8	63.6	64.3	65.099999999999994	65.8	66.5	67.3	67.900000000000006	68.599999999999994	69.099999999999994	69.599999999999994	70.099999999999994	70.5	70.900000000000006	71.3	71.599999999999994	71.900000000000006	72.099999999999994	72.3	72.5	72.7	73	73.2	73.3	73.5	73.7	73.900000000000006	74	74.2	74.3	74.400000000000006	74.5	74.599999999999994	74.7	74.8	74.8	74.900000000000006	75	75	75	75.099999999999994	75.099999999999994	75.099999999999994	75.2	75.2	75.2	75.2	75.3	75.3	75.3	75.3	75.3	75.400000000000006	19.720590124552043	21.613931085728556	23.386335135341369	25.03742234028315	26.708301600714243	28.342611814704401	29.998139563215208	31.682650818987355	33.372458481797452	35.119523141080606	36.802362350917555	38.50358199923906	40.172719237842827	41.911899044771857	43.610830645129319	45.288269644446025	46.879011089119565	48.254354053556888	49.331038941398369	50.143453344552299	50.720405284129725	51.177268673330445	51.544026714848769	51.833434682348724	52.094888196110773	52.325568422462098	52.518898398356662	52.695530303921359	52.870929331761346	53.008811865286788	53.139610334623839	53.290901883597208	53.407570233084144	53.561960264990084	53.682943136383614	53.801489050848453	53.931013223930805	54.031935555651238	54.145640940642295	54.259071195528534	54.371266601055851	54.496623682402678	54.609701498587086	54.722989734322439	54.824214061395999	54.956245987847538	55.061714565542161	55.184746334895657	55.327454503891587	55.446717486990323	55.600085053005252	55.718294868851089	55.871825676856034	56.034664041711856	56.209128799561569	56.39597323258689	56.617777228254894	56.861170201166594	57.100919281078454	57.382599101069488	57.744518648897056	58.124065137587827	58.560602591883239	59.090190614435826	59.684762102329557	60.350316450912885	61.058518551234769	61.75918743595993	62.44652538704063	63.119487700449028	63.713128403121672	64.311200120112261	64.815197346511724	65.381900028708458	65.955187274702496	66.494176540435859	67.004912022839804	67.494957458650845	67.958557329474587	68.393596702233722	68.812707818605119	69.214900288408813	69.585442280770309	69.941617890575188	70.264731897305609	70.595237934495515	70.904993430328489	71.197159902491308	71.460035441061351	71.729828336592206	71.986899623145888	72.245699233505349	72.484307511788558	72.678044561052303	72.881370940339821	73.087603915689769	73.264722501588267	73.378877703293526	73.616355230297017	73.766336577007877	73.879709096522376	74.026863718499882	74.16697417090613	74.29939419940689	74.421378518832569	74.550147944015407	74.682956304033098	74.757005339638411	74.833012158800898	74.923199465428453	74.995956986943142	75.098126769098002	75.202173883406587	75.263810408826259	75.322978222080366	75.351166098174687	75.40069480014985	75.467603737628636	75.571025217222981	75.600231184812415	75.646536887707867	Measured Data (°C)


Predicted Values (°C) 



Energy (predicted)	
0.10318127844299813	0.3060440795415223	0.50357178886579557	0.69751241603994107	0.88849029063581664	1.0772937743905748	1.2652829944616322	1.4523367503878672	1.6393954720476052	1.8261953256457841	2.0127474944596573	2.1995515304528874	2.3870329008467528	2.5755299083798788	2.7642837512371585	2.9521386275724302	3.1394337164142914	3.3289656927661446	3.5174616989735976	3.7026137908460095	3.8847398735324283	4.0644362369556868	4.2387233532753923	4.4089441898931998	4.5754555235402448	4.7390966102064871	4.9004664128491511	5.0586161988791094	5.2147892461038898	5.3703934447896371	5.523478101245896	5.6717431152654587	5.8200559741982207	5.9657453378310841	6.1089783588377582	6.2514792009398183	6.3923022171244206	6.5325630731374238	6.6718480914767238	6.8106771571890814	6.9469466555856618	7.0834199431666782	7.2181911532011798	7.3528779825139381	7.4882261062965618	7.6189238867618503	7.7499046096361504	7.8812665756462827	8.011241782069078	8.1407010627217957	8.2692100471986922	8.3948513587174531	8.5199838197259901	8.6427192877467949	8.7639112733223303	8.8851095263044204	9.0037118237722567	9.1189944872770514	9.2330557089792791	9.3472511138671663	9.4600005969862266	9.5705989657027288	9.6798281780341604	9.7856082255412193	9.8898344254144952	9.9897627945649425	10.086270885208426	10.176371956102313	10.262297941779831	10.342716909239547	10.41986837233908	10.491605123624433	10.562274578221645	10.630158024083325	10.692317062890211	10.749801350679077	10.803496578501255	10.853486013749833	10.899715580319535	10.943133161924539	10.984081735739016	11.021347229627601	11.0562097129593	11.089778713985503	11.121889135222322	11.152000081438407	11.18015732606888	11.207381073742573	11.233607260600278	11.258181881702393	11.281125628331324	11.303018255051379	11.323988635908458	11.343629120417699	11.362742905246328	11.380567843040195	11.39702957950993	11.414151049308481	11.429211174486719	11.443133002861337	11.45686734952781	11.469613444458505	11.481680152182079	11.493590045473107	11.504701977625535	11.515022883825758	11.524894916008403	11.535583212610478	11.545127524148402	11.554439651288126	11.564437287798739	11.57337964914522	11.581665184086155	11.590302600826757	11.598958409456696	11.60685576360936	11.615153343918216	11.623348752437398	11.631255025722478	11.639522955243645	11.647063013537796	0	0.21011786127611293	0.41472959864960079	0.61378910056133806	0.81349033443241459	1.0136629293590664	1.214625745887278	1.4171934333872884	1.6203181227822765	1.8251402737280003	2.027532666665925	2.2289848586068799	2.4285198610382763	2.628291550407611	2.8241401732046296	3.0177210796808041	3.2049936427044692	3.3870127015353635	3.5678133516910764	3.7450326404838363	3.9195296338070196	4.0906062074281957	4.2597542466254215	4.4248609590195622	4.5878342724441552	4.7485221833615903	4.9066104031045263	5.0636920196123407	5.2181355851917237	5.3719768490170026	5.5264948585479647	5.680405651975688	5.8318233983800916	5.9840545549749091	6.1328079266710072	6.2815828867679615	6.4292336014385265	6.5769376730535356	6.7244469040086896	6.8719426863677455	7.017571328184621	7.1616488831903151	7.3060696743869888	7.448695938975451	7.5907222618431263	7.7336567715798719	7.8736463335201536	8.013601902365231	8.154924963512677	8.2943262942363702	8.4335823042434885	8.5707888745441867	8.7065483262160512	8.8405839406298838	8.9730072042190763	9.1025525523861823	9.2327763043495192	9.3605356198706993	9.4841382019596256	9.6081343164065771	9.731141200845844	9.8519997327364859	9.9707856600182954	10.087402292151348	10.198477633026213	10.307332977947929	10.410675618296121	10.508937050901235	10.602065772350505	10.68967770886376	10.771326611513487	10.851274818482404	10.927598606922347	11.004796784195223	11.07919941657093	11.149098792393877	11.215302140181258	11.278807170412573	11.338874841178166	11.395242946728724	11.449529018017758	11.501628275946862	11.549626920472292	11.595761002208286	11.639386254610448	11.682197933064748	11.722319207936614	11.760161122351503	11.79598401334947	11.830929699818476	11.864226637479844	11.895971474928205	11.925104297368442	11.95197088567447	11.97830709920234	12.003245271754311	12.026187127823052	12.048072993212461	12.071731385705286	12.091156665515122	12.109387237339416	12.128446828185607	12.146593840036331	12.163746637384589	12.179545302837441	12.194451348545281	12.20811358690062	12.219471684338025	12.231089046288721	12.242771611836821	12.253965941286868	12.265427774714855	12.275361428443579	12.283341582927326	12.291009800710137	12.298206262796185	12.30639605492342	12.315054940206315	12.323133271530226	12.328688418723832	12.334695112423395	Measured Data (kWh)


Predicted Values (kWh) 



Energy (predicted)	
0.10318127844299813	0.3060440795415223	0.50357178886579557	0.69751241603994107	0.88849029063581664	1.0772937743905748	1.2652829944616322	1.4523367503878672	1.6393954720476052	1.8261953256457841	2.0127474944596573	2.1995515304528874	2.3870329008467528	2.5755299083798788	2.7642837512371585	2.9521386275724302	3.1394337164142914	3.3289656927661446	3.5174616989735976	3.7026137908460095	3.8847398735324283	4.0644362369556868	4.2387233532753923	4.4089441898931998	4.5754555235402448	4.7390966102064871	4.9004664128491511	5.0586161988791094	5.2147892461038898	5.3703934447896371	5.523478101245896	5.6717431152654587	5.8200559741982207	5.9657453378310841	6.1089783588377582	6.2514792009398183	6.3923022171244206	6.5325630731374238	6.6718480914767238	6.8106771571890814	6.9469466555856618	7.0834199431666782	7.2181911532011798	7.3528779825139381	7.4882261062965618	7.6189238867618503	7.7499046096361504	7.8812665756462827	8.011241782069078	8.1407010627217957	8.2692100471986922	8.3948513587174531	8.5199838197259901	8.6427192877467949	8.7639112733223303	8.8851095263044204	9.0037118237722567	9.1189944872770514	9.2330557089792791	9.3472511138671663	9.4600005969862266	9.5705989657027288	9.6798281780341604	9.7856082255412193	9.8898344254144952	9.9897627945649425	10.086270885208426	10.176371956102313	10.262297941779831	10.342716909239547	10.41986837233908	10.491605123624433	10.562274578221645	10.630158024083325	10.692317062890211	10.749801350679077	10.803496578501255	10.853486013749833	10.899715580319535	10.943133161924539	10.984081735739016	11.021347229627601	11.0562097129593	11.089778713985503	11.121889135222322	11.152000081438407	11.18015732606888	11.207381073742573	11.233607260600278	11.258181881702393	11.281125628331324	11.303018255051379	11.323988635908458	11.343629120417699	11.362742905246328	11.380567843040195	11.39702957950993	11.414151049308481	11.429211174486719	11.443133002861337	11.45686734952781	11.469613444458505	11.481680152182079	11.493590045473107	11.504701977625535	11.515022883825758	11.524894916008403	11.535583212610478	11.545127524148402	11.554439651288126	11.564437287798739	11.57337964914522	11.581665184086155	11.590302600826757	11.598958409456696	11.60685576360936	11.615153343918216	11.623348752437398	11.631255025722478	11.639522955243645	11.647063013537796	9.3622229338745186E-2	0.30041332242095581	0.50083875594211358	0.69453309893917925	0.88727014442928631	1.0790591198741346	1.270124635283731	1.4614074757563247	1.6520551023527104	1.8432107741861896	2.0312173403360374	2.2174167669017355	2.4010521938938871	2.5841386197440031	2.7630744484190606	2.9394866958539194	3.1100211576570369	3.2763804926647375	3.4430377053327126	3.6078714300672443	3.7712916707380546	3.932144762803909	4.0916376022801302	4.2476208869672138	4.4017517491619129	4.5538845690713163	4.7036871148432065	4.8525941753715394	4.9990447827114295	5.1450127409923079	5.2915975411402831	5.4375774175066942	5.581267542900922	5.7256951779415912	5.8669493239680328	6.0082425550376382	6.148487031624307	6.2888574539890731	6.429009174728626	6.5691715804302087	6.7075857102304042	6.8445543348161699	6.9819377663885325	7.1176507701759881	7.2528342583485843	7.3888725071062895	7.5222185899455836	7.655536646403406	7.7902293335626585	7.9232334170863794	8.0561377078135958	8.1872606979797915	8.3170149831832259	8.4452779878135278	8.5721832837552334	8.6965511280057246	8.8218385205805969	8.9451541791245166	9.064934750444559	9.185544913743195	9.3058002859938522	9.4249395552353388	9.54301504086283	9.6601003447382325	9.773138863948363	9.8856468065518772	9.9942312640484268	10.099213731867183	10.200455363904547	10.297095943157641	10.388375510380532	10.478169454537504	10.564310537487152	10.650770933274371	10.734140136165944	10.812809504018942	10.887622122254195	10.959663145266545	11.028063705488485	11.092490024766745	11.154761574594318	11.214743748322439	11.270208602780107	11.323708941943002	11.374482320253938	11.424266216907544	11.471091535173743	11.515415348030027	11.557524747003031	11.598521505362754	11.637724359645579	11.675234199110495	11.710015680512848	11.742449355152591	11.774103375692183	11.804185499903678	11.832212229871146	11.859045383957033	11.887084574400911	11.911140038461447	11.933797462978758	11.957005070677916	11.979181810010504	12.000220146437519	12.019668081648794	12.038082184312877	12.055291764133452	12.070228246468057	12.085226795177732	12.100050767029531	12.114305585589317	12.12864891428903	12.141407711288169	12.152313777843167	12.162831293064581	12.172737386303853	12.183302801798714	12.19419829512967	12.20440000334005	12.212325995515771	12.220508201236363	Measured Data (kWh)


Predicted Values (kWh) 



T outlet (predicted)	
20.2	21.9	23.8	26	28.1	30.2	32.200000000000003	34	35.799999999999997	37.5	39	40.5	41.8	43	44.1	45.1	46	46.9	47.7	48.4	49.1	49.7	50.2	50.7	51.2	51.6	51.9	52.3	52.6	52.9	53.2	53.8	54	54.2	54.5	54.7	54.9	55	55.2	55.4	55.6	55.4	55.9	55.7	55.9	56.4	56.2	56.4	56.5	56.7	56.9	57	57.2	57.4	57.6	57.7	58	58.2	58.4	58.7	59	59.3	59.6	60	60.4	61	61.5	62.2	62.8	63.6	64.3	65.099999999999994	65.8	66.5	67.3	67.900000000000006	68.599999999999994	69.099999999999994	69.599999999999994	70.099999999999994	70.5	70.900000000000006	71.3	71.599999999999994	71.900000000000006	72.099999999999994	72.3	72.5	72.7	73	73.2	73.3	73.5	73.7	73.900000000000006	74	74.2	74.3	74.400000000000006	74.5	74.599999999999994	74.7	74.8	74.8	74.900000000000006	75	75	75	75.099999999999994	75.099999999999994	75.099999999999994	75.2	75.2	75.2	75.2	75.3	75.3	75.3	75.3	75.3	75.400000000000006	20.2	22.211070596387032	24.160241296775574	26.043948059159753	27.918342394017632	29.783521062577297	31.641659248719314	33.501915265669375	35.355988209129286	37.214962735257465	39.043319961622686	40.853949190337957	42.638886801814856	44.41520887887021	46.137530431423947	47.782972340819477	49.220926113164595	50.346577567061402	51.173922176993301	51.772084393169358	52.225129845180398	52.582767606477582	52.878831779797267	53.128364112276898	53.346310095170452	53.540180016090261	53.714839118150856	53.875735987924749	54.023924650389702	54.163546548230535	54.29697872727337	54.42434560004903	54.545176409761837	54.662899264143206	54.775070028027336	54.884881804510044	54.992003974796788	55.097738362830881	55.202391297178131	55.306402839913659	55.408845303348627	55.510333961467936	55.612584312658271	55.71439102475901	55.816948355883824	55.921698716909034	56.026275123015651	56.133173937422718	56.244011828617296	56.356822905267819	56.473556425114474	56.593316319505433	56.717166608265437	56.845768459123832	56.980121834883342	57.120144825472195	57.271050572180179	57.431331478267168	57.600610691972285	57.787862998505688	57.995675180132054	58.227988120650522	58.492122788224066	58.798391373940255	59.150732642479717	59.576811414992413	60.070728094887862	60.562156251541388	61.101330160404693	61.670974727152007	62.249242993202351	62.846293767606632	63.437253520264456	64.042011583745449	64.632172262472992	65.19299097964371	65.72863513370045	66.245732657849075	66.737498542599454	67.201145157630563	67.649576530423602	68.08169987490129	68.48139056376678	68.867007693621773	69.232983711813475	69.591875364678231	69.929502238129032	70.249023210710163	70.552701648117448	70.848263198772429	71.130979878053921	71.401429506503689	71.652206817912699	71.886123501070401	72.114336063075882	72.331274361130738	72.53338967498658	72.726875444581538	72.929013440217247	73.102532643565112	73.265917630992078	73.433266776758757	73.593180249913559	73.744887986452397	73.885117320233718	74.017912668457413	74.141999223558742	74.249713710816181	74.357874508594648	74.4647682750511	74.567562008444185	74.670992185271274	74.762992674453898	74.841633811396306	74.917455101516907	74.988915267705394	75.065081569124374	75.143670287320376	75.217232484906333	75.274351762372433	75.333371596459799	Measured Data (°C)


Predicted Values (°C) 



Power (predicted)	
6.1908767065798873	6.0653306788389356	5.8729752990974982	5.7782459781956739	5.7026850266206583	5.6326202376024552	5.6095401927161781	5.6025739584628402	5.6279606149375718	5.5662581367679671	5.5790476054488609	5.5646397430742249	5.6458316094123981	5.6374560004811842	5.6896253030382278	5.6377112037114081	5.61821298575226	5.6793776679038359	5.6259575553951198	5.5711642192049444	5.4433617785701012	5.3598459705305688	5.2101920029994737	5.1030546575747193	4.986163327058212	4.8734686858701508	4.8218135782786469	4.6964932874921113	4.6536772003518712	4.6408643798787272	4.5879149370227692	4.4219193051555266	4.428446694000721	4.3160652807436026	4.2792519002648541	4.229320215561712	4.2142963520838936	4.2088777476617638	4.1894868600262276	4.1174310236382405	4.0543171244088487	4.1288082244249349	3.9966809826773342	4.0430764261419823	4.0483505948707332	3.886695491570912	3.9485114958876362	3.9695329593374025	3.9214196467725326	3.9001974762535285	3.8297601333954461	3.7941512800970618	3.7344230367755742	3.6796678460539076	3.5920815919144435	3.6258198528495069	3.5368062154750621	3.4253461496716833	3.4421919482661929	3.4083251834971278	3.3545573314723436	3.3091480048285606	3.2719094916440046	3.1359261431594536	3.1062496916774385	2.9560608197500788	2.8459777223508396	2.693009394732679	2.546484370223153	2.3436807737865069	2.2702790647424891	2.1218961226798077	2.1080196119266512	1.9986428491721995	1.8212841139836926	1.6992773622494031	1.5778116365264541	1.4739792969881838	1.3596950466470867	1.2797225816558526	1.2141526801113598	1.101624443715536	1.035859738619306	0.97312458805666435	0.94823101711824498	0.89764455379253483	0.85301013372040935	0.81156463940183132	0.79637337609244796	0.73997468668276267	0.70373715840621254	0.65910422891565479	0.59916471684299999	0.58131589548439555	0.54050879750150016	0.50172571514979369	0.46444142698490498	0.52144982612895907	0.42226920965220333	0.39813161655402657	0.42361450787170529	0.40526834600215034	0.38403817871522233	0.37323177875747054	0.3514673757799136	0.31830361796578877	0.27642730791015757	0.29842017788467495	0.29601584679453435	0.29890073021566221	0.32122499976009511	0.27638825966956337	0.23862779001161458	0.24173922791608179	0.23933050379421619	0.25446270447038571	0.27847627384192108	0.27391049868582507	0.22002193157284924	0.23911213132645401	0.21531459609032572	6.3035358382833886	6.138352121204635	5.9717850573521201	5.991037016132295	6.0051778477995548	6.0288844958463468	6.0770306250003108	6.093740681849642	6.1446645283717105	6.071771788137748	6.0435657582286435	5.9860500729418895	5.9931506810800368	5.8754586839105576	5.8074271942852285	5.6181768907099601	5.4605717649268364	5.4240195046713922	5.3165786637827983	5.2349097996954974	5.1322972086352845	5.0744411759167782	4.9532013718242309	4.8891994027377983	4.8206373275230483	4.7426465922880912	4.712448495234443	4.6333069673814871	4.6152379147583522	4.635540285928867	4.617323802831705	4.5425323921321015	4.5669346978445224	4.4626011508829375	4.4632488029086259	4.4295214401169405	4.4311221484502772	4.4252769286546103	4.4248734707716908	4.3688592545062654	4.3223266501708197	4.3326237359002029	4.2787879376538731	4.2607896860302477	4.2880352921023599	4.1996868582084455	4.1986670653522982	4.2396918344233923	4.1820399217108042	4.1776803002135274	4.1161971090209581	4.072783550155922	4.0210684324149719	3.9726979076757827	3.8863604450131608	3.9067125589000922	3.8327794656353915	3.708077462667795	3.7198834334085262	3.690206533178007	3.6257559567192628	3.5635778184542883	3.4984989639915485	3.3322602262459848	3.2656603476514716	3.1002792104457435	2.9478429781534095	2.7938616434781256	2.6283580953976751	2.4494670794918156	2.3984462090675183	2.2897136531982678	2.3159453181862983	2.2320789712712061	2.0969812746884187	1.9861004336214514	1.9051509069394865	1.8020301229677531	1.6910431665167189	1.6285821386710284	1.562977737873108	1.4399593357629055	1.3840224520798441	1.3087575720648323	1.2843503536289718	1.2036382461559922	1.1352574324466491	1.0746867299389709	1.0483705940701713	0.99890812984103483	0.95234512345081312	0.87398467320713924	0.80599764918082673	0.79008640583608314	0.74814517655913604	0.68825568206221099	0.65657596168227217	0.70975177478474716	0.58275839429506504	0.54691715472880498	0.57178772538577116	0.54441035552172601	0.51458392044771772	0.47395996358558379	0.44718137123517221	0.40986715066015844	0.3407429231221446	0.34852085852088677	0.35047696644297821	0.3358298835013962	0.3438550028396169	0.29800961186174452	0.23940463451239519	0.2300465334843167	0.21589386258144319	0.24569376381702976	0.25976655848685282	0.24234993971736221	0.16665441580819304	0.18020081098688706	0.16790909025737111	Measured Data (kW)


Predicted Values (kW) 



Power (predicted)	
6.1908767065798873	6.0653306788389356	5.8729752990974982	5.7782459781956739	5.7026850266206583	5.6326202376024552	5.6095401927161781	5.6025739584628402	5.6279606149375718	5.5662581367679671	5.5790476054488609	5.5646397430742249	5.6458316094123981	5.6374560004811842	5.6896253030382278	5.6377112037114081	5.61821298575226	5.6793776679038359	5.6259575553951198	5.5711642192049444	5.4433617785701012	5.3598459705305688	5.2101920029994737	5.1030546575747193	4.986163327058212	4.8734686858701508	4.8218135782786469	4.6964932874921113	4.6536772003518712	4.6408643798787272	4.5879149370227692	4.4219193051555266	4.428446694000721	4.3160652807436026	4.2792519002648541	4.229320215561712	4.2142963520838936	4.2088777476617638	4.1894868600262276	4.1174310236382405	4.0543171244088487	4.1288082244249349	3.9966809826773342	4.0430764261419823	4.0483505948707332	3.886695491570912	3.9485114958876362	3.9695329593374025	3.9214196467725326	3.9001974762535285	3.8297601333954461	3.7941512800970618	3.7344230367755742	3.6796678460539076	3.5920815919144435	3.6258198528495069	3.5368062154750621	3.4253461496716833	3.4421919482661929	3.4083251834971278	3.3545573314723436	3.3091480048285606	3.2719094916440046	3.1359261431594536	3.1062496916774385	2.9560608197500788	2.8459777223508396	2.693009394732679	2.546484370223153	2.3436807737865069	2.2702790647424891	2.1218961226798077	2.1080196119266512	1.9986428491721995	1.8212841139836926	1.6992773622494031	1.5778116365264541	1.4739792969881838	1.3596950466470867	1.2797225816558526	1.2141526801113598	1.101624443715536	1.035859738619306	0.97312458805666435	0.94823101711824498	0.89764455379253483	0.85301013372040935	0.81156463940183132	0.79637337609244796	0.73997468668276267	0.70373715840621254	0.65910422891565479	0.59916471684299999	0.58131589548439555	0.54050879750150016	0.50172571514979369	0.46444142698490498	0.52144982612895907	0.42226920965220333	0.39813161655402657	0.42361450787170529	0.40526834600215034	0.38403817871522233	0.37323177875747054	0.3514673757799136	0.31830361796578877	0.27642730791015757	0.29842017788467495	0.29601584679453435	0.29890073021566221	0.32122499976009511	0.27638825966956337	0.23862779001161458	0.24173922791608179	0.23933050379421619	0.25446270447038571	0.27847627384192108	0.27391049868582507	0.22002193157284924	0.23911213132645401	0.21531459609032572	6.2037327924663188	6.0127630056347332	5.8108302899119701	5.7821113647032103	5.7536692633454489	5.7319654622878922	5.7384852141778122	5.7194287978915703	5.7346701550043804	5.6401969844954358	5.5859827969709483	5.5090628097645498	5.4925927755034758	5.3680748602517268	5.2923674230457625	5.1160338540935202	4.9907800502310229	4.9997163800392581	4.9450117420359536	4.9026072201243096	4.8255927619756305	4.7847851842866413	4.6794985406125003	4.6239258658409739	4.5639845972821025	4.494076373156692	4.4672118158499901	4.3935182201966994	4.3790387484263604	4.3975440044392542	4.3793962909923296	4.310703761826832	4.3328290512200702	4.2376243807932568	4.2387969320881576	4.2073342976000685	4.2111126709429891	4.2045516221865853	4.2048721710474695	4.1524238940058584	4.1090587375729593	4.1215029471708755	4.0713901136236821	4.0555046451778782	4.081147462731165	4.0003824851788172	3.9995416937346704	4.0407806147775629	3.9901225057116156	3.9871287218165166	3.9336897049858441	3.8926285561030096	3.8478901389090607	3.8071588782511645	3.7310353275147312	3.7586217772461676	3.6994697563175754	3.5934171396012906	3.618304898959062	3.6076611675197068	3.5741780772446066	3.5422645688247139	3.5125591162620635	3.3911555763038952	3.3752382781054431	3.2575337248964966	3.1494740345626644	3.0372489611209224	2.8992173775928323	2.7383870166867483	2.693818324709139	2.5842324884894605	2.5938118736165574	2.5010760867472053	2.3600810355899258	2.2443785470575874	2.1612306903705139	2.0520168066581892	1.9327895783477984	1.868146494827168	1.7994652118436263	1.6639456337300111	1.6050101748868533	1.5232013493280963	1.4935168996081845	1.4047595479859558	1.3297143856885034	1.2632819691901347	1.2299027507917057	1.1760856284847769	1.1252951839474392	1.0434444420706135	0.97301023919226648	0.94962061618776594	0.90246372634481442	0.8408018990240258	0.80499462257659882	0.84117571331631991	0.72166392181607208	0.67972273551933671	0.69622823097475639	0.6653021799776575	0.6311500928104562	0.58343805633823631	0.55242307992247563	0.51628739461722795	0.44809447003816943	0.4499564612902649	0.4447191555539835	0.42764455679357366	0.43029986099139816	0.38276390997416326	0.32718199664993952	0.31552545664240744	0.29718279717813656	0.31696246484585244	0.3268647999286603	0.30605124631138175	0.23777976527165814	0.24546617161774964	0.22952077375758237	Measured Data (kW)


Predicted Values (kW) 
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